## Slide 1: The Hybrid MPGD-based photon detectors of COMPASS RICH-1
The COMPASS RICH-1 upgrade
The hybrid PD construction and installation
HV control, spark rates, noise level
Gain uniformity and stability
Hybrid PD preliminary characterization
Perspectives and Conclusions
Fulvio Tessarotto ( I.N.F.N. – Trieste )
on behalf of the COMPASS RICH Group

## Slide 2: COMPASS RICH-1 upgrade
P. Abbon et al., NIM A 577 (2007) 455
P. Abbon et al., NIM A 779 (2015) 69
COMPASS Spectrometer
hadron PID from 3 to 60 GeV/c; acceptance: H: 500 mrad V: 400 mrad;
trigger rates: up to ~100 KHz beam rates up to ~108 Hz; material: 2.4% Xo (beam region), 22% Xo (acceptance)
80 m3 C4F10, 21 m2 UV mirrors, 1.4 m2 MAPMTs, 4 m2 gaseous PDs
F. Tessarotto et al., JINST 9 (2014) C09011
MWPCs+CsI: successful but with important performance limitations, in particular in the case of the 4 central chambers

## Slide 3
The hybrid THGEM+Micromegas PDs
modular structure: one module = 600x300 mm2
Hybrid PD scheme
Standard Bulk Micromegas produced at CERN
good Micromegas gain uniformity
CsI
TH1
TH2
MM
quartz
Drift
8mm X 8mm pads
at positive HV
Capacitive coupling  APV25

## Slide 4: construction and quality control

## Slide 5: assembling

## Slide 6: CsI coating of THGEMs
Turbopump
THGEM
THGEM box
4 evaporators
piston
evaporators
QE measurement

## Slide 7: CsI QE measurement
  etching
19 CsI evaporations performed at CERN in 2015 - 2016
on 15 pieces: 13 THGEMs, 1 dummy THGEM,
and 1 reference piece (best from previous coatings)
11 coated THGEMs available, 8 used + 3 spares
mean THGEM QE:
~ 93% of reference
coated by T. Schnider and M. Van Stenis
Optical transparency: ~ 0.23

## Slide 8: CsI THGEM mounting

## Slide 9: The new COMPASS PDs

## Slide 10: Installation of hybrids on RICH_1

## Slide 11: Equipping the hybrids on RICH_1

## Slide 12: HV CONTROL

## Slide 13: sparks
beam intensity ppp on T6 (1013 per h)
Spark: event with I > 23 nA
during 2017 COMPASS run
time
spark rate well under control

## Slide 14
Noise figure for the 62208 ch.
MWPCs
MWPCs
Hybrids

## Slide 15: Noise level and pedestal stability
12 Detectors, 6144 Ch each.
single channel
6144 σ
values
39 APV Pedestal Runs during COMPASS 2017 run.
The APV-based F/E is the same for MWPCs +CsI and Hybrid PD’s
The niose levels are:
MWPC: ~ 600 e-
Hybrid: ~ 800 e-
The noise levels are very stable in time

## Slide 16
gain shearing among the layers and IBF
Effective gain*transfer of THGEM1 in Ar/CH4, with THGEM2 and MM at nominal voltages
nominal eff. gain: ~17000 with:
THGEM1 gain*transfer1: ~ 13
THGEM2 gain*transfer2: ~ 10
Micromegas gain: ~130
Effective gain of Mcromegas in Ar/CH4, with THGEM1 and THGEM2 at nominal voltages
The Ion Back Flow
has been
measured to be ~ 3%
(dedicated exercise)

## Slide 17: good gain uniformity
A specificgain equalization procedure has been developed and used
Sector | PD6S3 | PD6S2 | PD6S1 | PD6S0 | PD5S3 | PD5S2 | PD5S1 | PD5S0
Eff. Gain | 14322 | 14207 | 14346 | 14464 | 14675 | 14366 | 14349 | 14192
Ratio | 1.0020 | 0.9936 | 1.0037 | 1.0119 | 1.0266 | 1.0051 | 1.0039 | 0.9929
Eff. Gain | 14322 | 14024 | 14255 | 14073 | 14470 | 14291 | 14213 | 14099
Ratio | 1.0042 | 0.9811 | 0.9973 | 0.9845 | 1.0123 | 0.9998 | 0.9944 | 0.9863
Sector | PD2S3 | PD2S2 | PD2S1 | PD2S0 | PD1S3 | PD1S2 | PD1S1 | PD1S0
Average Eff. Gain |  | 14294 |  | σ | 159.40 | σ/Avg (%) | 1.1 | 
A specific gain equalization procedure has been developed and used
uniform at ~ 1%
Q.E. uniformity |  |  | 
1.09 | 1.14 | 1.03 | 0.99
0.90 | 0.88 | 0.90 | 1.08
σ = 9.3% |  |  | 
… compared to ~ 30% of old single “raw” PCB THGEMs
and ~9 % of CsI Q.E. variations
old data

## Slide 18: Gain stability in time
Chart: Date
individual chamber gain stabilization
individual corrections: σ/mean ~ 4%
global corrections: σ/mean ~ 7%
Chart: Date
| 42999.913993055554 | 43000.348946759259 | 43000.903275462966 | 43001.308310185188 | 43001.891215277778 | 43002.386261574073 | 43002.912129629629 | 43003.418252314812 | 43003.881504629629 | 43005.814363425925 | 43006.388993055552 | 43006.868611111109 | 43007.388449074075 | 43007.85765046296 | 43008.406527777777 | 43008.894236111111 | 43009.343344907407 | 43009.822129629632 | 43010.399386574078 | 43010.891388888886 | 43011.349722222221 | 43011.884560185186 | 43012.286122685182 | 43012.887418981481 | 43013.873344907406 | 43014.355844907404 | 43014.868900462963 | 43015.347002314818 | 43015.935543981483 | 43016.305752314816 | 43016.839085648149 | 43017.294965277775 | 43018.459317129629
 | 14928.01 | 14575.9587 | 13698.515 | 13370.28 | 13120.1162 | 12738.1313 | 12359.2681 | 13288.575 | 14604.4562 | 13485.155 | 13002.3575 | 13545.2131 | 13791.7463 | 13762.3525 | 13908.355 | 15122.2381 | 13905.8688 | 14714.5362 | 13302.4513 | 14649.6263 | 15008.3781 | 17313.37 | 14862.8669 | 15020.745 | 14412.25 | 14043.1675 | 14857.325 | 14595.0213 | 15861.0594 | 16098.385 | 13956.3713 | 15065.1488 | 14725.8094
gain stabilization using global p, T
14104.8 +- 91.7
13976.1 +- 117.1

## Slide 19: NICE RINGS
6.36 GeV pion
6.76 GeV pion
6.4 GeV pion
Hybrid PD
MAPMTs
MAPMTs
Hybrid PD
(in the 2017 run the Hybrid PDs were receiving Cherenkov photons from low p particles only)
ring center (calculated)

## Slide 20: Single photon angular resolution
in terms of angular resolution the response of the new Hybrid detectors
is similar but slightly superior to the MWPC one. MAPMT’s have larger pads
MWPC
MAPMT:
2.4 mrad
2.0 mrad
Hybrid PD’s
1.85 mrad

## Slide 21: Number of detected photoelectrons per ring
Hybrid PD
cathode n. 2
extrap. to 55.2 mrad, n. of det. ph.e.= 12.9
first part of the function = 10.3 +/- 0.4
second part of the function= 2.6 +/- 0.3
Critical chambers, have been changed from MWPC to Hybrid THGEM + Micromegas
the n. of det. ph.e. (55.2 mrad)
in cathode n.2 was ~8  10.3
MWPC
cathode n. 1
MWPC: 10.3
cathode n. 8
MWPC: 8.5
10.3
The number of detected photons per ring is in line with that of the good MWPC

## Slide 22: Perspectives
The characterization of the Hybrid PD performance in terms of PID is ongoing
The remaining MWPCs of COMPASS RICH-1 are likely to be replaced for 2021
Development of an optimized detector for high space resolution based on the hybrid THGEM + MM and “mini-pads”
Study the compatibility of these hybrid PDs with CF4 for a windowless RICH for
the Electron Ion Collider
Exploring the possibility to use a more robust photocathode in the far UV:
hydrogenated nano-diamond crystals
Talk by Shuddha Shankar Dasgupta
Poster by Chandradoy Chtterjee

## Slide 23: CONCLUSIONS
COMPASS RICH-1 has been upgraded with 1.4 m2 of MPGD-based PDs.
The Hybrid PD: 2 THGEMs (1 with CsI) + Micromegas are nicely operating.
They present good gain uniformity and stability, low IBF and clean rings.
1.85 mrad single photon angular resolution, 10 detected photons per ring.
A full characterization of the PID performance is ongoing.
More Hybrid PD’s will probably be mounted on RICH-1.
R&D for future RICH projects are considering the use of this technology.

## Slide 24
THGEM + CsI: 8 years of dedicated R&D
Effective gain = 0.91 · 106
Ar/CH4: 50/50
PARAMETERS:
Diam. = 0.4 mm
Pitch = 0.8 mm
Thickn. = 0.4 mm
Rim = 10 μm
a. u.
Photon yield & Charged Particles vs Drift Field

## Slide 25
The hybrid THGEM+Micromegas PDs
modular structure: one module = 600x300 mm2
Hybrid PD scheme
Standard Bulk Micromegas produced at CERN
good Micromegas gain uniformity
CsI
TH1
TH2
MM
quartz
Drift

## Slide 26
THGEM quality assessment
rejected piece
current monitor recording,
discharge counting
rejected
accepted
first 4 pieces: 1 rejected. Possibly recovered by repeating the cleaning treatment
ΔV(V)
Gain uniformity measurement
AMPTEK Mini-X Au used at 15 kV, 200µA + Cu foil provides 8 keV X-rays uniform illumination at a rate > 5 kHz cm-2 (for 1 cm Ar/CO2 70/30)

## Slide 27
The anodic PCB
8mm X 8mm pads
at positive HV
Signal read out via capacitive coupling pad readout and APV25 F/E boards
Strong technological effort from TVR Company for the PCB (multilayer 3.2 mm thick) to comply with specific requirements of planarity, surface quality, layer thickness uniformity, surface irregularities (E field).
anodic pad PCB produced by TVR
Tests on 2500 pads:
electrical continuity
and capacity meas.
 38-42 pF/pad
“surface anode” pad
“buried pad”
“Z drilling controlled
via”  planarity issue
470 MΩ resistor for each anodic pad

## Slide 28: The COMPASS THGEM design
12 sectors on both top and bottom, 0.7 mm separation
24 fixation points to guarantee THGEMs flatness
Thickness: 0.4 mm, hole diameter: 0.4 mm, pitch: 0.8 mm
border holes diam.: 0.5 mm
pillars in PEEK

## Slide 29: THGEM raw material selection
Our thickness uniformity requirements are stricter than those offered by producers  material selection
50 foils of 1245 mm x 1092 mm  cut out borders  800 mm x 800 mm  thickness measurement
Mitutoyo EURO CA776
coordinate measuring machine with ruby touch probe,
hosted in a thermalized room
for each foil 36 x 36 points in square pattern are measured
2 measurements (direct and reversed) to allow consistency checks.
  underpressure induced flatness

## Slide 30: THGEM raw material selection
  typical result for a good piece.
THGEM 313
THGEM 413
49 p.cs
2%<δ<3%
  from each foil twoTHGEMS can be produced:
  50 foils  100 raw THGEM pcb
  THGEM pcb size = 620 mm x 320 mm,
  active area = 581 mm x 287 mm
  δ for the 100 raw THGEM pcb (%)
  60 THGEMs have been produced by ELTOS
  all foils have been labelled and measured  database of local thickness of all THGEMS

## Slide 31
Production of the THGEMs at ELTOS
  stripping dry-film
  development
  etching
  image transfer
  multi-spindle drilling
  mounting
In Trieste a specific cleaning procedure is applied : polish with fine grain pumice powder, pressure water cleaning, ultrasonic Bath with Sonica PCB solution (PH11), distilled water rinsing and oven @ 160 ºC

## Slide 32
mechanical frames and wires
drift and field wires: Cu-Be, Au coated
4 mm pitch, 100 µm diam.
manual soldering
tension meter

## Slide 33: field shaping electrodes
THGEM border study
large field values at the chamber edges and on the guard wires
Field shaping electrodes in the isolating material protections of the chamber frames
isolating material (Tufnol 6F/45) protection