## Slide 1: CHARM Dosimetry challenges and new opportunities
C. Cangialosi, Marie-Curie Fellow
R2E Annual Meeting 2018
12/12/18 - CERN

## Slide 2: Overview
CERN, Dec. 12, 2018
Studies of constraints encountered in the CHARM Dosimetry. Indeed, a deep knowledge of these peculiarities become essential to characterize properly the mixed field of the facility during the test session.
Studies for the improvement of CHARM facility in term of new test opportunities, starting from 2021.
  Boron Carbide shielding employment to protect electronic against ThNs.
  Exploring the capabilities of CHARM facility to measure the ThNs cross section of SRAMs.

## Slide 3: Overview
CERN, Dec. 12, 2018
Studies of constraints encountered in the CHARM Dosimetry. Indeed, a deep knowledge of these peculiarities become essential to characterize properly the mixed field of the facility during the test session.
Studies for the improvement of CHARM facility in term of new test opportunities, starting from 2021.
  Boron Carbide shielding employment to protect electronic against ThNs.
  Exploring the capabilities of CHARM facility to measure the ThNs cross section of SRAMs.
RADECS 2017 Geneva, Switzerland, Oct. 2017.
C. Cangialosi et all. “Thermal Neutron SRAM Detector Characterization at the CERN Mixed-Field Facility, CHARM” IEEE Trans. Nucl. Sci., vol. 65, issue 8, pp. 1887-1893. - 2018

## Slide 4: CHARM Facility
0
1
2
3
4
5
6
7
8
9
10
11
12
13
14
1
2
3
4
Patch
Panels
NO accessible area
1 m
Scale
24 GeV Proton
Movable
shielding
T0
16
15
CuCIIC
Entrance
Lateral Position
Longitudinal Position
IN BEAM
PRIMARY PROTONS BEAM IMPINGES A METAL TARGET (POT): A SECONDARY RADIATION FIELD IS CREATED
3 KEY ELEMENTS:
Target
Movable Shielding
Positions
AlH - Aluminium Hole
Al - Aluminium
Cu - Copper
>16 test positions
C – Concrete (1,4)
I – Iron (2,3)
THE SPECTRA AND INTENSITY OF SECONDARY FIELD DEPEND ON THE POSITION
> 150 official configurations
POT/h = 3.38E+15
CERN, Dec. 12, 2018
Notes: Choosing the target, the shielding and the test position it is possible to define the spectra and the intensity of the field.

## Slide 5: CHARM Facility
CERN, Dec. 12, 2018
During the calibration session the Dose, the Fluence (RadMon) and the POT (SEC) are measured:
Each position ‘p’ and configuration ‘c’ can be calibrated with two factors Kdose and KHEH .
At CHARM the POT are proportional to the intensity of the radiation field, so the Radiation Level at CHARM are measured as a function of POT:
During a standard irradiation session measuring the POT is possible to retrieve the Rad. Level on the DUT.

## Slide 6: Studies of constraints encountered in the CHARM Dosimetry
2018 Nuclear Science Symposium (NSS) and Medical Imaging Conference (MIC) Sydney, Australia, from the 10th to 17th of November
S. Danzeca, C. Cangialosi et all. “Challenges in dosimetry and testing in the CERN CHARM mixed radiation field Facility”
CERN, Dec. 12, 2018

## Slide 7: Influence of IRRAD Facility
CERN, Dec. 12, 2018
CHARM
IRRAD
24 GeV
PS p+
ENTRANCE
  CHARM beam line is placed downstream to IRRAD
If massive and bulky samples are tested in IRRAD, the effective proton impinging on the target might be less that the one measured by the SEC.
This leads to an overestimation of the POT and consequently, an overestimation of dose and fluence levels calculate for the test run.
DUMP
MWPC
SEC

## Slide 8: Influence of IRRAD Facility
To assess the IRRAD impact on the CHARM dosimetry, the CHARM HEH k-factor where no samples are placed in IRRAD, are compared with the ones obtained when copper slabs of different thickness are placed in the IRRAD beam-line.
heh calibration factor retrieved for position 10 CuOOOO configuration |  | 
IRRAD Copper sample | kHEH [10-5·cm-2/POT] | Percentage difference with Normal Run
Normal run* | 7.44 | 0%
1.5 cm | 6.88 | -8%
3 cm | 6.03 | -19%
6 cm | 4.68 | -37%
* NO Samples on the IRRAD beam line |  | 
CERN, Dec. 12, 2018
Position 10
The effects of a sample 6 cm thick lead to radiation levels up to 37% lower than the ones without any samples.
The dose and the fluences on the user’s equipment need to be monitored during the test runs.
Notes: When IRRAD inserts some samples in the beam line, a decrease
of the counts of SEC2 is expected, as some primary protons are scattered from the beam
line direction. At difference with this expectation, we measured an increase of the counts.
This increase is caused by secondary particles, which are generated by the interaction
between the primary protons and the IRRAD sample. Secondary particles are emitted in
the same direction of the beam line and they are counted by the SEC2. Due to the low
momentum of these secondary particles, when they impinge inside the target, they do not
contribute to the generation of the mixed field of CHARM. In this way, the measurement
of SEC2 are overestimating the real number of POT.

## Slide 9: Beam position Influence on the Dose
CERN, Dec. 12, 2018
Position 13
Position 16
Position 1
0
1
2
3
4
5
6
7
8
9
10
11
12
13
14
1
2
3
4
Patch
Panels
NO accessible area
1 m
Scale
24 GeV Proton
Movable
shielding
MWPC
Notes: Position 1 (up to -60% diff) and Position 16 (up to -50%).
A=110cm, B=84cm, C=160cm
H-FWHM
V-FWHM
51.9 +/- 7.7
47.7+/- 5.5

## Slide 10: Beam position Influence on the Dose
CERN, Dec. 12, 2018
A
C
B
Beam
50
23
-33
x (mm)
Position 13 – Cu target |  |  | 
Beam position on the Horiz. axis (mm) | KDose - Percentage difference with Centered Run (%) |  | 
 | Position A | Position B | Position C
48.7±0.2 | 59% | 17% | 42%
23.0±0.6 | 27% | 22% | 43%
1.3±0.4 | 0% | 0% | 0%
-33.5±0.8 | -43% | -57% | -59%
The beam position influences the Rad. level measurement.
The K decrease going away from the beam.
This influence is also observed at test location 1 and 16.
The dose and the fluences on the user’s equipment need to be monitored during the test runs.
Position 13
Notes: Position 1 (up to -60% diff) and Position 16 (up to -50%).
A=110cm, B=84cm, C=160cm
In the direction of

## Slide 11: Self shielding effect – R10
CERN, Dec. 12, 2018
Possibility to test large volumes electronic equipment

## Slide 12: Self shielding effect – R10
CERN, Dec. 12, 2018
TE/EPC Test
Position 10 – CuOOOO | 
Radiation Level | Percentage difference between side A and side B (%)
 | 119 cm
Dose | -34%
HEH | -32%
Side A
Side B
The dose and the fluences on the user’s equipment need to be monitored during the test runs.

## Slide 13: Boron Carbide shielding employment to protect electronic against ThNs
14th Specialists' workshop on Shielding aspects of Accelerators,Targets, and Irradiation Facilities.
Gyeongju, Korea, Oct. 30 2018
C. Cangialosi et all. “Evaluation of future employment of Boron Carbide shielding at CERN High energy AcceleRator Mixed field (CHARM) Facility”.
CERN, Dec. 12, 2018
SATIF-14

## Slide 14
CERN, Dec. 12, 2018
SATIF-14
High appreciation in SATIF-14!

## Slide 15: Evaluation of a new type of shielding (B4C)
25% B - 3.5 mm
25% B – 7.0 mm
RadMon 1 Boron Free
RadMon 1
RadMon 2
Comparison of different B4C shielding:
  80% B content
  25% B content
  Evaluation of the shielding as a function of Boron sheet thickness (from 2mm to 7mm)
To asses the effectiveness of this type of shielding in accelerator-like environment.
The B4C shielding employment at CHARM can improve the facility test capability?
CERN, Dec. 12, 2018
Notes: Not used in the LHC.
Boron weight percent: 80%: 650 E/m2 ---> 2mm and 800E/m2 ---> 5mm.
Thermal neutron affettono l’elettronica, specialmente se c’e’ boro –COTS
Assorber, boron carbide shielding
Boron carbide mass content: 25% B: 400E/m2---> 3.2 mm and 800E/m2 ---> 7mm

## Slide 16: B4C shielding effect at CHARM
Position 3 |  |  |  |  | 
Facility Configuration |  |  |  |  | 
CuOOOO | 5.15E-05 | 4.16E-05 | 0.81 | 1.06 | 2.65
CuCIOO | 1.15E-05 | 2.21E-05 | 1.12 | 1.08 | 4.28
CuCIIC | 3.15E-06 | 2.65E-05 | 8.41 | 1.03 | 12.99
Position 3 |  |  |  |  | 
Facility Configuration |  |  |  |  | 
CuOOOO | 5.15E-05 | 4.16E-05 | 0.81 | 1.06 | 2.65
CuCIOO | 1.15E-05 | 2.21E-05 | 1.12 | 1.08 | 4.28
CuCIIC | 3.15E-06 | 2.65E-05 | 8.41 | 1.03 | 12.99
Pos. 3
POT=Protons impinging on the target
For a particular configuration the B4C shielding has no effect on the This is observed during all tests presented in this work.
The B4C sheet reduces the a factor:
~3 for CuOOOO
~ 4 for CuCIOO
~13 for CuCIIC
A similar behavior is observed with the Al target at the same position.
CERN, Dec. 12, 2018
Notes: Intensita piu basse

## Slide 17: B4C shielding effect at CHARM
Position 3 |  |  |  |  |  |  | 
Facility Configuration | Boron free | 80% - B content |  |  | 25% - B content |  | 
CuOOOO | 0.81 | 0.32 | 0.31 | 1.0 | 0.20 | 0.24 | 1.4
CuCIOO | 1.12 | 0.43 | 0.51 | 1.2 | -- | -- | --
CuCIIC | 8.41 | 0.66 | 0.86 | 1.3 | -- | -- | --
Position 3 |  |  |  |  |  |  | 
Facility Configuration | Boron free | 80% - B content |  |  | 25% - B content |  | 
CuOOOO | 0.81 | 0.32 | 0.31 | 1.0 | 0.20 | 0.24 | 1.4
CuCIOO | 1.12 | 0.43 | 0.51 | 1.2 | -- | -- | --
CuCIIC | 8.41 | 0.66 | 0.86 | 1.3 | -- | -- | --
The B4C sheet (both 80% and 25% B content) modifies the particle spectra in favour of HEH with respect to ThN, also for facility configuration with high R factor value.
The thickness of the B4C sheet plays a key role at higher R-factor value.
In configuration CuOOOO the sheet thickness is negligible for 80% B-sheets, but is significant for the 25% one.
CERN, Dec. 12, 2018
Notes: It gives information on the softness of the spectrum

## Slide 18: Conclusion and Outlook
The Irrad-influence, the beam position influence and the self-shielding effect of massive equipment, make the Dosimetry at CHARM is a real challenge. For this reasons the Radiation Level monitoring during user’s test is necessary.
2018:
More than 150 configurations.
2021:
The use of a rack covered of B4C sheet will increase the number of configurations exploitable at CHARM. It will enhance the facility test capability covering new radiation environments suitable for new applications.
Thank you all the CHARM Team!!!
CERN, Dec. 12, 2018
The tests a CHARM shows the B4C sheet an efficient solution to protect the electronics operating in the LHC and in the accelerator-like environment.
The B4C sheets with 80% of Boron seems the best solution for environment defined by spectra dominated by ThN.
Notes: We will still keep in charm

## Slide 19
Thank you for your attention!

## Slide 20: Application
Concrete
Rack covered with B4C
Pos. A
Pos. B
Pos. C
NA62 Experiment
Aim to study rare kaon decays
2017:
several failures in the readout of electronic equipment.
can induces failures to electronic components (FPGAs or SRAM).
2018:
Concrete shielding
B4C shielding
BatMon System
CERN, Dec. 12, 2018
Notes: In order to assess the radiation levels in the tunnel, and to validate the shielding effect put in place in the 2017, BatMons have been installed in the tunnel areas close to the sensitive equipment in the 2018. At the end of the 2017, two additional concrete blocks have been installed close to the LKr readout rack to reduce even further the High energy hadron (HEH) fluence coming from the target zone. In addition to this, the racks containing the electronics for the KTAG and LKr have been covered with sheets of Boron Carbide (B4C) to shield from the thermal neutrons (THN) which could have been the cause of several failures in the 2017 run.
NA62 will measure the rate at which the charged kaon decays into a charged pion and a neutrino-antineutrino pair.
The measurements carried out in the time frame 20/06/2018 - 18/07/2018 showed that the HEH and Thermal neutron out of the shielding are in the range of 7E7 per week. This value can potentially induces failures to electronic equipment such as FPGAs or SRAM memories. The shielding effectively reduces the HEH fluence by a factor ~10 as can be noted in Table 4 (Position1/Position2 and Position1/Position3). The boron carbide shielding is very effective to capture thermal neutron, indeed the thermal neutron fluence is reduced by a factor 28 with respect to the out shielding position (Position1/Position2) and of a factor 12 only considering the effect of the boron carbide (Position3/Position2).
pixel tracking detectors (GTK) tracking detectors
Liquid Krypton calorimeter detector, (LKr)

## Slide 21: Application
Shielding effect Evaluation |  | 
FLUENCE RATIO |  | 
 | 14.2 | 28.0
 | 9.2 | 2.8
 | 1.4 | 12.4
Shielding effect Evaluation |  | 
FLUENCE RATIO |  | 
 | 14.2 | 28.0
 | 9.2 | 2.8
 | 1.4 | 12.4
A
B
C
The Co-shielding reduces the by a factor ~10
B4C-shielding reduces the by a factor 12
The two shielding are very effective to capture ThN, indeed the is reduced by a factor 28.
CERN, Dec. 12, 2018
Notes: Liquid Krypton calorimeter detector, (LKr)

## Slide 22: Application Vs CHARM
A
B
C
CHARM conf.  AlHOOOO at Position 0 
NA62  Position A 
CERN, Dec. 12, 2018
Notes: Liquid Krypton calorimeter detector, (LKr)