## Slide 1: Radiation hardness in single-mode optical links for Accelerator Instrumentation
Carmelo Scarcella
Indico link: https://indico.cern.ch/event/760345/

## Slide 2: Outline
Optical Links for Accelerator Instrumentation
Versatile Link and Single-mode VTRx
project timeline
Edge-Emitting Laser selection
displacement damage
Wavelength division multiplexing CWDM
Summary and future steps

## Slide 3: Optical Links for Accelerator Instrumentation
The Accelerator Instrumentation Group (BE/BI) is moving towards common readout solutions
Sensor
or
Actuator
Analogue
Front-End
Card
Radiation zone
Timing/Trigger/Ctrl
&
Data Acquisition
Reach up to 3 km
Radiation-free zone
Digital
Front-End
Card
Digital
Back-End
Card
Optical link

## Slide 4: The GBT-based Expandable Front-End (GEFE)
Common hardware development ongoing for LS2 upgrades
GBTx
Rad-hard
DC-DC
ProAsic3
FPGA
FMC HPC
SM VTRx

## Slide 5: Project timeline
Rad-Hard Link | GBTx + SM VTRx | 
Rad-Hard DFE | GEFE & S-GEFE | 
Users | New SPS BPM system (“ALPS”) Motor control optical interface (“MCOI”) … | 
Total links | ~ 300 | 
Data-rates | GBTx Tx 4.8 Gbps Rx 4.8 Gbps | 
LS2
LS3/LS4

## Slide 6: Single-mode Versatile Link Transceiver - VTRx
Front-End pluggable module
Receiver
  COTS InGaAs Photodiode
  Transimpedance amplifier GBTIA v3
Transmitter
  COTS Edge emitter Fabry-Perot laser
  Laser driver GBLD v4.2
Calorimeter grade radiation tolerance
10 kGy TID
5 · 1014 n/cm2 MeV neutrons
Laser Diode
TOSA
TX
PIN + TIA
ROSA
RX
Laser Driver
edge
connector
I2C
PCB
https://espace.cern.ch/project-versatile-link/public/default.aspx

## Slide 7: Project timeline
Rad-Hard Link | GBTx + SM VTRx | LpGBT + New SM VTRx
Rad-Hard DFE | GEFE & S-GEFE | Distributed IO Tier (BE-CO) or S-GEFE 2
Users | New SPS BPM system (“ALPS”) Motor control optical interface (“MCOI”) … | LHC BPMs (LS3) SPS BLMs (LS3) / LHC BLMs (LS4) …
Total links | ~ 300 | ~ 5000 - 10000
Data-rates | GBTx Tx 4.8 Gbps Rx 4.8 Gbps | LpGBT Tx up to 10.24 Gbps Rx 2.56 Gbps
LS2
LS3/LS4

## Slide 8: CWDM Single-Mode Versatile link
Parameter | Value | Units
Max Uplink Bit Rate | 4.8 or 10.24 | Gb/s
Max Downlink Bit Rate | 4.8 | Gb/s
Wavelengths | 1270/1290/1310/1330 | nm
Total ionizing dose (TID) | 10 | kGy
Fluence | 5 · 1014 | n/cm2 MeV neutrons
4 x 10 Gb/s on a single fiber
Front-end
Radiation hard
Transceiver - VTRx
Back-end
Custom off-the-shelf
transceiver
Passive optics
Single-mode optical fibers
Optical MUX/DEMUX
Radiation zone
Radiation free zone

## Slide 9: CWDM Single-mode Versatile Link Transceiver - VTRx
Front-End pluggable module
Receiver
  COTS InGaAs Photodiode
  Transimpedance amplifier GBTIA v3
Transmitter
  COTS Edge emitter Laser
  Laser driver GBLD v4.2
Laser Diode
TOSA
TX
PIN + TIA
ROSA
RX
Laser Driver
edge
connector
I2C
PCB
011100010101101001010100
0111000101011010000110100

## Slide 10: Displacement damage – TOSA in n-beam
Single-mode TOSAs exposed to neutron beam at UC Louvain cyclotron facility (28/11/2018)
Irradiation with fluence up to 5 x 1014 n/cm2 20 MeV neutrons

## Slide 11: Displacement damage 1/2
Fluence
Moderate increase of threshold current for all tested devices
Full damage compensation possible adjusting bias current
Annealing reduces radiation damage
~ halves the effect in 10 years lifetime

## Slide 12: Displacement damage 2/2
10 days annealing
Negligible central wavelength shift
Laser peak wavelength within the CWDM Passband
Moderate slope efficiency decrease
Negligible optical modulation amplitude penalty within the specification radiation levels

## Slide 13: Edge-emitting Laser radiation tolerance
Two suitable Laser types showing moderate penalty due to displacement damage have been identified
TID test for optical components into TOSA package to be performed
Further radiation tests required during production volume procurement
e. g. opto die wafer qualification

## Slide 14: Coarse Wavelength Division Multiplexing
4 x 10 Gb/s on a single fiber
1270 nm
1290 nm
1310 nm
1330 nm
Ch1
Ch2
Ch3
Ch4
Based on optical MUX/DEMUX
passive bidirectional component
4x10 Gb/s on a single fiber
~ 2 dB insertion loss (4ch MUX)
Radiation tolerance to be investigated

## Slide 15: Summary and further work
Common solution for accelerator instrumentation optical links
based on the versatile link framework
targeting 10.24 Gb/s upstream operation
4 channel wavelength division multiplexing scheme (CWDM)
compatible with next generation rad-hard chipset for optical data links (LpGBT)
Project status
demonstration of 10.24 Gb/s upstream operation
Laser driver (GBLD) insensitive to TID in the specification range
moderate displacement damage of CWDM Edge-Emitting Lasers
Next steps
radiation tolerance validation of CWDM optical MUX
solutions for standard SFP cage compatibility
defining of final link architecture
moving towards parts procurement, production and qualification

## Slide 16: Radiation hardness in single-mode optical links for Accelerator Instrumentation
Carmelo Scarcella
Indico link: https://indico.cern.ch/event/760345/

## Slide 17
Backup slides

## Slide 18: Summary and further work
CWDM COTS EEL procurement
10.24 Gb/s uplink operation
Displacement damage EEL 5 · 1014 n/cm2 MeV neutrons fluence
GBLD Laser driver TID test
Progress
to date
Next
steps
CWDM MUX radiation tolerance
Standard SFP cage compatibility
Link specs definition and production

## Slide 19: CWDM Single-mode Versatile link
Common solution for accelerator instrumentation optical links
based on the versatile link framework
targeting 10.24 Gb/s upstream operation
4 channel wavelength division multiplexing scheme (CWDM)
compatible with next generation rad-hard chipset for optical data links (LpGBT)
Project status
demonstration of 10.24 Gb/s upstream operation
Laser driver (GBLD) insensitive to TID in the specification range
moderate displacement damage of CWDM Lasers
Next steps
radiation tolerance validation of CWDM optical MUX
solutions for standard SFP cage compatibility
defining of final link architecture
moving towards parts procurement and production
4 x 10 Gb/s on a single fiber
1270 nm
1290 nm
1310 nm
1330 nm
Ch1
Ch2
Ch3
Ch4

## Slide 20: Displacement damage 1/2
~ 10 days annealing
Fluence
Moderate increase of threshold current for all tested devices
Full compensation bias current compensation

## Slide 21: 10 Gbps VTx operation
All evaluated TOSAs rated for 10 Gbps operation
Custom rad-hard ASIC – GBLD V4.2
Ibias = 2 ÷ 43 mA
Imodulation = 4 ÷ 24 mA
Iemphasis = 0 ÷ 24 mA
Temphasis = 60 ÷ 90 ps
Laser Diode
TOSA
TX
PIN + TIA
ROSA
RX
Laser Driver
edge
connector
I2C
PCB
Imod
ILaser
Time
Ibias
Temp
Iemp
Enhancing the frequency response

## Slide 22: Uplink lane rate
Applications requiring high data rate can run the uplink at 10.24 Gb/s using pre emphasis on rising/falling edges
10.24 Gb/s is compatible with next generation rad-hard serialiser/deserialiser LpGBT
5 Gb/s
10 Gb/s