## Slide 1
F. Wan
M. D. Sumption
D. L. Zhang
and E. W. Collings
Microstructure and enhanced engineering critical current density of AIMI MgB2 strands processed with low temperature and long time
M.A. Rindfleisch
M3Or3B-03

## Slide 2: Outline
1. Purpose
2. Experimental results
1) Monofilamentary AIMI Strand
- Microstructural analysis
- Transport Critical Current Density
2) Multifilamentary AIMI Strand
- IC, JC and Filament number
- Microstructural analysis
- Transport JC and H. T. Condition
- Transport JC and Dy2O3 Doping
3. Concluding summary

## Slide 3: Purpose
Mg-Reactive-Liquid-Infiltration (Mg-RLI)/Internal-Magnesium-Diffusion (IMD) [1] processed MgB2 wire obtained high transport JCs
Notes: [1] World scientific series in applications of superconductivity and related phenomena-MgB2 superconducting wires, pp. 315-340 (2016)

## Slide 4: Purpose
Testing the transport JC of AIMI strands heat-treated with 625oC and 8 ~ 64 hours
Our group/HTR developed Mg-RLI-processed strand by optimizing strand architecture and selecting better raw materials.
Advanced-internal-magnesium-infiltration
(AIMI) strand.
H. T. Condition: 675 oC/1 ~ 4 h

## Slide 5: Monofilamentary Strand: Mg Infiltration
8 h
32 h
16 h
64 h
Monel
Nb
Heating Temperature
625 oC
Partial Infiltration
Full Infiltration
Full Infiltration
Full Infiltration
MgB2
B-rich Phase
OD: 0.55 mm
2mol% C-doped B

## Slide 6: Transport Layer JC versus Heating time
8 h
16 h
32 h ~ 64h
Layer JC = IC/AreaMgB2 Layer

## Slide 7: Layer JC versus Heating Temperature
675 oC
1 ~ 4 h
625 oC
8 h
Notes: [2] Li GZ et al Superconductor Science and Technology, volume 25, 11 2012

## Slide 8
Multifilamentary AIMI
MgB2 Strands
Multi stands have better electrical and thermal stability than mono strands
OD: 0.83 ~ 1.01 mm
Chemical Barrier/Outer Sheath: Nb/Monel or SS

## Slide 9: IC versus Filament Number
6
18
Mono
4.2 K
ICs of multi strands are higher than those of mono strands due to larger MgB2 area
625oC
8h

## Slide 10: Engineering JC
JE = IC/Areawhole strand= Layer JC * Fill Factor
Fill Factor = MgB2 Layer Area/ Whole strand Area

## Slide 11: Transport Je versus Filament Number
Filament Number | Fill Factor %
1 | 12.8
6 | 9.5
18 | 11.5
Mono
6
18

## Slide 12: Layer JC versus Filament Number
Filament Number | 10 T Layer JC ( 104A/cm2)
1 | 10.4
6 | 8.99
18 | 6.09

## Slide 13: Microstructural Analysis – 18-filamentary Strand
625oC/08h
Area | Mg : B | Phase
Area 1 | 1 : 2.42 | MgB2 + B-rich
Area 2 | 1 : 4.54 | B-rich
Area 3 | 1 : 2.05 | MgB2
Area 4 | 1 : 3.28 | B-rich
B-rich phases were distributed in MgB2 matrix

## Slide 14: Transport JC versus Heating Time
18 Filaments
625 oC
Heating time:8 ~ 14 hours

## Slide 15
Dy2O3/C Co-doping for
18-filamentary AIMI Strands

## Slide 16: Dy2O3 Doping
625 oC/8 h
625 oC/14 h
Dy2O3 doping level: 2wt% based on B

## Slide 17: Dy2O3 Doping
MgB2 short straight wires (5 cm)
Heating Temperature: 625 oC
Diameter: 0.83 ~ 0.84 mm
At 4.2 K, 10 T
IC = 60 A
Je = 1.06 × 104 A/cm2

## Slide 18: Dy2O3 Doping
MgB2 Spiral (1 m)
Diameter: 0.83 ~ 0.84 mm
Je (kA/cm2)
625oC
8 ~ 14h
675oC
1 ~ 4h
5 T
IC = 350 A
Je > 60 kA/cm2

## Slide 19: Dy2O3 Doping
625oC
8h
Uniform MgB2 layer in
low temperature strand
625oC
8 ~ 14h
675oC
1 ~ 4h

## Slide 20: Dy2O3 Doping
675 oC/4 h
Continuous B-rich layer

## Slide 21: Mg Infiltration into B layer
The molten Mg rod shrinked to several liquid Mg droplets to obtain a minimum surface area possible.
B Layer
Mg Rod
MgB2 Layer
Liquid Mg droplets

## Slide 22: Mg Infiltration into B Layer
Molten Mg “left” its original place

## Slide 23: Mg infiltration into B layer
MgB2 Layer
B-rich Layer

## Slide 24: Concluding summary
Monofilamentary AIMI MgB2 strands processed with low temperature and long time can obtain same transport properties as the strand processsed with high temperature.
Multifialmentary AIMI MgB2 strands have suppressed transport JCs due to precence of B rich phases distributed in MgB2 matrix.
Dy2O3 doping can significantly enhance the transport properties of multifilamentary MgB2 strands.
Low heating temperature induces the formation of relative uniform MgB2 layer in AIMI strands.

## Slide 25: Acknowledgements
This work was funded by the NIH grant