## Slide 1
Assessment of stability of fully-excited Nb3Sn Rutherford cable with modified ICR at 4.2 K and 12 T using a superconducting transformer and solenoidal magnet
C. J. Kovacs1, M. D. Sumption1, E. Z. Barzi2, A. V. Zlobin2, M. Majoros1
1 Center for Superconducting & Magnetic Materials (CSMM), Department of Materials Science & Engineering, The Ohio State University, USA
2 Applied Physics and Superconductivity Technology Division (APS-TD), Fermi National Accelerator Laboratory, USA
M2Po2E-01 [49] – LTS Cables - Fabrication and Characterization
Acknowledgments
This work was supported by the U.S. Department of Energy, Office of Science Graduate Student Research Program (SCGSR)
Conclusions
[1] E. Barzi et al. “Superconducting Transformer for Superconducting Cable Tests in a Magnetic Field” AIP Conference Proceedings, 1218, pp.421-428 (2010)
[2] C.J. Kovacs, M. Majoros, M.D. Sumption, and E.W. Collings, “Quench and stability of Roebel cables at 77 K and self-field: minimum quench power, cold end cooling, and cable cooling efficiency,” Cryogenics, 95, pp.57-63 (2018)
[3] C.S. Myers, M.A. Susner, L. Motowidlo, J. Distin, M.D. Sumption, and E.W. Collings, “Specific heats of composite Bi2212, Nb3Sn, and MgB2 wire conductors”, IEEE Trans. Appl. Supercond., 23, 3, (2013)
References
Multiple conductor options exist for next-generation high field accelerator magnets. Whether or not a hybrid, it is likely these magnets will incorporate Nb3Sn Rutherford cable.
The performance targets of the next-generation dipoles hasn’t been reached yet for a Nb3Sn magnet.
It will be important to have a low-cost, fast turn around measurement program to measure the full excitation Jc and stability performance of Nb3Sn Rutherford cable magnet scale composite.
Ideally, this measurement program could include many partners in universities and national labs by requiring lower cost and smaller footprint infrastructure.
In this research, a low-cost measurement system described in [1] was modified to handle additional instrumentation to perform stability measurements of fully excited Nb3Sn Rutherford cable in a LHe bath with applied fields up to 14 T.
The stability diagram generated from the experimental runs was compared to a theoretical analytical stability model.
Introduction
The Teslatron II measurement station at Fermilab has a 77 mm bore solenoid which can apply fields of 14-16 T at 4.2 K and 2.2 K respectably.
A spiral bifilar sample holder which is coupled with a 60-multiplication factor NbTi superconducting transformer was designed to reduce the integrated Lorentz forces on the probe and magnet assembly.
The cable was insulated with S-glass braided sheath but remained unimpregnated and therefore was in good contact with the liquid Helium.
Voltage taps were soldered near a strain gauge used to generate heat perturbations.
Nb3Sn strand and cable specifications
A steady state analytical stability model for cables in liquid cryogen derived in Kovacs et al. was modified to determine stability of the Nb3Sn Rutherford cable in LHe [2].
The resistivity of the stabilizer is mostly constant over the temperatures of concern and determined from RRR.
h is chosen to be 10 kW/m2K < 5.2 K and 1 kW/m2K ≥ 5.2 K.
Tcs = 4.52 K is chosen as when the surface cooling equals the joule heating at T = 5.2 K.
The model below assumes current sharing at soldered junctions, a linear Ic versus T, and a flat sloped temperature gradient from cold-end cooling.
Rutherford cable steady state thermal stability model
Fermilab spiral bifilar probe with 30 kA superconducting transformer: full-excitation stability measurements at 4.2 K with applied fields up to 14 T.
Full-excitation thermal stability measurement results
A laboratory scale system was modified to determine stability of a fully excited Nb3Sn Rutherford cable.
A steady state analytical model and dynamic analytical model resulted in similar values as experimental data, but they were not able to capture the I/Ic stability relationship.
Strand Type | Oxford RRP
Stack design | 132/169
Ternary Element (?) | Ti
Production year | 2012
Diameter, d, [mm] | 0.7
Ic (4.2 K, 12 T), [A] | 449
Jc (4.2 K, 12 T), [A/mm2] | 2649
Ic (4.2 K, 15 T), [A/mm2] | 219
Jc (4.2 K, 15 T), [A/mm2] | 1297
Twist pitch, [mm] | 13
Cu fraction, λ, [%] | 56.0
RRR (273 K/20 K) | 153
HT dwell step | 210 °/72 h + 400 °C/48 + 640 °C/50 h
Cable | T1
Strand Count | 40
Core (?) | Yes
Core width, [mm] | 9.5
Lay angle, [degrees] | 16.8
Width, [mm] | 14.7
Thickness (mid), [mm] | 2
Rutherford cable dynamic thermal stability model
Cp calculated from experimental data fit from PPMS data from Nb3Sn strand at 12 T [3]