## Slide 1: Progress of DLC Resistive Electrode
You LV
On behalf of resistive DLC collaboration
RD51 mini week, 05-12-2018
State Key Laboratory of Particle Detection and Electronics
University of Science and Technology of China

## Slide 2: Outline
R&D on thick-DLC
Application of thick-DLC
Copper coating on DLC

## Slide 3: Motivation
  The longer of the deposition time, the DLC is thicker and has a lower resistivity.
  Add hydrogen into the DLC can increase the surface resistivity significantly.
  Add hydrogen into the DLC by using the Ar/iC4H10 gas mixture.
  The higher isobutene flow, the higher surface resistivity.
  Current thin-DLC sample
Thickness : ~ 50 nm
Surface resistivity: 1 MΩ/□ to 100 MΩ/□
Resistivity uniformity: ~13% @15cm×15cm DLC
  Thick-DLC sample
The current thin-DLC sample have been successfully applied in μRWELL detector as resistive electrode.
Thickness : > 100 nm
Surface resistivity: ~MΩ/□ to ~TΩ/□
Resistivity uniformity: ~23% @25cm×25cm DLC
Thick-DLC can be applied in many MPGDs due to the thicker DLC coating with a wide range of adjustable surface resistivity.
More detail of the deposition process can be found in Y.Zhou, RD51 Collaboration Meeting, 28-09-2017

## Slide 4: Sample of thick-DLC
Tool for surface resistivity measurement
  The value measured by the tool have a scale factor of 10 relative to the absolute surface resistivity.
  Deposition parameters for 25cm × 25cm DLC sample:
Deposition time: 30 min
Target current: 2.8 A
Initial vacuum degree: 1.4×10-5 Torr
Bias voltage: 30V
Thickness: ~210 nm
  The typical resistivity uniformity:
23% (sigma/mean) @25cm×25cm
The height of the carbon target is about 30cm almost the same as our sample size. It results a larger surface resistivity at the edge of the target and lower at the central area.
17
32
19
27
32
18
27
32
26
25cm × 25cm DLC sample (Sigma/mean=23%)
Surface resistivity (MΩ/□)

## Slide 5: Resistivity & thickness
Fig. 3. Resistivity vs iC4H10 gas flow
Time: 30 min
Current: 2.8A
Thickness: 210 nm
C4H10: 3 sccm
Current: 2.8A
  Surface resistivity is sensitive to the hydrogen, it can be adjusted in wide range by changing the gas flow of iC4H10 .
  It can be adjusted more precise by controlling deposition time (DLC thickness ∝ deposition time).
iC4H10 (sccm)

## Slide 6: Resistivity vs voltage
Hydrogen: 3.2 Sccm
Thickness:～1 μm
  Dependence test of resistivity with voltage applied on the DLC sample.
The resistivity became stable immediately(～10s).
Resistivity is independent with the voltage, showing the ohmic behavior.
Test system (Keithley 6487)
Resistivity vs time
Resistivity vs voltage

## Slide 7: New combined structure (Cu/DLC/APICAL/Cu)
Combined structure (Cu/DLC/APICAL/Cu)
New combined structure (Cu/DLC/APICAL/Cu) is required to make high-rate μRWELL PCB.
High rate μRWELL PCB
The copper clad on the DLC is etched to dash strips and grounded at every a few mm.
The charges collected on the DLC can be quickly released via the grounded copper strips.
Technique of depositing copper on DLC needs to be developed.
This work was supported by a RD51 common project: DLC based electrodes for future resistive MPGDs.

## Slide 8
Coating procedures:
Copper coating on DLC
Coat Chrome (~50nm) on DLC
1 min “Chrome + Cu” coating
300 min Cu coating
Structure of APICAL substrate
The surface resistivity would change after deposition of the copper due to the high temperature.
More detail about the change of resistivity with the temperature will be studied.
Before copper deposition (left). After copper deposition (right).
The temperature in the chamber after 300min copper deposition is 188 centigrade.

## Slide 9
Chrome is too thick, need a very long etching time.
“Chrome + Cu” co-deposition layer can not be etched.
Etching chromium of the μRWELL PCB
Problem of copper deposition
Problem of the current copper deposition DLC
Optimization of the copper deposition
Adjust the thickness of chrome
Adjust the thickness of “Chrome + Cu” co-deposition layer
Change the transition layer (Titanium?)

## Slide 10
THANKS