## Slide 1: Controllable Critical Current Degradation of ReBCO CC by Post-Manufacturing Deoxygenation
Griffin Bradford, Xinbo (Paul) Hu, D. Abraimov, D.C. Larbalestier
Many thanks for discussions with Tom Painter who has pursued similar ideas and to Bill Starch for essential laboratory support
A portion of this work was performed at the National High Magnetic Field Laboratory which is supported by NSF cooperative agreement DMR-1644779 and the State of Florida.
Notes: Note for Slide:

## Slide 2: Outline
Motivations for controllable degradation of coated conductors
Methods
Results
Implications for future magnet designs
Notes: Note for Slide:

## Slide 3: The large anisotropy of REBCO makes many regions of a solenoid far too stable (Weijers: 32 T experience)
Angular Dependence of ReBCO at 30T
In 32 T, Ic for central pancakes was up to 1800 A when the end pancakes had Ic ~700 A and Ioperating was 174 A
Chart: MS&T:32T:COILS:32 T in Cell 4:Data files:[Field Hysteresis.xlsx]32 T cell4 HTS Only Test 4
Operating current
~35-40 K margin
(Tcs = 40-45 K)
~ 25-30 K margin
256 A = ~10 K margin
174 A = 0 K margin
REBCO solenoids quench in the end windings where Ic ~20% of central windings due to the large Ic anisotropy
Notes: Note for Slide:

## Slide 4: How best to address highly a variable stability margin?
Mix and match conductors from various companies with natural variation of Ic
Ask one or more particular conductor manufacturers to deliver low Ic, not just high Ic conductors?
Develop a post-delivery HT to controllably degrade the Ic so that conductor bought to one specification can be repurposed as best needed
O6.9: Tc 92K
O6.5 Tc ~ 60 K
Structural and Superconducting Properties of High-Tc Superconductors, 1999, Page 25, https://inis.iaea.org/collection/NCLCollectionStore/_Public/31/009/31009747.pdf
Notes: Note for slide: Easiest way to degrade I_c is by degrading T_c by withdrawing O from Cu-O chain sites
Note for slide: Removing oxygen and degrading Tc and thus Ic is our chosen route

## Slide 5: Methodology
We chose 32 T REBCO tapes made by SuperPower with thick Cu (50 mm on each side)
HT in Ar to avoid surface oxidation in range 200-240 C to be compatible with subsequent solder treatments
Measured Tc, Ic (77 K(SF) and 4.2 K (15 T)
Heat Treatment Profile
Typical Heat Treatment Profile
Treatments done in batch mode with 0.2 m long samples
Notes: Note for Slide:

## Slide 6: Tc can be reproducibly degraded but is not yet uniform, especially for longer HT
Tc fitting done by:
  Linear Fit between 40% & 60% of maximum moment
  Linear Fit of first 10 points
  Intersection of these fits at 0 and 1
  Breadth defined as DT at 10% & 90% of maximum moment
Longer and higher temperatures give broader transitions
Lowest Tc reached was ~72 K, with a spread of ~13 K
  Still retained an Ic of 14 A at 77K (SF), originally was 119 A
  Originally, Tc was ~86 K with a spread of ~3 K
Tc Changes with Treatments
Greater deoxygenation
Notes: Note for Slide: Ar treatment can predictably lower Tc, cannot equilibrate given zero partial oxygen pressure in environment, leaves behind a distribution of T_c (see breadth) and I_c(see T_c~72K but still SC)
Note for Slide: Fitting method gives T_c < 90K, people would find it unexpected, just explain that it is due to your fitting method, make comment that T_C is usually ~90

## Slide 7: Tc is degraded controllably by HT at 200-240 C
32 hours
2 hours
4 hours
16 hours
8 hours
1 hour
210 C
220 C
240 C
230 C
200 C
Notes: Note for Slide:

## Slide 8: After deoxygenation Ic(H,4K, H‖c) was systematically degraded
α = 0.7106
α = 0.7255
α = 0.7530
α = 0.8104
α = 1.014
Control
1 h
2 h
4 h
8 h
4.2 K, 15 T | Control | 8 h @ 200 C | 8 h @ 210 C | 8 h @ 220 C | 8 h @ 230 C | 8 h @ 240 C
Ic | 145 A | 125 A | 111 A | 87 A | 65 A | 37 A
α | 0.7106 | 0.7244 | 0.7446 | 0.7796 | 0.8311 | 1.014
Notes: Note for Slide:

## Slide 9: Ic(4.2 K,15 T) can be reduced to 25% very easily
Ic (4.2K,15T) originally was 145 A
8H @ 240C  Ic = 36 A, 80% decrease!
1 hour
2 hours
4 hours
8 hours
16 hours
32 hours
200 C
210 C
220 C
230 C
240 C

## Slide 10: α Increases with Longer and Hotter Treatments
Original α = 0.7106
200 C
210 C
220 C
230 C
240 C
2 hours
4 hours
8 hours
16 hours
32 hours
1 hour
Notes: Note for Slide: Alpha changing in 4.2K show contributions from O pin defects and nano-pin defects, 77K would only show nano-pin defects as O defects are thermally disordered at 77K. David: Not clear to me now what the 77 K is pointing to – I cannot believe the BZO NR have changed – but their effect certainly has changed
Note for Slide: A large alpha means rapid loss of Jc(H) due progressively weaker vortex pinning – this is thus a direct and important conclusion of your work. The implication of the 77 K changes is that the loss is NOT just due to point pinning loss but also to BZO NR loss too – this is interesting. I do not understand it and it deserves more study.

## Slide 11: Deoxygenation causes marked vortex pinning changes: 77 K, 1 T
Untreated
32 h @ 200C
8 h @ 240C
32 h @ 200C
8 h @ 240C
Notes: Note for Slide: you can say that TEM is planned but we do not expect the BZO-NR to have disappeared. We do know that the O-defect landscape has changed greatly as a result of pulling out O and also that Hc has dropped significantly so changing the pinning landscape significantly
Note for Slide: There is a marked loss of the c-axis pinning peak normally associated with alignment of vortices with the BaZrO3 nanorods (BZO-NR)

## Slide 12: YateStar: Degradation of properties over 50 cm seems to be quite uniform
Hall Array Plot of Ic(x,y) of tape subjected to 2H @ 250C
Initial defects are not exacerbated but do remain
c-axis Ic(77K,0.6T) is more affected than ab- plane Ic
Notes: Note from David: I find the 2nd bullet to be very interesting. I think that c-axis of BZO is about 7% more than optimally doped YBCO – c-axis INCREASES as O is taken out, reducing the mismatch – can you find out by how much? The intriguing possibility s that point defect distribution changes after more O is withdrawn – also that the thermodynamic Hc goes down strongly, reducing the pinning potential scale (0.5 muzeroHcsquared)

## Slide 13: Ic Surface Plots show smooth, progressive nature of the changes
Ic (4.2K,15T) originally was 145 A
8H @ 240C  Ic = 36 A, 80% decrease!
% of Original Ic vs B shows near linear dependence on B
Notes: Note for Slide:

## Slide 14: Observed Current Transfer Resistance @ 4K
No resistance seen at 77 K but all thick Cu 32 T samples showed it at 4.2 K
A thin Cu samples did NOT show R – so what?
  We presently interpret this as being caused by a more resistive REBCO-Ag interface.
  We do not believe this is inherent and it may even be useful in enhancing the quench propagation velocity
Levin, G A, et al. “The Effects of Superconductor–Stabilizer Interfacial Resistance on the Quench of a Current-Carrying Coated Conductor.” Superconductor Science and Technology, vol. 23, no. 1, 2009, p. 014021., doi:10.1088/0953-2048/23/1/014021.
Notes: Note for Slide:

## Slide 15: Ic loss is clearly by outward diffusion of oxygen
Ic loss is pretty well predicted by an Arrhenius plot with Q = 0.9 eV/atom
Ic loss correlates well to Tc loss
Notes: Note for slide:

## Slide 16: So what? 32 T could have had a uniform Ic across all pancakes, simplifying quench protection
Suppose we treat at 200 C for 36 hours
And treat this at 200 C for 30 hours
Standard Deviation of Ic ~ 354 A
With this method, a controllable degradation treatment for a given tape can be developed, allowing for Ic reduction in various parts of a magnet
The increased resistance could prove to be beneficial
More control over ReBCO in possession, not limited to its manufactured Ic
Simple and easily reproducible
Standard Deviation of Ic ~ 92 A
Notes: Note for Slide:

## Slide 17: Additional Thanks
Huub Weijers for the helpful plots of the 32T
All ASC members and graduate students for all their support
Notes: Note for Slide:

## Slide 18: END
Notes: Note for Slide:

## Slide 19: 20 Samples with varying HT from 4 h/200 C to 8h/240 C
20 samples were treated:
  4,8,16,32 h @ 200 C
  4,8,16,32 h @ 210 C
  2,4,8,16 h @ 220 C
  1,2,4,8 h @ 230 C
  1,2,4,8 h @ 240 C
  All vacuum-pumped, backfilled with Argon, and treated in flowing Argon
Temperature reached in ~ 1 hour
  All treatments follow this profile
  Allowed to cool-down to ~30 C in Argon before removing from furnace
All samples had Tc and Ic characterization
Treatment Profiles – 240 C
Treatment Profiles – 200 C
Notes: Note for Slide:

## Slide 20: Ic(4.2 K,5 T) versus Temperature and Duration

## Slide 21: Ic(4.2 K,10 T) versus Temperature and Duration