## Slide 1: Construction and Power Test of the Superferric Skew Quadrupole for HL-LHC
Marco Statera
INFN Milano - LASA

## Slide 2: OUTLINE
Scope: the High Order correctors magnets
Design
Construction and power test
Electrical failure
Second assembly and power test
Conclusions

## Slide 3: High Luminosity LHC
LHC integrated luminosity 300 fb-1 by 2023
HL LHC
  upgrade interacting regions 2024/26
  3000 fb-1 integrated luminosity by 2038
CERN courtesy

## Slide 4: THE LOW BETA SECTION
a2
73.6 m
IP
b6
a6
b5
a5
b4
a4
b3
a3
by P. Fessia
and the High Order Correctors

## Slide 5: HO CORRECTOR MAGNETS ZOO
MCQSXFP1
OD460
a5
b5
Tested 2018
MCDXFP1
a6
b6
Tested 2018
MCTXFP1
a2
a3
b3
Tested 2016
MCSXFP1
OD320
a4
b4
MCOXFP1
Tested 2017
tested 2019
design construction test
5 protoptypes
54 series magnets
MgB2 demonstrator
S. Mariotto
Tue-Af-Po2.18-06

## Slide 6: SUPERFERRIC DESIGN
NbTi superconding coils
Racetrack
Insulation by S2 glass reinforced material
Superferric design
Compact and modular
Strong contribution of the iron poles
Field quality influenced by the shape of the poles
magnet | Ic @ 4.2 K | Margin @4.2 K | Margin @1.9K
4P S | 315.5 A | 42.3 % | 57.1 %
6P | 225.5 A | 53.4 % | >60 %
8P | 230.2 A | 54.4 % | >60 %
10P | 255.7 A | 58.9 % | >60 %
12P N | 232.6 A | 54.9 % | >60 %
12P S | 230.2 A | 54.4 % | >60 %
Quench protection
No energy extraction (but 4P)
60% margin @ 1.9 K
Longitudinal dimension
Quench protection
Small dimension: 84kN series production (6 magnets)
constraints
coils
ARMCO iron
wedges
pole
CuBe rods

## Slide 7: MCQSXFP1
length | 538 mm
integrated field @ In @ r50 mm | 0.700 Tm
magnetic length | 401.1 mm
energy @Inom | 30.8 kJ
harmonics | B6= -30 U at low current B6= 30 U at Iop B10= -8 U ÷ -12 U
OD 460 mm
538 mm
connections on a PCB board (Arlon N85)
Inom= 182 A
COILS
  754 windings
  815 m of F 0.7 mm NbTi

## Slide 8: EM DESIGN
nominal current 174 A - field integral 0.7 Tm
ultimate current 197 A
modifed ideal pole shape
(wire EDM laminations)
QUENCH protection
OPERA + QLASA
1.5 W dump ressitor
ground in the middle
max temperature 145 K
max voltage 235 V
nominal
4.2 K
1.9 K

## Slide 9: Assembly
Saes Rial Vacuum
Dec. 2018
frame
frame
wedge
CuBe rod
CuBe rod
pcb
alignemnt rods
bridge to connection box

## Slide 10: First Cooldown and Energization
B2
B4
B3
B2
B3
B1
B1
B3
B2
B3
B3
B4
B2
B1
B1
Training up to nominal
Electrical problem
Event n.13 B4
Precursor
Recovered transitions in different coils
precursor

## Slide 11: Event n.15
deviation from standard decay
zero measured current
energy extraction

## Slide 12: Damaged Coil
B1
bridge
B3

## Slide 13: Numerical Model
Discharges between output wire and windings
Inner layers not damaged
Numerical model implemented
in LTSpice, Netlist forma (M. Prioli)
Coil 1 split into two parts:
  Coil 1A: 7 high-field layers bypassed by a short-circuit
  Coil 1B: 19 layers normally in series with the rest of the circuit
Mutual inductance matrix (5 x 5) computed in Opera
(S. Mariotto)
Quench originated in the high-field zone (Coil 1A)
  The resistance is not evenly distributed between coil 1A and coil 1B
  Simulated distribution is 37% for coil 1A and 63% for coil 1B
The short resistance is a variable
  It is initially high (~10 ), then decreases due to a local welding (~0 ) then increases (~1 )

## Slide 14: Numerical Model: Results
~10 
~0 
~1 
No short
Current decay deviation

## Slide 15: Two New Coils
all coils compliant
the 2 new coils installed
BTS2 foil
S2 tape
Machined from bulk
In & out
1.0 mm
0.15 mm
sheet

## Slide 16: Second Assembly Assessment
Coil
Geometry
HV ground insulation (2,5 kV)
Wire-wire insulation, turns
All coils are compliant
Magnet
Laminations’ profiles and slits
Alignment of the assembly
HV ground insulation of the magnet (up to 2 KV)
+ shorted winding
procedures validated
second assembly
coil replacement

## Slide 17: Power Test
Most quenches in new coils
Good stability after reaching 200 A (> Iult 197 A)
Stable 1 h @ ultimate after thermal cycle

## Slide 18: MAGNETIC FIELD AND INDUCTANCE
S. Mariotto
Single Hall Probe
Low accuracy positioning
Field quality measurement at LASA in 2019
several ramps
two assembly
Dinamic inductance measured during current ramps
several ramps

## Slide 19: Conclusion
The HL-LHC skew quadrupole corrector magnet was successfully designed and assembled
First power test had an electric failure
  The fault has been identified
  A mitigation was applied even if all the non damaged coils are compliant, also for series production
  New quality test introduced
Second assembly power test showed good results: ultimate current reached, stabiliity test (1 h @ultimate), good quench memory
Procedures validated
All High Order Correctors protoypes tested

## Slide 20
INFN & UNIMI - LASA team
F. Alessandria, G. Bellomo, F. Broggi, S. Mariotto, A. Paccalini, A. Pasini, D. Pedrini, A. Leone, M. Quadrio, M. Prioli, M. Sorbi, M. Statera, M. Todero, C. Uva
CERN A. Musso, E. Todesco
SAES getters M. Campaniello, P. Manini
SAES Rial Vacuum M. Canetti, F. Gangini
RODOFIL A. Zanichelli
Ph. by G. Fornasier
THANK YOU