## Slide 1
Production and use of inorganic scintillators
Jiri Parizek
Technology application specialist
parizek@crytur.cz
Krakow
April 1, 2019
Notes: 1

## Slide 2
CRYTUR History
Company portfolio
Crystal growing
Materials and processing
Company portfolio
Imaging systems and scintillation screens
Ionizing radiation detection units
Summary
Contents

## Slide 3
CRYTUR, spol s r.o.
Notes: 3
3

## Slide 4
Tradition in crystal growing and processing
1943-1952
1952-1966
1966-1992
1992-1995
1995-1998
1998-
Notes: 4
4

## Slide 5
200 employees
SME status
11 mil. EUR turnover
ISO 9001 certified
Advanced customer audit
CRYTUR
Experience & quality
Our own unique material processed in several advanced steps to complex product with the support of our strong R&D team, with the quality assurance over the complete supply chain.
Notes: 5
5

## Slide 6
Modern production facility - Na Lukách
CRYSTAL
GROWING
EXTENSION 2015
ADMIN
+
CNC MACHINING
RESEARCH
CENTER
02/2013
CLEAN ROOM
+
COATING
MACHINING
+
QUALITY CONTROL
CLEAN ROOM
+
MACHINING
+
ADMIN
2017
CRYTUR
Experience & quality

## Slide 7
New production facility - Koškova
Currently:
PbWO4 project
Induction growing
Precision optics
Plan:
Crystal growing
CNC machining
CRYTUR
Experience & quality

## Slide 8
MATERIALS
(grown as single-crystals)
Garnets YAG and LuAG
Perovskites YAP
Silicates, Tungstates (PWO)
Dopants: Ce, Nd, Tm, V, Yb, Pr, Er, Cr
Notes: 8
8

## Slide 9
CRIG (Crystal Improved Growth)
Based on Czochralski method
Patent EP 2675944
  6 l crucibles
  Tungsten crucible
  H2 atmosphere
  Special inside configuration
Strictly controlled process
Homogenous crystal ingots
TECHNOLOGIES
– Crystal Growth
Melting of oxide material
Introducing seed to the melt
Beginning of the crystal growth
Crystal pulling
Crystal boule cooling

## Slide 10
„World largest YAG stress-free crystals“
Diameter up to 6 inch
Weight up to 14 kg
Stress-free core
TECHNOLOGIES
– Crystal Growing

## Slide 11
Cutting (OD, ID, single and multi-wire)
Characterization (QC)
Grinding, Lapping, Polishing, CNC machining
Assembly and packing
Quality check (QC)
Process diagram
Manufacturing
ISO 7 – ISO 5 grade

## Slide 12
El. microscope, interferometers, spectrometers 0.2-5 μm,
XRD, 3D structural analysis, X-ray fluorescence etc.
back-up characterization techniques at university groups
Quality check

## Slide 13
BSE detection in electron microscopy – global market majority
Complete detection systems
Product line
ELECTRON MICROSCOPY
Rebeka
Karmen
Notes: 13
13

## Slide 14
14
Light conversion elements for LEDs
and laser diodes
White-LED conversion
Full light conversion elements
Optical elements
Remote laser excitation
Product line
LUMINOPHORES
Notes: 14
14

## Slide 15
Product line
SAPPHIRE AND
PRECISSION OPTICS
High precision crystal optics (sapphire, garnet)
Sapphire tubes and rods (Temperature measurement probes, ultra-high pressure probes, lightguides, laboratory equipment)
High precision ceramics
UV-light gemstone
Complex shapes,
high precision,
perfect surfaces
Notes: 15
15

## Slide 16
Laser rods primarily for medical and defence industries
Specialty materials – YAP, YAG, LuAG with Nd, Tm, V, Yb, Pr, Er, Cr, BaWO4...
Bonding, angles
Product line
LASERS
Notes: 16
16

## Slide 17
Scintillators & Detectors
X-ray imaging
Single photon counting
X-ray / γ-ray
neutron
Integrated solutions
Multipixel detector
Electron detector
Fiber detectors
Notes: 17
17

## Slide 18
Imaging screens
In Frames
On Substrates
Free-Standing
Optical inhomogeneity <5 %
Optical quality (S/D 0/0)
High light output
Excellent Radiation Hardness*
Long life-time
Chemical & Mechanical stability
Coatings & lithography patterns
*M. T. Lucchini et al. "Radiation Tolerance of LuAG:Ce and YAG:Ce Crystals Under High Levels of Gamma- and Proton-Irradiation," in IEEE Transactions on Nuclear Science, vol. 63, no. 2, pp. 586-590, April 2016.

## Slide 19
Imaging screens

## Slide 20
Scintillator | Emission wavelength [nm] | Density [g.cm-3] | Cleavage/ Hygroscopic | Photon Yield [ph/keV] | Decay [ns]
YAG:Ce | 550 | 4.55 | No/No | 35 | 70
LuAG:Ce | 535 | 6.73 | No/No | 25 | 70
LuAG:Pr | 315 | 6.73 | No/No | 19 | 20
CRY19 | 420 | 7.1 | Yes/No | 32 | 41
YAP:Ce | 370 | 5.37 | No/No | 25 | 25
CRY18 | 425 | 4.5 | Yes/No | 32 | 45
CsI:Tl | 565 | 4.51 | No/Yes | 45 | 900
GOS:Tb | 544 | 7.34 | -/No | 60 | 106
CWO | 475 | 7.9 | Yes/No | 12-15 | 5000
BGO | 480 | 7.13 | No/No | 8-10 | 300
Scintillation Materials
Imaging screen standards
YAG:Ce
Literature ~8 - 12 ph/keV
Theoretical value ~41 ph/keV
CRYTUR
~35 ph/keV

## Slide 21
LY Temperature Dependence
Imaging screens
Non-proportional response
*Khodyuk, Hass, Dorenbos „Nonportional response between 0.1-100 keV energy by means of highly monochromatic synchroton X-rays," in IEEE Transactions on Nuclear Science, vol. 57, .No. 3, June 2010.

## Slide 22
The scintillating single-crystals YAG:Ce an YAP:Ce exhibit very stable light output at wide range of temperatures and high radiation dose.
LY Temperature Dependence
Imaging screens
LY temperature depence

## Slide 23
YAG:Ce proton irradiation
Measurement performed at CERN
*M. T. Lucchini et al. "Radiation Tolerance of LuAG:Ce and YAG:Ce Crystals Under High Levels of Gamma- and Proton-Irradiation," in IEEE Transactions on Nuclear Science, vol. 63, no. 2, pp. 586-590, April 2016.

## Slide 24
YAG:Ce gamma irradiation
Measurement performed at CERN
*M. T. Lucchini et al. "Radiation Tolerance of LuAG:Ce and YAG:Ce Crystals Under High Levels of Gamma- and Proton-Irradiation," in IEEE Transactions on Nuclear Science, vol. 63, no. 2, pp. 586-590, April 2016.

## Slide 25
Scintillation Materials
New materials R&D
GAAG+
High density: 6.6 g/cm3
Light yield => lum. decay
Max. diameter 50 mm
Target: up to 70 mm
Optimization
in progress

## Slide 26
Scintillation Materials
New materials R&D
CRY060
~0.5 µm active layer on substrate
Emission: 410 nm
Fast ~ns
High photon LY
Applications
Imaging screen (EUV, X-rays)
Electron detection
TOF detectors
Mass spectrometry

## Slide 27
Single crystal vs powder
Single crystal
LuAG:Ce screen
20 um
Powder screen
P43 (GOS)
20 um (2um grain)
8 um
100 um

## Slide 28
Imaging Systems
Imaging systems - CRYCAM
Features
  Macro vs Micro system
  Perfect contrast (single crystal screens)
  Outstanding intrinsic resolution (1 µm)
  Highly customized (FOV up to 35 x 35 mm)
  Multiple imaging options
  OEM or end-user solution
Micro system
Application
  X-ray radiography
  X-ray tomography
  X-ray topography
  Beam viewer
Macro system

## Slide 29: X-ray radiography
Point-like
X-ray source
Imaging
X-ray detector
Object
Enlarged projection

## Slide 30
Imaging Systems
CRYCAM examples
Wasp on foam pedestal

## Slide 31
Imaging Systems
CRYCAM examples
Sting - detail

## Slide 32
Imaging Systems
CRYCAM examples
Poppy head
Carbon fiber reinforced polymer

## Slide 33
Imaging Systems
CRYCAM examples
Phase contrast!
Carbon Fibers, 7 µm
  Microfocus X-ray source
  1 µm spot
  Small focus to
  object distance

## Slide 34
Imaging Systems
CRYCAM examples
Cotton Stick – 3D tomography

## Slide 35
Imaging Systems
New design – FOP based cameras
Features
  Medium resolution down to 15-20 µm
  Improved light collection efficiency
  High speed acquisition
  Perfect contrast (single crystal screens)
  FOV 16 x 14 mm / 32 x 28 mm
  Multiple scintillator accessories
  OEM or end-user solution
FOT based system example
Related services
  Bonding to CCD (CCD/fiber optics/scintillator)
  Custom design

## Slide 36
Imaging Systems
FOP based camera example
CsI:Tl – HR version
LuAG screen
  Cu target, 40kV, 2 W

## Slide 37
Imaging Systems
Applications
  Medical applications (PET)
  Calorimeters
Tungsten shielded array of inorganic fibers
  Tailored solution
  Dimension: 13 x 13 x 100 mm3
  6 x 6 array of 1 x 1 mm2 fibers
  High resistence to radiation damage
  Very good light yield
Fiber materials
  YAG:Ce, LuAG:Ce
  New: LuAP:Ce (faster than LYSO:Ce)
Scintillators & Detectors
Matrix detectors example – special solutions

## Slide 38
X-ray / γ-ray detector family
LGD – γ-ray detector
X-ray detector
(counting / spectroscopy)
HT – X-ray detector for
high temperature environment

## Slide 39
X-ray detector
  Features
  Innovative YAP:Ce technology => Non-toxic substances (e.g. Be)
  Counting and spectroscopy
  Properties
  Energy range of 5 keV to 150 keV (50 % absorption)
  High count rate up to 106 pulses/s
  Detection area: Ø 37 mm (Ø 1.45 inch)
  Magnetic shielding: Mu-metal
  Application
  X-ray diffraction
  X-ray fluorescence
  DXA (double-energy X-ray analysis)
Chart: Energy [keV]
| 0 | 0.34482758620689657 | 0.68965517241379315 | 1.0344827586206897 | 1.3793103448275863 | 1.7241379310344829 | 2.0689655172413794 | 2.4137931034482758 | 2.7586206896551726 | 3.103448275862069 | 3.4482758620689657 | 3.7931034482758621 | 4.1379310344827589 | 4.4827586206896557 | 4.8275862068965516 | 5.1724137931034484 | 5.5172413793103452 | 5.862068965517242 | 6.2068965517241379 | 6.5517241379310347 | 6.8965517241379315 | 7.2413793103448274 | 7.5862068965517242 | 7.931034482758621 | 8.2758620689655178 | 8.6206896551724146 | 8.9655172413793114 | 9.3103448275862064 | 9.6551724137931032 | 10 | 10.344827586206897 | 10.689655172413794 | 11.03448275862069 | 11.379310344827587 | 11.724137931034484 | 12.068965517241379 | 12.413793103448276 | 12.758620689655173 | 13.103448275862069 | 13.448275862068966 | 13.793103448275863 | 14.13793103448276 | 14.482758620689655 | 14.827586206896552 | 15.172413793103448 | 15.517241379310345 | 15.862068965517242 | 16.206896551724139 | 16.551724137931036 | 16.896551724137932 | 17.241379310344829 | 17.586206896551726 | 17.931034482758623 | 18.27586206896552 | 18.620689655172413 | 18.96551724137931 | 19.310344827586206 | 19.655172413793103 | 20 | 20.344827586206897 | 20.689655172413794 | 21.03448275862069 | 21.379310344827587 | 21.724137931034484 | 22.068965517241381 | 22.413793103448278 | 22.758620689655174 | 23.103448275862071 | 23.448275862068968 | 23.793103448275861 | 24.137931034482758 | 24.482758620689655 | 24.827586206896552 | 25.172413793103448 | 25.517241379310345 | 25.862068965517242 | 26.206896551724139 | 26.551724137931036 | 26.896551724137932 | 27.241379310344829 | 27.586206896551726 | 27.931034482758623 | 28.27586206896552 | 28.620689655172416 | 28.96551724137931 | 29.310344827586206 | 29.655172413793103 | 30 | 30.344827586206897 | 30.689655172413794 | 31.03448275862069 | 31.379310344827587 | 31.724137931034484 | 32.068965517241381 | 32.413793103448278 | 32.758620689655174 | 33.103448275862071 | 33.448275862068968 | 33.793103448275865 | 34.137931034482762 | 34.482758620689658 | 34.827586206896555 | 35.172413793103452 | 35.517241379310349 | 35.862068965517246 | 36.206896551724142 | 36.551724137931039 | 36.896551724137929 | 37.241379310344826 | 37.586206896551722 | 37.931034482758619 | 38.275862068965516 | 38.620689655172413 | 38.96551724137931 | 39.310344827586206 | 39.655172413793103 | 40 | 40.344827586206897 | 40.689655172413794 | 41.03448275862069 | 41.379310344827587 | 41.724137931034484 | 42.068965517241381 | 42.413793103448278 | 42.758620689655174 | 43.103448275862071 | 43.448275862068968 | 43.793103448275865 | 44.137931034482762 | 44.482758620689658 | 44.827586206896555 | 45.172413793103452 | 45.517241379310349 | 45.862068965517246 | 46.206896551724142 | 46.551724137931039 | 46.896551724137936 | 47.241379310344826 | 47.586206896551722 | 47.931034482758619 | 48.275862068965516 | 48.620689655172413 | 48.96551724137931 | 49.310344827586206 | 49.655172413793103 | 50 | 50.344827586206897 | 50.689655172413794 | 51.03448275862069 | 51.379310344827587 | 51.724137931034484 | 52.068965517241381 | 52.413793103448278 | 52.758620689655174 | 53.103448275862071 | 53.448275862068968 | 53.793103448275865 | 54.137931034482762 | 54.482758620689658 | 54.827586206896555 | 55.172413793103452 | 55.517241379310349 | 55.862068965517246 | 56.206896551724142 | 56.551724137931039 | 56.896551724137936 | 57.241379310344833 | 57.586206896551722 | 57.931034482758619 | 58.275862068965516 | 58.620689655172413 | 58.96551724137931 | 59.310344827586206 | 59.655172413793103 | 60 | 60.344827586206897 | 60.689655172413794 | 61.03448275862069 | 61.379310344827587 | 61.724137931034484 | 62.068965517241381 | 62.413793103448278 | 62.758620689655174 | 63.103448275862071 | 63.448275862068968 | 63.793103448275865 | 64.137931034482762 | 64.482758620689651 | 64.827586206896555 | 65.172413793103445 | 65.517241379310349 | 65.862068965517238 | 66.206896551724142 | 66.551724137931032 | 66.896551724137936 | 67.241379310344826 | 67.58620689655173 | 67.931034482758619 | 68.275862068965523 | 68.620689655172413 | 68.965517241379317 | 69.310344827586206 | 69.65517241379311 | 70 | 70.344827586206904 | 70.689655172413794 | 71.034482758620697 | 71.379310344827587 | 71.724137931034491 | 72.068965517241381 | 72.413793103448285 | 72.758620689655174 | 73.103448275862078 | 73.448275862068968 | 73.793103448275858 | 74.137931034482762 | 74.482758620689651 | 74.827586206896555 | 75.172413793103445 | 75.517241379310349 | 75.862068965517238 | 76.206896551724142 | 76.551724137931032 | 76.896551724137936 | 77.241379310344826 | 77.58620689655173 | 77.931034482758619 | 78.275862068965523 | 78.620689655172413 | 78.965517241379317 | 79.310344827586206 | 79.65517241379311 | 80 | 80.344827586206904 | 80.689655172413794 | 81.034482758620697 | 81.379310344827587 | 81.724137931034491 | 82.068965517241381 | 82.413793103448285 | 82.758620689655174 | 83.103448275862078 | 83.448275862068968 | 83.793103448275858 | 84.137931034482762 | 84.482758620689651 | 84.827586206896555 | 85.172413793103445 | 85.517241379310349 | 85.862068965517238 | 86.206896551724142 | 86.551724137931032 | 86.896551724137936 | 87.241379310344826 | 87.58620689655173 | 87.931034482758619 | 88.275862068965523 | 88.620689655172413 | 88.965517241379317 | 89.310344827586206 | 89.65517241379311 | 90 | 90.344827586206904 | 90.689655172413794 | 91.034482758620697 | 91.379310344827587 | 91.724137931034491 | 92.068965517241381 | 92.413793103448285 | 92.758620689655174 | 93.103448275862078 | 93.448275862068968 | 93.793103448275872 | 94.137931034482762 | 94.482758620689651 | 94.827586206896555 | 95.172413793103445 | 95.517241379310349 | 95.862068965517238 | 96.206896551724142 | 96.551724137931032 | 96.896551724137936 | 97.241379310344826 | 97.58620689655173 | 97.931034482758619 | 98.275862068965523 | 98.620689655172413 | 98.965517241379317 | 99.310344827586206 | 99.65517241379311 | 100 | 100.3448275862069 | 100.68965517241379 | 101.0344827586207 | 101.37931034482759 | 101.72413793103449 | 102.06896551724138 | 102.41379310344828 | 102.75862068965517 | 103.10344827586208 | 103.44827586206897 | 103.79310344827587
55Fe@5,9keV | 0 | 0 | 500 | 1500 | 5000 | 12000 | 19747 | 27420 | 36653 | 47168 | 58501 | 68786 | 78051 | 85522 | 92475 | 95218 | 96036 | 93967 | 89167 | 83156 | 75561 | 67968 | 58835 | 50587 | 43002 | 35367 | 28938 | 23283 | 18247 | 14028 | 10585 | 8229 | 6273 | 4619 | 3259 | 2383 | 1722 | 1279 | 953 | 619 | 466 | 350 | 235 | 58

## Slide 40
LGD – γ-ray detector
  Features
  Scintillation detector based on YAP:Ce scintillation crystal
  Energy resolution (FWHM) ≤ 5.5 % … 137Cs@662 keV
  Energy resolution (FWHM) ≤ 18% … 241Am@59.9 keV
  No intrinsic background
  Fast detector for high count rate applications
  Minimal energy non-proportionality (max. 3 %)
  Properties
  Energy range of 20 keV to 800 keV (@50 % absorption)
  Detection area: Ø 44 mm (Ø 1.45 inch )
  Typical voltage 700 V
  Magnetic shielding: Mu-metal
  Application
  Spectroscopy with high resolution
Chart: Channel

## Slide 41
X-ray detector for HT
  Features
  High temperature resistivity up to 175 °C
  Ruggedized detector for harsh operating conditions
  Fast response
  All parts of the unit adapted for HT
  Application
  Densitometry at high temperatures
  Geology
  Level gauges
Chart: Temperature [°C]
| 25.76 | 35.44 | 53.9 | 73.740000000000009 | 93.740000000000009 | 113.78 | 133.80000000000001 | 150.78 | 175
YAP:Ce + HT PMT | 1 | 0.96447 | 0.92217 | 0.86889 | 0.80466 | 0.73346 | 0.65368 | 0.57412 | 0.4651
LuAG(Ce) + HT PMT | 1 | 1.0462 | 1.1769 | 1.2529 | 1.2205 | 1.1023 | 0.94157 | 0.79326 | 0.63105

## Slide 42
Summary
CRYTUR = reliable partner in scintillators and integrated solution
Niche application with single crystals and precise technologies
Long-term collaboration with international institutes
New opportunities welcome
Notes: 42
42

## Slide 43
Thank you for your attention!
Contacts:
CRYTUR, spol. s r.o.
Na Lukách 2283
511 01 Turnov
Czech Republic
crytur@crytur.cz
Jiri Parizek
Technology application specialist
parizek@crytur.cz
Notes: 43