## Slide 1: Beam impact response of irradiated materials M. Tomut* P. Simon, P. Bolz, P. Drechsel, A. Prosvetov, C. Trautmann, A. Schlüter, Ch. Kuhn, R. Müller, R. Knöbel, H. Weick, M. Guinchard, A. Bouvard, F.Harden, Y. Kadi * GSI, Darmstadt, Germany, Institute for Materials Physics, University of Münster, University of Kaiserslautern, Germany CERN

## Slide 2
Outline
Role of microstructure in materials response to beam impact
Radiation- induced target material degradation:
                swelling
                thermal diffusivity
                hardening- new stress-concentrators
                microimpact studies
                - dynamic hardness, damping, fatigue
                damage recovery at high temperature
Dynamic response in context of radiation damage
Simulations of dynamic thermal fracture of targets in the context of radiation damage

## Slide 3
FlexMat experiment at HiRadMat-
- Graphitic materials response to beam impact
- applications for high power targets and beam dumps
283 beam pulses
total of 1.24E15 pot
up to 1.3E11 ppb
FlexMat - June 2018
HiRadMat@SPS, CERN
FlexMat mounting in SPS tunnel at CERN
Role of microstructure
in materials response to beam impact

## Slide 4: Beam impact response of graphite - microstructure influence
1 μm
7 μm
10 μm
20 μm
Polycrystalline graphites with different grain sizes
LDV signal- velocities

## Slide 5: Beam impact response of other graphitic materials
PG / 1 μm
2D CFC
POCO Foam
3D CFC

## Slide 6
Radiation- induced thermo-mechanical
properties degradation

## Slide 7: Beam- induced swelling in graphite
Leads to additional stress at the edge of the beam spot on target
Swelling mechanism in irradiated graphite;
defect creation
Swelling measurements-profilometry

## Slide 8: Effects of beam- induced degradation of thermal diffusivity of graphite
Thermal simulation shows cooling problem with radiation-damaged graphite: - degradation of thermal diffusivity: 70-40 W/(m K) -> 15 W/(m K)
Super-FRS Beam Catchers
Tmax - 2500 K
radiation-damaged graphite
beam
Tmax - 900 K
pristine graphite
beam
(Ronja Knöbel, Helmut Weick, Super-FRS)

## Slide 9: Ion beam induced hardening in graphite
Hardness
E modulus
Hardness / E modulus
Dependence
on dE/dx
4.8 MeV/u
Xe → U

## Slide 10: Microimpact tests– derived parameters

## Slide 11: Microimpact tests- achieved strain rates

## Slide 12: Microimpact – dynamic hardness and damping evolution with fluence
Dynamic hardness
Damping constant
 | Strain rate [s-1]
Quasi static indentation | 10-2 to 10-1
Nanoimpact | 104
Ion beam impact | 103 to 105

## Slide 13: Multiple microimpact on irradiated graphite- fatigue
Cube Corner 20 mN max load; comparison pristine and irradiated samples
Time [s]
Depth [nm]
Fracture
Fatigue period
pristine
Irradiated, 7E13 Au i/ cm2
Embrittlement

## Slide 14
How to mitigate radiation damage effects in graphite
(production targets and beam catchers materials)
Young modulus
    at T> 900 ºC  beneficial effect on recovery of thermo-mechanical properties
      thermal diffusivity reaches 30 % of the pristine value (1500 ºC)
      Young modulus reaches pristine value
thermal diffusivity
Damage recovery by - operation at high temperatures (> 900 ºC)
- post-irradiation annealing
F. Pellemoine et al., Nucl.Inst.Meth.B, (2015) DOI:10.1016/j.nimb.2015.09.007
C.Hubert et al., Nucl.Inst.Meth.B, (2015) DOI:10.1016/ j.nimb.2015.08.056
DSC – defect annealing

## Slide 15
Dynamic response in context of radiation damage
-experiments with 4.8 MeV/u U at UNILAC, GSI

## Slide 16: Experimental details Irradiation parameters & set-up
Beam parameters
  4.8 MeV/u U28+
  Up to 1.5×1010 i/cm2 per pulse
  Up to fluences of 1×1014 i/cm2
IR camera
LDV
high-current mode (MEVVA source)
1-2 Hz
100-200 µm length of macropulse
100 µs
1 s

## Slide 17: Vibration of a disc – beam modified material in the central beam spot
Animation - Dr. Dan Russell, Grad. Prog. Acoustics, Penn State
vibration with one circular node
pristine sample
vibration with two circular nodes
modified material in the beam spot
vibration with one circular node
and one diameter node – beam hits eccentric

## Slide 18: Oscillation monitoring as a function of fluence
With radiation damage accumulation:
  Additional reflection at irradiated / non-irradiated interface
increase of frecquency
increase of damping
decrease of velocity
Polycrystalline isotropic graphite 140 μm
Target failure

## Slide 19: Measured maximum velocities - LDV
Decrease of maximum velocity with accumulated dose:
  Radiation damage:
  density reduction in beam spot
  internal friction
  plastic deformation processes

## Slide 20: Failure of graphite exposed to pulsed GeV 238U beam - accelerated radiation damage
5x1014 i/cm2 1014 i/cm2 1013 i/cm2 5x1012 i/cm2
radiation damage
 swelling
creep
stress concentrators + fatigue  crack
238U, 1.14 GeV; 1.5 x1010 i/pulse ; 150 µs, 1 Hz

## Slide 21
Simulations of dynamic thermal fracture of targets in the context of radiation damage

## Slide 22: Phase field modelling of brittle fracture induced by pulsed beams
Smooth field s approximates cracks
Set of coupled PDEs determines deformation, heat transfer and fracturing

## Slide 23: Fracturing of irradiated graphite cylinders at different beam-spot temperatures – Hoop stress

## Slide 24: Fracturing of irradiated graphite cylinders at different beam-spot temperatures

## Slide 25
Conclusions and Outlook
Dynamic response of irradiated materials to intense, short-pulse beam show in general earlier failure in the material that accumulated radiation damage
A complex puzzle has to be assembled as not all effects of accumulated dose and high beam intensity have a detrimental effect on the target lifetime
A concerted campaign, bringing together facilities for materials irradiation, materials characterization and those providing high-intensity pulsed beams, such as HiRadMat is needed
Mitigation of earlier failure by using functionally graded materials and components

## Slide 26
Too much stress ?
Thank you for your attention!