## Slide 1: Displacement cross section measurements at HiRadMat
International HiRadMat Workshop at CERN 10 Jul 2019
(JAEA/J-PARC) Shin-ichiro. Meigo,
H. Matsuda, Y. Iwamoto,
S. Hasegawa, F. Maekawa,
H. Iwamoto
(KEK/J-PARC) M. Yoshida, T. Nakamoto, T. Ishida,
and S. Makimura
Present study includes the results of “Measurement of displacement cross section at J-PARC for structural material utilized at ADS” entrusted to JAEA by MEXT

## Slide 2: Contents
Introduction
  Present and future plan of J-PARC
Displacement cross section experiment at J-PARC
Experiment at HiRadMat
Summary

## Slide 3
Neutron beam lines (23)
Bird’s eye photo
Transmutation
Facility (TEF)
(Phase II）
Hadron Experiment Facility
Neutrino Exp. Facility
(294km to Super KAMIOKANDE)
Materials & Life Science Facility (MLF)
3GeV Synchrotron
RCS (25Hz,1MW)
Linac
400MeV(50mA)
JRR-3M
800m to MLF
30GeV Synchrotron
MR (0.75MW)
J-PARC = Japan Proton Accelerator Research Complex
JFY2007 Beam
JFY2008 Beam
JFY2009 Beam

## Slide 4: Targets in Material Life Experimental Facility (MLF)
Muon production target
  Carbon graphite
  Highest μ- intensity
Neutron production target
  Mercury (Hg)
Thick. 2cm
Diam. Φ33cm
L 2m
W 34cm
SS container
Ptron
Hg
Light water
Safety hull
Double wall: Helium layer observed radiation
Highest pulse intensity in the world
8% beam loss

## Slide 5
Target for high-intensity hadron accelerator and superconductor in high radiation area
Proton beam window in J-PARC spallation neutron source: Aluminum alloy (f 0.6 m)
T2K beam window
Titanium alloy (Ti-6Al-4V)
SC magnet system in beam line of COMET (J-PARC)
For damage estimation of beam intercepting material, DPA is utilized based on displacement cross section.
High accuracy of the displacement cross-section is required.
Proton
3 GeV
Proton 30 GeV
Resistivity change due to radiation is crucial for Superconductor(SC) magnet sustaining damage.

## Slide 6: ADS proposed by JAEA
~ 30 MW
Beam window
Beam window: 20 dpa/year. Accuracy of dpa is required for damage estimation.
Belgium ADS program MYRRHA at SCK・CEN (Mol) approved 558 M€

## Slide 7: Transmutation Experimental Facility (TEF)
For R&D of ADS, 0.4 GeV beam by LINAC will be delivered to TEF.
Soviet submarine (LBE)

## Slide 8: Beam transport from RCS to MLF
3NBT
3-50BT
3-GeV RCS
50-GeV MR
Neutrino line
Material and Life Science Experimental Facility (MLF)
Neutron target
Muon target
road to coast
Length of 3NBT: 314m
Partial beam goes to MR
FX: 2.48 s, SX: 5.5 s
Ep: 3GeV
Power: 1MW
Already demonstrated
Rep.: 25Hz
JSNS
MUSE
FWHM ~150ns
600ns
600ns
Dump

## Slide 9: Proton Beam Window at MLF (A5083)
Lifetime estimation based on Post Irradiation Examination (PIE) for safety shroud (AlMg3) at SINQ in PSI
Considering difference of proton energy, to predict lifetime of the PBW with high accuracy for validation of calculation
Result at SINQ/PSI for 0.6GeV
Y. Dai, et al, J. Nucl Mat. 343 184 (2005)
Height: 3.8m
Weight：10t
Lifetime of PBW: Determined by He gas production (1200 appm) 2 years*
By recent PIE result of the SINQ (2400 apmm), lifetime may be applicable to 3 years.
* S. Meigo, et al, J. Nucl Mat. 450 141 (2012)

## Slide 10: 1 MW beam operation at MLF
Last year memorial snap shot at 1MW for 1 h test (2018/7/3)
Result of this year
Beam intensity trend at 1MW for 10.5 h test (2019/7/3)
Availability ~ 99%
1 MW

## Slide 11: PKA and DPA
DPA (Displacement per Atom) is estimated by calculation based on PKA.

## Slide 12: DPA and displacement cross section
Although DPA is widely utilized for estimation of damage, displacement cross section has not been enough validated.
    DPA = flux x Displacement cross section
  Displacement cross section has been measured only Cu and W for a few energies of protons less than 3 GeV
  Among calculations models, showing large discrepancies
N. Mokhov HPTW2016

## Slide 13: Measurement of DPA cross section at Kyoto univ.
Irradiation on metal at cryogenic temperature with GM cryocooler
By observing increase of electrical resistance, the cross section can be observed.
Measurement for Cu already performed at Kyoto university for 125 MeV proton
Experiment at J-PARC
Samples and GM placed at exit of 3-GeV synchrotron for various energy of proton 0.4 to 3 GeV
Other experiment performed at other sites for energy < 400 MeV

## Slide 14: Experimental condition
Temp rising ~20 K will be acceptable.
Lower beam intensity with accurate beam shape is preferable.
(1x1010 – 2x1013 protons/shot)
1 nA x 12h = 3x1014 protons
Several shots of beam at MLF
Y. Iwamoto et al.
Resist. and Temp. during beam irrad.
Recovering Resist. by annealing

## Slide 15
Beam dump
From RCS
To MLF
Measurement of cross section for 0.4～3 GeV proton
Experiment at the RCS with change of radiation license
With changing extraction timing of RCS, kinetic energy of proton can vary from 0.4 to 3 GeV.
Cold head and sample
Vertical view
Vacuum chamber with 4-K GM cooler
1 m
Beam
Under cryotemperature (~ 20 K), displacement cross section(s) was obtained by increase of resistivity (Δρcu) due to proton irradiation with average flux (f(E))
Cu wire (f 0.25 mm) with purity 99.999%
annealed 1,350 K
ρFP: Resistivity change by a Frankel pair (2.2x10-6 Ωm)
40 mm

## Slide 16
Experimental result
Resistance and temperature during irradiation
Experiment was carried out for protons with 0.8, 1.3, 2.2 and 3.0 GeV
To obtain resistance with high accuracy, 4 wire with delta mode with averaging was applied.
Beam width on the sample was obtained with the beam profile monitor.
Error is dominated with resistivity change by creation of the Frankel pair (23%).
50 shots
50 shots
50 shots
150 shots x 3.3x1012 = 5x1014protons
0.4μΩ
Ep (GeV) | Resistivity change (ΔΩm3X10-31) | σdpa (b)
0.8 | 2.35±0.31 | 1070±284
1.3 | 2.32±0.26 | 1053±270
2.2 | 2.49±0.21 | 1133±277
3.0 | 2.49±0.16 | 1010±244
Vertical beam profile

## Slide 17: Cascade sample holder
Experiment at 3NBT in J-PARC
RCNP (Osaka univ.) experiment by Iwamoto
To obtain Cu and Al data, cascade scheme applied.
Achieved ~5 K
Cascade target of 4 pieces (Al, Fe, Cu, W) applied
Temp ~19 K
In future improved to achieve ~5K

## Slide 18: Calculation with PHITS code
Displacement cross section with PHITS implemented following models
  Norgett-Robinson-Torrens (NRT) model
  Athermal recombination corrected (arc) model (Nordlund model)
    Nature comm. 9, 1084, 2018
NRT (Cu Ed 33 eV):
Nordlund (Cu Ed 33 eV):
ー NRT
ー Nordlund
Nd different for Td>83 eV
Nd: Number of displacement
Td: Displ. energy

## Slide 19: Comparison with models calculation
NRT model
overestimates ~ x3
arc model of Nordlund
good agreement
NRT/Nordlund
Present data imply that the DPA should be calculated with Nordlund model.
Ratio of NRT/Nord is constant above ~200 MeV.

## Slide 20: Comparison with MARS

## Slide 21: Displacement cross section for Al and W

## Slide 22: Displacement cross section above 30 GeV
As increase proton kinematic energy, heat density on material (W) increase
Regardless of the kinematic energy for Ep>30 GeV, displacement cross-section sustains almost constant
● Heat density
ー Bethe-Bloch
To solve the curious puzzle, the experiment should be carried out for high energy region.
30 GeV

## Slide 23: Disp. cross-section experiment at HiRadMat
Relatively easy experiment
Equipment
  GM cryo-cooler
  Vacuum chamber
    Those had be utilized at previous exepeiment at HiRad
  Instruments to observe sample resistance
Instruments can be placed at near the sample with low radiation (TT61)
Requirement of experiment
  Beam monitor and properties
  Beam scan procedure
Almost instruments are prepared. All we need is sample, sample holder and budget of travel.

## Slide 24: Experiment at FNAL
Budget already approved by MEXT for some of our collaborators
On 2021, the experiment will start for 120 GeV proton.
120 GeV proton
Cryo chamber and beam instruments will be placed
MT3

## Slide 25: Summary
Displacement cross section, measurement for 0.4〜30 GeV protons has conducted in J-PARC.
At FNAL, displacement cross section experiment for 120 GeV will be carried out.
To obtain the displacement cross section at 400 GeV, which is important for HL-LHC, the experiment should be performed at HiRadMat.

## Slide 27: Contribution for displacement
Fission and spallation fragment dominating