## Slide 1: Demands for Thermal Shock Experiments of Pulsed-Muon-Production Target Materials
HiRadMat workshop at CERN
10th July, 2019
J-PARC Center, MLF Division, Muon Section
High Energy Accelerator Research Organization, Institute of Material and Structural Science
(IMSS, KEK)
Shunsuke Makimura
Shunsuke.makimura@kek.jp

## Slide 2: Contents
Muon Science & Pulsed Muon
Muon Target at J-PARC
Previous Research at HiRadMat
  SiC-coated graphite
  NITE SiC/SiC
  TFGR W-TiC, tungsten alloy
Summary and
Expect to HiRadMat facility
J-PARC, Muon
S. Makimura, N. Kawamura, S. Matoba, T. Yamazaki, K. Shimomura, and Muon Section
J-PARC
T. Ishida, E. Wakai, and J-PARC
NITE-SiC/SiC
N. Nakazato, H. Kishimoto, J.S. Park, and Muroran Institute of Technology
A. Sato, D. Tomono, K. Ninomiya, M. Aoki and Osaka University
TFGR W-TiC, tungsten alloy
H. Kurishita, K. Niikura, H.C. Jung, M. Onoi, H. Ishizaki, and Metal Technology Co., LTD
HiRadMat
M. Calviani, I. L. Garcia, C. Torregrosa, J. B. Descarrega, E. Fornasiere and CERN collaboration
Irradiation, PIE, and SiC-coated graphite
P. Hurh, K. Ammigan, N. Simos, D. Senor, A. Casella, and RaDAITE collaboration

## Slide 3: Muon Science & Pulsed Muon
3

## Slide 4: Muon
Muon is classified with a lepton.
It is one of the most popular cosmic rays
A cosmic muon reach on your palm in a second.
m+: like the isotopes of hydrogen
m -: 200 times larger mass than electron
A pion decays into a muon and a neutrino.
The decay of the positive muon into a positron and two neutrinos occurs after a mean lifetime of 2.2 msec
4

## Slide 5: Topics explored by Muon Various & Unique science
Material and Life Science (m+)
Nondestructive Element Analysis (m-)
Fundamental Physics
Muon g-2,Mu HFS, m-e conversion etc.
Sample from Ryugu can be kept in a vacuum
Superconductor Hydrogen in matter
Ion diffusion Biomaterial etc. etc.
by mSR
Electron
Negative Muon
X ray
X ray
For ex.
Many useful semiconductors
(GaN, TiO2 etc. ) exhibit n type
conductivity. Why?
↓ Muonium ~ Hydrogen
Hydrogen impurity plays as a donor.
Characteristic Muonic X-ray ~ Higher transmittance by heavy mass of negative muon
Asteroid explorer~Hayabusa2 (JAXA)
Electron
Muon
The scheme was successfully validated at J-PARC MLF
Scientific Reports volume 4, Article number: 5072 (2014)
Hayabusa2 successfully touched down to Ryugu, and picked up the materials this morning!!
5
JAXA, University of Tokyo and collaborators

## Slide 6: Muon Facilities in the world
PSI (DC)
TRIUMF
(DC)
J-PARC
(pulse)
ISIS
(pulse)
RCNP, Osaka (DC)
Opportunity of experiments is limited.
Two kinds of muon facility
DC muon beam VS Pulsed muon beam
6

## Slide 7: continuous DC Muon vs. Pulsed muon
time
intensity
DC muon
Pulsed muon (150 ns, double pulse, 25 Hz)
40ms
Pulsed muon
Pulsed muon can be used with synchronized pulsed devices. e.g. laser resonant ionization of muonium
Synchronizing measurement with muon incident can be conducted to reduce background
Continuous DC muon
Fine time resolution – Sub-ps order Fast muon spin depolarization
High frequency (field) muon spin rotation is observable.
Low peak intensity is beneficial to avoid saturation of the positron detectors.
Pulsed muon and DC muon are complemental.
Demands for further peak intensity of pulsed muon!!
7

## Slide 8: Unique science by pulsed muon 1
Ultra slow muon generation laser resonant ionization of Mu
Transmission Muon Microscope
(Stage of feasibility study)
Applying re-accelerated high-quality muons
(Narrow time and energy width)
Electron Microscope can observe sample
less than 1mm thickness.
Muon Microscope can observe 200 times thicker samples,
because of 200 times heavier mass,
enabling us to observe alive cell through
a window!
To obtain higher-quality muon beam, higher peak intensity of muon synchronized with laser is essential.
8

## Slide 9: Unique science by pulsed muon 2 DeeMe: μ-e Conversion Search
Signal Window
BG Monitor
Prohibited phenomena in standard model
Current Upper Limits:
  BR[μ- Ti→ e- Ti] < 4.6 × 10-12@TRIUMF
  BR[μ- Au→ e- Au] < 7 × 10-13@PSI
DeeMe @ J-PARC MLF Muon Facility
  RCS: World-leading High-Power High-Purity Pulsed Proton Beam
  Novel Idea: μ-e Conversion in the primary production target itself
  S.E.S: 1×10-13(Graphite Target), 5×10-15(SiC Target)
Pulsed Proton Beam is a Key:
  To reduce Prompt Backgrounds
  To reduce/monitor Cosmic-Ray induced Backgrounds
Pulsed Proton Beam with SiC target realizes high sensitivity.
9

## Slide 10: Muon target at J-PARC
10

## Slide 11: Current Muon Target
P-Beam diameter; 14 mm (2s)
4kW heat @ 1MW proton beam
Thickness of graphite 20 mm
70 mm
Fixed target, from 2008 to 2014
Water-cooling by thermal conduction
Lifetime: Irradiation damage of graphite
1 year at 1 MW operation
Rotating target, from 2014
Cooling by thermal radiation
Lifetime: Bearings
Aiming Lifetime: 10 years at 1 MW operation
340 mm
Target material is polycrystalline graphite, IG-430U.
Fixed target was replaced with rotating target to disperse the radiation damage of graphite.
11
Mu target
N- target

## Slide 12: History of Beam operation
By Fixed target
By Rotating target
Oct. 2014
Rotating Target without replacement
Operational time:
17000 hours (Nov. 2014 ~ July. 2019)
6000 MWh
Rotation : ~16 M revolutions
(4.5 M revolutions /year @ 15r.p.m.)
Stable 500-kW operation in 1 year
12

## Slide 13: Almost 1-MW operation test
The 1-MW operation for 11 hours was successfully completed on 3rd July, 2019
Proton beam
Rotation shaft
Temperature of axis
Bearing
Graphite
T-left & T-Right to measure temp. of graphite
Thermally-insulated T.C.
The results were in good agreement with predictions from the simulations.
Thermal equilibrium
13

## Slide 14: MLF 2nd Target Station (TS2) Proposal of Future Project was submitted
Current MLF facility: tandem target
MLF 2nd target station: common target
1.5MW 25Hz
Double pulse
0.75MW 25Hz
Single pulse
RCS
TS1
0.75MW 12.5Hz
Single pulse
TS2
One of the plans for time structure
--Science by higher peak intensity
Extreme Condition
(High pressure, High external field)
Muon Micro Beam：small sample
Bio Science（soft matter）
Muon Micro Beam ：small protein crystal
Real Space, Real time（nonuniform system）
Muon Micro Beam, Stroboscopic measurement
Imaging, In situ, Operand, Element analysis
Industrial applications,
14

## Slide 15: Demands for New Target Materials
Chart: Energy [MeV]
Muon intensity
x 50
10-5
10-7
10-9
Energy [MeV]
Intensity [a.u.]
0 5 10 15
 | Density
 | g/cc
W | 19.3
Hg | 13.5
Pb | 11.4
PbBi | 10.6
Fe | 7.87
For MLF TS1:
Graphite is the most popular and excellent target material.
Demands for Graphite-substitute material
  Higher oxidation resistance:
  SiC-coated graphite
  Higher density: NITE SiC/SiC
Proton
Muon Target
Muon transport
Higher density leads higher efficiency of muon transport, because of lower spatial volume of mu/pion on target.
For MLF TS2:
Common target with Neutron target
Tungsten is desired for higher efficiency of Muon and Neutron production.
TFGR W-TiC tungsten: solution to recrystallize and irradiation embrittlement
TS1 vs TS2
15

## Slide 16: Why HiRadmat?
Rotating Target can disperse total heat density and radiation damage of target material. However,,,
Time width of proton beam for the pulsed muon is about 100 ns.
Too short to disperse the local heat density.
For application of new target materials,
Thermal shock resistance against H.E. proton beam is essential.
Unique aspect of H.E. proton irradiation
HiRadMat is an unique facility to investigate thermal shock
for higher peak intensity to new target materials.
Thermal shock on local volume of beam path
E; Young’s modulus
a; Th. Expansion
Compressive stress P by thermal shock
P
* R.T. | Graphite | SiC | Tungsten
E (GPa) | 11 | 440 | 411
a (ppm/K) | 6 | 4.3 | 4.5
Combination of proton-irradiation damage of materials must be considered as well.
Graphite: Excellent thermal resistant material
16

## Slide 17: Previous research at HiRadMat 1
SiC-coated graphite
Thanks to CERN collaboration
This program is supported by US-JP collaboration.
17

## Slide 18: Motivation of SiC-coated graphite
Graphite is easily oxidized at high temperature.
Hot graphite target
Unexpected air introduction to vacuum during beam operation
Graphite-oxidation contaminants complicate recovery.
In case of graphite target
IG-430U
SiC-coated graphite
Fresh
Fresh
20 min
60 min
Volume loss was observed on graphite and not observed on SiC coated graphite.
Oxidation tests of SiC-coated graphite
Much higher oxidation resistance
SiC-coating on graphite improves oxidation resistance.
18

## Slide 19: Proton Irradiation at BLIP, BNL and PIE tests under RaDIATE collab.
No. | Substrate Material | Crack | PIE (Newly revised, 14th March)
C-14 (Toyo-t) | IG-110U | Yes | SEM, TEM
C-9 (Toyo-t) | IG-110U | Yes | (TEM)
B-4 (Toyo-t) | IG-610U | No | HiRadMat
B-6 (Toyo-t) | IG-610U | No | SEM
No.2 (Ibiden) | ETU-10 | No | SEM after TDS, 1300K TDS,
14
6
2
9
4
SEM microscope analysis of cold specimens
SiC coating deposited by CVD is intact.
after re-polishing with no colloidal silica
Visual check of irradiated specimens
Crack was observed only on IG-110U substrate specimens, that was not designed for SiC coating
SiC coated IG-110 were finally broken to pieces
PIE testing at Pacific Northwest National Laboratory
19

## Slide 20: Thermal shock experiments at HiRadMat, HRT43
SiC-coated graphite / Titanium Alloy (cold & irradiated at BLIP) exposed to thermal shock at HiRadMat on 1st Oct, 2018
How did the SiC-coating on graphite behave ?
How different between irradiated at BLIP / un-irradiated ?
BOX-3
Ti-6Al-4V Gr5
Ti-3Al-2.5V Gr9
SiC-coated Graphite IG-630U
3 boxes with irradiated-specimens assembled at PNNL hot-cell
(Exported to CERN)
Sep.26
Oct.1(Mon)-2(Tue) 4:00am
exposure completed !
K.Ammigan, RaDIATE2018
Assembly at CERN-BA7
LDV signal
20

## Slide 21: Previous research at HiRadMat 2
NITE SiC/SiC
Thanks to CERN collaboration
This program is supported by JSPS KAKENHI Grant Number JP16H03994.
21

## Slide 22: Motivation of NITE SiC/SiC
 | Graphite ABLA | SiC ABLA
Proton 1MW | 2e15 | 2e15
Surface μ (4π) | 5.58e10 | 8.50e10
hs1ent | 6.25e8 | 9.93e8
Focal point | 1.62e8 | 2.75e8
Rate [1/s]
Higher transport efficiency by SiC target material, which is denser than graphite. (1.8 vs 3.2 g/cc)
For DeeMe, 6 times larger efficiency can be expected.
Beamline simulation for H line J-PARC, MLF through G4 beamline by T. Yamazaki
1.7 times larger surface-muon-yield at H-line experimental area.
Monolithic SiC
SiC/SiC
composite
Monolithic Silicon Carbide cannot be used as target material, because it is brittle.
NITE-SiC/SiC: developed at Muroran Institute of Technology for fusion material
Pseudo-ductility to disturb the propagation of crack
22

## Slide 23: Progress on NITE SiC/SiC as target material
392 MeV, 0.5 mA, 30 min. Proton-irradiation tests at RCNP, Osaka university
Higher residual radiation dose (400 times higher dose than that of graphite after 1 year cooling)
Tritium emission of NITE-SiC/SiC is completely different from CVD-SiC, probably, because of the effect of graphite matrix.
Sample holder at the irradiation test
Two tube furnace and 3H traps, which can distinguish HT with HTO.
Measurement of residual radionuclides for validation of simulation
Preliminary
23

## Slide 24: Thermal shock experiments at HiRadMat, HRT35
To confirm the resistance to thermal shock resiatance
NITE SiC/SiC was included in the experiments for coated low-Z absorbing materials for the Target Dump Internal in August 2017.
PIE testing conducted by J. Maestre C. Bahamonde and I. Lamas (Results of PIE from Slides of IWSMT14 at Iwaki)
Stripe-like damage was observed.
440 GeV, 1.2E11 protons/pulse, Gaussian, s=0.3 mm.
Results of SEM observation
(Top view, upstream, Deep impact)
Temperature rise: 2100 K
Disturbance of crack propagation was observed.
24

## Slide 25: Previous research at HiRadMat 3
TFGR W-TiC, tungsten
Thanks to CERN collaboration
This program is supported by MTC-KEK collaboration, This program is supported by JSPS KAKENHI Grant Number 19H01913.
25

## Slide 26: Tungsten as target material
Tungsten is expected as the target material.
For use of tungsten as muon production target, the boundary between cooling material and vacuum in beamline disturb transportation of muon. Thermal radiation cooling is desired. It should be used at high temperature. (MLF TS2, COMET, mu2e,,,)
H. Bolt et al., (2002)
Ductile to Brittle Transition Temperature should be less than room temperature.
J.Reiser et al. JNM, 423 (2012) 1.
G. Pintsuk et al.
Tungsten is brittle.
Brittleness is improved by heavy plastic working.
The use of W as target material is limited by “recrystallization embrittlement” and “irradiation embrittlement”.
brittle
Plastic working
Ductile
Recrystallization embrittlement
Irradiation embrittlement
26

## Slide 27: Motivation of TFGR W-TiC tungsten
Toughened Fine-Grained Recrystallized W-TiC, (TFGR W-TiC) is developed by Prof. Kurishita at Tohoku University. Now the activities are transferred to KEK and Metal Technology Co. LTD collaboration.
Equiaxed, fine grains with TiC precipitates
GB reinforced by TiC enrichment
No recrystallization embrittlement
High sink density: Resistance to irradiation is anticipated.
DBTT (nil-ductility tem.) < RT
Stress (MPa)
1500
500
1000
2000
2500
1320
1230
Strain
840
870
250
320
Z
10 mm t
0
X
Y
Number is fracture strength
2150
1.5 mm t
1100
Y
As-received
1240˚C x 1 hr anneal
Pure hot-rolled W
TFGR W-TiC
1650 degC GSMM
Fracture strength: 3.2 GPa
Mater. Trans. 54 (2013) 456-465.
3-points bending test at RT
27

## Slide 28: Progress of development for TFGR W-TiC
Purification of Powder
Mechanical alloying
Sintering
GSMM process
The apparatuses for fabrication is ready.
Revival of TFGR W-TiC is almost completed.
Future plans in up-coming three years:
Economical and Mass production under collaboration with industries
  Funding from Ministry of Economy, Trade and Industry was approved in June, 2019
Higher-temperature resistance by W-TaC
  Funding, JSPS Kakenhi was approved in April, 2019
Study for irradiation effect
  Ion-irradiation at HIT, Tokyo University in Aug. 2019,
  and H.E. proton irradiation under RaDIATE collaboration
New Sintering & GSMM apparatus
Confidential!!
28

## Slide 29: Thermal shock experiments at HiRadMat, HRT48 PROTAD, Sep. 28, 2018
Beam Parameters | 
Beam energy | 440 GeV
Max. bunch intensity | 1.2 x 1011
No. of bunches | 1 – 288
Max. pulse intensity | 3.5 x 1013 ppp
Max. pulse length | 7.2 µs
Gaussian beam size | 1σ: 0.1 – 2 mm
TFGR W-TiC was included in HRT48.
We are waiting for PIE testing.
29

## Slide 30: Summary & Expect to HiRadMat facility
30

## Slide 31: Summary & EXPECT to Hiradmat facility
Summary
Pulsed muon contributes to various, brand-new and unique science in material science, fundamental physics, and industrial use.
Higher peak intensity is desired in muon community, i.e. MLF TS2.
Further thermal shock resistance is required to the new target materials.
Developments of new target material, SiC-coated graphite, NITE SiC/SiC, and TFGR W-TiC are in progress, including thermal shock testing at HiRadMat.
Expect to HiRadMat Facility
HiRadMat is an unique facility to investigate thermal shock for higher intensity to new target materials.
I always appreciate kind collaborations with CERN and RaDIATE.
My personal suggestion to HiRadMat as one of the users
How to connect between the results of HiRadMat and the evaluation of actual long-term operation
Saving time of PIE testing after irradiation, Upgrade of remote handling replacement?
31

## Slide 32: Back up slides

## Slide 33
What happened to Muon Target?
Flexible couplings
Rotating target
Wrong directions of machining
Broken flexible coupling
Machining for key should be solid line.
Rotation motor
Rotating target has been successfully operated for 4 years.
On this regular maintenance: replacement of rotation feedthrough from air to vacuum, the flexible coupling was broken.
During operation, it was intact.
We found the mistake of the machining process.
We can replace the broken one.
But the problem is that two couplings are used in the rotating target. The lower one cannot be replaced easily.

## Slide 34
For beam operation,
and replacement of target
It has been confirmed that the rotating target is not damaged with 500-kW proton beam even without rotation through FEM simulation . Furthermore Monitoring system is upgraded.
The main issue is emission of tritium.
The exhaust of vacuum pump is temporarily stored in a buffer tank system and is vented after measurement of concentration of RI.
500-kW operation is now going on.
The target will be replaced with a new and appropriate one during next new-year maintenance interval.

## Slide 35
Insufficient research for irradiation effect of W-TiC
Before irr.
After irr.
521
1039
1164
1108
1034
619
HV
Nanostructured W-0.5TiC/Ar)
Nanostructured W-0.5TiC/H
Pure W (Commercially available, SR）
Vickers microhardness
・ No radiation hardening
DHV = 98
H.Kurishita et al. JNM 377 (2008) 34.
Tirr = 873K, 2×1024n/m2 (En >1 MeV),
0.08 dpa, JMTR
W/O GSMM
H.Kurishita et al. Phys. Scr. T159(2014)014032
TFGR-W
Tirr = RT, 1-2×1019ions/m2 (2.4 MeV Cu2+),
2-4 dpa, Tohoku Univ. IMR
Tirr = RT, 1×1021D2+/m2 (2.0 keV D2+)
Thermal Desorption Spectroscopy of D2
The D retention in pure W is significantly increased by Cu2+ irradiation, while that in TFGR is relatively insensitive to the damage level.
Irradiation effect research of TFGR is mainly for D retention.

## Slide 36: Current status of W development (1) Preparation and handling of purified powders
Setup of High-purity glove box (GB) with vacuum chamber/furnace for handing highly pure powders without gaseous contaminations
Purification and (remote) handling of starting powders (W, TiCx,) and MAed powders (W-Ti-C)
Fully degassing of MA vessels and balls, HIP capsule etc. before use
 | High-Purity GB, KEK/MTC |  |  | Typical GB, KEK/NIFS |  | 
Impurity | O | N | Mo | O | N | Mo
Content (wt%) | 0.091 | 0.009 | 1.98 | 1.0 | 0.18 | 1.25
Powders in Ta boat for purification
Comparison of impurity content in MAed powder

## Slide 37: Current status of W development (2) Mechanical Alloying (MA) in vacuum
Setup of 3MPDA high energy ball mill with cooling system (~ -20ºC) to prevent strong adhesion of MAed powder to the vessel inner walls
MA: Introduction of ultrafine grains (~20 nm) and alloying by using high energy ball milling
Mo impurity (~ 2%) coming from TZM balls and vessels
3MPDA
(a) SEM, (b) EDS(Ti) mapping for MAed W-1.2%TiC powder
Powder with hard balls in a vessel (TZM)
(a)
(b)
The MA Vessel is filled with
Previous work: Hydrogen, This work: Vacuum
3MPDA: 3 Mutually Perpendicular Directions Agitation

## Slide 38: Current status of W development (3) HIP (Hot Isostatic Pressing)
HIP: Densification of MAed powder without exposure to air
Densified compacts with equiaxed, ultra-fine grains
HIPed W-1.2wt%TiC compact
Density : 17.92 g/cm3
 | Ti | C | O | N | Mo
HIPed compact | 0.88 | 0.23 | 0.038 | 0.010 | ---
MAed powder | --- | --- | 0.091 | 0.009 | 1.98
Chemical compositions (wt%) of W-1.2%TiC before and after HIP
Steel capsule filled with MAed W-1.2%TiC powder
3h

## Slide 39: GSMM (Grain boundary sliding-based microstructural modification) process
GSMM : Reinforcement of intrinsically weak GBs in W by enhancement and optimization of TiC precipitation and their segregation
Removal of the residual bubbles/pores through GB diffusion
g (shear strain)
g = 0
g = 1
g = 2
Shear stress
N. Wakai, Materia 45 (2006) 644.
8f x 20 mm
Reduction ratio: 85.3%
1650ºC
Superplastic deformation by GB sliding at high temperature
The number of GSMM operations at 1650ºC attempted to date is 10 times with various final loads
by using superplastic deformation, driven by GB sliding, where the recrystallized, equiaxed grain geometry is maintained and active grain rotation and extensive relative displacement of the adjacent grains are operative.

## Slide 40: Three point bend (3PB) testing at RT
3PB testing : Demonstrate that the fabricated W alloys exhibit very high fracture strength ( > 2~3 GPa) and appreciable ductility at RT in the nanostructured, recrystallized state
Specimen deflection during 3PB testing
3PB specimen
1.1 mm x 0.9 mm x 15 mm
3PB test fixture used
Overview of 3PB testing at RT and 0.3mm/min

## Slide 41: 3PB test results at RT
W-1.2wt%TiC in the nanostructured, recrystallized state
#8 specimen: MA-HIP-GSMM (RR : 82. 9%)
Very high fracture strength of 2590 MPa and slight ductility at RT
→ TFGR (Toughened, Fine Grained, Recrystallized) W- 1.2%TiC alloy
#8 specimen broken in two pieces after testing
In order to manufacture much more ductile W-1.2%TiC alloys, the microstructure of the #8 specimen has thoroughly been examined.

## Slide 42
SEM
Microstructures of #8 specimen SEM, EDS
Ti
EDS
O
C
3 mm
A large precipitate of titanium oxy-carbide with approximately 1 mm diameter observed is attributable to locally insufficient progress of the MA process; the starting TiC phase has not completely been decomposed into Ti and C solutes in the W matrix by MA. The optimization of the MA process is required for ductility enhancement of W-1.2%TiC alloy.
TEM analysis by Prof. Sakamoto at Ehime University will come soon.