## Slide 1
Material Testing Demands by Heavy-Ion Pulsed Beams – by FAIR
Helmut Weick, GSI Helmholtzzentrum
HiRadMat workshop, 11.07.2019
In-Flight Rare Ion Production
FAIR / Super-FRS
Beam Power Comparison
Targets and Beam Catchers
Material Tests at GSI

## Slide 2: Production of RIBs In-Flight
adapted from T. Kubo, NIM B 376,102 (2016)
pulsed beams for storage rings
HIAF-HFRS

## Slide 3
How to produce Rare Isotopes ?
Fragmentation
Removal of nucleons in quasi-free nucleon-nucleon collisions
neutrons (N)
protons (Z)

## Slide 4: Production Cross sections
Projectile fragmentation
Projectile fission
Target
Projectile 129Xe
Main Fragment
238U
Fusion (only at lower velocity)
Tin isotopes by different methods

## Slide 5: FAIR Facility for Antiproton and Ion Research
0.4-2.7 GeV/u U28+, 5x1011/pulse
11 GeV/u Au79+, 1010/pulse
28 GeV protons, 2x1013/pulse
Darmstadt May 2019
fast or slow extraction

## Slide 6: Beam Comparison
 | HiRadMat | HiRadMat | FAIR | GSI | GSI | 
 | protons | Pb | U28+ | U28+ | U73+ | 
E / m = | 437 | 173.5 | 1.5 | 0.125 | 1.0 | GeV/u
dE/drx = | 0.00211 | 12.8 | 13.8 | ~35 | 14.5 | GeV/(g/cm2)
dE/dmion = | ~0.94 | 817 | 878 | 2228 | 922 | GeV/g
N / bunch = | 1.5e11 | 5e7 | 5e11 | 2e10 | 2.5e9 | 
bunches = | 288 | 52 | 1 | 1 | 1 | 
dE/dm = | ~26.0 | 0.34 | 70.3 | 7.1 | 0.37 | kJ/g
pulse length Dt = | 7.2 | 5.2 | 0.09 | 0.4 | 0.1 | ms
Ds = c Dt = | 27.4 | 19.8 | 0.34 | 1.52 | 0.38 | mm
* incl. build-up
*
GSI / FAIR beams only one bunch per pulse.
*
Energy deposition in copper for sx= sy = 0.5 mm beam spot.
In peak of 2-dim Gaussian: dE/dmion = 1 / (2p s2) * dE/drx

## Slide 7: DE for Pb-ions
Radial distribution
of point-like beam
FLUKA, Ekaterina Kozlova
FLUKA in mode DEFAULT does not
give a good dE/dx description,  rescaled according to ATIMA predictions
DE in graphite target (r = 1.84 g/cm3)
high DE region dominated
by beam spot size
for 173 GeV/u

## Slide 8
dE/dx for Relativistic Heavy Ions
DLLS(Z1,v)
Lindhard-Sørensen extension,
includes nuclear size effect for g >> 1.
- d/2 +DLe+,e-
Fermi density effect
for relativistic velocities
+ e+,e- pair production
0

## Slide 9
The fate of accelerated ions
Yeah, I am an accelerated ion.
By the way, what
do you do with accelerated ions?
Aaarrgh !

## Slide 10
Super-FRS (Super-Conducting Fragment Separator)
target
degrader
Brmax = 13 Tm
238U28+ 0.4-2.7 GeV/u
to CRing
740 MeV/u
Brmax = 7 Tm
~ 300 MeV/u
Brmax = 20 Tm
main sep
200m
7 m
33 SC multiplets
rad. hard dipole 95 t
presep
33 SC multiplets

## Slide 11: Separation
All fission fragments after target, 1.5 GeV/u 238U --> 4 g/cm2 12C
3x1011 U/s
Protons
Neutrons

## Slide 12: Separation
Separation only by Br
LISE++ Simulation
S = 5x109/s
Protons
Neutrons

## Slide 13: Separation
Separation after pre-separator (Br-DE-Br)
LISE++ Simulation
S = 3x108/s
Protons
Neutrons
Protons
Neutrons

## Slide 14: Separation
Separation after main separator (Br-DE-Br) x (Br-DE-Br)
LISE++ Simulation
Protons
Neutrons

## Slide 15: Beam Interaction Points
unreacted primary beam
wanted fragment beam
shielding
plug
plug
magnets
beam
absorbers
Beam Catcher Chamber
3 m
pumping
duct
CSIR-CMERI Durgapur
Avik Chatterjee,
Abhijit Mahapatra
4.2 m
KVI-CART
Michel
Lindemulder
Target plug,
Graphite wheel

## Slide 16: Material Choice
a simple temperature and stress calculation
pressure
Instantaneous energy deposition
Initial compressive pressure,
wave propagates to boundary
tensile stress.
low A  low DT
polycrystalline graphite,
more nuclear x-section
less slowing-down by
electrons.
at high T
Li
Be
graphite
h-BN
AlBeMet
Al
Ti (6Al-4V)
Cu-OFC
W
Ta
glidcop
yield strength / stress
for 5x1011 U on 1cm2
INCONEL
stainless
steel
plastic deformation
not exactly elastic,
cyclic stress, cracks?

## Slide 17: Liquid Lithium Jet - Spall Strength
Hydro-dynamical calculation:
Negative
pressure!
Calculated spall strength Ps of
liq. Li is only -0.09 kbar = -9 MPa
Li jet will break after 210 ns,
many droplets with v > 100 m/s
Anna Tauschwitz et al., NIM A 591 (2008) 447

## Slide 18: Energy Deposition and Absorber Design
graphite
copper
heat sink
water cooled
490 mm
graphite
beryllium
beam
copper
~ 300 kg

## Slide 19
Beam Spot on Absorber
n-rich
settings
n-deficient
new optics setting
Optics fixed for fragment beam,
primary beam of different
magnetic rigidity, DBr/Br ≤ 30%
DE includes Bragg peak.
spot sizes: 0.7 cm2 - 3 cm2

## Slide 20: Beam Absorber Simulation
Use Gaussian beam spot and 17.2 kW (1500 MeV/u 238U)
beam comes in 50ns pulses with 28.6kJ every 1.67s.
CSIR-CMERI Durgapur
Amit Kumar with
ANSYS + LS-Dyna
Apply radiation damage only
in inner region of beam spot
301 K
l =15 W/m-K in radiation damaged areas
graphite SGL 6650
after reaching thermal equilibrium
Tmax → 1504 K
tensile stress by reflected pressure wave on outside
σ1max → -19 MPa
compression in
hot spot on inside
σ3min → 50 MPa
beam
absorber
divided into
6 segments

## Slide 21
Beam Catcher Stress
ok, according to Coulomb-Mohr criterion for brittle materials with factor > 1.5
initial compression around beam spot
reflected pressure wave
tensile stress, outer face
time [ms]
pressure [MPa]
Amit Kumar with LS-Dyna
initial energy = 1500 MeV/u, 740 MeV/u
T_max = 1504 K, 720 K
DT_max = 134 K, 310 K
max. pressure = 11 MPa, 23 MPa
min. pressure = -6.0 MPa, -8.4 MPa
1st pulse
pulse in thermal equilibrium (>300s)
pressure [MPa]
time [ms] – 300s
A
E

## Slide 22
Tests at FRS Target Stations, GSI 2014
Cu
graphite
pre-irrad.
on target 1: sx = 0.4 mm, sy= 1.0 mm
on target M: sx= 1.2 mm, sy= 1.4 mm
glassy carbon
1x1010 U29+/pulse at 125 MeV/u,
long pulse FWHM ~ 500ns
copper-
diamond
in peak ~2 kJ/g => Cu melts
Tantalum melts in beam spot, but
cannot drill through cm thick target
in 100 pulses (range = 0.55 mm).
in graphite:
E/mmax = 2.9 kJ/g => DT ~1400 K (target 1)
E/mmax = 0.75 kJ/g => DT ~ 360 K (target M)
but no clear shock wave front, too long pulses.
graphite, Mo-graphite, beryllium,
flexible graphite (SIGRADUR),
Cu
Al
20mm
Ø=20mm targets, t <1mm
No effect after 100-1000 pulses on:
from
GSI-UNILAC
Ronja Knöbel, HW
Marilena Tomut

## Slide 23
Radiation Damage by Heavy Ions
Track formation at high dE/dx (high Z ions Uranium, Pb, Au)
track diameter few nm, at fluence 1014/cm2 track next to track
surface of HOPG graphite hit by U ions
At 0.4 - 1.5 GeV/u lower dE/dx
damage reduced by factor ~1000
ok for target wheel
- but beam stops in beam catcher
Big effect at low velocity (Bragg peak)
Use UNILAC at GSI (8.6 MeV/u),
for sample preparation,
Low activation for maximum damage.
Limited area max. 1cm2, range = 0.1 mm.
30 nm x 30 nm
With 3x1011 U/s max. fluence ~ 1017 /cm2
on same spot of target wheel or catcher.
Efficiency of track formation at higher velocity?
Recrystallization into what structure? (glass-like)

## Slide 24: S334, Experimental Setup
GSI plasma physics cave (HHT) 2007, together with CERN
238U
Laser
Doppler
Vibrometer
238U beam at 350 MeV/u
≤ 2.5•109 238U/pulse
300ns (FWHM) pulse
σx = σy ≈ 0.365 mm
cylinder targets, d=10 mm, L=10mm (graphite, Cu, W, Pb)
Roman Wilfinger, Jacques Lettry, Dmitry Varentsov, Serban Udrea,
Aleksandra Kelic, et al.
elastic response (5x108/pulse)
Roman Wilfinger

## Slide 25: Elastic Radial Stress Wave
(1) . . . Compression wave,
(2) . . . Tension wave,
(3) . . . Compression → reflection → tension front,
(4) . . . Tension → reflection → compression front.
Laser- Doppler Vibrometer
(1)
(2)
(3)
(4)
Pulse 2486:
- Intensity: 2.5x109 238U part/spill
- Beam-spot size: s = 0.365 mm
- Graphite sample d=10 mm, L=10 mm
DE/Dm = 1.3 – 1.7 kJ/g in max. of peak
DT (from deposited energy) ~ 700 K
calc. pressure +42 .. -25 MPa

## Slide 26: Downscale for Testing ?
Future: enlarged beam spots to make target survive.
Today: test with small beam spot on downscaled prototype.
Peak energy can be reached, but stress at critical surfaces?
Also time structure needs to be scaled down.
Problem in 2014 test, bunch compression cavity was broken.
Dt (FWHM) ~ 0.5 ms, v=2.2 mm/ms, sample 1mm thick, spot~1mm
Now new 2nd cavity in SIS-18 => Dt (FWHM) = 100 ns possible.
SIS-100: 9 cavities to merge four SIS-18 pulses to one 90ns pulse,
by barrier bucket and bunch compression cavities.
16 mm
2.2 mm
HiRadMat is good, but more difficult with 288 bunches over 7.2ms.
SPS bunch compression for LHC but no bunch merging.
PS booster pulses?
Test with stress concentrator geometry.
Match size for positive superposition ?
However, A. Bertarelli’s talk yesterday, 1/10 downscaled LHC jaws,
a reasonable “shock” front can be formed.
beam
20cm

## Slide 27
Summary - Conclusion
HiRadMat with Pb beam no gain compared to proton beam.
Lower energy density and Pb projectile fragments very fast.
Heavy-Ion Testing should be done at lower energy facility.
Proton beam reaches values for FAIR testing.
Superposition of many bunches requires improved simulation.
Key questions for FAIR: What is the best carbon material?
No damage outside beam spot -> properties preserved
in spot dramatic changes (see talk M. Tomut).
High dose heavy-ion
irradiation at low E
Pulsed beam testing
with real shapes with
in beam diagnostics

## Slide 28
empty

## Slide 29: Thermal Simulations by CMERI - consider radiation damage -
Amit Kumar
with ANSYS
950 K
300 K
modified material
l =15 W/m-K in center (c1-c3)
l =15 W/m-K, shaped better
fresh SGL 6650
Apply radiation damage only
in inner regions of spot (c1..c3)
Use Gaussian beam spot and 17 kW (1500 MeV/u 238U)
301 K
301 K
1504 K
2210 K
to copper heat sink

## Slide 30: Energy Deposition in Copper Cylinder
thesis Herta Richter, TU Vienna 2011
FLUKA simulation of DE by 350 MeV/u 238U beam on copper cylinder
GeV/cm3 per primary
Eur. Phys. J. A 42, 301–306 (2009)

## Slide 31: Target Ladder Scan
scan y1
scan y2
scan x
MW11
7mm Ti
N
0
26+
25+
x