## Slide 1: Simulation of energy deposition and radiation damage effects for HiRadMat experiments using Monte Carlo tools
12/7/2019
Andreas Waets
On behalf of EN-STI-BMI
summarizing material from A. Lechner, E. Skordis, A. Bertarelli, D. Carbajo Perez, M. Frankl, I. Lamas Garcia, F. Cerutti, V. Vlachoudis, F. Salvat-Pujol, C. Accettura

## Slide 2: Scope
(HL-)LHC
2.3E11 particles/bunch
7 TeV/c
International HiRadMat
Workshop 10-12/7/19
HiRadMat irradiation experiments are carried out to investigate the behaviour of beam-interacting components in complex accelerator environments.
LIU and HL-LHC components see higher intensity to provide higher luminosity, tested with lower intensity beam in HRMT:
SPS
1.2E11 particles/bunch
440 GeV/c
HRMT
TDI/TDIS: Injection protection absorbers
TDI/TDIS
TCDI: Transfer line collimators
TCDI
IR7 collimators
IR7
COLLIMATORS
(I) How are FLUKA Monte Carlo simulations used for both preparation and analysis of HRMT tests?
(II) Experiment carried out to assess shock thermomechanical response of irradiated materials: how can radiation damage be calculated in FLUKA and used as link between experiment and real accelerator
Notes: Not having LIU intensities in HiRadMat before LS2 (will see)

## Slide 3: Monte Carlo simulations
N = 1000000
S ≈ 70.1 %
International HiRadMat
Workshop 10-12/7/19
N = 2
N = 20
DETERMINE DOMAIN +
STATISTICAL PROPERTIES OF INPUTS
GENERATE RANDOM SET
OF INPUTS
PERFORM DETERMINISTIC
CALCULATION WITH SET
ANALYZE RESULTS STATISTICALLY
Earth’s surface
pwater + pland = 1
Uniform sampling of Earth’s surface
Repeat experiment to gather sufficient statistics
Aggregate result,
calculate ratio Nwater/(Nland + Nwater)
Error drops as 〜 1/√N

## Slide 4: Implementation in FLUKA
International HiRadMat
Workshop 10-12/7/19
DETERMINE DOMAIN +
STATISTICAL PROPERTIES OF INPUTS
GENERATE RANDOM SET
OF INPUTS
PERFORM DETERMINISTIC
CALCULATION WITH SET
ANALYZE RESULTS STATISTICALLY
Combinatorial geometry
Magnetic fields
Hadron-nucleus, nucleus-nucleus, decay, low energy neutrons, muon (incl. photonuclear), photon interactions, ...
Condensed history tracking for charged particles, with single scattering option, transport of charged particles in magnetic fields
Wide range of possible particle sources, beam distributions, coupling with optics tracking codes
Energy (power, dose) deposition, fluence, displacement per atom, residual nuclei production, activation, ...
E. Skordis
Ref: A. Fasso et al. Prog. In Nucl. Science and Technology, Vol. 2, p769-775 (2011)
Notes: Ref: Fluka
Emphasize use of ideal materials with uniform material density, not changing during interaction

## Slide 5: Workflow methodology
International HiRadMat
Workshop 10-12/7/19
Analysis of beam-matter interaction from an engineering perspective, in sequence:
Physics: determine how much energy and where has been deposited
Thermodynamics: determine which temperature distribution has been induced in the body
Thermomechanical: determine which deformations, dynamic response and phase transitions have been generated
Iterative process used to determine optimal beam parameters for HRMT experiments
Physics
Thermodynamics
Thermomechanical
Energy
Temperature, density,
pressure
Stress, strain, damage
From: A. Bertarelli, Beam Induced Damage Mechanisms and Their Calculation, Joint Accelerator School 2014
Notes: Beam-matter analysis from an engineering perspective (Lecture Alessandro)
Complex geometry, complex material behavior, complex boundary conditions …
Damage phenomena induced by high energy, high intensity particle beams bring matter to extreme regimes where practical experience and material knowledge is very limited. The analysis of these phenomena must rely on methodologies integrating and coupling several disciplines , numerical tools and experimental verification in a multiphysics approach.

## Slide 6: Energy deposition studies for HRMT
International HiRadMat
Workshop 10-12/7/19
TDIS (HRMT 45)
Injection beam stopper (segmented) designed to protect the machine in case of injection kicker malfunctioning
Goal: Reproduce a state of temperature/stresses in the back-stiffener comparable to that induced by the worst-case potential impact of the HL-LHC beam
Assess integral jaw performance after beam impact (flatness, …)
Achievable beam parameters in HRMT (before LS2): bunch trains presently extracted to HiRadMat have a smaller intensity than the bunch trains which will be transferred from the SPS to the LHC in the HL-LHC era

## Slide 7: Energy deposition studies for HRMT
International HiRadMat
Workshop 10-12/7/19
Several FLUKA simulation loops carried out to find out the right beam settings (impact parameter) to achieve in the experiment a comparable energy deposition in the stiffener as in the real case.
Using FEA simulations (ANSYS) the defined test settings should lead to reasonably similar peak temperatures/stresses at the back-stiffener as in the real case
TDIS (HRMT 45)
?
M. Frankl

## Slide 8: Energy deposition studies for HRMT
FLUKA
International HiRadMat
Workshop 10-12/7/19
TDIS (HRMT 45)
ANSYS
ANSYS
Using FEA simulations (ANSYS) the defined test settings should lead to reasonably similar peak temperatures/stresses at the back-stiffener as in the real case
38 mm
52 mm
 | HL-LHC injection | HRMT 45
Intensity/bunch | 2.3E11 | 1.2E11
Impact parameter (mm) | 38 | 52
Beam impact parameter determined to be representative for worst-case HL-LHC beam mis-kicked injected bunch scenario
M. Frankl
D. Carbajo Perez

## Slide 9: Energy deposition studies for HRMT
International HiRadMat
Workshop 10-12/7/19
TDI (HRMT 35)
TDI showed severe damage on Ti coating after dismantling. HRMT irradiation experiment carried out to gain information for future beam intercepting devices, other coating configurations tested on low-Z materials such as MoGr.
Assumed beam parameters:
Beam-size: σx = σy = 300 μm
Number of bunches: 288
Intensity: 1.2E11 ppb
M. Frankl
I. Lamas Garcia
Accuracy of beam parameters (including beam spot size) critical for this experiment:
  Possible misalignment in form of jaw vertical translation is considered indirectly by the various impact parameters (-0.4 σy to 1 σy)
  Rotational misalignment with angles of -200 to +300 µrad is accounted for (simulated only for Mo-coating and an impact parameter of 1 σ)

## Slide 10: Energy deposition studies for HRMT
International HiRadMat
Workshop 10-12/7/19
Remarks
Monte Carlo simulation method limitations:
  Assuming (coating) material is perfectly flat, homogeneous and isotropic
  Assume bulk density for coating materials
  No real-time evolution of material degradation
  Challenges in calculating physical observables
  AD target (HRMT 27): Antiproton production target; Energy deposition, dose rate and activation calculations
C. Torregrosa
Other examples:
  TCDI (HRMT 44): Transfer line collimators, necessity for replacement of the current employed materials; Shower studies to determine required focal strength for HRMT beam.
  “MuliMat” (HRMT 36): Determine the behaviour under high intensity proton beams of a broad range of materials relevant for collimators; Energy deposition maps
D. Horvath
Notes: Include pictures of experiments

## Slide 11: Scope
(HL-)LHC
2.3E11 particles/bunch
7 TeV/c
International HiRadMat
Workshop 10-12/7/19
SPS
1.2E11 particles/bunch
440 GeV/c
IR7
COLLIMATORS
(I) How are FLUKA Monte Carlo simulations used for both preparation and analysis of HRMT tests?
(II) HiRadMat beam cannot be used to cause significant radiation damage in target materials (DPA, gas production, …)
Beam intercepting devices in HL-LHC are expected to accumulate radiation damage throughout operation but should retain functionality in worst-case impact scenario
Future experiments in HRMT can test pre-irradiated materials or components for shock thermomechanical response
Radiation damage in materials can be linked to displacement per atom (DPA) quantity calculated in FLUKA
Radiation damage simulations are the only way to link experiment and real accelerator environment
Notes: IR7 collimators not expected to endure shock absorption but must be ready as backbone of machine protection system
Great interest to test pre irr materials for shock response

## Slide 12: Radiation damage
International HiRadMat
Workshop 10-12/7/19
The displacement per atom (DPA) quantity is a measure of the amount of radiation damage incurred during irradiation, can be used to relate radiation damage to change of macroscopic material properties.
Cannot be measured experimentally, can only be measured indirectly (so far)
Indirect through study of macroscopic effects (electric and thermal conductivities, radiation hardening, swelling…)
Quantitative interpretation:
  3 dpa means each atom in the material has been displaced from its site within the structural lattice an average of 3 times
  0.01 DPA implies 1 out of 100 atoms has been displaced.
FLUKA
E. Skordis
Notes: Macroscopic changes: visual but also resistivity (linear w/ radiation damage)

## Slide 13: Radiation damage: DPA
International HiRadMat
Workshop 10-12/7/19
Total stopping power = electronic (inelastic) + nuclear (elastic, Coulomb)
DPA is related to non-ionizing energy loss (NIEL), a strong function of projectile type, energy and charge as well as material properties
Can be induced by all particles in the cascade in high energy (GeV-TeV) accelerator environments
  All shower particles can contribute to NIEL/DPA, in particular recoils from nuclear interactions, but also EM showers. At lower energies NIEL/DPA is dominated by heavy recoils
  Low energy neutrons scatter through nuclear interactions, creating recoil atoms
  Partition function decreases with energy and increases with charge: low energy heavy ions dominate NIEL
Notes: Slides Wednesday Meigo: 18
Transport limit at 1 keV

## Slide 14: Radiation damage: DPA
International HiRadMat
Workshop 10-12/7/19
A Frenkel pair is a compound crystallographic defect formed when an atom or ion leaves its place in the lattice (leaving a vacancy), and lodges nearby in the crystal (becoming an interstitial), displacing neighbouring atoms, resulting in an atomic displacement cascade.
Sufficient T,
cascade
Insufficient T,
recombination, phonons, ...
DPA can be calculated as:
Vacant lattice site
X Displaced atom
Electronic stopping
dominates
Nuclear stopping
dominates
Number of Frenkel pairs according to Norgert, Robinson and Torrens:
  ξ: Partition function, fraction that goes into nuclear stopping
  T: primary (“knock-on” particle) energy
  κ: Recombination efficiency, fraction of surviving defects
  Eth: Damage threshold, recoil energy above which pair is produced.

## Slide 15: Radiation damage in FLUKA
International HiRadMat
Workshop 10-12/7/19
Charged particles/heavy ions:
  NIEL calculation during transport (MC)
  Below transport threshold: calculate integrated nuclear stopping power
  At elastic/inelastic collisions: calculate recoil
Neutrons:
  E > 20 MeV: calculate recoil
  E < 20 MeV: group- or pointwise treatment
Knock-on energy
from MC shower particles
(Surviving) Frenkel
pairs
Stoller
DPA
Limitations of MC simulation methodology:
  Only user input is damage threshold (averaged)
  No crystal structure
  No lattice effects (compounds)
  Recombination properties
Notes: Stoller from Molecular Dynamics calculations

## Slide 16: Radiation damage in FLUKA
International HiRadMat
Workshop 10-12/7/19
Assessment of long-term radiation damage in HL-LHC collimators (IR7)
(Amount of protons lost over lifetime) x (DPA in collimation system per lost proton)
BLM response in LHC extrapolated to HL-LHC era, assuming amount of protons lost per year is proportional to integrated stored beam intensity (2018 scaling factor: 1E17 protons lost in HL era)
DPA predictions for primary collimators (TCP):
  Comparison between collimator materials (CFC, MoGr
  High DPA values in concentrated surface volume
  Lower DPA averaged over longer transverse area
Similar approach for H, He production
E. Skordis
 | DPA
CFC (10μm x 10μm) | 0.05 -0.1
CFC (400μm x 400μm) | 0.005
MoGR (10μm x 10μm) | 0.3 - 0.4
MoGR (400μm x 400μm) | 0.02

## Slide 17: Radiation damage in FLUKA
International HiRadMat
Workshop 10-12/7/19
Testing of (coated) collimator material samples in GSI
Preparation of GSI irradiation campaign of coated and uncoated HL-LHC collimator materials (MoGR, Graphite, CfC) with 4.8 MeV/u 48Ca ion beam
Goal: Perform thermo-mechanical and electrical resistivity measurements at CERN on pristine and irradiated samples at GSI
FLUKA simulations carried out to determine irradiation time (fluence) needed in order to achieve comparable displacement damage as in the HL-LHC era, reachable in few 10h beam time
Estimate activation of samples after irradiation
C. Accettura

## Slide 18: Summary and outlook
International HiRadMat
Workshop 10-12/7/19
Monte Carlo shower codes like FLUKA are essential for simulating beam-matter interactions for HiRadMat irradiation experiments.
FLUKA has been extensively used for the preparation and analysis of LIU- and and HL-LHC-related HiRadMat tests, including tests for the HL-LHC collimators, the new HL-LHC injection protection absorber, and the new SPS-to-LHC transfer line collimators
  Determination of HRMT beam parameters
  Analysis by using energy deposition maps as input for FEA tools to assess thermomechanical responses
DPA as a quantity is a measure for macroscopic effects which can be determined in experiments, implementation in FLUKA based on models to incorporate material properties:
  Damage in HL-LHC collimators quantified by DPA based on extrapolated amount of losses for HL operation.
  Fluence necessary to achieve similar DPA levels in collimators samples
Monte Carlo shower simulations in FLUKA provide the link between experiments and the actual accelerator environment.
Energy deposition, radiation damage, gas production studies for beam-intercepting devices in HL-LHC ongoing.
HiRadMat shock response tests of irradiated collimator components envisaged.