## Slide 1: Material procurement of seamless cavities and characterization of spun half-cells
Carolina Abajo
EN/MME
Manufacturing of Seamless cavities - CERN-LNL meeting 07·11·2018

## Slide 2: 1. LNL – Material requirements
Large size copper discs
Manufacturing of 400 MHz seamless cavities
Φ1500mm
1
Manufacturing of Seamless cavities - CERN-LNL meeting

## Slide 3: 2. CERN strategy & suppliers
Firm | Cu OFE | Comments | Alternative
Schmelzmetall | No offer | No Dimensions | DECLINE
ILF products | No offer |  | DHP BSEN1652
Goodfellow | No offer |  | Cu 99,9% CW024 C106H H (DHP)
Prometall | No offer |  | CW0211A R240 Demi dur
SISO | No offer |  | Cu DHP demi dur R240
Tresoldi metalli | No offer |  | DECLINE
Hauselmann | No offer |  | Cu DHP R240 Demi dur
Luvata | No offer | max rolling width 1020mm | DECLINE
Aurubis | No offer | max rolling width 1100mm | DECLINE
Metal sheets | No offer | max thickness 3mm | DECLINE
Metelec | No offer | max thickness 3mm | DECLINE
Matthey | No offer |  | DECLINE
Wieland | No offer |  | DECLINE
Columbia metals | No offer |  | DECLINE
Aviva | No offer | (3x) 3060.7x1231.9x4.7mm | DECLINE
Eisenmetall | No offer | 1000x2000mm | DECLINE
Ametra metall | No offer |  | DECLINE
Amco metall | No offer |  | DECLINE
Swissmetal | No offer |  | DECLINE
KME | OFFER | 6000Kg min | 
MKM | OFFER | out of specs. surface | 
Bikkar | OFFER | unreacheable firm | 
Carl Shreiber | OFFER | closed | 
Cu OFE
CERN specs
Ø1500mm
2
Manufacturing of Seamless cavities - CERN-LNL meeting

## Slide 4
Cu | Cu % | Other elements | Rp0.2 | Rm | Elongation min A 50 |  | cold froming propierties
OFE | 99.99 |  | 220-260 | <140 | 33 | 40-65 | Excellent
OF | 99.95 | Pb 0.005 | 220-260 | <140 | 33 | 40-65 | Excellent
HCP | 99.95 | P(0.002-0.007)Pb0.005 | 220-260 | <140 | 33 | 40-65 | Excellent
DHP | 99.99 | P (0.015-0.04) | 220-260 | <140 | 33 | 40-65 | /
Cu OFE
CERN specs
Ø1500mm
Cu OFE Alternatives
Ø1500 mm
2. CERN strategy & suppliers
3
Manufacturing of Seamless cavities - CERN-LNL meeting

## Slide 5
Firm | Cu OFE | Comments | Alternative
Schmelzmetall | No offer | No Dimensions | No offer
ILF products | No offer |  | DHP BSEN1652
Goodfellow | No offer |  | Cu 99,9% CW024 C106H H (DHP)
Prometall | No offer |  | CW0211A R240 Demi dur
SISO | No offer |  | Cu DHP demi dur R240
Tresoldi metalli | No offer |  | No offer
Hauselmann | No offer |  | Cu DHP R240 Demi dur
Luvata | No offer | max rolling width 1020mm | No offer
Aurubis | No offer | max rolling width 1100mm | No offer
Metal sheets | No offer | max thickness 3mm | No offer
Metelec | No offer | max thickness 3mm | No offer
Matthey | No offer |  | No offer
Wieland | No offer |  | No offer
Columbia metals | No offer |  | No offer
Aviva | No offer | (3x) 3060.7x1231.9x4.7mm | No offer
Eisenmetall | No offer | 1000x2000mm | No offer
Ametra metall | No offer |  | No offer
Amco metall | No offer |  | No offer
Swissmetal | No offer |  | No offer
KME | OFFER | 6000Kg min | 
MKM | OFFER | out of specs. surface | 
Bikkar | OFFER | unreacheable firm | 
Carl Shreiber | OFFER | closed | 
Cu OFE
CERN specs
Ø1500mm
Cu OFE Alternatives
Ø1500 mm
2. CERN strategy & suppliers
4
Manufacturing of Seamless cavities - CERN-LNL meeting

## Slide 6: 2. CERN strategy & suppliers
Firm | Cu OFE | Comments | Alternative
Schmelzmetall | No offer | No Dimensions | No offer
ILF products | No offer |  | DHP BSEN1652
Goodfellow | No offer |  | Cu 99,9% CW024 C106H H (DHP)
Prometall | No offer |  | CW0211A R240 Demi dur
SISO | No offer |  | Cu DHP demi dur R240
Tresoldi metalli | No offer |  | No offer
Hauselmann | No offer |  | Cu DHP R240 Demi dur
Luvata | No offer | max rolling width 1020mm | No offer
Aurubis | No offer | max rolling width 1100mm | No offer
Metal sheets | No offer | max thickness 3mm | No offer
Metelec | No offer | max thickness 3mm | No offer
Matthey | No offer |  | No offer
Wieland | No offer |  | No offer
Columbia metals | No offer |  | No offer
Aviva | No offer | (3x) 3060.7x1231.9x4.7mm | No offer
Eisenmetall | No offer | 1000x2000mm | No offer
Ametra metall | No offer |  | No offer
Amco metall | No offer |  | No offer
Swissmetal | No offer |  | No offer
KME | OFFER | 6000Kg min | 
MKM | OFFER | out of specs. surface | 
Bikkar | OFFER | unreacheable firm | 
Carl Shreiber | OFFER | closed | 
Cu OFE
CERN specs
Ø1200-1150mm
Cu OFE
CERN specs
Ø1500mm
Cu OFE Alternatives
Ø1500 mm
5
Manufacturing of Seamless cavities - CERN-LNL meeting

## Slide 7: 2. CERN strategy & suppliers
Firm | Cu OFE | Comments | Alternative
Schmelzmetall | No offer | No Dimensions | No offer
ILF products | No offer |  | DHP BSEN1652
Goodfellow | No offer |  | Cu 99,9% CW024 C106H H (DHP)
Prometall | No offer |  | CW0211A R240 Demi dur
SISO | No offer |  | Cu DHP demi dur R240
Tresoldi metalli | No offer |  | No offer
Hauselmann | No offer |  | Cu DHP R240 Demi dur
Luvata | No offer | max rolling width 1020mm | No offer
Aurubis | No offer | max rolling width 1100mm | No offer
Metal sheets | No offer | max thickness 3mm | No offer
Metelec | No offer | max thickness 3mm | No offer
Matthey | No offer |  | No offer
Wieland | No offer |  | No offer
Columbia metals | No offer |  | No offer
Aviva | No offer | (3x) 3060.7x1231.9x4.7mm | No offer
Eisenmetall | No offer | 1000x2000mm | No offer
Ametra metall | No offer |  | No offer
Amco metall | No offer |  | No offer
Swissmetal | No offer |  | No offer
KME | OFFER | 6000Kg min | 
MKM | OFFER | out of specs. surface | 
Bikkar | OFFER | unreacheable firm | 
Carl Shreiber | OFFER | closed | 
Cu OFE
CERN specs
Ø1200-1150mm
Cu OFE
CERN specs
Ø1200-1150mm
Cu OFE
CERN specs
Ø1500mm
Cu OFE Alternatives
Ø1500 mm
6
Manufacturing of Seamless cavities - CERN-LNL meeting

## Slide 8: 2. CERN strategy & suppliers
Inspection certificate 3.1, EN 10204
Ultrasonic testing
No possibility to characterise the material
Material characterisation in terms of composition and surface state after Electropolishing
Before forming
After forming
7
Manufacturing of Seamless cavities - CERN-LNL meeting

## Slide 9: 2. CERN strategy & suppliers
Material preparation procedure at CERN
Supply chain- stores
US inspections
NDT
Water jet cutting
Protection layer (Pavatex)
Between the sheet and the equipment
Cleaning
Teflon holder
Annealing
Reception
Material certificate
3.1 EN 10204
SS holder
Film
New dimensions  new supplier?
Aurubis: maximum width is 1100 mm and MOQ is 2000 kg.
8
Manufacturing of Seamless cavities - CERN-LNL meeting

## Slide 10
Up to 20 discs in one cycle
Ø940mm
2. CERN strategy & suppliers
9
Manufacturing of Seamless cavities - CERN-LNL meeting

## Slide 11: 3. Annealing of Cu OFE in CERN
E. Cantergiani EDMS 1711461
Base material OFE Cu th.3mm
600°C – 2h in vacuum 10-6-10-7mbar
10
Manufacturing of Seamless cavities - CERN-LNL meeting

## Slide 12: 4. Control of cavities at CERN
Shape profile
Thickness profile
Diameter and circularity
Metrology
Manufacturing of Seamless cavities - CERN-LNL meeting
11

## Slide 13: Half cells characterisation
Hardness Profile
Equator
Iris
Mechanical properties
Longitudinal
Transverse
4. Control of cavities at CERN
UTS
YS
Stress and hardness relation
Manufacturing of Seamless cavities - CERN-LNL meeting
12

## Slide 14: 5. Manufacturing procedure of half cells
Hardness Profile
No annealing
20 years ago
Chart: Position along the profile of the half cell
| 1 | 2 | 4 | 6 | 8 | 10 | 11 | 12 | 13 | 14 | 16 | 17 | 18
Reference LHC half cells 20 years ago | 100 | 95 | 110
Equator
Iris
200°C
290°C
Manufacturing of Seamless cavities - CERN-LNL meeting
13

## Slide 15: 5. Manufacturing procedure of half cells
Hardness Profile
No annealing
Intermediate annealing
20 years ago
Fully annealed iris
Chart: Position along the profile of the half cell
| 1 | 2 | 4 | 6 | 8 | 10 | 12 | 14 | 16 | 17 | 18
Intermediate annealing 620C-1h | 78.4 | 81.26 | 84.34 | 84.5 | 76.52 | 67.86 | 71.9 | 58.36 | 55.42 | 41.28 | 41.3
Reference LHC half cells 20 years ago | 100 | 95 | 110
Equator
Iris
Base material
Equator
Iris
200°C
290°C
Manufacturing of Seamless cavities - CERN-LNL meeting
14
%Cold Work
Recrystallization temperature

## Slide 16
Intermediate annealing during spinning of half-cells
EDMS 1986651 P.Pastuszak
“The cavity succeeds on all criteria established in this report (Global failure 1, Local failure, Non-linear buckling), which are in accordance with ASME code. The cavity is judged safe by authors and suitable for use in the LHC RF cryomodule.”
5. Manufacturing procedure of half cells
Manufacturing of Seamless cavities - CERN-LNL meeting
15

## Slide 17: 5. Manufacturing procedure of half cells
Hardness Profile
Influence of annealing temperature
No annealing
Intermediate annealing
20 years ago
Fully annealed iris
Chart: Position along the profile of the half cell
| 1 | 2 | 4 | 6 | 8 | 10 | 12 | 14 | 16 | 17 | 18
Intermediate annealing 620C-1h | 78.4 | 81.26 | 84.34 | 84.5 | 76.52 | 67.86 | 71.9 | 58.36 | 55.42 | 41.28 | 41.3
Reference LHC half cells 20 years ago | 100 | 95 | 110
No Annealing | 91.6 | 89.975 | 96.76 | 98.76 | 88.94 | 85.92 | 90.1 | 92.26 | 97.44 | 102.68 | 104.96
290°C
Equator
Iris
Base material
Equator
Iris
290°C
%Cold Work
Recrystallization temperature
Manufacturing of Seamless cavities - CERN-LNL meeting
16

## Slide 18: 5. Manufacturing procedure of half cells
Hardness Profile
Influence of annealing temperature
No annealing
Intermediate annealing
20 years ago
Fully annealed iris
Chart: Position along the profile of the half cell
| 1 | 2 | 4 | 6 | 8 | 10 | 12 | 14 | 16 | 17 | 18
Intermediate annealing 620C-1h | 78.4 | 81.26 | 84.34 | 84.5 | 76.52 | 67.86 | 71.9 | 58.36 | 55.42 | 41.28 | 41.3
Reference LHC half cells 20 years ago | 100 | 95 | 110
No Annealing | 91.6 | 89.975 | 96.76 | 98.76 | 88.94 | 85.92 | 90.1 | 92.26 | 97.44 | 102.68 | 104.96
No annealing - post annealing 200C | 93.78 | 93.68 | 87.94 | 88.58 | 94.54 | 101.26 | 101.5
200°C
290°C
Equator
Iris
Base material
Equator
Iris
250°C
290°C
Manufacturing of Seamless cavities - CERN-LNL meeting
17
%Cold Work
Recrystallization temperature

## Slide 19: 5. Manufacturing procedure of half cells
Hardness Profile
Influence of annealing temperature
No annealing
Intermediate annealing
20 years ago
Fully annealed iris
Chart: Position along the profile of the half cell
| 1 | 2 | 4 | 6 | 8 | 10 | 12 | 14 | 16 | 17 | 18
Intermediate annealing 620C-1h | 78.4 | 81.26 | 84.34 | 84.5 | 76.52 | 67.86 | 71.9 | 58.36 | 55.42 | 41.28 | 41.3
Reference LHC half cells 20 years ago | 100 | 95 | 110
No Annealing | 91.6 | 89.975 | 96.76 | 98.76 | 88.94 | 85.92 | 90.1 | 92.26 | 97.44 | 102.68 | 104.96
No annealing - post annealing 200C | 93.78 | 93.68 | 87.94 | 88.58 | 94.54 | 101.26 | 101.5
No annealing- post annealing 250C | 90.24 | 90.62 | 84.46 | 85.64 | 87.5 | 86.2333 | 94.74 | 101.62 | 102.34
200°C
290°C
Equator
Iris
Base material
Equator
Iris
250°C
290°C
Manufacturing of Seamless cavities - CERN-LNL meeting
18
%Cold Work
Recrystallization temperature

## Slide 20: 5. Manufacturing procedure of half cells
Hardness Profile
Influence of annealing temperature
No annealing
Intermediate annealing
20 years ago
Fully annealed iris
Chart: Position along the profile of the half cell
| 1 | 2 | 4 | 6 | 8 | 10 | 12 | 14 | 16 | 17 | 18
Intermediate annealing 620C-1h | 78.4 | 81.26 | 84.34 | 84.5 | 76.52 | 67.86 | 71.9 | 58.36 | 55.42 | 41.28 | 41.3
Reference LHC half cells 20 years ago | 100 | 95 | 110
No Annealing | 91.6 | 89.975 | 96.76 | 98.76 | 88.94 | 85.92 | 90.1 | 92.26 | 97.44 | 102.68 | 104.96
No annealing - post annealing 200C | 93.78 | 93.68 | 87.94 | 88.58 | 94.54 | 101.26 | 101.5
No annealing- post annealing 250C | 90.24 | 90.62 | 84.46 | 85.64 | 87.5 | 86.2333 | 94.74 | 101.62 | 102.34
No annealing - post annealing 290C | 85.4 | 89.94 | 83.74 | 87.34 | 86.5 | 83.0333 | 79.48 | 46.98 | 56.76
200°C
290°C
Equator
Iris
Base material
Equator
Iris
200°C
250°C
290°C
Manufacturing of Seamless cavities - CERN-LNL meeting
19
%Cold Work
Recrystallization temperature

## Slide 21: 5. Manufacturing procedure of half cells
Chart: Position along the profile of the half cell
| 1 | 2 | 4 | 6 | 8 | 10 | 12 | 14 | 16 | 17 | 18
Intermediate annealing 620C-1h | 78.4 | 81.26 | 84.34 | 84.5 | 76.52 | 67.86 | 71.9 | 58.36 | 55.42 | 41.28 | 41.3
Reference LHC half cells 20 years ago | 100 | 95 | 110
No Annealing | 91.6 | 89.975 | 96.76 | 98.76 | 88.94 | 85.92 | 90.1 | 92.26 | 97.44 | 102.68 | 104.96
Annealing before deforming the iris | 84.3 | 87.1 | 99.8333 | 91.0667 | 84.8 | 77.1667 | 86.2333 | 86.0667 | 95.84 | 94.32 | 98.04
Hardness Profile
Influence of annealing temperature
No annealing
Intermediate annealing
20 years ago
Fully annealed iris
200°C
290°C
Equator
Iris
Base material
Equator
Iris
200°C
250°C
290°C
New forming procedure
Manufacturing of Seamless cavities - CERN-LNL meeting
20

## Slide 22: 6. Final remarks
Final required mechanical properties
In case of intermediate annealing during forming is needed
New suppliers/new dimensions
In order to fulfill the technical specifications of CERN
To take into account…
Manufacturing of Seamless cavities - CERN-LNL meeting
21