## Slide 1: GaN for large fluence irradiation monitoring
1 Vilnius University, Institute of Photonics and Nanotechnology
2 CERN
J.Vaitkus, E.Gaubas, T.Ceponis, J.Pavlov, V.Rumbauskas
Motivation
Characterization techniques
Results on AT GaN
Commercial GaN LED structures as dosimeters
Summary.
Outline: WP15 task for VU: contribution to radiation monitoring & imaging.

## Slide 2: The devices for integrated fluence monitoring and radiation field imaging based on Si properties
The device for the contactless fluence monitoring delivered to CERN.
The device for 2D integrated fluence imaging up to 3“.
Si
To remind previous contributions
The “trapping” time

## Slide 3: GaN promise
Variations of the current transients (in the tentative detectors made of GaN:Mg and GaN:Mn for the 290 fs laser pulses at 315nm wavelength excitation) dependent on neutron irradiation fluence.
J. Grant et al J.Vaitkus et al. / NIMA 576 (2007) 60–65

## Slide 4: Characterization techniques (1):
The PPIS were implemented using excitation by a tuneable wavelength laser and measurements of the photo-response by applying microwave probed photoconductivity transient (MW-PC) technique.
Tuneable wavelength femtosecond-nanosecond lasers (210 to 2300 nm) were employed.
Pulsed photoionization spectroscopy (PPIS)

## Slide 5: Characterization techniques (2):
Pulsed barrier evaluation by linearly increased voltage (BELIV)
Proton induced luminescence spectroscopy (PIL)
TCT

## Slide 6
Γ - the broadening parameter
Results on AT GaN irradiated by 1 MeV neutrons
GaN:Mn
GaN:Mg
 | Non-irradiated |  | Irradiated with Φ=1016 cm-2 |  | 
GaN:Mn | Photo-activation energy (eV) | Γ | Photo-activation energy (eV) | Γ | Defect type
 | EMn-1=1.40 | 0.05 | EMn-1irr=1.42 | 0.08 | Mn related
 | EMn-2=1.98 | 0.25 | EMn-2irr=1.98 | 0.22 | Might be oxygen related
 | EMn-3=2.40 | 0.15 | EMn-3irr=2.37 | 0.25 | GaI or NI
 | EMn-4=2.97 | 0.25 | EMn-4irr=2.96 | 0.28 | Unidentified
GaN:Mg | EMg-1=1.30 | 0.02 | − | − | Donor/acceptor state
 | EMg-2=1.70 | 0.15 | EMg-1irr=1.71 | 0.22 | VNMgGa
 | EMg-3=2.07 | 0.23 | EMg-2irr=2.05 | 0.27 | VGa
 | EMg-4=2.39 | 0.15 | EMn-3irr=2.37 | 0.25 | GaI or NI
 | − | − | EMg-4irr=2.45 | 0.16 | Unidentified or NI
 | EMg-5=3.00 | 0.32 | EMg-5irr=3.00 | 0.35 | Unidentified
 | EMg-6=3.30 | 0.2 | EMg-6irr=3.30 | 0.27 | MgI

## Slide 7
(a) -Variations of cross-sections of the photon-electron coupling and of trap concentration as a function of excitation photon energy in the pristine AT-grown GaN samples doped with Mg and Mn. Vertical arrows indicate the peak positions of the PPIS steps, ascribed to different centres.
(b) – Variations of the predominant TR-PL spectral peaks with neutron irradiation fluence. In the inset (i) variations of TR-PL spectra are depicted. (The excitation - 290 fs laser pulses, 315nm wavelength)
E. Gaubas, T. Čeponis, et al, “Pulsed photo-ionization spectroscopy of traps in as-grown and neutron irradiated ammonothermally synthesized GaN”, www.nature.com/scientificreports; Scientific Reports (2019) 9:1473
AT GaN

## Slide 8
GaN LED-based structures for remote dosimetry
Evolution of the BELIV current transients for the reverse (a) and forward (b) biased GaN LED (PL = 45 s). (a) LED irradiated with the proton fluences of 0 (1); 51014 p/cm2 (2); 81014 p/cm2 (3); 11015 p/cm2 (4); 21015 p/cm2 (5); 31015 p/cm2 (6); and 51015 p/cm2 (7), respectively (UP,R = 6 V). (b) Pristine LED (1-3) and LED irradiated with the fluence of 51015 p/cm2 (1 – 3) for peak voltage UP,F of 1 V (1 and 1’), 2 V (2 and 2’), and 3 V(3 and 3’).
E. Gaubas, T.Ceponis, D. Meskauskas, J. Pavlov, A.Zukauskas, V. Kovalevskij,V. Remeikis Sensors and Actuators A 267 (2017) 194–199

## Slide 9
TCT transients (a) and peak-current (b) as a function of reverse-bias voltage measured on pristine and heavily irradiated LED-based sensor.
GaN LED-based structures for remote dosimetry
E. Gaubas, T.Ceponis, D. Meskauskas, J. Pavlov, A.Zukauskas, V. Kovalevskij,V. Remeikis Sensors and Actuators A 267 (2017) 194–199

## Slide 10
Evolution of the proton induced luminescence spectra as a function of 1.6 MeV proton fluence.
In the inset,- a picture of the proton-induced luminescence on GaN LED-based sensor, installed within irradiation chamber.
GaN LED-based structures for remote dosimetry
E. Gaubas, T.Ceponis, D. Meskauskas, J. Pavlov, A.Zukauskas, V. Kovalevskij,V. Remeikis Sensors and Actuators A 267 (2017) 194–199
(b) – Comparison of spectra of the laser induced photoluminescence and electroluminescence, recorded on pristine LED.

## Slide 11
– The as-recorded short-circuit current (ISC) as a function of proton flux for the initial irradiation stages of a few seconds.
- The as-recorded ISC (measured for a fixed proton flux,- ISC,ff) as well as YG-L intensity as a function of the irradiation fluence. Lines serve as the eye-guides to depict the experimental dependences of ISC and YG-L on flux and fluence.
GaN LED-based structures for remote dosimetry
E. Gaubas, T.Ceponis, D. Meskauskas, J. Pavlov, A.Zukauskas, V. Kovalevskij,V. Remeikis Sensors and Actuators A 267 (2017) 194–199

## Slide 12: Summary
  The AT-GaN material performance showed insignificant changes after neutron irradiation with large fluences (up to 51016 e/cm2 ).
  GaN LED-based sensors can be used for the synchronous detection of hadron irradiation by recording the optical (B-L) and electrical signals (ISC and TCT transients).
Acknowlegments: This project has received part of funding from the European Union’s Horizon 2020 Research and Innovation programme under Grant Agreement no. 654168, and from Lithuanian Research Council.

## Slide 13: Thank you for your attention !
1579-1832