## Slide 1: Diagnostics of hot anode surface by optical methods
S. Gortschakow, St. Franke, D. Gonzalez, R. Methling, D. Uhrlandt
Leibniz Institute for Plasma Science and Technology
Greifswald, Germany

## Slide 2: Outline
Introduction
Motivation
Optical methods for temperature determination
  Application examples:
    Measurements in the post-arc phase
    Measurements during the active phase
    Surface with impurities
  Summary and outlook

## Slide 3: Introduction
972 km from Padua
235 km from Berlin, 265 km from Hamburg
Padua
Greifswald

## Slide 4: Introduction
Leibniz Institute for Plasma Science and Technology (INP)
Institute of Physics (IfP) of Greifswald University
Max Planck Institute for Plasma Physics (IPP) Nuclear fusion reactor Wendelstein 7-X
Greifswald - Center of Plasma Science

## Slide 5: Introduction
Leibniz Institute for Plasma Science and Technology (INP)
Application-driven research
surface modification and chemistry
process diagnostics and monitoring
biomaterials and surfaces
plasma medicine, plasma decontamination
high-voltage techniques
switching and welding arcs
49 laboratories
200 employers
annual budget 20 M€

## Slide 6: Introduction: switching arc research
Charging voltage | 50 V – 3500 V
Min current | 1.3 kA@ 50 Hz
Max current | 100 kA @ 50 Hz
TRV level | 41.5 kV @ 1000 Hz DAC
Charging voltage | 500 V – 18000 V
Min current | 100 A@ 50 Hz
Max current | 10 kA @ 50 Hz
Other features | No TRV Flexible frequency 16 Hz – 1000 Hz, pulsed DC operation
since 06.2015
since 07.2019

## Slide 7: Introduction: switching arc research
vacuum circuit breaker
Volume 0.003 – 10 l
Stroke 0.5 – 25 mm
Operation velocity 0.1 - 5 m/s
model circuit breaker
Volume 52 l
Mountings for various electrodes
Stroke 0.5 - 25 mm
Operation velocity 0.5 - 4 m/s

## Slide 8: Motivation
Electrodes in high-power applications
  current transfer
  interaction with substrate
  material source (vacuum arcs, welding, coating)
  source of problems – damage through erosion → contamination of plasma, gas, walls with electrode material, strong surface deformation → operation failure
  Processes to be understand, behavior to be characterized
  heating and cooling dynamics
  behavior of melted surface
  erosion behavior → vapor and droplets
  interaction with plasma
Monitoring of electrode temperature is crucial for phenomena understanding and device optimization

## Slide 9: Motivation
Vacuum circuit breakers
  environmentally friendly operation
High-current operation
  (strong) electrode melting and evaporation
  atomic vapour as possible source for restrikes
  hot anode – major source of atomic vapour
  Focus on the anode surface temperature measurements
Cathode
Anode
cathode
anode
diffuse
footpoint
intense mode
anode spot
anode plume
success
failure

## Slide 10: Motivation

## Slide 11: Optical diagnostics: advantages and disadvantages
“Classical” method (thermocouple) fails
  probes will be damaged when placed within the region of interest
  signal distortion due to EM fields
  high spatial (and temporal) resolution required
Clear advantages of optical methods
  non-invasive
  qualitative and quantitative measurements possible
  high spatial resolution – local properties
  high temporal resolution – dynamics
  applicable in a wide parameter range due to variability of methods
Some disadvantages of optical measurements
  optical access to the object necessary
  radiation intensity must be sufficient
  distortions in the optical pathway through hot fluxes and plasma itself
  costs of the devices, complex apparatus and evaluation methods

## Slide 12: Optical diagnostics: basics of temperature determination
Black-body radiation acc. to Planck’s law
One measured value, but two unknowns – standard solution ways
  known emissivity from other measurements or theory
  measurements at two different wavelengths

## Slide 13: Optical diagnostics: basics of temperature determination
Data for emissivity
  Mostly known for “clean” surfaces
  measured at idealized conditions
  however emissivity depends on
    chemical composition
    surface roughness
    surface “state” – solid, liquid, boiling, phase transition…
    view angle
Best solution – ín-situ measurements simultaneously with temperature measurements

## Slide 14: Optical diagnostics: basics of temperature determination
Two-colour pyrometry
  Assumption and Wien approximation
  Assumption could be too rough due to
    complex chemical composition
    surface roughness
    surface “state” – solid, liquid, boiling, phase transition…
Best solution – small difference between the wavelengths, but (!) significant errors  careful choice of wavelength range necessary

## Slide 15: Optical diagnostics: methods
Selected methods
  Pyrometry (commercial)
  Thermography (commercial)
  Optical Emission Spectroscopy (OES) (scientific)
  High-speed camera (HSC) techniques enhanced by filter (scientific)
Method choice and requirements
  sensitivity  surface should emit radiation (T high enough)
  possible distortions  plasma radiation is either absent or can be excluded from consideration  oxides and surface impurities influences the results  smooth surfaces/low roughness preferable

## Slide 16: Optical diagnostics: pyrometry
Advantages
Commercially available devices (pyrometer)
Acquisition time between 10µs and 1s
Temperature range 200-4000 K
Simple setup and arrangement
Determination of the cooling dynamics possible
Disadvantages/ restrictions
Emissivity of the surface must be known (exception two-colour pyrometer)
Special optics (windows) depending on the temperature and spectral range necessary
Time resolved measurements with rough spatial resolution (min spot size 0.5 - 1mm)
Kleiber Pyroskop

## Slide 17: Optical diagnostics: thermography
Advantages
  Commercially available devices
  2D temperature distribution at one shot
  Temperature range 200-5000 K
  Simple setup and arrangement
  Determination of the cooling dynamics possible
Disadvantages/ restrictions
  Emissivity of the surface must be known (exception – two color cameras)
  Special optics (windows) depending on the temperature and spectral range necessary
Time resolved measurements with full size typically with 60 -125 Hz, but (!) temporal resolution with reduced number of pixels possible (up to 10 kHz)
IR camera VarioCAM with 60 Hz techniques
IR camera FLIR with 125 Hz techniques

## Slide 18: Optical diagnostics: emission spectroscopy
Advantages
Time resolve measurements possible
Simultaneous determination of surface emissivity possible
Flexibility by choice of spectral range
Characterization of surface impurities possible
Disadvantages/Restrictions
Light intensity calibration necessary (tungsten strip lamp)
Space resolved measurements along the slit
Additional optical setup necessary
Projection of the entrance slit
Temperature distribution

## Slide 19: Optical diagnostics: high-speed camera techniques
Advantages
Time resolved measurements
2D picture of the surface
Manageable effort for setup
Disadvantages/Restrictions
Special optical filters (MIF, narrow band)/ optical modules necessary
Light intensity calibration necessary
Possible impurities of the surface should be taken into account
HSC MotionPro Y4
Temperature distribution
HSC image

## Slide 20: Optical diagnostics: method applicability
  Ignition phase
  High-current phase (active phase)
  Current zero crossing
  Post-arc phase
T measurement possible
 | ignition | High-current | CZ | post-arc
pyrometry | - | (+) | + | -
thermography | - | (+) | + | -
OES | - | (+) | + | +
HSC | - | (+) | + | -

## Slide 21: Practical examples
Clean surface with known chemical composition – CuCr contacts for vacuum arcs
Measurements in post-arc phase by
  NIR spectrometer
Measurement in the active phase
  pyroscopic measurements
  2D temperature profiles by enhanced high-speed camera techniques
  use of current cut-off techniques
Surface with impurities
  characterization of cold metal transfer welding by OES and HSC

## Slide 22: Practical examples
Operation conditions:
Pulsed current, sinusoidal, 10 ms, 1- 20 kA
Electrodes diameter 10-60 mm; maximum distance 10 mm
Rough unpolished surface
Electrodes are moving from closed position (1 m/s)
Arc initialization (“breakdown”) from bridge explosion
Arc plasma separates the electrode from diagnostic setup
Simplification:
Anode is fixed, cathode is moving

## Slide 23: Measurements in post-arc phase by NIR
Plasma!
+
=
NIR 900-1600 nm
NIR optics
acquisition times

## Slide 24: Measurements in post-arc phase by NIR
W strip lamp
calibration
window transmission
background correction
determination of T and 
T


## Slide 25: Measurements in active phase by pyroscope
Measurements parallel to surface for approximation of plasma contribution
Plasma contribution sufficiently low
Corrected signal gives reasonable temperature
parallel measurement
surface measurement

## Slide 26: Measurements in active phase by pyroscope
Cu-Cr eutectic melting temp.
1.
2.
3.
Temperature maximum around 6 ms, i.e. after current maximum
Accelerated temperature decay after 6 ms up to Cu-Cr eutectic melting point (at 2020 K).
Plateau closely after current zero (occurs at different temperatures)

## Slide 27: Measurements in active phase by pyroscope
Good agreement between temperatures from pyroscope and from NIR spectra
Higher currents lead to higher anode surface temperatures
Uncertainties NIR spectrometer: ± 100 K
Uncertainties pyroscope: ± 200 K around maximum, ± 50 K around eutectic point, ± 100 K at lower detection limit
Lower thermal radiation for Cu
No continuum emission observed after CZ with NIR
Due to comparable emissivity the anode surface temperatures for Cu should be considerably lower than for Cu-Cr

## Slide 28: Measurements in active phase by HSC
+
=
plasma only
Planck + plasma
inspection angle 9.2°
Without correction for plasma background radiation.
With correction for plasma background radiation

## Slide 29: Measurements in active phase by HSC
Quantitative temperature from calibration with addition measurements, like e.g. NIR spectroscopy

## Slide 30: Measurements in the active phase: current cut-off
Current flow through test object VI was switched artificially to zero by means of bypath SC
Diagnostics by
3 channel rackmount spectrometer VIS 200-1000 nm / NIR 880-1700 nm / NIR 1.6-2.4 µm
High-speed NIR camera 1.5 – 1.7 µm, 6100 fps with 128 x 24 pix resolution

## Slide 31: Measurements in the active phase: current cut-off
Current cut-off within Δt ~ 0.56 ms
Temperature about 3300 K before and about 4000 K after anode spot type 2

## Slide 32: Measurements in the active phase: current cut-off
Before CZ: plasma radiation dominates emission  no information on anode temperature
After CZ: fit to Planck curve  anode surface temperature determinable

## Slide 33: Measurements in the active phase: current cut-off
Higher anode surface temperatures and longer cooling in case of anode spot type 2
Peaks in temperature curve from thermography (lines) due to changing emissivity during solidification process – in spectroscopic method (dots) the emissivity was adapted during Planck curve fitting

## Slide 34: Example 5: Surface with impurities
High-speed camera
Spectrograph
CMT welding – pulsed arc operation

## Slide 35: Example 5: Surface with impurities
HSC image
Material steel S235
Slit length 12 mm
Results after current cut-off
H. Schöpp, A. Sperl, R. Kozakov, G. Gött, D. Uhrlandt, G. Wilhelm, J. Phys. D: Appl. Phys. 45(2012) 235203

## Slide 36: Example 5: Surface with impurities
1300
1810
2300
Kelvin
Planck-fit for each spatial position
Colder slag due to higher emissivity

## Slide 37: Summary and outlook
Summary
Various of optical methods for temperature determination is available
In case of an arc discharge: “easy case” – measurements in the post-arc phase; “complex case” – measurements during the active phase
Combinations of various methods increase applicability range
Outlook
Further development is necessary for temperature measurements within the active phase
Increase of temporal resolution
Further results will be presented at ISDEIV2020/Padova (IT), ICEC2020/ St. Gallen (CH) and GD2020/Greifswald

## Slide 38: You are kindly invited to participate in

## Slide 39: Thank you very much for your attention!
Dr. Sergey Gortschakow
Leibniz Institute for Plasma Science and Technology
Address: Felix-Hausdorff-Str. 2, 17489 Greifswald
Phone: +49 - 3834 - 554 463, Fax: +49 - 3834 - 554 301
Email: sergey.gortschakow@inp-greifswald.de
Web: www.leibniz-inp.de

## Slide 40: Introduction
Cu-Cr butt,
15 kA,
120-180 mT
It is not possible to deduce an unambiguous temperature dependence of the electrode emissivity.
Uniform emissivity of e = 0.3 was taken for evaluation of spectra.
Temperatures obtained for several assumptions of fixed emissivities (determined for the example of 5 spectra).
Assuming e = 0.3: => uncertainty ± 50 K => acceptable!

## Slide 41: Literature
H. Schöpp, A. Sperl, R. Kozakov, G. Gött, D. Uhrlandt, G. Wilhelm, J. Phys. D: Appl. Phys. 45(2012) 235203
R. Methling, M. Kurrat, T. Pieniak, St. Franke, D. Uhrlandt, B. Weber, S. Gortschakow, Proc. of 28th ISDEIV, V 2, 2018
R. Methling, St. Franke, S. Gortschakow, M. Abplanalp, R.-P. Sütterlin, Th. Delachaux, K. O. Menzel, IEEE TPS 45 (2017)

## Slide 42: Introduction
Greifswald – a Hanseatic City founded 1248
57000 habitants, University town since 1456, one of the centers of North German Brick Gothic at the Baltic Sea coast