## Slide 1
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019
Investigations of the transition from field electron emission
to plasma discharges (glow discharges and micro-arcs)
with extended use of the Fowler-Nordheim plot
(Abstract ID: 110)
Wolfram Knapp#*
#Otto-von-Guericke-Universität Magdeburg, Universitätsplatz 2, D-39106 Magdeburg, Germany
*Knapptron GmbH - Vacuum Electronics, Privatweg 3, D-39291 Möser, Germany
E-mail contacts: #wolfram.knapp@ovgu.de or *dr.who.knapp@t-online.de
-> Posters with abstract ID 110, 111 and 116

## Slide 2
OUTLINE:
1. Introduction
2. Electron field emission with micro-arc discharges
3. Transitions from electron field emission to plasma discharges
  - Types of stable plasma discharges: glow and micro-arc discharges
  - Smooth transition (electron field emission glow discharge)
  - Sudden transition (electron field emission micro-arc discharge)
  - Graphical evaluation method
4. Extended use of the Fowler Nordheim plot for energetic evaluation
5. Plasma-physical approach
6. Conclusion and outlook
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 3
1. Introduction Otto von Guericke
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 4
Introduction Otto von Guericke
and his experiment with the Magdeburg hemispheres
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 5
Historical Introduction
Otto von Guericke and his electrostatically experiment
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019
Fig. 1. Otto von Guericke and his electrostatically experiment with charged sulphur ball and bird's feather. In the year 1672 he had a correspondence with Gottfried Wilhelm Leibniz (9 letters). One topic was a discussion about observed discharge effects (spark discharges) [1].
[1] O. v. Guericke, G. W. Leibniz, “Leibniz und Gericke im Diskurs – Die Exerpte aus den Experimenta Nova und der Briefwechsel”
(Latin and German); Editors: B. Heinicke, W. Knapp, P. Rubini, P. Streitenberger, DE GRUYTER, Berlin (2018).

## Slide 6
Introductions Field emission measurement with IE > 1 mA (DC)
Fig. 1. Field-emission characterization: IE = f(U) diagram with a voltage reduction for currents > 1.5 mA [1].
[1] W. Knapp, “Field-emission investigations of micro-structured stainless steel 1.4301 (ASTM 304) for extended use of vacuum components
as very large FE cathode arrays.” Poster contribution IVNC 2017.
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 7
2. Electron field emission with micro-arc discharges
Longterm FE stability measurement with breakdowns (vacuum micro-arcs)
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019
Stability measurements with 20 mA pulsed current
10 ms pulse-on time, 50% duty cycle (ton/(ton+toff) = ton/T = 0.5)
Emission stable for 70 hours, voltage decreasing => no degradation
Degradation started at t = 70h, number of arcs increased
ton

## Slide 8
2. Electron field emission with micro-arc discharges Demages of CNT emitters
[1] D. Wenger, W. Knapp, B. Hensel, S. Tedde, „Transition of Electron Field Emission to Normal Glow Discharge“,
IEEE Transaction on Electron Devices 61 (11), p. 3864 (2014).
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019
Undamaged CNT bundles

## Slide 9
Introduction Otto von Guericke Gesellschaft (Society) Magdeburg
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 10
1. Introductions IVNC 2017, July 10 – 14, 2017 in Regensburg, Germany
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 11
1. Introductions IVNC 2017, July 10 – 14, 2017 in Regensburg, Germany
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 12
1. Introductions IVNC 2017, July 10 – 14, 2017 in Regensburg, Germany
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 13
3. Transitions from FE to plasma discharges 3 types of stable plasma discharges
1. corona discharge 2. normal glow discharge 3. arc discharge
(I < 1 A: micro-arc discharge)
[1] https://www.plasma-universe.com/Electric_glow_discharge
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 14
3. Transitions from FE to plasma discharges (video):
Types of stable plasma discharges: corona, glow and micro-arc discharges (2)
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 15
3. Transitions from FE to plasma discharges (video):
Types of stable plasma discharges: corona, glow and micro-arc discharges (1)
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 16
[1] W. Knapp, “Field-emission investigations of micro-structured stainless steel 1.4301 (ASTM 304) for extended use of vacuum components
as very large FE cathode arrays.” Poster contribution IVNC 2017.
Fig. 1. Field-emission characterization: IE = f(U) diagram with
a voltage reduction for currents > 1.5 mA [1].
Fig. 2. Field-emission characterization: IE = f(t) diagram with
corresponding vacuum pressure curve p = f(t).
3. Transitions from FE to stable plasma discharges:
Example for DC operation with smooth transition
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 17
The Fowler Nordheim equation: is non-linear!
3. Transitions from FE to stable plasma discharges: Example for pulse operation
[1] D. Wenger, W. Knapp, B. Hensel, S. Tedde, „Transition of Electron Field Emission to Normal Glow Discharge“,
IEEE Transaction on Electron Devices 61 (11), p. 3864 (2014).
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 18
3. Transitions from FE to plasma discharges Graphical evaluation method: 4 steps
1st step: IU semi-logarithmic diagram (FE diagram) 2nd step: IU linear diagram with linearity test for UGD and RS
3rd step: IU linear diagram with VRS correction 4th step: UI diagram (plasma physics)
1st example:
smooth transition
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 19
3. Transitions from FE to plasma discharges
Smooth transition from field emission to glow discharge!
1. Breakdown voltage :
(1)
( - critical field, – distance of electrodes)
2. Reduced breakdown voltage (with FE):
(2)
( – tip field enhancement factor of FE cathode)
breakdown (sudden transition)
smooth transition
Fig. 1. U-I characteristic with smooth transition and corresponding
schema of gas discharge
Fig. 2. Equivalent circuit diagram for different stationary conditions: 1 - leakage (e.g. insulation resistance),
2 - field electron emission,
3 - normal glow discharge with constant voltage characteristic,
4 - micro-arc discharge (for currents I > 1A).
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 20
3. Transitions from FE to stable plasma discharges: Example for pulse operation
[1] D. Wenger, W. Knapp, B. Hensel, S. Tedde, „Transition of Electron Field Emission to Normal Glow Discharge“,
IEEE Transaction on Electron Devices 61 (11), p. 3864 (2014).
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 21
Sample ID | Substrate | Area [mm²] | Maximum current [mA] | Maximum current density [A/cm²] | Threshold field for 10 / 100 mA/cm² [V/µm] | 
SIE 245 | Silicon | 51 | 371 | 0.73 | 9.0 | 11.1
SIE 246 | Silicon | 51 | 285 | 0.56 | 8.4 | 10.5
SIE 249 | Silicon | 28.3 (51) | 273 | 0.97 | 8.2 | 10.0
SIE 250 | Silicon | 12.6 (51) | 215 | 1.70 | 7.8 | 9.3
SIE 251 | Silicon | 3.1 (51) | 57 | 1.85 | 9.9 | 13.0
SIE 252 | Silicon | 0.8 (51) | 16 | 2.00 | -- | 13.7
SIE 253 | Silicon | 51 | 341 | 0.67 | 6.9 | 8.8
SIE 262 | Stainless steel | 63 | 402 | 0.64 | 8.6 | 10.6
3. Transitions from FE to plasma discharges Field emission measurement
20 µm
MWCNTs 5000x
Fig. 1 FE characteristic I = f(U) of large array CNT emitter
cathodes and measured values Tab. 1 (photo of sample
SIE 262 in I-U diagram [left]).
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 22
3. Transitions from FE to stable plasma discharges: Optical observation
Figures:
Observation of glow discharges during FE measurements
glow-to-arc transition
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 23: glow-to-arc transition

## Slide 24
[1] W. Knapp, “Field-emission investigations of micro-structured stainless steel 1.4301 (ASTM 304) for extended use of vacuum components
as very large FE cathode arrays.” Poster contribution IVNC 2017.
Fig. 1. Analysis of high-current FN measurement with pulse mode operating and smooth FE-to-GD transition.
FE – Field Emission, rectangle pulse form current, current curve is an exponential functions (cf. FN equation),
TA - Townsend avalanche, exponential functions with low time constant
-> resulting cathode current: IC = IFE + ITA
(X-axis in Fig. 1.: Time t ~ extraction voltage Uext [voltage ramp]),
3. Transitions from FE to plasma discharges:
Example for pulse operation with smooth transition from FE to GD
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019
FE
TA

## Slide 25
3. Transitions from FE to plasma discharges (in a micro electron source)
Sudden transition from field emission to micro-arc discharge
Fig. 1. Electrical measuring circuit and non-scaled scheme of micro electron source with SEM images:
(a) cathode-side view of micro-grid detail and (b) Si-tips array cathode, inside: geometry of single Si-tip field emitter [1, 2].
Fig. 2. Transition from field electron emission (FE) to stable plasma dis-charge, e.g. micro-arc discharge (µArc): Linear diagram of measured characteristic and linearity test after transition with Rserial = 10 MOhm.
[1] R. Schreiner, C. Langer, C. Prommesberger, R. Ławrowski, F. Dams, M. Bachmann, F. Düsberg, M. Hofmann, A. Pahlke, P. Serbun, S. Mingels, G. Müller, “Semiconductor field emission electron sources using a modular system concept for applications in sensors and X-ray sources”, Technical Digest, 2015 28th IVNC, 13-17 July 2015, Guangzhou, China.
[2] W. Knapp, C. Langer, C. Prommesberger, M. Lindner, R. Schreiner, “Investigations of the transition from field electron emission to stable plasma discharge in a micro electron source at vacuum pressure.” Poster contribution, IVNC 2017.
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 26
3. Transitions from FE to plasma discharges
Sudden transition from field emission to micro-arc discharge
Fig. 1. Example of sudden transition (voltage breakdown)
from field electron emission (FE) to stable plasma discharge,
e.g. micro-arc discharge (µArc), with swapping the diagram axes from field-emission I = f (U) to plasma characteristics U = f(I) [1].
Fig. 2. U-I Scheme of plasma discharges with measurement 1 of Fig. 1
(the simplified scheme based on the image in [2]).
[1] W. Knapp, C. Langer, C. Prommesberger, M. Lindner, R. Schreiner, “Investigations of the transition from field electron emission to stable plasma discharge in a micro electron source at vacuum pressure.” Poster contribution, IVNC 2017.
[2] J. Reece Roth, „Industrial Plasma Engineering: Volume 2 - Applications to Nonthermal Plasma Processing“, CRC Press, 2001, ISBN 0750305452, p. 39 (or: https://www.plasma-universe.com/Electric_glow_discharge).
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 27
4. Extended use of Fowler Nordheim plot
Standard use: calculation of field enhancement factor ß
Fig. 2 Fowler-Nordheim plot (FN plot) of FE measurements in Fig. 1. and with graphic presentation of slope m for ßCNT calculation [2]:
[1] W. Knapp, D. Schleussner, “Field-emission characteristics of carbon buckypaper”, JVST B 21 557-561 (2003).
[2] W. Knapp “Field-emission investigations of micro-structured stainless steel 1.4301 (ASTM 304) for extended use of vacuum components as very large FE cathode rrays.” Poster, IVNC 2017.
Fig. 1 Field-emission (FE) characterization of three stainless steel samples SS1, SS2 and SS3, and CNT Buckypaper with the same area for comparing [1]. For sample SS3 the current density value J = 30 µA/cm2 lies significantly below the saturation characteristic.
ßCNT = - (B ∙ Φ3/2) / m
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 28
4. Extended use of Fowler Nordheim plot Energetic evaluation of charge transfers
For novel investigations of the transition from field emission to stable plasma discharges an extended use of FN plot is proposed.
For this the inverse voltage (x-axis of the FN plot) is extended with factor 1 (= I∙t / I∙t):
1/U = I∙t / U∙I∙t = Q/E (1),
where U is the voltage, I the current, t the time,
Q the sum of all transported charges and
E the energy required for this.
The ordinate of Fowler-Nordheim plot will be unchanged.
The relation Q/E is a possible option for energetic evaluation.
The operation compass is important for basic orientation.
The direction Q/E maximum (red arrow or x-axis: 1/U) is the direction of energetically optimal charge transfer.
It can be seen that the micro-arc discharge has a charge transfer with the least energy input.
Fig. 1. FN plot of presented measurement SS3 [1] with smooth transitions. UGD is the constant voltage of normal glow discharge.
[1] W. Knapp “Field-emission investigations of micro-structured stainless steel 1.4301 (ASTM 304) for extended use of vacuum components as very large FE cathode rrays.” Poster, IVNC 2017.
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 29
4. Extended use of Fowler Nordheim plot Energetic evaluation of charge transfers
RS = 100 kΩ, FE-cathode: stainless steel SS3 [1] RS = 10 MΩ, FE-cathode: array of Si-tips [2]
Fig. 1. FN plot of presented measurement SS3 [1] with smooth transitions. UGD is the constant voltage of normal glow discharge.
Fig. 2. FN plot for energetic evaluation of the transition from
field electron emission to plasma discharges, as presen-
ted and detailed explained in [2, 3], with: 1 – leakage
current, 2 – field emission, 3 – normal glow discharge,
3 - 4 – glow-to-arc transition, 4 – micro-arc discharge.
[1] W. Knapp “Field-emission investigations of micro-structured stainless steel 1.4301 (ASTM 304) for extended use of vacuum components as very large FE cathode rrays.” Poster, IVNC 2017.
[2] W. Knapp, C. Langer, C. Prommesberger, M. Lindner, R. Schreiner, “Investigations of the transition from field electron emission to stable plasma discharge in a micro electron source at vacuum pressure.” Poster contribution, IVNC 2017.
[3] D. Wenger, W. Knapp, B. Hensel, S. T. Tedde, „Transition of Electron
Field Emission to Normal Glow Discharge“, IEEE Transaction on Electron Devices 61 (11), p. 3864 (2014).
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 30
4. Extended use of Fowler Nordheim plot Energetic evaluation of charge transfers
Fig. 1. FN plot of presented measurement SS3 [1] with smooth transitions. UGD is the constant voltage of normal glow discharge.
Fig. 2. Scheme of extended FN plot with smooth transition from field emission to glow discharge (based on Fig. in slide 117/132 [2]).
[1] W. Knapp “Field-emission investigations of micro-structured stainless steel 1.4301 (ASTM 304) for extended use of vacuum components as very large FE
cathode arrays.” Poster, IVNC 2017.
[2] R. Forbes “INTRODUCTION TO FIELD ELECTRON EMISSION AND ITS THEORY (TUTORIAL LECTURE)” IVNC2013, Roanoake, July 2013.
Critical point: “Ideal” FE and GD have identical electrical parameters (U and I)! -> A differentiation is difficult.
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 31
5. Plasma-physical approach
[1] D.B. Go, A. Venkattraman: Microscale gas breakdown: ion-enhanced field emission and the modified Paschen´s curve (Topical Review),
J. of Phys. D: Appl. Physics 47 (2014) 503001.
-process: Townsend
se-process
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 32
5. Plasma-physical approach with vacuum-physical comments
[1] D.B. Go, A. Venkattraman: Microscale gas breakdown: ion-enhanced field emission and the modified Paschen´s curve (Topical Review),
J. of Phys. D: Appl. Physics 47 (2014) 503001.
with
3 sources of gas molecules [ = f(T) ]:
gas desorption from electrode surfaces:
molecules /
2. outgassing from electrodes
3. evaporation of electrode material
ionization and ion collection of gas molecules in the electron beam
transition from electron emission to stable plasma discharge ()
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 33
Rserial = 100 kΩ Rserial = 80 Ω Rserial = 22 kΩ
glow discharge micro-arc discharge hybrid: glow & arc discharge
5. Plasma-physical approach: Breakdowns with different R-limitations
[1] W. Knapp, “Vakuummikro- und Vakuumnanoelektronik mit Feldemission – Besonderheiten der Spannungsfestigkeit bei Abständen unter 10 µm“
(in German), Vakuum in Forschung und Praxis (ViP), Vol. 28, Nr. 6 (Nov. 2016) 42-48.
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 34
5. Plasma-physical approach with vacuum-physical comments
[1] W. Knapp, “Vakuummikro- und Vakuumnanoelektronik mit Feldemission – Besonderheiten der Spannungsfestigkeit bei Abständen unter 10 µm“
(in German), Vakuum in Forschung und Praxis (ViP), Vol. 28, Nr. 6 (Nov. 2016) 42-48.
with
3 sources of gas molecules [ = f(T) ]:
gas desorption from electrode surfaces:
molecules /
2. outgassing from electrodes
3. evaporation of electrode material
ionization and ion collection of gas molecules in the electron beam
transition from electron emission to stable plasma discharge ()
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 35
5. Plasma-physical approach: Breakdowns in small electrode gaps < 10 µm
[1] D.B. Go, A. Venkattraman: Microscale gas breakdown: ion-enhanced field emission and the modified Paschen´s curve (Topical Review),
J. of Phys. D: Appl. Physics 47 (2014) 503001.
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 36
5. Plasma-physical approach: Breakdowns in small electrode gaps < 10 µm
electrode gaps < 3 µm: independent of ambient pressure!
[1] W. Knapp, “Vakuummikro- und Vakuumnanoelektronik mit Feldemission – Besonderheiten der Spannungsfestigkeit bei Abständen unter 10 µm“
(in German), Vakuum in Forschung und Praxis (ViP), Vol. 28, Nr. 6 (Nov. 2016) 42-48.
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 37
5. Plasma-physical approach: Breakdowns in small electrode gaps < 10 µm
[2] M. A. Bilici, J. R. Haase, C. R. Boyle, D. B. Go, R.M. Sankaran, “The smooth transition from field emission to self-sustained plasma
in microscale electrode gaps at atmospheric pressure”, J. Appl. Phys. 119 223301 (2016).
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 38
5. Plasma-physical approach: Breakdowns in small electrode gaps < 10 µm
Fig. 1. Equivalent circuit diagram for different stationary conditions:
1- leakage (e.g. insulation resistance),
2 - field electron emission,
3 - normal glow discharge with constant
voltage characteristic,
4 - micro-arc discharge. For IµArc << 10A:
[2] M. A. Bilici, J. R. Haase, C. R. Boyle, D. B. Go, R.M. Sankaran, “The smooth transition from field emission to self-sustained plasma
in microscale electrode gaps at atmospheric pressure”, J. Appl. Phys. 119 223301 (2016).
Note: Direct Rserial (RS1) measurement is possible because normal glow discharge has a constant voltage characteristic, cf. 3 in Fig. 1.
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 39
5. Plasma-physical approach: Breakdowns in small electrode gaps < 10 µm
[1] W. Knapp, “Vakuummikro- und Vakuumnanoelektronik mit Feldemission – Besonderheiten der Spannungsfestigkeit bei Abständen unter 10 µm“
(in German), Vakuum in Forschung und Praxis (ViP), Vol. 28, Nr. 6 (Nov. 2016) 42-48.
In b):
1 – plateau (modificated Paschen curve)
2 – reduction of breakdown voltage
3 – micro-arc characteristic
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 40
5. Plasma-physical approach: Breakdowns in small electrode gaps < 10 µm
[1] W. Knapp, “Vakuummikro- und Vakuumnanoelektronik mit Feldemission – Besonderheiten der Spannungsfestigkeit bei Abständen unter 10 µm“
(in German), Vakuum in Forschung und Praxis (ViP), Vol. 28, Nr. 6 (Nov. 2016) 42-48.
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 41
5. Plasma-physical approach: Breakdowns in small electrode gaps
5. Plasma-physical approach: Breakdowns in small electrode gaps < 10 µm
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 42
5. Plasma-physical approach: Breakdowns in small electrode gaps
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 43
5. Plasma-physical approach: Breakdowns in small electrode gaps
5. Plasma-physical approach: Breakdowns in small electrode gaps < 10 µm
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 44
6. Conclusion and outlook
Fig. 1. Trends of efficiency of charge transfers
[1] W. Knapp, “Energetic evaluation of the transition from field electron emission to plasma discharges with extended use of the
Fowler- Nordheim plot.”, constributed talk IVNC 2017, Regensburg July 10 – 14, 2017, TECHNICAL DIGEST, p. 34.
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 45
6. Conclusion and outlook
Fig. 1. Field-emission enhanced stable vacuum micro-arc discharge in the range of about 200 µA.
[2] W. Knapp, C. Langer, C. Prommesberger, M. Lindner, R. Schreiner, “Investigations of the transition from field electron emission to stable plasma discharge in a micro electron source at vacuum pressure.” Poster contribution, IVNC 2017, Regensburg July 10 – 14, 2017, TECHNICAL DIGEST, p. 166 .
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 46
Schema of comparison field emission (FE) – glow discharge (GD)
Advantages of glow disharge (GD):
For ECF > EFE in short A-C distance: better conditions for field electron emission!
During GD other electron emission mechanisms are efficient:
secundary electron emission, photo emission, thermionic emission (for higher current)
3. Because VGD < VFE (I = const.): energy at a reduced rate (Steenbeck minimum).
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 47
6. Outlook: Electron field emission with micro-arc discharges:
-> Early detection with special ionization gauge!
Fig. 1. Stress tests with micro-discharges (emitter–anode distance: 100 µm):
current-voltage curve of first IE (1) and second IE (2) measurement with
corresponding total pressure p (1), and video images (see Fig. 2.).
Mark A: first micro-discharge (FIG. 7. in [1]).
Fig. 2. Video images of field-emission zone during
stress test with micro-discharges (FIG. 8. in [1]).
o
O
Fig. 3. Magnification of image 4
with corona luminescent.
[1] W. Knapp, D. Schleussner, “Field-emission characteristics of carbon buckypaper”, JVST B 21 557-561 (2003).
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 48
Fig. 2. Plot of cold field-emission current density vs emitter area (including passive parts) based on literature data for CNTs, W tips, and Spindt arrays (FIG. 14 in [1]). Lines of equal currents are shown for 1 mA and 100 mA. The diagram had to be extended for sample SS3 (Fig. 1)
6. Outlook FE with low current density
[1] W. Knapp, “Ionization gauge with large-area stainless steel field-emission cathode”, Knapptron Lab research report, 2017 (unpublished).
[2] G. Gärtner, “Historical development and future trends in vacuum electronics (review article)“, JVST B 30 060801_1-14 (2012).
Fig. 1. Schematic circuit and ionization gauge construction for testing with novel large-area stainless steel field-emission cathode [1].
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 49
6. Conclusion and outlook
It was shown that transitions from field electron emission to stable plasma discharge are very important for field emission applications in the current range above 0.1 … 1.0 mA.
The transitions can be very different, e.g. emission-to-glow transitions are often smooth. This can be a major problem for the correct analysis of field-emission characteristics.
In order to confirm this transition from field electron emission into a normal glow discharge a graphical evaluation method was developed.
In this contribution we report of the first time on an extended use of the Fowler-Nordheim plot for energetic evaluation of charge transfers in vacuum electronics.
First results explained clearly, the transitions from field electron emissions to normal glow discharges and/or micro-arc discharges are physically conditioned, especially in the case of higher emission currents and long-term emissions.
In the next steps different field emitter cathodes will be investigated regarding their robustness and resistance against glow and micro-arc discharges.
Therefore the extended use of the Fowler-Nordheim plot will have an enhanced role in future field emission characterizations.
It is recommended to check all field emission measurements in the current range above 0.1 mA. Only in this way is it possible to avoid misunderstandings or even inadequate or incorrect evaluations of field emitters and field-emitter materials.
For better understanding: a) vacuum pressure measurement
b) optical observation of cathode – anode distance
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019

## Slide 50
Thank you very much
for your attention!
Thank you very much
for your attention!
Wolfram Knapp
„Investigations of the transition from electron field emission to plasma discharges
(glow discharge and micro-arcs) with extended use of Fowler-Nordheim plot”
8th International Workshop on Mechanisms on Varcuum Arcs, Padova , 15-19 Sept. 2019