## Slide 1: Dynamic coupling between particle-in-cell and atomistic simulations
Mihkel Veske, Andreas Kyritsakis, Kyrre N. Sjobaek, V. Zadin, A. Aabloo and F. Djurabekova
Helsinki Institute of Physics and Department of Physics
University of Helsinki
Finland

## Slide 2: Outline
The plasma onset stage of vacuum BD and its importance for BD mitigation
Two schools of thought: “explosive emission” vs “thermal evaporation”
Concurrent ED-MD simulations on nanotips
The thermal runaway process
Integrating with PIC simulations
Results
Conclusions

## Slide 3: Vacuum breakdown stages
e-
Cathode
+
Anode
-
UHV
Sharp tips on surface, field enhancement, electron emission
Stage 1
Anode
UHV
Extinction of energy, plasma cools- recombines, crater remains
Cathode
Stage 4
Stage 3
Cathode -
Anode
+
UHV
Ionization, plasma formation-expansion, high current, voltage collapse
Cathode
Anode
UHV
Plasma onset: thermal runaway, neutral evaporation
Stage 2
+
-

## Slide 4: Importance of stages 2,3: power flow limits
Calculated Sc @ 100 MHz
Jan Paszkiewicz
Soft Cu electrode,
Anton Saressalo
Can we use this as a design way to mitigate Vacuum breakdown?
First we need to understand it
What is the limiting factor for BD initiation?
What makes the available EM power to be sufficient in some cases, while insufficient in other?

## Slide 5: Vacuum breakdown stages
e-
Cathode
+
Anode
-
UHV
Sharp tips on surface, field enhancement, electron emission
Stage 1
Anode
UHV
Extinction of energy, plasma cools- recombines, crater remains
Cathode
Stage 4
Stage 3
Cathode -
Anode
+
UHV
Ionization, plasma formation-expansion, high current, voltage collapse
Cathode
Anode
UHV
Plasma onset: thermal runaway, neutral evaporation
Stage 2
+
-

## Slide 6: Plasma ignition: schools of thought
Explosive emission (ECTON model):
  Tip heats up by Joule heating (FE current)
  The heat accumulates while the shape stays constant
  Extreme temperatures
  Direct phase transition from metal to plasma
Thermal runaway - evaporation:
  Tip heats by Nottingham & Joule and melts on top
  Maxwell stress pulls and sharpens it
  Molten material at high temperatures emits vapor
  Vapor ionizes by e collisions (and field ionization)
  Ions sputter out more vapor
  Plasma gradually builds up

## Slide 7: ArcPIC results
H. Timko et. al., Contrib. Plasma. Phys. 4, 229 (2015).
Animation by K. Sjobaek
Plasma can ignite emitter assuming a small tip that:
  Emits e with an enhancement β>35
  Releases >15 evaporated neutrals per 1000 e.
What is the origin of those neutrals?
What are the mechanisms in Stage 2 that produce the necessary vapor?

## Slide 8: Hybrid MD-ED-Emission-Heat
Thermal runaway: complex process that involves various phenomena that have to be taken into account in the calculations

## Slide 9: The concurrent algorithm
Atoms (MD)
FEM mesh
Electric Field
Surface emission currents
Current distribution,
Nottingham heat
Temperature distribution
Velocity
perturbration
Sur. charge distribution
Force perturbation

## Slide 10: Thermal runaway
  A. Kyritsakis et. al, J. Phys. D: Appl. Phys. 51, 225203 (2018)
  Eappl=0.8GV/m
  Mean evaporation rate (first to last evaporation events) rCu= 75±11 atoms/ps
  Mean current re = 2807±153 e/ps
  rCu/e= 0.025±0.003 atoms/e
  The assumption of the ArcPIC simulations (0.015 atoms/e) was not unrealistic at all

## Slide 11: Problem 1: Space-charge limited Field Emission in 3D
In reality, no field emitter is flat and the 1D model is inadequate
Standard treatment: Equivalent Planar Diode (EPD) model to correct for the field enhancement factor
EPD fails for a simple reason: The electron beam spreads and J is not constant as in the 1D case
NEED for PIC simulations

## Slide 12: Problem 2: connecting stages 2 and 3
Stage 2 (runaway)
Stage 3 (Plasma onset)
Stage 2&3 (multi-scale)

## Slide 13: Problem 3: Does the runaway stop?
What happens if we continue?
Does the process continue providing necessary evaporation for a sufficient time to ignite plasma?

## Slide 14: Incorporating PIC in FEMOCS
Atoms (MD)
FEM mesh
Electric Field
Particles (e), Positions, Injections
PIC
Current distribution
Temperature distribution
Velocity
perturbration
Sur. charge distribution
Force perturbation

## Slide 15: Runaway with full PIC-FEMOCS simulations
rthin = 17nm, rwide = 54nm
Eappl = 600MV/m (closer to reality)

## Slide 16: Results I
M. Veske, et. al. https://arxiv.org/abs/1906.08125

## Slide 17: Results II
Power flux density in a cylinder of 10nm radius: 9.5 MW/mm2
Similar to SC limit calculations [1]
[1] A. Grudiev et. al. Phys. Rev. accel. beam. 12 102001

## Slide 18: Evaporation rates

## Slide 19: Outlook for plasma onset simulations
Ultimate goal: direct connection of stages 2 and 3, simulation of the full BD process
Including other particle species (Cu, Cu+, Cu++ etc)
  Managing boundary injection between MD and PIC domains (quite challenging)
  Simulating larger systems for longer times to check whether the runaway continues
Understanding the limitations of the arc ignition progress with respect to:
  Power flow and related quantities
  Tip size, shape, β, etc

## Slide 20: Conclusions
Getting closer to understanding the transition from intense FE to arc plasma, more complex simulation methods required
Experiments show that the anode does not play a significant role on BDs. Even the anode flare seems to be caused by cathode material
Now we know how to properly calculate the biased diffusion parameters, preliminary results indicate a possibility to grow tips by this mechanism
Surface defects do not affect FE dynamics apart from a slight φ lowering. More evidence that field enhancement is most probably geometric

## Slide 21
THANK YOU