## Slide 1: Quantitative analysis on electric field variation in SiPMs for scintillation detection applications
KAIST
Kyung Taek Lim
Crete – July 10th, 2019

## Slide 2: Scintillation detection
 | Peak emission (nm) | Light yield (ph/MeV)
BGO | 480 | 9,000
LYSO | 420 | 30,000
LaBr3 | 380 | 60,000
CsI(Tl) | 540 | 65,000
NaI(Tl) | 415 | 38,000
Plastic | 380-420 | 10,000
J. Murphy, “SensL Technology Update,” 2013
Spectral response in various scintillators
Light yield in common scintillators
Scintillation detection:
Scintillator + Photodetector (e.g., PMT, SiPD)
Scintillators (organic or inorganic) emit photons after interacting with ionizing radiation, e.g., x-rays and γ-rays
Scintillator specific variables:
Emission wavelength
Light yield
Decay time
Attenuation length
Source
Photodetector
Scintillator
Output
pulse
Introduction

## Slide 3: Scintillation detection applications
Nuclear Medicine
PET/CT, PET/MRI, SPECT
High Energy Physics
CALIC AHCAL, CMS HCAL
Astrophysics
Cherenkov telescope, Neutrino detectors
Hazard and Threat Detection
Gamma camera, RPM, Dosimeter
Silicon photomultiplier (SiPM)
Photomultiplier tube (PMT)
FireflySci
Hamamatsu
Solid state technology
Robust & compact
Low voltage (< 100 V)
Insensitive to magnetic field
Vacuum tube technology
Bulky size
High voltage (~ 103 V)
Sensitive to magnetic field
Introduction

## Slide 4: Silicon photomultiplier (SiPM)
Avalanche
breakdown
in a GAPD
~ 105
Micrograph of microcell arrays
(x100 zoom)
A cross-section of a GAPD with a passive quenching resistor
Single pixel SiPM at KAIST-NNFC
Silicon photomultiplier (SiPM):
  102 ~ 103 of microcells (GAPD, G-APD, GM-APD, SPAD…) connected in parallel
Active area → 11 mm2 ~ 1010 mm2
Different packages available: single or tiles of SiPMs to cover large areas
Typically coupled with scintillators for X-ray, gamma-ray detection applications
E. Hergert and S. Piatek, Testing Detectors: Understanding key parameters of silicon photomultipliers, 2014
F. Acerbi and S. Gundacker, NIMA 926, 16–35 (2019)
Introduction
Notes: Output signal ∝ Chronological superposition of current pulses from fired microcells
SiPM pros: Single photon sensitivity, good photon number resolution (up to tens/100 photons), high PDE, tunable sensitivity (peak in NUV, green, NIR), high dynamic range, good timing resolution, compact and rugged, high gain comparable to PMts, insensitivity to magnetic field.
In the past decade, silicon photomultipliers have been considered as potential candidate in various scintillation detector applications owning to their numerous advantages over traditional PMTs such as high internal gain, fast response, single photon sensitivity, compactness, and insensitivity to magnetic field.
So what is silicon photomultiplier or an SiPM?
SiPM is a solid-state photodetector composed of an array of Geiger-mode avalanche photodiodes connected in parallel to a common electrode so that the output signal is equal to the summation of triggered or fired GAPDs, which in turn, would be proportional to the incident photon flux.
Also referred to as a microcell, GAPD is composed of an abrupt p/n junction with a guard-ring that surrounds the p/n junction for preventing edge breakdown. In addition, a quenching resistor is integrated in series for passive quenching.
What makes GAPD unique is that the condition for p/n junction is engineered specifically so that the electric field has a sharply defined peak at the metallurgical junction with its magnitude exceeding 105 V/cm.
As a result, GAPD operates in a limited Geiger-mode where we have a self-sustaining avalanche multiplication with a gain of 105 ~ 106. Moreover, the voltage at which the carriers gain sufficient energy to initiate an avalanche breakdown is defined as the breakdown voltage.
This pn junction, or sometimes called as the well structure of GAPD, is crucial in determining the GAPD characteristics.

## Slide 5: SiPM-based system parameters
SiPM structure parameters
Well structure
(p/n junction)
Guard ring
Quenching resistor (Rq)
Epitaxial layer
ARC layer
Photon number resolving capability
Timing capability
SiPM characteristics
Target application
considerations
Power consumption
Gain
Dynamic Range
Dark Count Rate
Photon detection efficiency
Signal shape
Breakdown voltage
Temperature dependencies
Trade-offs between the DCR and PDE with respect to the electric field in the depletion region.
and other considerations such as large dynamic range, large-area systems, and so on…
  Well structure (p/n junction) determines the electric field profile in a GAPD
Introduction

## Slide 6: Trade-offs between DCR and PDE
Factors influencing PDE
  An example of Pt calculation
h+
e-
Trivial solutions for enhancing PDE:
Increase fill factor → Device geometry optimization
Increase quantum efficiency → ARC optimization
Increase electric field strength → Well structure
  , : impact ionization rate of e, h (E)
DCR = DCRdiff + DCRSRH + DCRtunnel
Field enhanced Shockley–Read–Hall generation
Band–to–band
tunneling
Factors influencing DCR
Trivial solutions for reducing DCR:
Reduce impurity concentration → Wafer & fabrication technology
Increase detection threshold → Readout circuit design
Decrease electric field strength → Well structure
  Design and fabricate SiPMs with different E-field profiles
  Evaluate Δ E on SiPM performance through photon-number resolving capability (RSiPM)
Motivation

## Slide 7: Device Structure & Simulation
  Three p-well implantation doses and their corresponding simulated peak electric field
  n-on-p SiPMs with three peak E-field strengths
  Simulated 1D E-field profiles as a function of depletion depth (μm)
  2D TCAD simulation
Depth
(μm)
  Cross-sectional diagram of a GAPD
n-on-p
Structure
E-field
Distribution
Materials & Methods

## Slide 8: Reverse I–V Curves
Measurement setup
- Voltage range: 0 – 70 V
- Cell type: 65-μm single microcell
- Wafer–level I–V measurements
  Reverse I–V of single types with three ϕp-well conditions
  Reverse I–V of single types as a function of Vex
Ipre-BD
Ipost-BD
Sample selection
- VBD,avg
(over 40 samples)
  Tape-out wafer @ NNFC
  Samples on ceramic packaging
  Ipost-BD: Multiplied bulk leakage current
Result & Discussion

## Slide 9: Dark Count Rate (DCR)
  DCR of fabricated samples with three ϕp-well conditions
  Temperature dependency of DCR in fabricated samples
Vex = 2.0 V
Vex = 2.0 V
  Arrhenius plot of fabricated samples with three ϕp-well conditions
  Δ Activation energy (EA) vs. E-field
    0.43 eV → 0.46 eV → 0.51 eV (approaches Eg,Si/2)
    Increase in the effective band energy seen by the carrier
    Less influence of field-enhanced mechanisms on SRH generation of carriers
    → Larger effective carrier lifetime, τg.
Result & Discussion

## Slide 10: Photon detection efficiency (PDE)
  PDE of fabricated samples with three ϕp-well conditions
Shift in peak sensitivity
Enhanced E-field in the “extended” depletion region in Device #3
Result & Discussion

## Slide 11: Photon number resolving capability
Nph = 20000
    Fm: Avalanche multiplication
    Fdark: Dark count rate
    Fdup: Correlated noise
    FPDE: Photon detection efficiency
    Fnl: Non-linearity
Concept of photon-number-resolution*
*S. Vinogradov, et al., Trans. Nucl. Sci, 58, 9-16, (2011)
Nph = 5000
Nph = 50000
  RSiPM of GAPDs with three ϕp-well conditions for Nph = 5000, 20000, and 50000 photons (Vex = 2.0 V)
Result & Discussion

## Slide 12: RSiPM mapping (Nph, λ)
Device #1
Device #2
Device #3
1.0 V
1.5 V
2.0 V
2.5 V
Nph
λ
RSiPM
Input range
- Nph: 5.0x102 ~ 10x104 photons
- λ: 375 ~ 700 nm
Result & Discussion
Notes: Therefore, to account for as many scintillation detector applications as possible, RSiPM in each device has been calculated for Nph ranging from 500 to 100000 photons and wavelengths from 375 to 700 nm and for excess voltage of 1.0, 1.5, 2.0 and 2.5 V.
For all three devices, the trend of RSiPM at low Nph is similar to that of the results presented before for Nph = 500 case where the curve has a convex shape.
In terms of the wavelength, the curve shape is also similar to those observed before where RSiPM degrades with increasing wavelength, reaching the worst value at the peak sensitivity, and then improves again beyong the peak wavelength.
Although similar behaviors were observed for RSiPM for each sample in terms of Nph, wavelengths, and Vex, these do not imply the indifference of RSiPM with respect to three "∅" _"p−well" conditions. In fact, there is a significant difference in RSiPM among the three samples, that is, the magnitude of RSiPM at a given Vex and particularly at high Nph.
What is interesting is that the degradation of RSiPM with respect to wavelength at high Nph becomes more noticeable with increasing Vex. Furthermore, the maximum value of RSiPM or equivalently, the point where it has the worst photon-number resolving capability, increases greatly with increasing Vex.

## Slide 13: RSiPM mapping (Nph, λ)
  Δ RSiPM vs. E-field @ λ = 530 nm, Vex = 2.5 V
    ΔRSiPM is negligible at low Nph (< 10000 photons)
    ΔRSiPM becomes noticeable when Nph > 20000 photons
    At higher Nph (> 20000 photons), Device #2 has the best RSiPM while Device #3 has the worst RSiPM for all Vex
Device #2 at Vex = 2.5 V
Nph (photons)
Wavelength (nm)
Device #1 at Vex = 2.5 V
Nph (photons)
Wavelength (nm)
Device #3 at Vex = 2.5 V
Nph (photons)
Wavelength (nm)
Result & Discussion
Notes: Although similar behaviors were observed for RSiPM for each sample in terms of Nph, wavelengths, and Vex, these do not imply the indifference of RSiPM with respect to three "∅" _"p−well" conditions. In fact, there is a significant difference in RSiPM among the three samples, that is, the magnitude of RSiPM at a given Vex and particularly at high Nph. Assuming that all devices are biased at Vex = 2.5 V, in comparison to Device #1, the magnitude of RSiPM at low Nph is similar to that of Device #2. As Nph increases, however, the magnitude of RSiPM of Device #2 becomes smaller than that of Device #1, and the gap becomes larger with increasing Nph.
Given that the fabrication environment is fixed, reducing the electric field in the depletion region can be considered a reasonable approach for scintillation detector applications with very high photon fluxes, e.g., Nph > 30000.
At a high Nph, the photon-number resolving capability of an SiPM is driven by the PDE; thus, having a lower PDE benefits the device by making it reach the saturation level slowly due to the non-linearity, as in the case of Device #2
In contrast, SiPMs with high PDE could be a better choice for scintillation detector applications with moderate photon fluxes (a few thousands) despite their higher DCRs. In a typical PET application, for example, it is better to have a higher detection efficiency and spatial resolution so that having a relatively high DCR can be tolerated as long as the device meets the minimum requirements projected by the PET system.

## Slide 14: RSiPM comparison
SiPM specification: n-on-p/ 65-μm micro-cell/ 2.95x2.95 mm2
    Decrease E-field (but not too much) for scintillation detection applications with high Nph
    Increase E-field for scintillation detection applications with moderate or low Nph
Result & Discussion
Notes: In this research, electric field variations in SiPMs have been extensively studied to highlight the importance of electric field engineering when designing devices for scintillation detector applications. In particular, this research examined the degree to which the electric field could affect SiPM behavior and demonstrated how the photon-number resolving capability of an SiPM (RSiPM) can serve as an indicator in designing a device for a target application under the given, but limited, fabrication conditions.
In this research, we have achieved the following:
Design and fabrication of SiPMs with various electric field profiles by having three p-well implantation doses ("∅" _"p−well" ) in descending order
Measurements of important SiPM parameters such as VBD, gain, DCR, temperature dependency (VBD, gain, and DCR), PDE, and crosstalk
Quantitative demonstration of the trade-off relationship between the DCR and PDE with respect to electric field variations quantitatively
Examined how a slight reduction in the peak electric field strength can alter the influence of field-enhanced thermally generated carriers contributing to the DCR as well as the temperature dependencies of the VBD
Examined how the extended electric field distribution in the deep depletion region can enhance the PDE in a long wavelength regime despite its lower peak electric field strength under the lowest "∅" _"p−well" condition
Successful demonstration of RSiPM as a function of Nph and wavelengths for each "∅" _"p−well" condition using measured SiPM parameters.
Demonstrated how reduction of the electric field could be a reasonable approach for scintillation detector applications with a very high photon flux ( Nph > 30000)
Demonstrated how a high electric field could be a better choice for scintillation detector applications with a moderate photon flux (a few 103 photons).

## Slide 15: Conclusion
Demonstrated the trade-offs between DCR and PDE with respect to ΔE:
  SiPM performance quite sensitive to ΔE in the depletion region
  Evaluated RSiPM (Nph, λ) of SiPMs with three E-field profiles for scintillation detection applications:
  Overall, RSiPM is strongly driven by the PDE
  Non-linearity becomes significant with increasing Nph due to the limited Ncell
Lower E-field (but not too low) could be favorable for high Nph, e.g., CsI(Tl) or LaBr3
Higher E-field could be a better choice for moderate or low Nph, e.g., LYSO or plastic
What about non-scintillation detection applications such as fluorescence spectroscopy or Light Detection and Ranging (LiDAR)?
Notes: In this research, electric field variations in SiPMs have been extensively studied to highlight the importance of electric field engineering when designing devices for scintillation detector applications. In particular, this research examined the degree to which the electric field could affect SiPM behavior and demonstrated how the photon-number resolving capability of an SiPM (RSiPM) can serve as an indicator in designing a device for a target application under the given, but limited, fabrication conditions.
In this research, we have achieved the following:
Design and fabrication of SiPMs with various electric field profiles by having three p-well implantation doses ("∅" _"p−well" ) in descending order
Measurements of important SiPM parameters such as VBD, gain, DCR, temperature dependency (VBD, gain, and DCR), PDE, and crosstalk
Quantitative demonstration of the trade-off relationship between the DCR and PDE with respect to electric field variations quantitatively
Examined how a slight reduction in the peak electric field strength can alter the influence of field-enhanced thermally generated carriers contributing to the DCR as well as the temperature dependencies of the VBD
Examined how the extended electric field distribution in the deep depletion region can enhance the PDE in a long wavelength regime despite its lower peak electric field strength under the lowest "∅" _"p−well" condition
Successful demonstration of RSiPM as a function of Nph and wavelengths for each "∅" _"p−well" condition using measured SiPM parameters.
Demonstrated how reduction of the electric field could be a reasonable approach for scintillation detector applications with a very high photon flux ( Nph > 30000)
Demonstrated how a high electric field could be a better choice for scintillation detector applications with a moderate photon flux (a few 103 photons).

## Slide 16
Thank you for your attention
Crete – July 10th, 2019

## Slide 17: Gain & Crosstalk
  Δ Gain vs. E-field
    3.3106 → 2.6106 → 1.9106 at Vex = 2.5 V
    Lower ϕp-well results in a wider depletion width → Smaller Cd → Reduction in the cell gain
  Gain of fabricated samples with three ϕp-well conditions (33 array)
  Crosstalk probability of 3x3 types with three ϕp-well conditions
  Δ Crosstalk probability (PCT) vs. E-field
    Optical photons generated during the avalanche multiplication and triggering probability → proportional to Vex.
    PCT is proportional to gain → Reduction in the PCT with decreasing electric field.

## Slide 18: Progress in SiPM technology
Improvement in DCR
Improvement in PDE
 | 2007 | 2013 | 2017
PDE (%) | ~ 10 | ~ 40 | ~ 55
DCR (MHz/mm2) | ~ 10 | ~ 0.1 | ~ 0.05
CT (%) | > 20 | < 10 | < 1
AP (%) | > 20 | < 10 | < 3
N. Otte, “A review of silicon photomultipliers,” 2017
C. Betancourt et al., Siena Workshop, 2016
F. Acerbi et al., IEEE J. Quant. Elec., 54 (2018)
n-on-p
Improvement in CT and AP
F. Acerbi et al., IEEE Trans. Nucl. Sci., 62 (2015) 1318-1325
Improvement in Rq
T. Nagano, IEEE NSS 2013
F. Acerbi et al., IEEE J. Sel. Top. Quantum Electron, 62 (2018) 1318-1325
Improvement in DR