## Slide 1
Surface effects for electron cloud
R. Cimino LNF-INFN
Thanks to F. Ruggiero

## Slide 2
Introduction:
E-cloud mitigation methods in a global scenario: compatibility with impedance, vacuum, etc.
The seed of e-cloud: number of photoelectrons (PY) and their effect to the surface.
How surface sensitive is SEY?
- Role of Temperature, overlayer thickness, etc
Conclusions
OUTLINE

## Slide 3
Pumping slots
Pumping slots
shields
Cu layer
Cooling tubes
“Saw teeth”
The global scenario: e- cloud methods must be compliant with all BS features.
For LHC:
V. Baglin et al. CERN-ATS-2013-006

## Slide 4
Pumping slots
Pumping slots
shields
Cu layer
Cooling tubes
“Saw teeth”
Alternative solution: Laser treated materials (see: Oleg Talk)
The global scenario: e cloud methods must be compliant with all BS features.
For LHC:
V. Baglin et al. CERN-ATS-2013-006

## Slide 5
R. Valizadeh et al. , Appl. Phys. Lett. (2014)
R. Valizadeh et al. , Appl. Surf. Sci. (2017)
surface morphology of LASE
Limiting SEY with LASE-Cu
Is it compliant with all BS functionalities?
Very low SEY
See Oleg Talk
R. Valizadeh, et al. Appl. Phys. Lett. 105, 231605 (2014)

## Slide 6
Pumping slots
Pumping slots
shields
Cu layer
Cooling tubes
“Saw teeth”
The global scenario: e cloud methods must be compliant with all BS features.
For LHC:
V. Baglin et al. CERN-ATS-2013-006

## Slide 7
Pumping slots
Pumping slots
shields
Cu layer
Cooling tubes
“Saw teeth”
The global scenario: e cloud methods must be compliant with all BS features.
For LHC:
V. Baglin et al. CERN-ATS-2013-006
Impedance issues?

## Slide 8
Pumping slots
Pumping slots
shields
Cu layer
Cooling tubes
“Saw teeth”
The global scenario: e cloud methods must be compliant with all BS features.
For LHC:
V. Baglin et al. CERN-ATS-2013-006
Impedance issues?
Oleg will answer to this!

## Slide 9
Pumping slots
Pumping slots
shields
Cu layer
Cooling tubes
“Saw teeth”
The global scenario: e cloud methods must be compliant with all BS features.
For LHC:
V. Baglin et al. CERN-ATS-2013-006
Vacuum issues?
and temperature fluctuations

## Slide 10: When Operating at Low Temperature
Working Pressure
(<10-11 mbar)
Beam screen Temperature Range
LHC
Synchrotron Radiation Power = 0.13 W/m
FCC
Synchrotron Radiation Power = 40 W/m
Independently on the substrate treatment, the thermal stability against small BS T fluctuation has to be guaranteed

## Slide 11: We studied thermal stability @ LNF within EuroCirCol collaboration
Temperature Programmed Desorption (TPD) and Mass Spectrometry measurements
Equipment : QMS (Hiden HAL 101 Pic)
Secondary Electron Yield (SEY) measurements
Equipment : Electron gun, Faraday cup
LNF-cryogenic manipulator
Sample at 15-300 K
Ultra high vacuum systems
main chamber
preparation
chamber
fast-entry lock

## Slide 12: TPD from unbaked lase-Cu for temperature induced vacuum transients study
poly-Cu
Representative of Laser treated Cu
Comparative study of TPD from flat poly-Cu and LASE-Cu unbaked samples using different gases
(Ar, CH4, CO and H2 )

## Slide 13: TPD from unbaked lase-Cu for temperature induced vacuum transients study: Ar
L. Spallino, M. Angelucci, R. Larciprete, R. Cimino,
Appl. Phys. Lett. 114, 153103 (2019)
Single TPD peak at ~30 K corresponding to the desorption of a condensed thick Ar layer
Desorption temperature determined by the weak Ar-Ar van der Waals interaction energies
Ar on poly-Cu

## Slide 14
L. Spallino, M. Angelucci, R. Larciprete, R. Cimino,
Appl. Phys. Lett. 114, 153103 (2019)
Single TPD peak at ~30 K corresponding to the desorption of a condensed thick Ar layer
Desorption temperature determined by the weak Ar-Ar van der Waals interaction energies
TPD peak at ~30 K corresponding to the desorption of a condensed thick Ar layer together with a broad TPD profiles, whose peak temperatures and widths depend on the Ar dose
Ar on poly-Cu
Ar on LASE-Cu
TPD from unbaked lase-Cu for temperature induced vacuum transients study: Ar

## Slide 15: TPD from unbaked lase-Cu for temperature induced vacuum transients study: Ar
TPD characteristics determined by the sponge-like structural features of LASE-Cu
5 mm

## Slide 16
Conceptually identical results have been obtained with CH4
L. Spallino, M. Angelucci and R. Cimino, to be published
TPD from unbaked lase-Cu for temperature induced vacuum transients study: CH4

## Slide 17
L. Spallino, M. Angelucci and R. Cimino, to be published
Conceptually identical results have been obtained with CO
TPD from unbaked lase-Cu for temperature induced vacuum transients study: CO

## Slide 18: TPD from unbaked lase-Cu for temperature induced vacuum transients study: H2
L. Spallino, M. Angelucci and R. Cimino, to be published
TPD of 100 L H2 dosed on poly-Cu and LASE-Cu samples held at T~15-18 K
No TPD signal should be observed by considering the H2 vapor suture pressure curve!!!
The wide distribution of high energy adsorption sites within the inner pore is responsible for the H2 TPD signal from LASE-Cu sample

## Slide 19: TPD from unbaked lase-Cu for temperature induced vacuum transients study
Saturated vapour pressure from Honig and Hook (1960)
Further studies and electron/photon stimulated desorption are necessary to validate/optimize LASE-Cu at low T.
L. Spallino, M. Angelucci and R. Cimino, to be published
Low SEY AND Low impedance AND Vacuum compatibility, etc. must be granted!

## Slide 20
Introduction:
E-cloud mitigation methods in a global scenario: compatibility with impedance, vacuum, etc.
The seed of e-cloud (and of single bunch inst.): number of photoelectrons (PY) and their effect to the surface.
How surface sensitive is SEY?
- Role of Temperature, overlayer thickness, etc
Conclusions
OUTLINE

## Slide 21
Experimental Parameters
Phot. Energy range 351800 eV
Beam height h=0.3 mm
Incident Beam measurement
GaAsP Photodiodes (4x4mm) (0.1*4mm)
Incident angle 0.25, 0.5, 1°
We can measure PY and R in operational conditions
The Beamline
The Reflectometer
A.A.Sokolov,et al,Proc.of SPIE92060J-1-13(2014)
A. Sokolov, et al., Journal of Synchrotron Radiation 25, 100 (2018).

## Slide 22
Cu LHC
LHC Saw Tooth
LASE Cu
The sample studied:
Cu (different Roughness)
LHC - Saw Tooth
LASE
Cu+ amorphous Carbon Thin Film
And: NEG, Stainless Steel, ...
50 mm
5 mm

## Slide 23
Selected results: Photo Yield
E. La Francesca et al: submitted to PR ST
In all cases, PY is higher at higher photon energies.
The PY dependence on qi is consistently dimmed and finally washed out when surface Ra is increasing.
In all cases, the Cu-L2-3 absorption edge at 930-950 eV is visible and cause an increase in the measured PY.
In all spectra we measure a significant effect due to the C K-edge at 280 eV and O K-edge at 530 eV (surf. Contaminants)
Roughness does influence the PY. The lower is Ra, the highest is the measured PY.

## Slide 24
Surface Chemistry Changes
(Conditioning)
Preliminary results on PSD
from small samples @ DAFNE
Photo Stimulated
Desorption
Photon / Electron Scrubbing comparison
Pressure Evolution
Photon interaction studies (RT) @ DAFNE-L

## Slide 25
SEY
Photo Yield
Strong variation of surface conditions at “low dose”
Slow variations at
“high doses”
Finale State SEY=1.3
Surface Modifications
Photon Scrubbing
Preliminary results
from small samples
Studied on the same surface
Photon interaction studies (RT) @ DAFNE-L

## Slide 26
Surface Modifications
XPS
XPS Map
Modification of Carbon C-1s
From sp3 to sp2
Same chemical process of Electron Scrubbing
Scrubbing Area
Spot Dimension
But SEYMax Decreases to 1.3
as for low energy electrons
Preliminary results
Still in progress!
Photon interaction studies (RT) @ DAFNE-L

## Slide 27
Introduction:
E-cloud mitigation methods in a global scenario: compatibility with impedance, vacuum, etc.
The seed of e-cloud: number of photoelectrons (PY) and their effect to the surface.
How surface sensitive is SEY?
- Role of Temperature, overlayer thickness, etc
Conclusions
OUTLINE

## Slide 28
L. A. Gonzalez et al., AIP Adv. (2017)
SEY behavior is strongly influenced by the chemical state of the surface
Contaminants from atmosphere ~ 5 - 20 nm

## Slide 29
L. A. Gonzalez et al., AIP Adv. (2017)
SEY at LT (20 K) ~ SEY at RT but...
SEY is highly sensitive to the presence of adsorbates, even at sub-monolayer coverages
SEY of cold surfaces influenced by gas physisorption

## Slide 30: SEY Surface sensitivity: gases on LT Cu
Kuzucan et al., J. Vac. Sci. Technol. A (2012)
CO thick layer coverage
SEY is an intrinsic material property strongly sensitive to the surface composition and chemical state
L. Spallino, M. Angelucci and R. Cimino, to be published
V . Baglin, et al Proceedings of EPAC 2000, Vienna, Austria
H2O thick layer coverage
Ar thick layer coverage
Element and coverage specific

## Slide 31
We followed the growth of thin a-C layers on Cu with XPS to measure its thickness
Increasing C
-Preliminary-
How a Coating modify SEY? (the case of a-C on Cu)
XPS
Graphite road
a-C thermal evaporator
A. Novelli et al., in preparation

## Slide 32
We followed the growth of thin a-C layers on Cu with XPS to measure its thickness
Increasing C
Cu 2p
C 1s
-Preliminary-
How a Coating modify SEY? (the case of a-C on Cu)
Graphite road
a-C thermal evaporator
A. Novelli et al., in preparation

## Slide 33
We followed the growth of thin a-C layers on Cu with XPS to measure its thickness
Increasing C
Cu 2p
C 1s
-Preliminary-
How a Coating modify SEY? (the case of a-C on Cu)
In XPS:
where d is the unknown thickness and l is the inelastic mean free path.
A. Novelli et al., in preparation

## Slide 34
We followed the growth of thin a-C layers on Cu with XPS to measure its thickness
Increasing C
Cu 2p
C 1s
-Preliminary-
How a Coating modify SEY? (the case of a-C on Cu)
In XPS:
where d is the unknown thickness and l is the inelastic mean free path.
We also calibrate the 1ML Carbon signal with the one emitted from Gr/Cu (1 Ml)
A. Novelli et al., in preparation

## Slide 35
By simultaneously follow SEY changes with a- C thickness we can measure SEY dependence on actual a-C coverage.
Increasing C
-Preliminary-
How a Coating modify SEY? (the case of a-C on Cu)
dmax, Emax sets to their (a-C) final values quite soon, while minor changes still occurs at higher doses in the very low (< ~ 20 eV) and quite high primary energy (> ~400 eV) part.
A. Novelli et al., in preparation

## Slide 36
By simultaneously follow SEY changes with a- C thickness we can measure SEY dependence on actual a-C coveradge.
Increasing C
-Preliminary-
How a Coating modify SEY? (the case of a-C on Cu)
A. Novelli et al., in preparation

## Slide 37: How a Coating modify SEY? (the case of C on Cu)
Could follow dmax vs C coverages
dmax
Could follow Emax vs C coverages
 15-20 Ml (~ 5-6 nm) of a-C determines SEY properties.
Carbon Coverage (ML)
Carbon Coverage (ML)
In Graphite:
1 ML ~ 3.4 Å
Emax
A. Novelli et al., in preparation

## Slide 38: Do we learn something on Scrubbing?
To have a fully scrubbed Surface, we need more than 5-6 nm of (low SEY) a- C covering our surface.
Original Contaminant thickness depends on the material and material cleaning. (can be between 4 to 20 nm)
During irradiation (ph and e-) both desorption and substrate chemical modifications occurs.
Are we always sure that we are left with the minimum C coverage to reduce SEY below 1.1 ?
Why photons and low energy electrons (below 50 eV) behaves differently than high energy electrons (above 50 eV up to 3keV)?

## Slide 39: Conclusions
All new materials should be validated in all aspects in a global approach.
Laboratory experiments have been and must be refined.
Material studies in conditions as close as possible to operating ones (preparation, Low Temperature & geometry) is mandatory.
There are still open aspects in the scrubbing process.
Very thin coatings (about 6 nm for a-Carbon) are enough to completely reduce clean poly - Cu SEY to the one of a-C.

## Slide 40
Tanks to the technical support of DAФNE-L Team:
A. Grilli, M. Pietropaoli, A. Raco, V. Tullio, V. Sciarra and G. Viviani
Thank you for your attention
Thanks to EuroCirCol project and to its scientific community
Thanks to the low temperature team at LNF:
M. Angelucci, A. Liedl, R. Larciprete e L. Spallino.
Thanks to MICA supporting project funded by INFN-SNC5
Thanks to CERN-INFN bilateral agreement K E 3 7 2 4 / T E / H L - L H C - Addendum N o. 4 to Agreement TKN3083