## Slide 1: Advances in HTS Modeling
Marco Breschi
University of Bologna, Italy
Acknowledgement: L. Cavallucci, F. Grilli, P. L. Ribani
WAMHTS-5, Budapest, April 11th 2019

## Slide 2: Outline
Introduction
HTS tape modeling
From tapes to cables
  Twisted Stacked Tape Cable
  Roebel cables
Scaling up: coils and magnet systems
Discussion

## Slide 3: Outline
Introduction
HTS tape modeling
From tapes to cables
  Twisted Stacked Tape Cable
  Roebel cables
Scaling up: coils and magnet systems
Discussion

## Slide 4: Main issues and problem scales…
Issues
High aspect ratio
Anisotropy
Strong non-linearity
Inhomogeneity of critical current
Interface properties
Problem dimensions (3D)
Multiphysics
Scale
Layer/filament
Tape
Cable
Coil
Magnet systems
REBCO tape
Roebel Cable
Hybrid 32 T NHMFL magnet

## Slide 5: …and modeling solutions
Modeling techniques
Field models (FEM, FEM-BEM, variational methods..)
  Homogenization
  Multi-scale
  Change of coordinates
  Reduced dimensionality
  Statistical approach (for Ic longitudinal variations)
Circuit models
  Lumped parameters
  Distributed parameters
Hybrid models (field model + circuit model)

## Slide 6: Outline
Introduction
HTS tape modeling
From tapes to cables
  CORC
  Twisted Stacked Tape Cable
  Roebel cables
Scaling up: coil and magnet systems
  Insulated coils
  Non insulated coils
Discussion

## Slide 7: HTS tape modeling: circuit models
Marco Breschi, WAMHTS-5, Budapest, April 11th 2019
Lumped or distributed parameter circuit models
[2] M. Breschi, P. L. Ribani, X. Wang, J. Schwartz, Supercond. Sci. Technol., Vol. 20, L9 – L11, 2007.
[1] Y. Fu, O. Tsukamoto, M. Furuse, IEEE Trans. Appl. Supercond., Vol. 13, pp. 1780 – 1783, 2003.
[3] D. Colangelo, B. Dutoit, Supercond. Sci. Technol., Vol. 27, 124005, 2014
Notes: 3

## Slide 8: HTS tape modeling: circuit models
Marco Breschi, WAMHTS-5, Budapest, April 11th 2019
Lumped or distributed parameters circuit models
2
1
3
4
0
Ni
2
1
3
4
0
Cu
Measured at 77 K, It = 58 A (40% Ic), pulse height = 3.42 V
Nickel substrate and copper not equipotential
Different voltages measured on the two sides of the tape
Resistive heater pulses applied on the copper side of the tape
[2] X. Wang, A. Caruso, M. Breschi, G. Zhang, U. Trociewitz, H. Weijers, J. Schwartz, IEEE Trans. Appli. Supercond., Vol. 15, n. 2, pp. 2586 – 2589, 2005.
Notes: 3

## Slide 9
Marco Breschi, WAMHTS-5, Budapest, April 11th 2019
The resistance of the buffer layer is greater than the transverse resistances between YBCO and Ag layers
Current redistribution length (4 cm – 10 cm) towards the substrate greater than towards the Ag and Cu layers (1 cm - 2 cm)
Current redistribution during quench
[2] M. Breschi, P. L. Ribani, X. Wang, J. Schwartz, Supercond. Sci. Technol. 20 L9 – L11, 2007.
HTS tape modeling: circuit models
Tuning the contact resistances can affect the quench propagation velocity
Notes: 3

## Slide 10: HTS tape modeling: different architectures
Marco Breschi, WAMHTS-5, Budapest, April 11th 2019
Understanding the crucial role of transverse resistances in the quench development led to alternative tape architectures
New tape architectures with higher NZPV
[5] C. Lacroix, F. Sirois, Supercond. Sci. Technol., 035003, 2014.
[4] Levin GA, Barnes PN, Rodriguez JP, Connors JA, Bulmer JS., IEEE Trans. Appl. Supercond., Vol. 19, 2009
Current flow diverter
Increasing NZPV with increasing interfacial resistance
Notes: 3

## Slide 11
Marco Breschi, WAMHTS-5, Budapest, April 11th 2019
HTS tape modeling: field models
3D model and mixed dimensional method (2D – 3D)
[6] W. K. Chan, P. J. Masson, C. Luongo., IEEE Trans. Appl. Supercond., Vol. 20, pp. 2370 - 2380, 2010
Copper stabilizers and substrate meshed in 3-D, YBCO layer meshed as a 2-D shell.
Notes: 3

## Slide 12
Marco Breschi, WAMHTS-5, Budapest, April 11th 2019
HTS tape modeling: field models
2D model with change of coordinates
To cope with the high aspect ratio, the tape thickness is multiplied by a constant parameter N
Triangular mesh
[7] M. Casali, M. Breschi, P. L. Ribani, IEEE Trans. Appl. Supercondu., vol. 25, n. 1, 6862876, 2015
Notes: 3

## Slide 13: HTS tape modeling: field vs circuit model
Marco Breschi, WAMHTS-5, Budapest, April 11th 2019
Computation time [s] | RECOVERY | QUENCH
Circuit | 188 | 89
FEM | 6329 | 1371
Significant reduction of computation time with circuit model relative to field model
Notes: 3

## Slide 14: Outline
Introduction
HTS tape modeling
From tapes to cables
  Twisted Stacked Tape Cable
  Roebel cables
Scaling up: coils and magnet systems
Discussion

## Slide 15: From tapes to cables: twisted stacked tape cable (slotted core)
Marco Breschi, WAMHTS-5, Budapest, April 11th 2019
Twisted stacked cable (ENEA Frascati)
Electro-thermal field model based on homogenization technique
[8] M. Breschi, et al., IEEE Trans. Appl. Supercondu., vol. 25, n. 3, 4800505, 2015
Notes: 3

## Slide 16: From tapes to cables: homogenization
Longitudinal current flow
Transverse current flow
The error on MQE due to homogenization can reach 30 %
Increasing the number of degrees of freedom, modeling stacks requires homogenization techniques
Resistances are taken in parallel for the longitudinal flow, and in series for the transverse flow, obtaining anisotropic properties
[8] M. Breschi, et al., IEEE Trans. Appl. Supercondu., vol. 25, n. 3, 4800505, 2015
Notes: 3

## Slide 17
Computation of current and temperature distribution during quench.
From tapes to cables: 3D - thin strip
Electromagnetic and thermal network model for quench analysis, AC loss and field quality
[9] J. Van Nugteren., «High Temperature Superconductors Accelerator Magnets», Ph.D. dissertation, University of Twente, 2016

## Slide 18
From tapes to cables: Roebel cable reduced dimensionality approach
The Roebel cable is described by means of a 1D FEM model.
At each mesh point, the model unknowns are the temperatures Ti and voltages Vi of each tape
Electrothermal model for quench calculation
The heat diffusion equation can be written for the i-th tape as
Joule power due to the current exchange between the i-th and j-th tapes in contact
thermal conduction between the i-th and j-th tapes in contact
heater thermal disturbance
[10] L. Cavallucci, M. Breschi, P. L. Ribani and Y. Yang, IEEE Trans. Appl. Supercond., vol. 28, no. 4, Jun. 2018.

## Slide 19
From tapes to cables: Roebel cable reduced dimensionality approach
The contact between different tapes is described through non-uniform conductances
The electric potential at the reference terminal of the cable is set to 0
The current distribution is set on each tape at the other terminal
Coupling with the thermal model

## Slide 20
From tapes to cables: Roebel cable reduced dimensionality approach
[11] Q. Zhang, et. al., IEEE Trans. Appl. Supercond., vol. 28, no. 4, Jun. 2018.
Experiment at the University of Southampton
A 2 m long Roebel cable with 15 strands YBCO tapes (Bruker EST) was wound into a pancake coil of 7 turns with 72 mm inner diameter.
A length of fiberglass ribbon was co-wound as electrical insulation layer; the coil was then impregnated with epoxy resin.
At the 4th turn of the coil, a miniature heater was attached to tape #7 at the inner face of the turn
Quench experiments were performed at 77 K, 450 A transport current

## Slide 21
From tapes to cables: Roebel cable reduced dimensionality approach
Model vs experiment
A good agreement was found between the experimental and numerical results

## Slide 22
From tapes to cables: Roebel cable reduced dimensionality approach
Quench propagation in the longitudinal and radial direction
The temperature distribution at the end of the heater pulse shows the effects of the heat transverse between tapes of the cable and from turn to turn
For some tapes, the heat redistribution between turns is faster than within the same turn

## Slide 23: Outline
Introduction
HTS tape modeling
From tapes to cables
  Twisted Stacked Tape Cable
  Roebel cables
Scaling up: coils and magnet systems
Discussion

## Slide 24
Scaling up: full coil models
Multiscale coil model composed of a homogenized coil and a localized embedded multilayer tape module (inset)
[12] W. K. Chan, J. Schwartz, IEEE Trans. Appl. Supercond., vol. 22, no. 5, 4706010, 2012.
[13] E. Härö and A. Stenvall, IEEE Trans. Appl. Supercond., vol. 24, no. 3, 4900705, 2014.
Coil represented in some parts as a homogenous mixture of cable and insulation, in other parts as structures including cable and insulation layers
[9] J. Van Nugteren., Ph.D. dissertation, University of Twente, 2016

## Slide 25
Scaling up: 32 T NHMFL magnet model
HTS insert coil #1 (10.7 T)
HTS insert coil #2 (6.3 T)
[14] H. W. Weijers et al., IEEE Trans. Appl. Supercond., vol. 24, no. 3, Jun. 2014, Art. ID. 4301805.

## Slide 26
Only one 2D pancake is discretized with a mesh. At each mesh point, a set of heat balance equations is written for an array of temperatures
Axial heat flux between pancakes
RG10, RCZ DISTRIBUTED THERMAL RESISTANCES
[15] M Breschi, L Cavallucci, P. L. Ribani, A. V. Gavrilin, and H. W. Weijers, Supercond. Sci. Technol., vol. 29, 2016, Art. no. 055002.
Scaling up: 32 T NHMFL magnet model

## Slide 27
Lumped parameter circuit describing the mutual induction coupling between the insert and the 17-sections outsert
Coil constitutive law
The resistances of coil 1 and coil 2 can be computed from the power dissipated in all pancakes
Scaling up: 32 T NHMFL magnet model

## Slide 28
A local peak of the insert transport current during the discharge is due to the inductive coupling between the insert and the outsert
The model was first validated versus the tests of prototype coils made of 12 pancakes
Outsert currents during quench
Scaling up: 32 T NHMFL magnet model

## Slide 29
The model was then applied to analyze the self field quench test of the 32 T magnet (no current in the outsert)
Lower Field Angle θ
at t = 1.05 s
Pancake Terminal Voltages
at t = 1.05 s
Hot Spot Temperature
at t = 1.05 s
Peak Field
at t = 1.05 s
The most dangerous hot spot locations derive from a trade-off between magnetic field and field angle impacting Jc
Scaling up: 32 T NHMFL magnet model

## Slide 30: Outline
Introduction
HTS tape modeling
From tapes to cables
  Twisted Stacked Tape Cable
  Roebel cables
Scaling up: coils and magnet systems
Discussion

## Slide 31: Discussion: simulations
Impressive advances have been made in the last 15 years in the modeling of HTS devices, from single tape to full coils
The crucial techniques adopted are homogenization, reduced dimensionality and multi-scale approach
To improve the models as predictive tools, we could benefit from:
Shared material properties and parameterizations of the critical surface for wide ranges of temperature, field
Interface properties (electrical and thermal contact resistances)
Improvement of computation speed (parallel computing)
Predictive analysis and comparison between models and dedicated experiments

## Slide 32: Discussion: design
Concerning quench and current distribution, much more analytical work was performed for LTS than for HTS (different times of the theory development ?)
Results available for the LTS can be extended to HTS, but not always (NI coils, Roebel cables, etc)
Analytical formulae for the calculation of current distribution time constants and lengths, quench energy, propagation velocity, would be useful for the design of HTS based magnets

## Slide 33: Thank you for your attention
M. Breschi