## Slide 1
Field Quality Analysis in the HTS Dipole Insert-Magnet Feather M2 with the Finite Element Method
09-12 July 2019
L. Bortot1,2, M. Mentink1, C. Petrone1, S. Schöps2, J. Van Nugteren1, A. Verweij1

## Slide 2: High-Temperature Superconductors
Cuprate compounds (CuO2) doped with rare earth elements (La, Bi-Sr-Ca, Y-Ga-Ba …)
Higher Tc and Bc0 respect to the traditional low-temperature superconductors (LTS)
Higher performance comes with higher prices!
.. But in the early 2000s it was
Chart: J_eng(T) @ 5T
Chart: J_eng(B) @ 1.9K
ReBCO | 5.7212 | 5.6242 | 5.5183 | 5.4139 | 5.3111 | 5.2099 | 5.1102 | 5.0121 | 4.9154 | 4.8203 | 4.7266 | 4.6344 | 4.5437 | 4.4544 | 4.3665 | 4.2799 | 4.1948 | 4.111 | 4.0286 | 3.9475 | 3.8677 | 3.7892 | 3.712 | 3.636 | 3.5613 | 3.4878 | 3.4156 | 3.3445 | 3.2746 | 3.2059 | 3.1384 | 3.072 | 3.0067 | 2.9426 | 2.8795 | 2.8176 | 2.7567 | 2.6968 | 2.638 | 2.5803 | 2.5235 | 2.4678 | 2.413 | 2.3593 | 2.3064 | 2.2546 | 2.2036 | 2.1536 | 2.1045 | 2.0564

## Slide 3: Outline
Introduction
Motivation
Formulation
Verification Theoretical references
Validation Measurements from Feather2
Summary and Outlook
Feather2 magnet: net magnetic flux density contribution due to screening currents (first quadrant)
B(T)
Notes: From Oberkampf book: […].veriﬁcation can simply be described as “solving the equations right” and validation as “solving the right equations.”

## Slide 4: Introduction: Field Quality
Magnet aperture 2D magnetostatic field
General Solution: Fourier expansion series
, live on boundary
skew and normal magnetic field multipoles
Determined by measurements (rotating coil)
Distortion Factor (metrics for field quality)
Cross section of the beam pipe
The LHC
Notes: Add field harmonics plot.

## Slide 5: Introduction: Field Multipoles
Normal field multipoles for the reference circumference
B1 dipole
B2 quadrupole
B3 sextupole
B4 octupole
B5 decapole
B6 dodecapole

## Slide 6: Introduction: Screening (Eddy) Currents
ReBCO tape in an external magnetic density :
Magnetic field variation :  Screening currents
 Persistent magnetization
Large filament size (4~12 mm), significant persistent magnetization:
Field quality, especially at low field
Thermal behavior, principal Joule loss contribution
■ Copper ■ ReBCO ■ Substrate

## Slide 7: Motivation
Design of future HTS magnets for accelerators
Screening currents dynamics shall be taken into account
Field error due to screening currents shall be corrected, especially at low field
A code with this purpose shall be:
Numerically stable
Scalable to accelerator magnets
Validated, reliable, maintainable
Optionally:
Capable of field-circuit coupling
Efficient
Our contribution
Investigation and extension of a suitable field formulation
Implementation in a proprietary software (*), using the Finite Element Method
Scaling of the field formulation to an HTS magnet (Feather2)
(*) COMSOL Multiphysics® v. 5.3. www.comsol.com. Last access: 01/07/2019

## Slide 8: Formulation: 1) Mixed Fields
Mixed potentials
Domain decomposition
solved in (air, iron), where
solved in (conductors), where :
T soved everywhere
Discrete weak formulation:
Finite material properties  bounded condition number  Numerical stability
Ampere-Maxwell
Faraday
Heat Balance
Field coupling
Circuit coupling

## Slide 9: Formulation: 2) Model Order Reduction
Model order reduction  Speed-up
  High aspect ratio
  Tapes as surfaces in (lines in )
2D transverse field configuration
Tapes as lines in
Electric field balance in the superconductor
External ,Resistive , Inductive
Current sharing resolved with root finding algorithm
with
as voltage distribution function
external voltage supply
  Input, if voltage driven model
  Lagrange multiplier, if current driven model
Roebel Cables  Transposition  Even current distribution in the tapes
Model order reduction
: air
: coil

## Slide 10: Outline
Introduction
Motivation
Formulation
Verification Theoretical references
    Critical State (Bean) Model
    Skin Effect
    Field Dependency
Validation
Summary and Outlook
Notes: Some of the verifications. Mention Current dependency, PEC behavior, comparison with other formulations..

## Slide 11: Verification – 1. Critical State (Bean) Model
Scenario: magnetic field diffusion
  ,
Geometry: slab of infinite height, modelled as stack of tapes
Source: boundary field
Reference: Analytical solution:
Chart: 
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
 | 0 | 1 | 1 | 0 | 0 | -1 | -1 | 0 | 0
: air
: conductor
Computational domain
Chart: 
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
 | 0 | 1 | 1 | 0 | 0 | -1 | -1 | 0 | 0
Chart: 
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
 | 0 | 1 | 1 | 0 | 0 | -1 | -1 | 0 | 0
Source term

## Slide 12: Verification – 1. Critical State (Bean) Model
Numerical Solution: magnetic field diffusion
Magnetic flux density and normalized current density distribution
Chart: 
Chart: 
Chart: 
Chart: 
Chart: 
Chart: 
Chart: 
Chart: 
B (T)
J/Jc (-)
x (mm)
x (mm)
x (mm)
x (mm)
 Distributions consistent with theory
time

## Slide 13: Verification – 2. Skin Effect
Scenario: magnetic field diffusion
  ,
Geometry: bulk material, modelled as stack of tapes
Source: boundary field
Reference: Analytical solution:
  Gaussian error function
  Similarity variable
  Magnetic diffusivity
Chart: 
| 0 | 0.999 | 1 | 2 | 3
 | 0 | 0 | 1 | 1 | 1
: air
: conductor
Computational domain
Chart: 
| 0 | 0.999 | 1 | 2 | 3
 | 0 | 0 | 1 | 1 | 1
Source term

## Slide 14: Verification – 2. Skin Effect
Numerical Solution: magnetic field diffusion
Magnetic flux density distribution in the conductive slab
Magnetic flux density distribution at x=1 mm, as function of time: numerical solution (sol) and analytical solution (ref)
Chart: Field at x = 1 mm
| 0 | 2.6315789473684199 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40 | 41 | 42 | 43 | 44 | 45 | 46 | 47 | 48 | 49 | 50
sol | 0 | 0.48451 | 0.5175 | 0.57514 | 0.61614 | 0.64721 | 0.67179 | 0.69186 | 0.70865 | 0.72297 | 0.73537 | 0.74624 | 0.75587 | 0.76448 | 0.77224 | 0.77929 | 0.78571 | 0.79161 | 0.79704 | 0.80208 | 0.80675 | 0.81111 | 0.81519 | 0.81902 | 0.82262 | 0.82602 | 0.82923 | 0.83227 | 0.83516 | 0.83792 | 0.84054 | 0.84305 | 0.84545 | 0.84775 | 0.84996 | 0.85209 | 0.85414 | 0.85612 | 0.85803 | 0.85988 | 0.86167 | 0.86341 | 0.86509 | 0.86674 | 0.86833 | 0.86989 | 0.87141 | 0.87289 | 0.87434 | 0.87534
ref | 0 | 0.48451 | 0.62432 | 0.68975 | 0.7295 | 0.75723 | 0.7778 | 0.7939 | 0.80698 | 0.8178 | 0.827 | 0.83495 | 0.84187 | 0.848 | 0.85347 | 0.85838 | 0.86284 | 0.86689 | 0.87061 | 0.87534
 Consistent with theory [6]
Chart: Field diffusion
| -2 | -1.5 | -1 | -0.5 | -0.01 | 0 | 1E-4 | 2.0000000000000001E-4 | 5.0000000000000001E-4 | 0.81632653061224503 | 1.0204081632653099 | 1.22448979591837 | 1.4285714285714302 | 1.6326530612244901 | 1.83673469387755 | 2.0408163265306096 | 2.2448979591836702 | 2.4489795918367299 | 2.6530612244898002 | 2.8571428571428603 | 3.06122448979592 | 3.2653061224489801 | 3.4693877551020398 | 3.6734693877550999 | 3.87755102040816 | 4.0816326530612299 | 4.28571428571429 | 4.4897959183673493 | 4.6938775510204094 | 4.8979591836734704 | 5.1020408163265305 | 5.3061224489795906 | 5.5102040816326499 | 5.7142857142857206 | 5.9183673469387799 | 6.12244897959184 | 6.3265306122449001 | 6.5306122448979602 | 6.7346938775510194 | 6.9387755102040796 | 7.1428571428571397 | 7.3469387755101998 | 7.5510204081632697 | 7.7551020408163298 | 7.9591836734693899 | 8.1632653061224492 | 8.3673469387755102 | 8.5714285714285694 | 8.7755102040816304 | 8.9795918367346914 | 9.1836734693877595 | 9.3877551020408188 | 9.5918367346938798 | 9.7959183673469408 | 10
t=0 | 1 | 1 | 1 | 1 | 1 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
t=1 | 1 | 1 | 1 | 1 | 1 | 1 | 0.81914 | 0.64751 | 0.49284 | 0.3605 | 0.25308 | 0.17015 | 0.10944 | 0.067257 | 0.039447 | 0.022057 | 0.011746 | 0.0059514 | 0.0028662 | 0.0013108 | 0.00056855 | 0.00023351 | 9.1027e-05 | 3.3455e-05 | 1.1649e-05 | 3.8174e-06 | 1.18e-06 | 3.4225e-07 | 9.3286e-08 | 2.3853e-08 | 5.7594e-09 | 1.3159e-09 | 2.8347e-10 | 5.7014e-11 | 1.0749e-11 | 1.8971e-12 | 3.141e-13 | 4.8688e-14 | 7.0741e-15 | 9.6624e-16 | 1.2451e-16 | 1.5182e-17 | 1.7522e-18 | 1.9259e-19 | 2.0284e-20 | 2.0427e-21 | 1.9829e-22 | 1.86e-23 | 1.6925e-24 | 1.4976e-25 | 1.2847e-26 | 1.0775e-27 | 8.8053e-29 | 7.0718e-30 | 1.09e-30
t=5 | 1 | 1 | 1 | 1 | 1 | 1 | 0.90893 | 0.81905 | 0.7315 | 0.64732 | 0.5675 | 0.49266 | 0.42347 | 0.36031 | 0.30342 | 0.25284 | 0.20844 | 0.16998 | 0.1371 | 0.10935 | 0.086234 | 0.067234 | 0.051818 | 0.039474 | 0.029719 | 0.02211 | 0.016254 | 0.011805 | 0.0084706 | 0.0060039 | 0.0042058 | 0.0029119 | 0.0019914 | 0.0013452 | 0.00089759 | 0.00059141 | 0.00038431 | 0.00024739 | 0.00015655 | 9.8192e-05 | 6.0729e-05 | 3.7076e-05 | 2.2345e-05 | 1.3282e-05 | 7.7971e-06 | 4.5229e-06 | 2.5849e-06 | 1.4586e-06 | 8.1271e-07 | 4.4739e-07 | 2.4322e-07 | 1.3151e-07 | 7.3086e-08 | 4.4929e-08 | 3.66e-08
t=10 | 1 | 1 | 1 | 1 | 1 | 1 | 0.93921 | 0.87877 | 0.81903 | 0.76033 | 0.70303 | 0.64733 | 0.59354 | 0.54189 | 0.49259 | 0.4458 | 0.40165 | 0.36023 | 0.32159 | 0.28577 | 0.25275 | 0.22247 | 0.19489 | 0.1699 | 0.14739 | 0.12723 | 0.10928 | 0.093395 | 0.079416 | 0.067186 | 0.056556 | 0.04737 | 0.039472 | 0.032721 | 0.026983 | 0.022135 | 0.018063 | 0.014663 | 0.01184 | 0.0095092 | 0.0075971 | 0.0060373 | 0.0047726 | 0.0037534 | 0.0029372 | 0.002288 | 0.0017753 | 0.001374 | 0.001063 | 0.00082543 | 0.00064873 | 0.00052061 | 0.00043494 | 0.00038486 | 0.000369
t=50 | 1 | 1 | 1 | 1 | 1 | 1 | 0.97423 | 0.9485 | 0.92282 | 0.89724 | 0.87181 | 0.84651 | 0.82139 | 0.79648 | 0.77182 | 0.74742 | 0.72332 | 0.69955 | 0.67613 | 0.65308 | 0.63043 | 0.60821 | 0.58644 | 0.56514 | 0.54433 | 0.52403 | 0.50427 | 0.48505 | 0.4664 | 0.44834 | 0.43088 | 0.41404 | 0.39783 | 0.38226 | 0.36734 | 0.35309 | 0.33952 | 0.32663 | 0.31444 | 0.30295 | 0.29217 | 0.28211 | 0.27277 | 0.26416 | 0.25628 | 0.24914 | 0.24274 | 0.23708 | 0.23218 | 0.22802 | 0.22462 | 0.22197 | 0.22007 | 0.21893 | 0.21855

## Slide 15: Verification – 3. Field Dependency
Scenario: AC loss due to screening currents
  ,
  as power law
Geometry: single tape, orthogonal to the field
Source: boundary field
Reference: Analytical solution: AC loss (J/cycle), penetration field
  if ,
  if
: air
: conductor
Chart: 
| 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9 | 0.95 | 1
 | 0 | 0.30902 | 0.58779 | 0.80902 | 0.95106 | 1 | 0.95106 | 0.80902 | 0.58779 | 0.30902 | 1.2251e-16 | -0.30902 | -0.58779 | -0.80902 | -0.95106 | -1 | -0.95106 | -0.80902 | -0.58779 | -0.30902 | -2.4503e-16
Source term
Chart: 
| 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9 | 0.95 | 1
 | 0 | 0.30902 | 0.58779 | 0.80902 | 0.95106 | 1 | 0.95106 | 0.80902 | 0.58779 | 0.30902 | 1.2251e-16 | -0.30902 | -0.58779 | -0.80902 | -0.95106 | -1 | -0.95106 | -0.80902 | -0.58779 | -0.30902 | -2.4503e-16
Computational domain

## Slide 16: Verification – 3. Field Dependency
Numerical Solution: AC loss due to screening currents
Ac loss per cycle, as function of the applied field
Ac loss per cycle, as function of frequency, for
Chart: AC loss / Cycle
| 5.0000000000000001E-4 | 1E-3 | 2E-3 | 5.0000000000000001E-3 | 0.01 | 0.02 | 0.05 | 0.1 | 0.2 | 0.5 | 1 | 2
n = 5 | 8.4185e-08 | 7.7364e-07 | 7.6021e-06 | 0.00015513 | 0.0014552 | 0.012318 | 0.14834 | 0.63661 | 1.945 | 6.7766 | 16.3147 | 38.338
n = 20 | 1.4463e-08 | 1.5982e-07 | 1.2841e-06 | 3.477e-05 | 0.00046778 | 0.0057847 | 0.10672 | 0.52501 | 1.5837 | 4.9632 | 10.8423 | 23.0321
n = 50 | 1.4463e-08 | 1.4384e-07 | 1.1724e-06 | 2.8572e-05 | 0.00034185 | 0.0046122 | 0.095894 | 0.49295 | 1.5053 | 4.6531 | 9.9837 | 20.8184
Chart: AC loss / Cycle
| 1E-3 | 0.01 | 0.1 | 1 | 10 | 100 | 0 | 0 | 0 | 0 | 0 | 0
n = 5 | 0.0045649 | 0.0027402 | 0.0014519 | 0.00071958 | 0.00034493 | 0.00016302 | 0 | 0 | 0 | 0 | 0 | 0
n = 20 | 0.00070325 | 0.00057325 | 0.000466 | 0.00039121 | 0.00030674 | 0.00024807 | 0 | 0 | 0 | 0 | 0 | 0
n = 50 | 0.0004085 | 0.0004092 | 0.00034013 | 0.00032062 | 0.00029195 | 0.00027318 | 0 | 0 | 0 | 0 | 0 | 0
n = 100 | 0.00032443 | 0.00031125 | 0.00029951 | 0.00029178 | 0.00029228 | 0.00026142 | 0 | 0 | 0 | 0 | 0 | 0
 Consistent with theory
Notes: Meissner is reversible. Losses per cycle are always zero

## Slide 17: Outline
Introduction
Motivation
Formulation
Verification
Validation Crosscheck and Benchmark Measurements on Feather2: Field quality assessment
    Magnetic Field Quality
    Screening Current Effects
Summary and Outlook

## Slide 18: Crosscheck
Reference model based on the formulation,
available at http://www.htsmodelling.com
2D model of a Single HTS tape in self-field
Source: ,
Chart: Ohmic loss per cycle
| 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75 | 2
Ref. - 1Hz | 1.3507e-05 | 0.00022572 | 0.0012866 | 0.0069381 | 0.22171 | 1.5876 | 4.4346 | 8.6839
Ref. - 10Hz | 1.1861e-05 | 0.00017642 | 0.00095176 | 0.0037462 | 0.026446 | 0.16322 | 0.44802 | 0.87306
Ref. - 100Hz | 1.0655e-05 | 0.00014301 | 0.00072965 | 0.0025082 | 0.0073745 | 0.021555 | 0.050323 | 0.09312
Ref. - 1000Hz | 1.8165e-05 | 0.00015917 | 0.00062696 | 0.0016612 | 0.0034905 | 0.0063376 | 0.010404 | 0.015849
A-H - 1Hz | 1.4392e-05 | 0.00022396 | 0.0012754 | 0.006917 | 0.22164 | 1.5872 | 4.4345 | 8.6839
A-H - 10Hz | 1.1751e-05 | 0.00017469 | 0.00094137 | 0.0037227 | 0.026403 | 0.16307 | 0.4478 | 0.87295
A-H - 100Hz | 7.6794e-06 | 0.00013445 | 0.0007044 | 0.0024372 | 0.0072274 | 0.021355 | 0.050083 | 0.092956
A-H - 1000Hz | 2.5608e-06 | 0.000101 | 0.00046883 | 0.0013431 | 0.0029579 | 0.0055583 | 0.0094031 | 0.014658
Chart: Ohmic loss per cycle
| 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75 | 2
Ref. - 1Hz | 1.3507e-05 | 0.00022572 | 0.0012866 | 0.0069381 | 0.22171 | 1.5876 | 4.4346 | 8.6839
Ref. - 10Hz | 1.1861e-05 | 0.00017642 | 0.00095176 | 0.0037462 | 0.026446 | 0.16322 | 0.44802 | 0.87306
Ref. - 100Hz | 1.0655e-05 | 0.00014301 | 0.00072965 | 0.0025082 | 0.0073745 | 0.021555 | 0.050323 | 0.09312
Ref. - 1000Hz | 1.8165e-05 | 0.00015917 | 0.00062696 | 0.0016612 | 0.0034905 | 0.0063376 | 0.010404 | 0.015849
A-H - 1Hz | 1.4392e-05 | 0.00022396 | 0.0012754 | 0.006917 | 0.22164 | 1.5872 | 4.4345 | 8.6839
A-H - 10Hz | 1.1751e-05 | 0.00017469 | 0.00094137 | 0.0037227 | 0.026403 | 0.16307 | 0.4478 | 0.87295
A-H - 100Hz | 7.6794e-06 | 0.00013445 | 0.0007044 | 0.0024372 | 0.0072274 | 0.021355 | 0.050083 | 0.092956
A-H - 1000Hz | 2.5608e-06 | 0.000101 | 0.00046883 | 0.0013431 | 0.0029579 | 0.0055583 | 0.0094031 | 0.014658
1 Hz
10 Hz
100 Hz
1000 Hz
Markers: (ref)
Lines:

## Slide 19: Benchmark
Forecasts on expected computational time:
1 tape
5 tapes
10 tapes
Same physics…
Increased computational cost
Chart: Computational time
| 1 | 5 | 10
H | 0.048611 | 0.20833 | 0.5
A-H | 0.0027778 | 0.0041667 | 0.005 | 0.026111 | 0.052778
8 h
CPU: Intel Core i7-3770 @ 3.40GHz. RAM: 32 Gb. OS: Win 10

## Slide 20: Feather2 Dipole Insert Magnet
Courtesy of J. Van Nugteren
Central and wing decks, for upper and lower coils
Current leads
External support cylinder

## Slide 21: Measurements on Feather2
Scenario: magnetic field quality in the Feather M2 insert dipole magnet
  ,
  as anisotropic power law, derived from data @ 77 K
  Uncertainty in material properties
Geometry: tapes modelled as lines
Source: measured current
Reference: measurements carried out by C. Petrone (CERN)
Computational domain
: air
: coil
: iron

## Slide 22: Modelling of Jc (T, B, )
available only for Need for a lift factor
Calibrated with the measured critical current
Gauged with (magnetostatic simulation)
 Anisotropy included in the model, but uncertainty on material properties

## Slide 23: Field Quality Assessment
Pre-cycle first magnetization
Steps of 250 A, plateaus of 120 s: decay of inductive effects
Evaluation points ,
FEM simulation
Magnetic field quality calculation
Persistent screening currents contribution: Calculation of change in magnetic field quality (assuming screening currents as dominant mechanism)
Chart: t (s)
| 0 | 30 | 150 | 200 | 320 | 370 | 490 | 540 | 660 | 710 | 830 | 880 | 1000 | 1050 | 1170 | 1220 | 1340 | 1390 | 1510 | 1560 | 1680 | 1730 | 1850 | 1900 | 2020 | 2070 | 2190 | 2220 | 2340
 | 0.1 | 0.25 | 0.25 | 0.5 | 0.5 | 0.75 | 0.75 | 1 | 1 | 1.25 | 1.25 | 1.5 | 1.5 | 1.75 | 1.75 | 1.5 | 1.5 | 1.25 | 1.25 | 1 | 1 | 0.75 | 0.75 | 0.5 | 0.5 | 0.25 | 0.25 | 0.1 | 0.1
 | 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75 | 1.5 | 1.25 | 1 | 0.75 | 0.5 | 0.25
 | 0 | 1 | 1.75 | 1.75 | 1 | 0.1 | 0.1
Total magnetic flux density (T), 1 quadrant
B(T)

## Slide 24: Results – FEM Simulation
Normalized current density in the coil, shown for the first quadrant
a)
b)
c)
Current density distribution in the coil:
Same external current, different time steps
Computational time: 120k DoF, 0.9 h (*)
a)
b)
c)
J/Jc (-)
J/Jc (-)
J/Jc (-)
(*) CPU: Intel Core i7-3770 @ 3.40GHz. RAM: 32 Gb. OS: Win 10
Notes: Influence of screening currents

## Slide 25: Validation – 4. Magnetic Field Quality
field multipoles, as function of the normalized staircase time
Chart: 
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 0.16682 | 0.33069 | 0.6035 | 0.87668 | 1.15 | 1.422 | 1.6339 | 1.7861 | 1.9218 | 2.0439 | 2.1607 | 2.2749 | 2.3876 | 2.4621 | 2.389 | 2.2779 | 2.1649 | 2.0486 | 1.9265 | 1.7905 | 1.6379 | 1.4253 | 1.1523 | 0.87777 | 0.60397 | 0.33096 | 0.16715
sim | 0.14074 | 0.27788 | 0.41502 | 0.55203 | 0.68894 | 0.8258 | 0.96264 | 1.0994 | 1.236 | 1.3717 | 1.5052 | 1.6361 | 1.7626 | 1.8788 | 1.9823 | 2.0803 | 2.1757 | 2.2698 | 2.3636 | 2.4568 | 2.3661 | 2.2744 | 2.1814 | 2.0866 | 1.9886 | 1.8845 | 1.767 | 1.6396 | 1.5079 | 1.3737 | 1.2376 | 1.1006 | 0.96351 | 0.82637 | 0.68925 | 0.55214 | 0.41503 | 0.27791 | 0.14078
Chart: 
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 396.176 | 287.8211 | 239.1869 | 222.0029 | 214.3159 | 212.4014 | 214.2419 | 219.2723 | 220.9041 | 215.385 | 205.7201 | 194.2002 | 182.0771 | 174 | 174.1 | 192.395 | 202.9659 | 211.8436 | 217.1225 | 215.7858 | 211.6595 | 211.3379 | 215.8072 | 227.1275 | 246.8658 | 296.6789 | 403.7129
sim | 320.0853 | 248.7077 | 225.5965 | 215.1322 | 209.3754 | 205.5531 | 202.8011 | 200.8588 | 199.8246 | 199.8985 | 200.577 | 202.7649 | 207.1983 | 210.8754 | 208.7164 | 202.927 | 195.1216 | 186.3934 | 177.2141 | 167.9082 | 176.2786 | 184.6441 | 192.7971 | 200.4033 | 206.4032 | 209.0362 | 206.2008 | 203.3 | 202.8044 | 203.7059 | 205.0536 | 207.405 | 210.6531 | 214.8353 | 220.2992 | 228.2263 | 241.2036 | 267.2084 | 345.3282
Chart: 
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 68.7505 | 45.678 | 35.0365 | 30.9446 | 28.6503 | 26.5144 | 24.1974 | 21.2663 | 17.5851 | 14.6967 | 12.8643 | 11.7389 | 11.0782 | 10.84 | 11.088 | 11.6944 | 12.6825 | 14.4331 | 17.2236 | 20.9468 | 23.9186 | 26.3363 | 28.7482 | 31.4138 | 35.6783 | 46.2221 | 69.108
sim | 61.4558 | 41.2189 | 35.0234 | 31.9337 | 29.967 | 28.6082 | 27.5781 | 26.7855 | 26.1205 | 25.3861 | 24.5498 | 23.3887 | 21.4993 | 18.8405 | 16.6943 | 15.3611 | 14.6057 | 14.1898 | 14.041 | 14.0722 | 14.3001 | 14.6165 | 15.1238 | 15.9591 | 17.3832 | 19.61 | 22.2689 | 24.1055 | 25.2416 | 26.1382 | 26.9814 | 27.7605 | 28.653 | 29.7705 | 31.2311 | 33.374 | 36.9909 | 44.4431 | 67.2964
Chart: 
| 8.3270002777777768E-2 | 0.15268336111111108 | 0.22217659722222222 | 0.29185969444444448 | 0.36127797222222219 | 0.41690402777777774 | 0.45855190277777774 | 0.5 | 0.54188712500000003 | 0.58359297222222217 | 0.63875945833333336 | 0.70818063888888894 | 0.77788315277777775 | 0.84714761111111114 | 0.91661162361111104
meas | 0.32836 | 0.60123 | 0.87414 | 1.1473 | 1.4189 | 1.6303 | 1.782 | 1.9169 | 1.7827 | 1.6312 | 1.4197 | 1.1477 | 0.87399 | 0.60078 | 0.32807
0 deg | 0.054389 | 0.13668 | 0.27384 | 0.41089 | 0.54782 | 0.68474 | 0.82163 | 0.95847 | 1.0952 | 1.2318 | 1.3674 | 1.5007 | 1.6315 | 1.7575 | 1.8728 | 1.9762 | 1.8736 | 1.7584 | 1.6321 | 1.5012 | 1.3676 | 1.2318 | 1.095 | 0.95808 | 0.82116 | 0.68425 | 0.54733 | 0.41038 | 0.27343 | 0.13647 | 0.054264
Chart: 
| 8.3270002777777768E-2 | 0.15268336111111108 | 0.22217659722222222 | 0.29185969444444448 | 0.36127797222222219 | 0.41690402777777774 | 0.45855190277777774 | 0.5 | 0.54188712500000003 | 0.58359297222222217 | 0.63875945833333336 | 0.70818063888888894 | 0.77788315277777775 | 0.84714761111111114 | 0.91661162361111104
meas | 268.5344 | 228.6497 | 215.4613 | 210.3915 | 210.5213 | 213.9242 | 220.2013 | 222.3 | 221.1285 | 216.4372 | 215.5462 | 218.3265 | 226.817 | 243.7866 | 287.6951
0 deg | 386.2262 | 280.5091 | 247.3264 | 231.9384 | 222.7761 | 216.7518 | 212.7355 | 210.0629 | 208.7265 | 208.406 | 208.8699 | 211.2385 | 216.039 | 219.4111 | 216.8338 | 219.6605 | 217.011 | 213.6754 | 212.8643 | 214.047 | 216.126 | 219.3914 | 223.7655 | 229.1627 | 236.4414 | 247.3545 | 265.7473 | 302.9339 | 415.5836
Chart: 
| 8.3270002777777768E-2 | 0.15268336111111108 | 0.22217659722222222 | 0.29185969444444448 | 0.36127797222222219 | 0.41690402777777774 | 0.45855190277777774 | 0.5 | 0.54188712500000003 | 0.58359297222222217 | 0.63875945833333336 | 0.70818063888888894 | 0.77788315277777775 | 0.84714761111111114 | 0.91661162361111104
meas | 39.8036 | 31.8946 | 28.8959 | 27.1225 | 25.358 | 23.2981 | 20.4954 | 16.98 | 20.6136 | 23.5531 | 25.9182 | 27.8832 | 29.7798 | 33.0702 | 41.2508
0 deg | 64.5533 | 42.6031 | 35.7611 | 32.2885 | 30.1699 | 28.7176 | 27.7233 | 26.9918 | 26.3705 | 25.6468 | 24.8465 | 23.7173 | 21.8142 | 19.1782 | 17.1092 | 19.3649 | 22.1104 | 24.1216 | 25.4375 | 26.4591 | 27.3749 | 28.2139 | 29.1309 | 30.2364 | 31.6956 | 33.9056 | 37.6863 | 45.5399 | 69.8648
Chart: 
| 9.0992116434202561E-2 | 0.18195318981200725 | 0.27291271376591875 | 0.36391773802304422 | 0.45482680412371135 | 0.5 | 0.54535864160097025 | 0.63601561552456043 | 0.72710236810188 | 0.81809164038811399 | 0.90898068526379627
meas | 0.16017 | 0.3238 | 0.48709 | 0.65054 | 0.81375 | 0.89515 | 0.81365 | 0.65027 | 0.48676 | 0.32339 | 0.16009
0 deg | 0.052761 | 0.13504 | 0.27197 | 0.40878 | 0.54547 | 0.68197 | 0.81828 | 0.95466 | 0.81864 | 0.68209 | 0.54534 | 0.40857 | 0.27176 | 0.1349 | 0.052784
Chart: 
| 9.0992116434202561E-2 | 0.18195318981200725 | 0.27291271376591875 | 0.36391773802304422 | 0.45482680412371135 | 0.5 | 0.54535864160097025 | 0.63601561552456043 | 0.72710236810188 | 0.81809164038811399 | 0.90898068526379627
meas | 408.6229 | 295.2836 | 260.6113 | 245.7667 | 238.9375 | 238.3 | 243.5962 | 255.1541 | 274.1876 | 312.4602 | 429.2418
0 deg | 413.4029 | 298.6497 | 263.4089 | 248.3578 | 241.7463 | 239.392 | 238.8263 | 240.5296 | 247.3744 | 259.5205 | 278.954 | 317.7925 | 434.7402
Chart: 
| 9.0992116434202561E-2 | 0.18195318981200725 | 0.27291271376591875 | 0.36391773802304422 | 0.45482680412371135 | 0.5 | 0.54535864160097025 | 0.63601561552456043 | 0.72710236810188 | 0.81809164038811399 | 0.90898068526379627
meas | 64.8761 | 43.6858 | 36.7633 | 33.551 | 31.7576 | 31.42 | 32.5056 | 34.7951 | 38.5903 | 45.7734 | 67.6648
0 deg | 72.6661 | 47.0821 | 38.8651 | 35.1972 | 33.183 | 32.1981 | 32.0163 | 32.6592 | 34.3344 | 37.0526 | 41.2849 | 49.747 | 75.0961
B1 (T)
b3 (units)
b5 (units)
4.5 K
25.0 K
68.0 K
t (s)
t (s)
t (s)
 Very good agreement with measurements
Measurement
Simulation
Notes: Multipoles dominated by geometry and iron errors.
High multipoles due to the non optimized iron yoke (magnet is an insert)
Multipoles minimized for operational conditions in background field Screening currents only small contribution

## Slide 26: Validation – 5. Screening Currents
field multipole variations, as function of current (in kA)
Chart: 
| 0.29957012 | 0.60028197999999999 | 1.1006214999999999 | 1.6008191000000003 | 2.0986528 | 2.5993179 | 3.0016338 | 3.2984656999999999 | 3.5995850000000003 | 3.8981686999999998 | 4.2014339999999999 | 4.5019495000000003 | 4.8017586999999997
meas | 1.3544 | 1.1051 | 1.9063 | 4.4086 | 9.3474 | 13.6006 | 16.153 | 17.6595 | 19.2431 | 19.3901 | 16.8988 | 12.3109 | 5.8023
sim | 0.17712 | 0.18129 | 0.10459 | 0.034776 | 0.42488 | 1.2704 | 2.3111 | 3.5322 | 4.9068 | 6.4841 | 8.4736 | 10.9665 | 14.0313 | 17.6576 | 23.1819 | 25.9661 | 25.8476 | 23.3996 | 18.458 | 10.4672
Chart: 
| 0.29957012 | 0.60028197999999999 | 1.1006214999999999 | 1.6008191000000003 | 2.0986528 | 2.5993179 | 3.0016338 | 3.2984656999999999 | 3.5995850000000003 | 3.8981686999999998 | 4.2014339999999999 | 4.5019495000000003 | 4.8017586999999997
meas | 7.5369 | 8.8578 | 7.6789 | 5.1246 | 1.4913 | -1.0635 | -2.5824 | -3.4865 | -3.7816 | -3.5413 | -2.7543 | -1.8051 | -0.7092
sim | 48.5617 | 25.2429 | 18.5007 | 15.6071 | 13.0941 | 10.9238 | 9.2822 | 7.852 | 6.5462 | 5.229 | 3.8073 | 2.2275 | 0.53505 | -0.99758 | -1.8393 | -2.3132 | -2.5237 | -2.3245 | -1.7493 | -0.93546
Chart: 
| 0.29957012 | 0.60028197999999999 | 1.1006214999999999 | 1.6008191000000003 | 2.0986528 | 2.5993179 | 3.0016338 | 3.2984656999999999 | 3.5995850000000003 | 3.8981686999999998 | 4.2014339999999999 | 4.5019495000000003 | 4.8017586999999997
meas | 0.3575 | 0.54406 | 0.64176 | 0.46927 | 0.09792 | -0.17809 | -0.27878 | -0.31948 | -0.36157 | -0.26363 | -0.18183 | -0.044517 | 0.009789
sim | 12.1545 | 5.8405 | 3.2242 | 1.9675 | 1.4403 | 1.2642 | 1.1623 | 1.0749 | 0.975 | 0.86092 | 0.75204 | 0.69185 | 0.71681 | 0.76964 | 0.76958 | 0.68882 | 0.59794 | 0.51814 | 0.4267 | 0.2591
Chart: 
| 0.59954401999999996 | 1.0993202 | 1.5996714999999999 | 2.1013898000000002 | 2.6012013999999999 | 3.001709 | 3.3015737000000001
meas | -1.5373 | -2.3197 | -0.77252 | 1.9049 | 4.1991 | 4.694 | 3.9606
0 deg | -0.63013 | -1.0677 | -2.0652 | -2.5651 | -2.4856 | -2.4744 | -2.3833 | -1.9795 | -1.1557 | 0.062771 | 1.2897 | 2.4462 | 3.484 | 4.3087 | 3.9264
Chart: 
| 0.59954401999999996 | 1.0993202 | 1.5996714999999999 | 2.1013898000000002 | 2.6012013999999999 | 3.001709 | 3.3015737000000001
meas | 19.1607 | 15.1369 | 11.3557 | 7.935 | 5.025 | 2.5131 | 0.92724
0 deg | 55.7143 | 29.3574 | 22.4248 | 18.4209 | 15.4161 | 13.6654 | 12.411 | 11.03 | 9.3284 | 7.3994 | 5.641 | 3.9944 | 2.4369 | 0.97204 | 0.24939
Chart: 
| 0.59954401999999996 | 1.0993202 | 1.5996714999999999 | 2.1013898000000002 | 2.6012013999999999 | 3.001709 | 3.3015737000000001
meas | 1.4472 | 1.1755 | 0.88389 | 0.76068 | 0.56016 | 0.25494 | 0.1182
0 deg | 11.3078 | 5.3115 | 2.9367 | 1.9252 | 1.6171 | 1.5257 | 1.5188 | 1.4076 | 1.2221 | 1.0044 | 0.81233 | 0.59096 | 0.40433 | 0.29617 | 0.1867
Chart: 
| 0.30009200000000003 | 0.60008161999999998 | 0.90006613000000002 | 1.2002006999999999 | 1.5000188000000001
meas | -0.9215 | -4.5647 | -3.6451 | -3.0726 | -1.1658
0 deg | 0.2425 | -1.4646 | -2.2609 | -2.1564 | -1.3568 | 1.2655 | 3.8036
Chart: 
| 0.30009200000000003 | 0.60008161999999998 | 0.90006613000000002 | 1.2002006999999999 | 1.5000188000000001
meas | 20.6189 | 17.1766 | 13.5763 | 9.3873 | 4.6586
0 deg | 20.1855 | 21.3373 | 19.1428 | 15.5451 | 11.1627 | 5.6281 | 1.1376
Chart: 
| 0.30009200000000003 | 0.60008161999999998 | 0.90006613000000002 | 1.2002006999999999 | 1.5000188000000001
meas | 2.7887 | 2.0876 | 1.8269 | 1.2441 | 0.74801
0 deg | 3.8008 | 2.43 | 2.665 | 2.4198 | 1.8554 | 1.1515 | 0.46114
kA
kA
kA
 Good agreement with measurements, considering uncertainty in
B1 (T)
b3 (units)
b5 (units)
4.5 K
25.0 K
68.0 K
Measurement
Simulation

## Slide 27: Summary and Outlook
Summary
- weak formulation for FEM:
Excellent agreement with theory
Consistency with Feather2 measurements
Stable, scalable and fast (few hours for ~ tapes in 2D models)
Thank you for your attention!
Outlook
Include heat balance equation
Develop field-circuit coupling interface
Include the models in the STEAM co-simulation framework
Run field quality analysis and optimization
Run quench protection studies (e.g., Feather2 in FRESCA2)

## Slide 28: References
Bíró, O. "Edge element formulations of eddy current problems." CMAM 169.3-4 (1999): 391-405.
Carpenter, C. J. "Comparison of alternative formulations of 3-dimensional magnetic-field and eddy-current problems at power frequencies." Proceedings of the Institution of Electrical Engineers. Vol. 124. No. 11. IET Digital Library, 1977.
Brambilla, R., Grilli, F., Martini, L., Bocchi, M., & Angeli, G. (2018). A finite-element method framework for modeling rotating machines with superconducting windings. IEEE Transactions on Applied Superconductivity, 28(5), 1-11.
Zhang, H., et al. "An efficient 3D finite element method model based on the T–A formulation for superconducting coated conductors.“ SuST, 30.2 (2016): 024005
Schöps, S., et al. "Winding functions in transient magnetoquasistatic field-circuit coupled simulations." COMPEL: The International Journal for Computation and Mathematics in Electrical and Electronic Engineering 32.6 (2013): 2063-2083
Russenschuck, S. Field computation for accelerator magnets: analytical and numerical methods for electromagnetic design and optimization. John Wiley & Sons, 2011.
Knoepfel, H. E., Magnetic fields: a comprehensive theoretical treatise for practical use. John Wiley & Sons, 2008
Brandt, E H., "Superconductors of finite thickness in a perpendicular magnetic field: Strips and slabs." Physical review B 54.6 (1996): 4246
Van Nugteren, J., et al. "Powering of an HTS dipole insert-magnet operated standalone in helium gas between 5 and 85 K." SuST 31.6 (2018): 065002.

## Slide 30
Annex

## Slide 31: …Why HTS?
Circular accelerators for particle physics:
circular orbit
Just for fun
LHC tunnel + HTS dipoles everywhere @ 4.2 K, 30 T:
Collision energy of the Future Circular Collider (FCC): ]
… not so far away after all!

## Slide 32: Verification – Current dependency
Scenario: AC loss due to screening currents
  ,
  as power law
Geometry: single tape
Source: External current
Reference: previous work, e.g. [ref1]:
  if
  if field fully penetrated, const
Chart: 
| 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9 | 0.95 | 1
 | 0 | 0.30902 | 0.58779 | 0.80902 | 0.95106 | 1 | 0.95106 | 0.80902 | 0.58779 | 0.30902 | 1.2251e-16 | -0.30902 | -0.58779 | -0.80902 | -0.95106 | -1 | -0.95106 | -0.80902 | -0.58779 | -0.30902 | -2.4503e-16
: air
: conductor
Chart: 
| 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9 | 0.95 | 1
 | 0 | 0.30902 | 0.58779 | 0.80902 | 0.95106 | 1 | 0.95106 | 0.80902 | 0.58779 | 0.30902 | 1.2251e-16 | -0.30902 | -0.58779 | -0.80902 | -0.95106 | -1 | -0.95106 | -0.80902 | -0.58779 | -0.30902 | -2.4503e-16
Source term
[ref1] Grilli, F, et al. "Computation of Losses in HTS Under the Action of Varying Magnetic Fields and Currents." IEEE Transactions on Applied Superconductivity 24.1 (2014): 78-110.
Computational domain

## Slide 33: Verification – Current dependency
Solution of the transport + screening currents problem
Ac loss per cycle, as function of frequency, for . Trends are highlighted with dashed lines
Chart: AC loss / Cycle
| 1 | 10 | 50 | 100 | 250 | 500 | 750 | 1000 | 1250 | 1500 | 2000
n = 5 | 7.3834e-11 | 4.2243e-08 | 7.6652e-06 | 7.8292e-05 | 0.0017731 | 0.021031 | 0.10252 | 0.37937 | 1.2711 | 3.6481 | 20.1038
n = 20 | 1.1431e-11 | 8.0604e-09 | 1.1447e-06 | 1.4877e-05 | 0.00049992 | 0.0078275 | 0.045615 | 0.28617 | 18.7752 | 858.3055
n = 50 | 5.5355e-09 | 7.8244e-07 | 9.7064e-06 | 0.00035447 | 0.0059341 | 0.035477 | 0.24419 | 9737.4123
Ac loss per cycle, as function of the applied current. Trends are highlighted with dashed lines
Chart: AC loss / Cycle
| 1E-3 | 0.01 | 0.1 | 1 | 10 | 100
I/Ic=10% | 2.3048e-05 | 1.8532e-05 | 1.4914e-05 | 1.2047e-05 | 9.669e-06 | 7.8387e-06
I/Ic=50% | 0.013402 | 0.010154 | 0.0078172 | 0.0060806 | 0.0047594 | 0.0037509 | 0 | 0 | 0 | 0
I/Ic=75% | 0.10953 | 0.065904 | 0.045621 | 0.033349 | 0.025099 | 0.019222 | 0 | 0 | 0
 Consistent with previous research

## Slide 34: Magnetic field dynamics in superconductors
Type I: Meißner Effect
Thermodynamical state, reversible
London equation
  , if
Type II: Abrikosov fluxons
Flux pinning and motion, irreversible
Power-law (phenomenological)
Faraday Law (eddy currents)
Bc1
Bc2
Tc
B
T
Type I
Type II
B-T Diagram

## Slide 35: Formulation - Mixed potentials
formulation, weak form:
Ampere-Maxwell Law
Faraday Law
Constraint on transport current
reluctance
current
resistance
flux
voltage
Advantages
finite conditon number
magnetostatic problem
Drawback
Weak form to be implemented

## Slide 36: High-Temperature Superconductors
Cuprate compounds (CuO2) doped with rare earth elements (La, Bi-Sr-Ca, Y-Ga-Ba …)
Higher Tc and Bc0 respect to the traditional LTS competitors
Higher performance comes with higher prices!
.. But in the early 2000s it was
Chart: J_eng(T) @ 5T
Chart: J_eng(B) @ 1.9K
ReBCO | 5.7212 | 5.6242 | 5.5183 | 5.4139 | 5.3111 | 5.2099 | 5.1102 | 5.0121 | 4.9154 | 4.8203 | 4.7266 | 4.6344 | 4.5437 | 4.4544 | 4.3665 | 4.2799 | 4.1948 | 4.111 | 4.0286 | 3.9475 | 3.8677 | 3.7892 | 3.712 | 3.636 | 3.5613 | 3.4878 | 3.4156 | 3.3445 | 3.2746 | 3.2059 | 3.1384 | 3.072 | 3.0067 | 2.9426 | 2.8795 | 2.8176 | 2.7567 | 2.6968 | 2.638 | 2.5803 | 2.5235 | 2.4678 | 2.413 | 2.3593 | 2.3064 | 2.2546 | 2.2036 | 2.1536 | 2.1045 | 2.0564

## Slide 37: Tapes and Cables
Tapes
ReBCO - Rare Earth Barium Copper Oxide tape
Batches of and beyond
Cost driven by production process
Features
Multi-layer, multi material
Aspect ratio ~ (tape), ~ (HTS layer)
HTS as anisotropic, nonlinear mono-filament
AC losses: eddy currents
Cables
Roebel geometry (1912)
“Coil-able”, bended on the long edge
Fully transposed: even current distribution
Aligned-coil concept against AC losses
■ Copper ■ ReBCO ■Substrate
Source: CDS. Coiled Roebel cable (Henry Barnard, CERN).

## Slide 38: Formulation - PEC Limit Behavior
[1] Knoepfel, Heinz E. Magnetic fields: a comprehensive theoretical treatise for practical use. John Wiley & Sons, 2008.
Chart: AC loss / Cycle
| 1E-3 | 0.01 | 0.1 | 1 | 10 | 100
1.E-5 | 1.6483e-14 | 1.6483e-13 | 1.6501e-12 | 1.6487e-11 | 1.6483e-10 | 1.6499e-09
1.E-10 | 1.6456e-09 | 1.6456e-08 | 1.646e-07 | 1.6465e-06 | 1.6465e-05 | 0.00016502
1.E-15 | 0.00016447 | 0.0016301 | 0.008795 | 0.0028338 | 0.00042808 | 6.245e-05
1.E-20 | 6.2522e-05 | 1.0852e-05 | 2.493e-06 | 5.1255e-07 | 5.8408e-08 | 5.8664e-09
1.E-25 | 5.8666e-09 | 5.8669e-10 | 5.8669e-11 | 5.8669e-12 | 5.867e-13 | 5.867e-14
Chart: m(B) - normalized

## Slide 39: Field multipoles without eddy currents
Staircase Scenario at 4.5 K
“Eddy” considers the HTS tape dynamics
“No Eddy” assumes a homogeneous current density in the tapes
Chart: B1
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 0.16682 | 0.33069 | 0.6035 | 0.87668 | 1.15 | 1.422 | 1.6339 | 1.7861 | 1.9218 | 2.0439 | 2.1607 | 2.2749 | 2.3876 | 2.4621 | 2.389 | 2.2779 | 2.1649 | 2.0486 | 1.9265 | 1.7905 | 1.6379 | 1.4253 | 1.1523 | 0.87777 | 0.60397 | 0.33096 | 0.16715
eddy | 0.14269 | 0.27979 | 0.41689 | 0.55398 | 0.69107 | 0.82813 | 0.96518 | 1.1022 | 1.239 | 1.3749 | 1.5087 | 1.64 | 1.7668 | 1.8835 | 1.9875 | 2.0861 | 2.1821 | 2.2769 | 2.3713 | 2.4653 | 2.3743 | 2.2821 | 2.1887 | 2.0933 | 1.9948 | 1.89 | 1.772 | 1.6444 | 1.5126 | 1.3783 | 1.2419 | 1.1047 | 0.96738 | 0.83003 | 0.69266 | 0.55528 | 0.41791 | 0.28051 | 0.1431
no eddy | 0.054817 | 0.13704 | 0.27407 | 0.41109 | 0.5481 | 0.68511 | 0.82211 | 0.9591 | 1.096 | 1.2328 | 1.3687 | 1.5025 | 1.634 | 1.7613 | 1.8792 | 1.9862 | 2.0883 | 2.1878 | 2.2858 | 2.3828 | 2.4789 | 2.3828 | 2.2858 | 2.1878 | 2.0883 | 1.9862 | 1.8792 | 1.7613 | 1.634 | 1.5025 | 1.3687 | 1.2328 | 1.096 | 0.9591 | 0.82211 | 0.68511 | 0.5481 | 0.41109 | 0.27407 | 0.13704 | 0.054817
Chart: b3
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 396.176 | 287.8211 | 239.1869 | 222.0029 | 214.3159 | 212.4014 | 214.2419 | 219.2723 | 220.9041 | 215.385 | 205.7201 | 194.2002 | 182.0771 | 174 | 174.1 | 192.395 | 202.9659 | 211.8436 | 217.1225 | 215.7858 | 211.6595 | 211.3379 | 215.8072 | 227.1275 | 246.8658 | 296.6789 | 403.7129
eddy | 208.7441 | 182.8188 | 173.9306 | 169.432 | 166.7044 | 164.7608 | 163.2491 | 162.2379 | 161.8604 | 162.2516 | 163.1606 | 165.6545 | 170.4561 | 174.2853 | 172.0882 | 166.1619 | 158.1509 | 149.1862 | 139.7017 | 130.0044 | 138.278 | 146.6228 | 154.7428 | 162.3052 | 168.1661 | 170.5539 | 167.1716 | 163.4738 | 161.949 | 161.8093 | 162.0165 | 162.8702 | 164.1695 | 165.9088 | 168.3242 | 171.873 | 177.3644 | 188.0321 | 218.8501
no eddy | 193.3873 | 193.3767 | 193.3664 | 193.3567 | 193.3477 | 193.3465 | 193.3603 | 193.4304 | 193.8276 | 194.5772 | 195.2913 | 197.1637 | 200.3971 | 200.8202 | 194.2371 | 183.9559 | 171.9312 | 159.3324 | 146.6693 | 134.1758 | 146.6693 | 159.3324 | 171.9312 | 183.9559 | 194.2371 | 200.8203 | 200.3971 | 197.1637 | 195.2913 | 194.5772 | 193.8276 | 193.4304 | 193.3603 | 193.3465 | 193.3477 | 193.3567 | 193.3664 | 193.3767 | 193.3873
Chart: b5
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 68.7505 | 45.678 | 35.0365 | 30.9446 | 28.6503 | 26.5144 | 24.1974 | 21.2663 | 17.5851 | 14.6967 | 12.8643 | 11.7389 | 11.0782 | 10.84 | 11.088 | 11.6944 | 12.6825 | 14.4331 | 17.2236 | 20.9468 | 23.9186 | 26.3363 | 28.7482 | 31.4138 | 35.6783 | 46.2221 | 69.108
eddy | 50.0348 | 31.0474 | 24.5565 | 21.2737 | 19.2818 | 17.9156 | 16.899 | 16.131 | 15.4606 | 14.7093 | 13.8704 | 12.7436 | 10.9246 | 8.3058 | 6.1501 | 4.791 | 4.0286 | 3.6225 | 3.4948 | 3.5618 | 3.7663 | 4.0605 | 4.5547 | 5.3929 | 6.8418 | 9.1112 | 11.8371 | 13.7811 | 15.0529 | 16.0453 | 16.9144 | 17.6775 | 18.5107 | 19.5974 | 21.118 | 23.3724 | 27.0275 | 34.2361 | 55.1732
no eddy | 22.7371 | 22.734 | 22.7314 | 22.7294 | 22.7278 | 22.7245 | 22.7157 | 22.688 | 22.5636 | 22.1793 | 21.517 | 20.3725 | 18.3529 | 15.5322 | 13.1939 | 11.6699 | 10.7556 | 10.1882 | 9.8361 | 9.6363 | 9.8361 | 10.1882 | 10.7556 | 11.6699 | 13.1939 | 15.5322 | 18.3529 | 20.3725 | 21.517 | 22.1793 | 22.5636 | 22.688 | 22.7157 | 22.7245 | 22.7278 | 22.7294 | 22.7314 | 22.734 | 22.7371
Chart: b7
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 3.7792 | 2.3458 | 1.6227 | 1.2263 | 0.86529 | 0.56157 | 0.37796 | 0.35561 | 0.70747 | 1.1489 | 1.4986 | 1.7397 | 1.9484 | 2.074 | 1.9658 | 1.7814 | 1.514 | 1.1556 | 0.69635 | 0.34529 | 0.34038 | 0.45991 | 0.69695 | 1.0219 | 1.3776 | 2.0558 | 3.502
eddy | 10.2157 | 4.0881 | 1.9953 | 0.93811 | 0.29826 | 0.13139 | 0.43937 | 0.66833 | 0.85194 | 0.98077 | 1.0502 | 1.1015 | 1.0824 | 0.82466 | 0.41796 | 0.066984 | 0.19912 | 0.42263 | 0.62965 | 0.83389 | 0.71831 | 0.57067 | 0.39804 | 0.18083 | 0.12179 | 0.48111 | 0.67519 | 0.63637 | 0.54604 | 0.441 | 0.28172 | 0.076793 | 0.16688 | 0.49128 | 0.95067 | 1.6374 | 2.782 | 5.0634 | 11.7085
no eddy | 0.04484 | 0.044284 | 0.043799 | 0.043385 | 0.043048 | 0.04272 | 0.042082 | 0.041727 | 0.043914 | 0.022804 | 0.025391 | 0.067504 | 0.17534 | 0.53307 | 1.0218 | 1.4387 | 1.76 | 2.0288 | 2.2657 | 2.4781 | 2.2657 | 2.0288 | 1.76 | 1.4387 | 1.0218 | 0.53306 | 0.17534 | 0.067504 | 0.025391 | 0.022804 | 0.043914 | 0.041727 | 0.042082 | 0.04272 | 0.043048 | 0.043385 | 0.043799 | 0.044284 | 0.04484

## Slide 40: Main Differences
Cable architecture:
LTS – filamentary compound
HTS – multi-layer tape
Resistivity : power law
anisotropic
CERNcourier.com
www.fujikura.co.uk
Tape cross section

## Slide 41: Formulations
Conductivity based:
: magnetic vector potential
  ill-conditioned mass-conductivity matrix ( condition number)
Resistivity based:
: magnetic field strength
  everywhere, unphysical eddy currents , computationally inefficient
-: current vector potential-scalar magnetic potential
  cohomology basis functions for net currents in multiply connected domains
Mixed fields (from literature)
-: magnetic vector potential + magnetic field strength
Developed for 2D rotating machinery. Current driven, no external coupling
-: current vector potential + magnetic vector potential Current driven, no external coupling, suitable only for slabs