## Slide 2: On the magnet mechanics during a quench: Three-Dimensional Finite Element Analysis Of a Quench Heater Protected Magnet
Jose Ferradas University of Geneva & CERN TE-MSC-MDT
Paolo Ferracin CERN TE-MSC-MDT
Carmine Senatore University of Geneva
Giorgio Vallone Lawrence Berkeley National Lab.
09/07/2019
CHATS On Applied Superconductivity 2019
On behalf of a group of amazing experts:
G. Ambrosio, H. Bajas, M. Bajko, L. Bottura, L. Brouwer, B. Castaldo, M. Guinchard, S. Izquierdo Bermudez, J.V. Lorenzo Gomez, F.J. Mangiarotti, J.C. Perez, E. Ravaioli and E. Tapani Taakala

## Slide 3: OUTLINE
1.- Introduction – Quench processes and superconducting magnets
6.- Final conclusions
3.- Finite element modelling for the analysis of the magnet mechanics during a quench
4.- 2D FE Analysis of a quench heater protected magnet
5.- 3D FE Analysis of a quench heater protected magnet
2.- MQXF – The low-β quadrupole for HL-LHC

## Slide 4: OUTLINE
1.- Introduction – Quench processes and superconducting magnets
6.- Final conclusions
3.- Finite element modelling for the analysis of the magnet mechanics during a quench
4.- 2D FE Analysis of a quench heater protected magnet
5.- 3D FE Analysis of a quench heater protected magnet
2.- MQXF – The low-β quadrupole for HL-LHC

## Slide 5: INTRODUCTION
New high-field Nb3Sn accelerator magnets are pushing the boundaries of magnet design and quench protection towards new limits.
Their large stored energy and current densities pose new challenges for the community…
Quench processes and superconducting magnets
Courtesy of L. Bottura
Courtesy of L. Bottura
Scaling of the energy per unit length with the bore field
Maximum magnetic field for state of the art superconducting accelerator magnets

## Slide 6: INTRODUCTION
… but also the electro-mechanical limits of the conductor become a parameter of extreme importance.
Quench processes and superconducting magnets
Thermo-mechanical stresses
Quench
Risk of magnet damage / conductor degradation
The study of quench processes and their intrinsic mechanics becomes essential!
We need tools capable of predicting the mechanical response of the magnet during a quench
Digression on thermal stresses: Thermal buckling in railway tracks
Source: [Business Insider]
Courtesy of L. Bottura

## Slide 7: INTRODUCTION
At the same time one cannot forget that the accurate simulation of quench transients is a real multiphysics effort:
- Electromagnetic study ~ Safe voltage levels
- Thermal analysis ~ Safe temperature level
- Mechanical analysis ~ Safe stress levels
Quench processes and superconducting magnets
This is the result of a chain of events triggered by a quench in an LHC bus-bar
Courtesy of Marta Bajko
Damage in HL-LHC coil as a result of an electrical fault
Courtesy of Paolo Ferracin
This is the result of a quench in the pre series magnet during its qualification test
Courtesy of Marta Bajko

## Slide 8: INTRODUCTION
Perform the 2D and 3D analysis of the magnet mechanics during a quench in relevant operation conditions using ANSYS APDL.
The HL-LHC MQXF Low-β quadrupole magnet, our playground field.
Magnet protected with quench heaters (placed in the outer layer of the coils), quench at nominal current. Characterize the magnet response.
The method should combine the necessary multi-physics models. They will provide the input for the mechanical model.
Main goal of today: Show that the methodology works.
Objective
Mechanical model
Thermal-electric model
Electro-magnetic model
3D MQXF magnet mechanical model
(G. Vallone, 2017)

## Slide 9: OUTLINE
1.- Introduction – Quench processes and superconducting magnets
6.- Final conclusions
3.- Finite element modelling for the analysis of the magnet mechanics during a quench
4.- 2D FE Analysis of a quench heater protected magnet
5.- 3D FE Analysis of a quench heater protected magnet
2.- MQXF – The low-β quadrupole for HL-LHC

## Slide 10: MQXF
Nominal gradient: 132.6 T/m
Nominal current: 16470 A
Peak field in the conductor at Inom : 11.4 T
Aperture: 150 mm
Magnet outer radius: 630 mm
Stored energy at Inom: 1.17 MJ/m
Fx / Fy (per octant) at Inom = +2.47 / -3.48 MN/m
Fz (Whole magnet) at Inom = 1.17 MN
MQXF Low-β quadrupole magnet
Courtesy of Giorgio Vallone
Mechanical concept: Aluminium shell pre-loaded with bladders.
First time for an accelerator magnet.

## Slide 11: MQXF
Nominal gradient: 132.6 T/m
Nominal current: 16470 A
Peak field in the conductor at Inom : 11.4 T
Aperture: 150 mm
Magnet outer radius: 630 mm
Stored energy at Inom: 1.17 MJ/m
Fx / Fy (per octant) at Inom = +2.47 / -3.48 MN/m
Fz (Whole magnet) at Inom = 1.17 MN
MQXF Low-β quadrupole magnet
Courtesy of Paolo Ferracin
Mechanical concept: Aluminium shell pre-loaded with bladders.
First time for an accelerator magnet.

## Slide 12: OUTLINE
1.- Introduction – Quench processes and superconducting magnets
6.- Final conclusions
3.- Finite element modelling for the analysis of the magnet mechanics during a quench
4.- 2D FE Analysis of a quench heater protected magnet
5.- 3D FE Analysis of a quench heater protected magnet
2.- MQXF – The low-β quadrupole for HL-LHC

## Slide 13: FE QUENCH ANALYSIS
Modelling strategy
3D Thermal-Electric quench simulation
2D/3D Electromagnetic model
Mechanical model
2D/3D ROXIE electromagnetic model
Magnetic field on each conductor

## Slide 14: FE QUENCH ANALYSIS
Modelling strategy
3D Thermal-Electric quench simulation
2D/3D Electromagnetic model
Mechanical model
2D/3D ROXIE electromagnetic model
Magnetic field on each conductor
Main focus of today’s talk

## Slide 15: FE QUENCH ANALYSIS
Modelling strategy
3D Thermal-Electric quench simulation
2D/3D Electromagnetic model
Mechanical model
2D/3D ROXIE electromagnetic model
Magnetic field on each conductor

## Slide 16: FE QUENCH ANALYSIS
3D MQXF Thermal-Electric model
Adiabatic boundary conditions

## Slide 17: FE QUENCH ANALYSIS
ANSYS SOLID278
3-D 8-Node Thermal Solid
8 nodes 3-D space
DOF: TEMP
ANSYS SOLID226
3-D 8-Node Coupled-Field Solid
8 nodes 3-D space
DOF: TEMP, VOLT
From previous episodes (ASC 2018)…
divided in time steps
Solve time step
Compute new I, B & update props.
Critical Surf. Param.
Check each element’s quench status
Non-conductor domains
Conductor

## Slide 18: FE QUENCH ANALYSIS
Magnetic field on each conductor using ROXIE load lines.
LLB [T A-1]
Modelling the full current decay
On the assumption of a quench heater protected magnet without external dump:
Equation solved by the code with a step-by-step method. It provides a piecewise exponential decay for the current.
The model updates RQ and Ld at each time step.
Inter filament Coupling Losses (IFCL) are included in the formulation [1].
Bs: Total field (under the effect of IFCC)
Ba: Applied magnetic
As: Total area of strands
Ac: Total area of the conductor
lf: Filament twist-pitch
ρeff: Effective transv. resistivity
µ0: Magnetic perm. of vaccum
[1] j. Ferradas Troitino et al, “On the magnet mechanics during a quench: 2D Finite element analysis of a quench heater protected magnet” Submitted for publ.

## Slide 19: FE QUENCH ANALYSIS
Model results and validation
The model could be validated using the extensive experimental campaign for MQXFS magnets:
Quench Integral (QI) tests
Simulation results obtained under the explained assumptions.
An “error bar” should be always considered!
QI ~ Less than 10% difference w.r.t. experimental data in all tests

## Slide 20: FE QUENCH ANALYSIS
The model could be validated using the extensive experimental campaign for MQXFS magnets:
Quench Heaters (QH) tests
Simulation results obtained under the explained assumptions.
An “error bar” should be always considered!
Model results and validation
Delay precision ~ Around 1 ms at Inom
Max. discrepancy ~ 14%
Thermal behaviour matched

## Slide 21: FE QUENCH ANALYSIS
Modelling strategy
3D Thermal-Electric quench simulation
2D/3D Electromagnetic model
Mechanical model
2D/3D ROXIE electromagnetic model
Magnetic field on each conductor

## Slide 22: FE QUENCH ANALYSIS
2D & 3D MQXF Mechanical model
PLANE82 – structural 2D quadratic
Surf./Surf. contact elements (CONTA172/TARGE169).
Plane stress assumption, verified against 3D models and measurements.
Exploit the quadrupole symmetry.
Linear elastic material properties.
Coil simulated as a block with smeared properties (isotropic).
Adds:
Half-magnet length, longitudinal symmetry B.C.
Longitudinal loading
*Validation results in the backup slides
Courtesy of Giorgio Vallone

## Slide 23: OUTLINE
1.- Introduction – Quench processes and superconducting magnets
6.- Final conclusions
3.- Finite element modelling for the analysis of the magnet mechanics during a quench
4.- 2D FE Analysis of a quench heater protected magnet
5.- 3D FE Analysis of a quench heater protected magnet
2.- MQXF – The low-β quadrupole for HL-LHC

## Slide 24: 2D MECHANICS OF A QH PROTECTED MAGNET
Case study: Nominal current training quench
15 ms Detection + Validation time example.
  Inner layer pole turn quenched
  (Highest peak field conductor)
Magnet protected with outer layer QH:
  Reference MQXF conductor parameters.
  Results: 34 MIITS → Peak T at the end of disch. = 264 K
Adiabatic estimation of hot spot temp.

## Slide 25: 2D MECHANICS OF A QH PROTECTED MAGNET
2D Mechanical results: Azimuthal stress
Cool-down
Assembly
End of quench discharge
Nominal Operation
96 MPa*
118 MPa*
114 MPa
140 MPa*
Careful interpretation needed!
*Singular corner values
More information in the 3D part
100 MPa

## Slide 26: 2D MECHANICS OF A QH PROTECTED MAGNET
2D Mechanical results: Stress evolution
Peak Von Misses equivalent stress at the end of the discharge ~ 146 MPa
  Stress evolution during quench is important.
VM Eqv.
Radial
Shear
* Not necessary at the same place
OL Midplane
IL Pole

## Slide 27: 2D MECHANICS OF A QH PROTECTED MAGNET
2D Mechanical results: Full nominal characterization
Analysis on the peak stress impact respecting project tolerances:
Results under the coil block assumption
Conductor Parameters: 100< RRR <200
1.0 < Cu2SC < 1.4
Detection + Validation: 10 ms < time < 20 ms
Preload effect: Nom-20 MPa < Nominal preload < Nom+20 MPa
Corner nodes neglected
Delta in hot spot temp. ~ 20 K

## Slide 28: 2D MECHANICS OF A QH PROTECTED MAGNET
Three main conclusions
For our reference case and under the modelling assumptions:
The peak stress during a quench in the coil block is not defined by the hot spot temperature. Rather than that, it is governed by an average/global temperature in the coil: Dissipated energy
In global terms, the parametric study shows that the mechanical response for a quench at nominal current does not change if the design parameters are kept within the established tolerances.
The quench transient adds an additional azimuthal compression of 40 MPa to the pole turn (Compared with the value after cool down).

## Slide 29: OUTLINE
1.- Introduction – Quench processes and superconducting magnets
6.- Final conclusions
3.- Finite element modelling for the analysis of the magnet mechanics during a quench
4.- 2D FE Analysis of a quench heater protected magnet
5.- 3D FE Analysis of a quench heater protected magnet
2.- MQXF – The low-β quadrupole for HL-LHC

## Slide 30: 3D MECHANICS OF A QH PROTECTED MAGNET
Case study: Nominal current training quench
The reference case is simulated in 3D
  ~ 34 MIITS → Peak T at the end of the discharge = 252.5 K
  (Effect of longitudinal heat propagation)

## Slide 31: 3D MECHANICS OF A QH PROTECTED MAGNET
Case study: Nominal current training quench
A closer look to the 3D coil temperature (Insulation not shown)

## Slide 32: 3D MECHANICS OF A QH PROTECTED MAGNET
3D Mechanical results at the end of the discharge
Peak at Straight section = 137 MPa
Peak at coil ends = 154 MPa
AZIMUTHAL STRESS
(Straight section results similar to 2D ~ 140 MPa)
Some areas in the coil ends see a higher stress. Some others see tension.

## Slide 33: 3D MECHANICS OF A QH PROTECTED MAGNET
3D Mechanical results at the end of the discharge
RADIAL STRESS
Peak radial stress below 100 MPa

## Slide 34: 3D MECHANICS OF A QH PROTECTED MAGNET
3D Mechanical results at the end of the discharge
Local peak at Straight section = -71 MPa
LONGITUDINAL STRESS
For reference, after Cool down = +20 MPa
End of the discharge
SPECIAL FOCUS ON HOT SPOT REGION
Needs further study.
Work on-going with mech. model.

## Slide 35: 3D MECHANICS OF A QH PROTECTED MAGNET
3D Mechanical results at the end of the discharge
SHEAR STRESSES
SXY (Cartesian)
SYZ (Cartesian)
SXZ (Cartesian)

## Slide 36: 3D MECHANICS OF A QH PROTECTED MAGNET
Main conclusions and identified next steps
2D and 3D analysis of the quench mechanics give similar values in the straight section when singularities are neglected.
A peak azimuthal stress of 140 MPa appears close to the hot spot as a result of the thermal gradients. All other stresses remain well below that value.
Longitudinal stresses are very important close to the hot spot region. They need further study.
A more detailed analysis is necessary. Currently the 3D mechanical model is being re-checked by CERN and LARP. A new analysis will come soon.
This can be seen as a proof-of-concept right now.

## Slide 37: OUTLINE
1.- Introduction – Quench processes and superconducting magnets
6.- Final conclusions
3.- Finite element modelling for the analysis of the magnet mechanics during a quench
4.- 2D FE Analysis of a quench heater protected magnet
5.- 3D FE Analysis of a quench heater protected magnet
2.- MQXF – The low-β quadrupole for HL-LHC

## Slide 38: CONCLUSIONS
A methodology for the 2D and 3D study of the magnet mechanics during a quench has been presented.
It uses a combination of finite element models in ANSYS APDL with other usual tools used in the magnet community.
The different models have been validated with experimental measurements separately.
The method allows to extract essential information about the magnet behavior during a quench.
The 3D case needs to be further studied. The model is currently being re-checked.
More to come in the following months… stay tuned!

## Slide 40: INTRODUCTION
Many codes available in the community. From lumped elements formulations to Finite Element (FE) models.
Since FE models are our main tool for the simulation of the magnet mechanics during the assembly and operation…
Quench simulation in superconducting magnets
Could we integrate the analysis of the magnet mechanics during quench in these models?
The efforts on using ANSYS APDL to model quench processes started long time ago, now new and more advance techniques are available1
Temp. distribution in a racetrack coil during a quench
(P. Ferracin)
1L. Brower, ANSYS User defined elements for quench simulation
Temp. distribution in a MQXF coil during a quench
(J. Ferradas)
2018
2004

## Slide 41: MQXF
MQXF Low-β quadrupole magnet: Mechanical concept
Bladder Operation / Key Insertion (Azimuthal Loading)
Longitudinal Loading
Pressure vessel welding
Cool-down
Powering

## Slide 42: FE QUENCH ANALYSIS
Model results and validation
Very good agreement along the experimental campaign, both 2D and 3D.
Assembly and magnet powering
Loading
Cool-Down
Pole
Shell

## Slide 43: 2D MECHANICS OF A QH PROTECTED MAGNET
2D Mechanical results: Stress evolution
Peak Von Misses equivalent stress at the end of the discharge ~ 164 MPa
  Stress evolution during quench is important
VM Eqv.
Radial
Shear
* Not necessary at the same place
Most conservative, keeping corner nodes

## Slide 44: 3D MECHANICS OF A QH PROTECTED MAGNET
3D Mechanical results before quench
3D Azim. Stress after Cool-down
2D Azim. Stress after Cool Down
Before quench load step, very similar stress results when comparing 3D to 2D
Less problematic corner nodes
(With corner nodes active 130 MPa*)
118 MPa*
111 MPa
Remember plane stress assumed.