## Slide 1: session V: Electro-thermal modeling
Thermal analysis of AC loss heated Nb3Sn coil samples for the High Luminosity upgrade of the LHC (Kirtana Puthran)
Electro-thermal 1D model of the SIS100 superconducting dipole magnet (Piotr Szwangruber)
PSpice modeling of the inrush and fault currents in a 21 MVA HTS transformer (Paweł Surdacki)
1D and 2D finite-element approaches to extract the resistivity of the superconductor material from pulsed current measurements on HTS (Nicolo Riva)
Analysis of Current Distirbution during Quench in a Pancake coil wound with REBCO Roebel cable (Marco Breschi)
M. Lewandowska, D. Bocian

## Slide 2: session V: Electro-thermal modeling
Thermal analysis of AC loss heated Nb3Sn coil samples for the High Luminosity upgrade of the LHC (Kirtana Puthran)
  experimental setup ready,
  initial measurements and analyses performed,
  „rich” research plan.
    Thermal behaviour of samples at higher heat loads to be measured.
    Exploration/Measurement of thermal conductivity of materials.
    Development of phenomenological model to account for presence of He in solid porous materials.
    Modelling directional thermal conductivity of materials, especially SC and insulating.
    Refinement of Kapitza resistance boundary condition.
    Speeding up simulation time?

## Slide 3: session V: Electro-thermal modeling
Electro-thermal 1D model of the SIS100 superconducting dipole magnet (Piotr Szwangruber)
  New Finite Difference Method quench calculation software was developed
    unconditionally stable implicit scheme
    innovative adaptive time stepping algorithm
    flexible topology of the coil supply and protection circuit (option: Rd, cold by-pass, etc.)
    yoke’s magnetic characteristics taken into account in the inductance function
    options: 3D for potted coils, cooling by He bath, heaters
  Simulation results are in good agreement with available measurements
  Plans
    commercial MATLAB → Python (OOP, classes, scalability)
    upgrade of the electrical model (warm cables, line capacitance, de-centralised?, etc.)
    SIS100 transient effects study
    user friendly Graphical User Interface (GUI)
    Nuclotron-type cable: development of a 3D thermal model (force-flow cooling), implementation of cylindrical coordinate system

## Slide 4: session V: Electro-thermal modeling
PSpice modeling of the inrush and fault currents in a 21 MVA HTS transformer (Paweł Surdacki)
The PSpice program allowed for the creation of computer model of highly non-linear electrical component like SC tape.
The results obtained from the computer modelling are in a good agreement with the laboratory measurements of the physical model of the 10 kVA SC transformer.
Electrical circuit simulation seems to be a reliable and fast tool for the simplified analysis of SC devices.
The computer analysis conducted in the PSpice program can be an important verification element of the superconducting transformers’ structure.
The computer model presented in the paper well describes the phenomenon of the inrush current and short-circuit current of SC transformers.
Using the given relations at the transformer design stage, it is possible to predict the maximum values of the inrush current and short-circuit current impulses and the time of decay of this current wave. It can be determined whether the superconducting windings will go to a resistive state, as well as calculate how long this state will last and how much heat will be released in the windings. This allows to calculate the temperature of the windings, and thereby to eliminate the risk of their thermal damage.

## Slide 5: session V: Electro-thermal modeling
1D and 2D finite-element approaches to extract the resistivity of the superconductor material from pulsed current measurements on HTS (Nicolo Riva)
The problems usually arising in the characterization of the flux flow regime, namely excessive heating and interlayer current sharing, have been addressed
We retrieved and preliminary validated the overcritical resistivity curves
We developed and successfully used a 1D Finite Volume thermal model to reduce the computational efforts
We addressed the problem due to a lack of knowledge of material properties (in particular Silver)
Further pulsed measurements on HTScc samples (external magnetic field and different temperatures)
Further improvement of the 1D Finite Volume model (accuracy and computation time)
Application of the 1D FV to an extended sensitivity analysis and implementation in LabView
Development of model in relevant scenarios to compare with constitutive laws
How the overcritical current curves we measured impact HTS devices?
Plans:

## Slide 6: session V: Electro-thermal modeling
Analysis of Current Distirbution during Quench in a Pancake coil wound with REBCO Roebel cable (Marco Breschi)
Based on a homogenization procedure, and a single 1D mesh, the electro-thermal model is able to describe consistently the heat and current redistribution between tapes during quench.
An electro-thermal model for the analysis of quench in Roebel cable is applied to study a 7 turns pancake wound with of a 2 m long cable made of 15 strands.
Given the reduced dimensionality of this 1D (quasi-2D) approach, the computational burden is reduced relative to 2D or 3D models, still retaining a good description of the main physical phenomena
The computed voltages and temperatures are in good agreement with the experimental results; the heat exchange in transverse direction across the cable and from turn to turn can be described
The current redistributes along the whole coil length due to the terminal contact resistances. The heater disturbance determines a redistribution current of about 8.0 kA/m2 mainly located in a 0.3 m long region around the heater.
The impact of the heater power pulse on quench energy was analyzed. The conduction seems the dominant mechanism in the cooling of the heated region. At low values of the heater power, the QE of the coil increases since the liquid nitrogen bath has more impact on the cooling balance.