## Slide 1: Review of collimator Vacuum Performance International review of the HL-LHC collimation system 11th – 12th February 2019
Giuseppe Bregliozzi
TE-VSC

## Slide 2: Outline
LHC Room temperature vacuum acceptance requirements
  Overview of collimators acceptance test: From LHC installation phase to present-day
New MoGr based collimators
  Production process optimization
  Series vacuum validation
  New vacuum acceptance criteria & simulations
Molybdenum coating optimization
Summary & Conclusion
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019

## Slide 3: Vacuum Requirements for Collimators
Materials used in the collimators:
    All materials shall be qualified regarding their outgassing: < 10-12 mbar∙l/s∙cm2
    All trapped volumes shall be avoided as well as contact between large surfaces: Insert outgassing channels
From EDMS 428155
Pumping Speed:
    Effective pumping speed is limited at 20 l∙s by the space available or the conductance of the surrounding vacuum chambers
    In order to be able to achieve the required static pressure of 5∙10-9 mbar the total flux of the collimator should not exceed ≈ 1∙10-7 mbar∙l/s
“As an indication, the allowed outgassing flux of the secondary collimator (based on the existing draft design) will be exceeded if assuming an operating temperature below 50C and 200 cm2 of graphite jaws with a local overheating (50C < T < 100C)”
“Any deviation from this total outgassing flux or from the operating temperature,….,imply an additional pumping speed to ensure the required gas density profile and the vacuum stability”
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019

## Slide 4: Vacuum Requirements for Collimators Accepted Gases Species
H2
CH4
CO
CO2
    Maximum total outgassing ≈ 1∙10-7 mbar∙l/s
Affect the saturation level of NEG coating
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
Sign of contaminations

## Slide 5: NEG Alloy: Pumping Mechanism
A NEG material is a metallic alloy that can pump most of the gases present in a vacuum system after thermal dissolution of its native oxide layer (activation process).
Heating in vacuum
Oxide dissolution -> activation
T = Ta
T = RT
Native oxide layer
Reactive metallic surface
T = RT
No pumping
Pumping
NEGs do not pump hydrocarbon at room temperature and rare gases.
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019

## Slide 6: NEG Pumping Mechanism
6
H2:
Diffuses into the getter bulk even at room temperature,
Small quantities of H2 do not affect the pumping of other gases. High quantity could induce embrittlement and consequently peel-off of the coating
N2:
No Diffusion in the bulk and the absorption takes place underneath the first monolayer of the surface,
Six adsorption sites to pump a single N2 molecule -> N2 capacity ≈ about 7 times lower than for CO
Do not affect the pumping speed of CO
CO & CO2:
Molecules chemically absorbed on the getter surface
No Diffusion in the bulk and affect the pumping speed of all the other gases,
CO capacity ≈ 5·1014 molecules/cm2
O2 & H2O:
The capacity of NEG for O2 and H2O is about 10 times larger than for CO
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019

## Slide 7: A small overview of the outgassing measurements for the collimators From the LHC installation phase to present
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019

## Slide 8: LHC Installation phase: 2007-2009
Averaged outgassing rate of about 160 fully assemblies: Tests performed in Bldg.252
Acceptance limit of 110-7 [mbar∙l/s]
Tolerated limit of 210-7 [mbar∙l/s]
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
At that time an overestimation of the effective pumping speed was done implying an overestimation of the degassing rate
Further improvement of the bake-out cycles and installation
* Degassing rate: Average value

## Slide 9: From LS1 to present-day: Overview
Averaged outgassing rate of about 70 fully assemblies: Performed in Bldg.113 & 867
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
Acceptance limit of 110-7 [mbar∙l/s]
* Degassing rate: Average value

## Slide 10: LS1 to present: Case of TCSPM prototype
Averaged outgassing rate of about 70 fully assembly: Performed in Bldg.113 & 867
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
Acceptance limit of 110-7 [mbar∙l/s]
* Degassing rate: Average value
NEG Cartridges Integration

## Slide 11: Vacuum measurements for the TCSPM & TCPPM with molybdenum carbide-graphite (MoGr) jaws
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019

## Slide 12: Summary of UHV test on MoGr
2016-2018: Single block optimization -> C.Accettura Master degree
  Validation of production process -> Vacuum tests, TDS, FIB, SEM, …
First half of 2018: Not compliant first pre-series
Up to June 2018: Series of test on samples to reassess production cycle
Second half of 2018: Start production and test of each full batch
  Partial revision of acceptance criteria
  Pre-series 2
  Batch 3
  Batch 4
  Batch 4.5 (1 jaw for coating pre-series, test ongoing)
  Batch 5 -> Ongoing
  Batch 6
  …
Second half of 2018: Coating process optimization
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019

## Slide 13: Optimization of the production cycle: Reproducibility
Series of tests were performed to asses a new production cycle: More than 44 blocks.
Total H2 outgassing rate lower than the detection limit of the test bench < 210-10 [mbarl/s];
Total CO2 outgassing rate lower than the detection limit of the test bench < 210-12 [mbarl/s];
High outgassing rate of CH4 is detected on all the different blocks;
Traces of Ar indication of ‘closed’ porosity of the material;
Clear traces of Ne coming from the venting after vacuum firing;
The scans are clean and no traces of heavy masses higher than 50 amu are detected;
The absolute total outgassing of the blocks is very close to the acceptance limit, however, the dominant gases are CH4 and N2, not H2 as usually expected for baked metallic materials.
Production cycle was validated and material outgassing was reproducible and no apparent variations among different batches and pieces were detected

## Slide 14: Estimation of internal air leak rate
Accumulation tests were performed and internal leak rate could be estimated by DP increase over time and/or by an Ar calibrated leak
Ion pump in the system is switched off
Active NEG is still pumping the system -> H2, CO/N2, CO2
All species not pumped by the NEG should increase
On a metallic not porous materials the pressure increase is due to CH4 thermal outgassing
CH4 increase -> As expected
Ne increase -> Neon is used as venting gas after vacuum firing thermal treatments and it fills the porosity present in the materials
Ar -> Constitute 1% of air. Its increase is due to trapped air on pores of the bare material
LHC Acceptance limit: 510-9 mbarl/s
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
Internal air leak needs to be mitigated by the installation of localized remote controlled NEG cartridges

## Slide 15: Summary of UHV test on MoGr
2016-2018: Single block test to optimize -> C.Accettura Master degree
  Production process -> Vacuum tests, TDS, FIB, SEM, …
First half of 2018: Not compliant pre-series
Up to June 2018: Series of test on samples to reassess production cycle
Second half of 2018: Test on each full batch
  Partial revision of acceptance criteria
  Pre-series 2
  Batch 3
  Batch 4
  Batch 4.5 (1 jaw for coating pre-series, test ongoing)
  Batch 5 -> Ongoing
  Batch 6
  …
Second half of 2018: Coating process optimization
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019

## Slide 16: Production batches: Repeatability
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
Date | Batch # | Thermal treatment | Q [mbar*l/s] Qlimit= 5·10-8 | Int. leak [mbar*l/s] Qlimit= 5·10-9
August 2018 | 2 | 72h, 950°C vacuum firing +Ne venting | 4.0·10-8 | 2.0·10-8
October 2018 | 3 | 72h, 950°C vacuum firing +Ne venting | 6.5·10-9 | 4.0·10-9
December 2018 | 4 | 72h, 950°C vacuum firing +Ne venting | 2.0·10-8 | -
Kept under night in Ne atmosphere after vacuum firing
Total outgassing rate below acceptance limits;
Hydrogen outgassing lower with respect to the detection limits;
CH4 and internal leak outgassing rates dominants;
Clear presence of Ne coming from the venting after vacuum firing.
Total of 59 blocks

## Slide 17: Partial revision of the acceptance criteria
Difficult to apply ‘standard’ acceptance criteria due to the undetectable H2 level: Not possible to normalised to H2 content.
The material is considered non conform due to the high level of internal air leak
Simulations are used to analyse the impact of:
  Total CH4 outgassing rate -> Inelastic nuclear ionization cross section
  Internal leak rate -> Possible remedies by the installation of NEG cartridges
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019

## Slide 18: Vacuum simulation: Pressure distribution
Example of vacuum sector A5L7
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
2 x TCSG
Inelastic nuclear cross-section for a specific atom at rest with an LHC beam proton.

## Slide 19: Total impact of CH4 outgassing
Example of vacuum sector A5L7
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
2 x TCSG
Inelastic nuclear cross-section for a specific atom at rest with an LHC beam proton.
1 TCSPM
1 x TCSG
CH4 outgassing is within the limit
Limit for H2 gas density for a 100h beam lifetime
9.810+14

## Slide 20: Total impact of internal air leak: NEG saturation
Air leak 210-8 [mbarl/s]
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
NEG saturation evolution uncontrolled

## Slide 21: Mitigation of internal leak: NEG cartridge installation
Example of vacuum sector A5L7
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
NEG saturation under control
1 TCSPM
1 x TCSG

## Slide 22: Final Summary: Uncoated MoGr
CH4 impact on the total outgassing rate:
  The impact of CH4 molecules considering the inelastic nuclear cross-section is about factor 5 and within the acceptance limits.
High internal air leak rate:
  The measured internal leak rate would saturate 3m on NEG-coated beam pipe in less than a months inducing a further pressure increase: dominated by N2;
  The use of NEG cartridges allows to keep N2 level under control and within the acceptance limits;
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
Can we accept higher outgassing rate?
What’s the impact on the machine performance?

## Slide 23: LSS7 MD4828: Vacuum bump
Motivation: Testing the effect of pressure bumps in LSS7 on beam losses and beam lifetime. This test could allow reviewing the vacuum specifications for new equipment in the LSS7 (Just in the LSS7) and could be of input for the future collimator production.
Principle: Heating up all NEG getters cartridges in both lines of vacuum sector A5L7 (about 20 m in length). 100% of H2 is released up to a maximum pressure of about 110-6 mbar.
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
300 BCMs Bunches
Increase of bunch intensity losses  0.05%

## Slide 24: Pressure profile simulation: H2 gas density
Localized H2 outgassing rate of  6 x 510-5 mbarl/s
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
No important impact on beam lifetime and beam losses
At the limits of embrittlement for the NEG coating!
It is clear that in LSS7 we could have the margin to increase the vacuum acceptance criteria
However, the total H2 outgassing rate and equivalent CH4 and N2 should be carefully analyzed.
3 order of magnitudes than the acceptance criteria

## Slide 25
Reminder: IP4 gas injection
Gas injection in IP4 for fluorescence studies
Pressure was increased to ~4E-7 mbar of Neon (~4 times higher than what in the BGVs)
Losses on TCTPH.4L5.B1 slowly rising up over minutes, which eventually led to dump at ~5 TeV
Friday @2:35pm

## Slide 26: Summary of UHV test on MoGr
2016-2018: Single block test to optimize -> C.Accettura Master degree
  Production process -> Vacuum tests, TDS, FIB, SEM, …
First half of 2018: Not compliant pre-series
Up to June 2018: Series of test on samples to reassess production cycle
  Revision of acceptance criteria
Second half of 2018: Test on each full batch
  Pre-series 2
  Batch 3
  Batch 4
  Batch 4.5 (1 jaw for coating pre-series, test ongoing)
  Batch 5 -> Ongoing
  Batch 6
  …
Second half of 2018: Coating process optimization
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019

## Slide 27: Coating producer evaluation
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
 | Surface + Thermal treatment | Q [mbar*l/s] | Int. leak [mbar*l/s]
Uncoated samples | US+72h, 950°C vacuum firing +Ne venting | 2.0·10-8 | 2.0·10-8
CERN Coating | US+72h, 950°C vacuum firing +Ne venting | 1.0·10-7 | 4.0·10-8
DTI Coating | US+72h, 950°C vacuum firing +Ne venting | 5.0·10-8 | 2.0·10-8
Polytechnic Coating | US+72h, 950°C vacuum firing +Ne venting | 1.0·10-7 | 3.0·10-8
Company | Technique | Sputtering | Venting gas
DTI | PVD-HiPIMS | Krypton | No info
Polyteknik | PVD | Argon | No info
CERN | PVD | Krypton | Argon
DTI sample individuated as the best one
Compliant for electrical resistivity and adhesion

## Slide 28: DTI sample
As before coating
 | Q [mbar*l/s] | Int. leak [mbar*l/s]
Uncoated | 2.0·10-8 | 2.0·10-8
DTI Coating | 5.0·10-8 | 2.0·10-8
DTI Coating after 400C thermal treatment | 2.0·10-8 | 2.0·10-8
Total outgassing within acceptance limits after the coating
Thermal treatment at 400°C for 6h and Neon venting overnight
After thermal treatment back to pre-coating values
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
CH4

## Slide 29: Coating validation: Pat-Handy Pull-test
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
Adhesion test: Rupture at 5.2 MPa in the bulk
No delamination between coating and substrate
Poly
DTI
CERN

## Slide 30: Coating validation: bake-out in degraded vacuum
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
Following the 8th HL-LHC collaboration meeting (S.Gilardoni presentation), further investigation in coating adhesion after thermal treatment in a vacuum degraded environment were assessed:
  1st Bake-out: 24h @ 250 ºC with air-leak @ P = 2*10-3 mbar No peel-off observed with cross-hatch scotch test.
  2nd Bake-out: 24h @ 250 ºC with air-leak @ P = 1*10-2 mbar No peel-off observed with cross-hatch scotch test.
The coated block has already undergone 6h @ 400°C thermal treatment.

## Slide 31: Summary & Conclusion (1/2)
Vacuum acceptance tests:
  Since the LHC installation phase, about 230 fully assembled collimators were tested and just a few of them resulted non conform from the vacuum point of view;
  Quality check allows detecting non-conformities during all these years;
For the LS2 collimators upgrade, a close collaboration between WP12 and WP5 allow having overcome problems and better understand this new material for low impedance collimators.
Vacuum simulations & Pressure bump MD
Simulations have shown that a high CH4 outgassing rate is within the acceptance criteria and does not have an impact on beam lifetime;
Pressure bump machine development has shown that we could potentially increase the existing vacuum acceptance criteria in LSS7, but a careful and detailed analysis should be performed to address embrittlement, beam losses, impact on radiation and possible NEG saturation mitigations.
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019

## Slide 32: Summary & Conclusion (2/2)
Molybdenum carbide-graphite bulk material:
The total outgassing rate is close to the acceptance limit 5x10-8 [mbarl/s] when scaled to the whole collimator;
Despite the fact that the total outgassing rate is dominated by methane, the effect on the beam lifetime will be negligible;
The virtual leak rate in some cases is higher than the acceptance threshold by at least a factor of 2: This negative effect could be mitigated by the installation of remote-controlled NEG cartridges.
The Mo coating provided by DTI company complies with our standard of adherence and total outgassing rate
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
At present and from a vacuum requirement point of view, TE-VSC does not see any obstacle to the continuation of the production of such collimators

## Slide 33: Thanks you for your attention
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
Special thanks to the VSC-BVO teams for all the acceptance tests, the VSC-SSC teams for all the CERN coatings, adherence tests and TDS measurements, C.Accettura and F.Carra for some slides, the fruitful discussion and support for the acceptance tests and a better understanding of the materials.

## Slide 34: Coating validation: Focus ion beam imaging
G.Bregliozzi - International review of the HL-LHC collimation system – 11-12/02/2019
Poly
DTI
CERN
Bulk-coating interface: No apparent local defect and significant interface at the interface
Pictures from E. Garcia (MME/MM)