## Slide 1: 6 GHz cavities coating status
CERN-INFN-STFC Agreement N. KE2722/BE/FCC
Regular video meeting, 1st of February 2019

## Slide 2: 6 GHz cavities coating status
Very promising results  4 Nb on Cu flat Q cavities coated

## Slide 3: 6 GHz cavities coating status
Very promising results  4 Nb on Cu flat Q cavities coated
Reproducibility issue  Improvement of the surface quality is mandatory

## Slide 4: Vibro tumbling
Same concept of CBP, but vibration instead of rotation
Already explored at LNL in 2013
  High Removing Rate (around 6 µm/h)

## Slide 5: Vibro tumbling
Same concept of CBP, but vibration instead of rotation
Already explored at LNL in 2013
  High Removing Rate (around 6 µm/h)
  Unstable system
  Low reproducibility
  Abbandoned technology

## Slide 6: New LNL 6 GHz vibro tumbling
Eccentric motor (vibration)
Unbalanced mass motor

## Slide 7: New LNL 6 GHz vibro tumbling
Eccentric motor (vibration)
Steel wire rope shock absorber

## Slide 8: New LNL 6 GHz vibro tumbling
Eccentric motor (vibration)
Steel wire rope shock absorber
Self aligning bearing

## Slide 9: New LNL 6 GHz vibro tumbling
6 GHz cavity
Eccentric motor (vibration)
Steel wire rope shock absorber
Self aligning bearing
Test cavity
Coupons

## Slide 10: New LNL 6 GHz vibro tumbling
6 GHz cavity
Eccentric motor (vibration)
Step motor (rotation)
Steel wire rope shock absorber
Self aligning bearing

## Slide 11: New LNL 6 GHz vibro tumbling
6 GHz cavity
Eccentric motor (vibration)
Step motor (rotation)
Inverter
Steel wire rope shock absorber
Self aligning bearing

## Slide 12: Vibro tumbling in action
Vibration
Rotation

## Slide 13: Vibro tumbling parameters
Media
Volume
Frequency
Time
Temperature

## Slide 14: Media explored on Cu cavities
BIG SIZE MEDIA
Allumina cones embedded in ureic resin  high RR
Stainless steel  high RR but contaminate and bend cavity
SiC  powder produced block the RR
ScotchBrite  low RR
Teflon balls  remove contaminants, but embedded in surface
POWDERS
Al2O3  no effect
Si(am.) and Si(crys.)  no effect
Al  no effect
B4C  no effect
ZrO2  no effect

## Slide 15: Cu working protocol (3 steps)
Al2O3 Piramids (Rosler RKG 6 PQ) + Rodastel30 (wet process)
Cu powder 200 mesh (dry process)
Coconut powder (dry process)

## Slide 16: Cu working protocol (3 steps) – Removing Rates
Al2O3 Pyramids (Rosler RKG 6 PQ) + Rodastel30 (wet process)
High RR  ≈ 5 μm/h
Cu powder 200 mesh (dry process)
Polishing effect (remain powders on the surface)  ≈ 0,1 μm/h
Coconut powder (dry process)
Polishing effect (Cu powders removal effect)  ≈ 0,3 μm/h

## Slide 17: Cu working protocol (3 steps) – Treatments time
Al2O3 Pyramids (Rosler RKG 6 PQ) + Rodastel30 (wet process)
> 2 h  foam production reduce RR and corrosion start (presence of H3PO4)
Cu powder 200 mesh (dry process)
> 2 hours  pitting starts (Why?)
Coconut powder (dry process)
2 hours

## Slide 18: Volume of media
Influence surface quality and RR
Very important on Cu powders step
Chart: VB with Cu powders
| 65 | 75 | 80 | 90 | 100
 | 0.00375 | 0.016667 | 0.0192 | 0.0073333 | 0

## Slide 19: Temperature
Step 1 and 3 work at room temperature
Step 2 produce heating of the cavity  could be use to monitorize the polishing effect
Chart: VB with Cu powders
| 65 | 75 | 80 | 90 | 100
 | 0.00375 | 0.016667 | 0.0192 | 0.0073333 | 0
overheating up to 90 ºC
~ 30 ºC
~ 50 ºC

## Slide 20: Frequency effect
  Not fully explore yet
  Qualitative speaking, RR increase with frequency
  High and low frequency may damage the vibrotumbling system
  A good compromise is 200 Hz

## Slide 21: Results on Coupons
Test cavity with 2 coupons
Comparision with grinding polishing
Roughness characterizations

## Slide 22: Vibro-Tumbling – Grinding comparision
Scratched
500 ± 60 nm
Ra

## Slide 23: Vibro-Tumbling – Grinding comparision
Grinding
Scratched
550 ± 60 nm
500 ± 60 nm
Ra

## Slide 24: Vibro-Tumbling – Grinding comparision
Grinding
Scratched
SUBU5
240 ± 60 nm
550 ± 60 nm
500 ± 60 nm
Ra

## Slide 25: Vibro-Tumbling – Grinding comparision
Grinding
Scratched
SUBU5
VT Pyramids
VT Cu powders
VT Coconuts
240 ± 60 nm
290 ± 30 nm
380 ± 20 nm
520 ± 30 nm
550 ± 60 nm
500 ± 60 nm
Ra

## Slide 26: Vibro-Tumbling – Grinding comparision
Grinding
Scratched
SUBU5
VT Pyramids
VT Cu powders
VT Coconuts
SUBU5
100 ± 10 nm
240 ± 60 nm
290 ± 30 nm
380 ± 20 nm
520 ± 30 nm
550 ± 60 nm
500 ± 60 nm
Ra

## Slide 27: Vibro-Tumbling – Grinding comparision
Grinding
Scratched
SUBU5
VT Pyramids
VT Pyramids
VT Cu powders
SUBU5
VT Coconuts
VT Cu powders
VT Coconuts
SUBU5
100 ± 10 nm
220 ± 30 nm
240 ± 60 nm
330 ± 20 nm
400 ± 20 nm
510 ± 20 nm
290 ± 30 nm
380 ± 20 nm
520 ± 30 nm
550 ± 60 nm
500 ± 60 nm
Ra

## Slide 28: Vibro-Tumbling – Grinding comparision
Grinding
Scratched
SUBU5
VT Pyramids
VT Pyramids
VT Cu powders
SUBU5
VT Coconuts
VT Cu powders
VT Coconuts
SUBU5
100 ± 10 nm
220 ± 30 nm
240 ± 60 nm
330 ± 20 nm
400 ± 20 nm
510 ± 20 nm
290 ± 30 nm
380 ± 20 nm
520 ± 30 nm
550 ± 60 nm
500 ± 60 nm
Ra

## Slide 29: Results on cavities
Results on cavities
Comparision with grinding on cavities

## Slide 30: Cavity #31
GRINDING
VT – PYRAMIDS (4 h)
VT – Cu Powders (2 h)
VT – Coconut (2 h)
CUT OFF
IRIS
CELL

## Slide 31: Cavity #28 Maize instead of Copper powders
GRINDING
VT – PYRAMIDS (4 h)
VT – Maise (2 h)
VT – Coconut (2 h)
CUT OFF
IRIS
CELL

## Slide 32: Conclusions and next steps
Vibro-tumbling improve the surface finishing compare to grinding with Removing Rates comparable to CBP
RF tests to test improvement in performance reproducibility
Scalable to 1,5 – 1,3 GHz

## Slide 33: Thank you for the attention!