## Slide 1: Evaluation the first SOI pixel detector with 3D integration technology
15 Dec 2019
T. Tsuboyama (KEK)
for the SOIPIX collaboration

## Slide 2
Motivation for the 3D integration in pixel sensors.
3D integration technologies
Micro bump bonding for the SOI pixel sensor
Summary

## Slide 3
In HSTD12 (2018) we presented the plan for the 3D stacking of the SOI pixel sensor.
Various improvement of technology were performed.
The first chip was delivered in July 2019.
The results, including the response to charged tracks will be reported in this presentation.

## Slide 4: Overview of 3D stacking
Belle2
  In the present and future high luminosity collider experiments, the high signal rate and background environment is anticipated.
  Detection efficiency of sensors should not be degraded.
  Occupancy reduction is essential for the design of the pixel vertex detector.
  Reduction of occupancy with time resolution is quite beneficial.
ATLAS
Time resolution

## Slide 5: Integration of additional readout chip
For the commercial image sensors, the first trial was to move the peripheral circuits to the second chip and stacked by using TSV, through silicon via.
This is not an answer for HEP. We have to increase the performance of the circuit in each pixel.
The benefits of pixel-by-pixel connection.
  Parallel data processing.
  Low power operation thanks to minimum parasitic capacitance.
Logic
Memory
Pixel
Logic
Memory
Pixel

## Slide 6: 3D bonding methods
Direct bonding
  Utilize the diffusion bonding of flat and clean surfaces.
  When two surface is attached tightly the molecules can be merged with proper temperature and pressure.
  Metal-metal surface or SiO2 surface can be fused by itself.
  This method is suitable for mass production of image sensors, where, the LSI production, bonding and post processes can be done in one fab.
Micro bump bonding
  Forming bumps made of soft metal (In, Au) on the silicon surface.
  Put the wafers face to face and pressed and heated for the electric connection.
  Low viscosity glue is injected between two chips for mechanical stability.
  Mechanical tolerance is determined by the height of the bumps.
  Suitable for small size production.

## Slide 7: Method-I: Direct Bonding Interconnect
Two wafers are prepared.
The bonding surface is flattened and cleaned.
Aligned and attached. Apply suitable pressure and heat for the diffusion bonding of pads.
SiO2 surfaces is also fused, resulting in the stable structure.
Widely used for the mass production of high-end image sensors.
Slide from Valerio Re, Vertex2018

## Slide 8: Progress of 3D bonding in FNAL
Fermilab led a consortium to demonstrate 3 dimensional electronics – a 4+ year effort.
A working 3D process was demonstrated using 2-tier 3D Global Foundries 0.13 mm TSV wafers. FNAL chips for ILC(VIP), CMS(VICTR) and X-ray imaging (VIPIC) in collaboration with Tezzaron and Ziptronix.
This took about 18 months longer than anticipated – Tezzaron copper bonding issues finally solved by using Ziptronix DBI process
LEFT (bottom)
chips
Right (top)
chips
Slide from R. Lipton Vertex2017

## Slide 9: Method-II: Micro Bump bonding
Metal bumps are formed on the bump pads.
Two chips are aligned and pushed to establish electric connection.
The procedure is close to that of hybrid pixel sensors, however, by using SOI chip, an advanced 3D stacking is enabled.
Si
High R-Si

## Slide 10: Formation of metal micro bumps
The early development was done by using indium bumps.
The bumps were made with photolithographics method
The stacking is performed in Tohoku Microtech (T-micro)
Zycube 2008
m
m
m

## Slide 11: Au cone bumps
Piling up gold nano particles on the under-bump-metal.
Dimensions: 3 in diameter, 3 in height and 6 spacing.

## Slide 12: Formation of gold cone bumps
Pros and cons of the gold cone bump method.
Pros: High efficiency and low resistivity.
Cons: Spraying gold particles takes long time.

## Slide 13: Micro gold cylinder bump bonding
Gold cylindrical bump method is introduced to solve
Process time: Sputtering
Reduction of the contact stress:

## Slide 14: Formation of micro gold cylinders
We collaborate with Tohoku Microtec
Gold cylinders after combined

## Slide 15: Results
Bonding pressure: 0.05 N / bump  0.003 N/bump
Even the silicon – CdTe bonding became possible
The low resistivity is kept
Silicon ROIC
CdTe sensor

## Slide 16: 3D stacking procedure of SOI pixel chip
Si
High R-Si
Si
High R-Si
Si
High R-Si
Lower Chip
Upper Chip
Bump Metal deposition & patterning
Au cylinder Bump formation
Prepare upper and lower chip
Step 1
Step 2

## Slide 17
Si
High R-Si
Si
High R-Si
Lower & Upper Chip alignment
Press and heat for Bonding
Adhesion Glue injection
Step 4
Step 3
High R-Si
Upper silicon removed.
Upper Metal (Bonding pad) deposition & pattering
Step 5

## Slide 18
High R-Si
The stacking can be repeated in the same procedure
Step 6

## Slide 19: 3D design tool
Virtuoso with Special rule files.
Virtual layers are automatically generated between upper and lower chips that unify the chips geometrically and logically.
The DRC (design rule check) and LVS (layout versus schematic) can be applied for the whole pixel system.
MET5 (upper)
PV (upper)： VIA
ZC1 (upper)：Bump
ZC5 (upper)：Bump ID
ZC6 (lower)：Bump ID
ZC1 (lower)：Bump
PV (lower)： VIA
MET5 (lower)
Upper-tier
port
Lower-tier
port
Layout
Upper chip
LVS1
(Virtual connect)
LayoutZ
Lower chip
DRC, LVS
Stacking
Stacking
Unified
DRC＆LVS2
Dummy Gen.
Special VIA Gen.
Special
DRC/LVS rule
DRC, LVS

## Slide 20: SOFIST: A SOI pixel sensor designed for ILC
Preamplifier, comparator, hit charge memories and time-stamp memories are integrated.
For the ~1 ms long bunch train, multiple hits data are stored in each pixel.
The data is read out in the 200 ms interval of ILC beam collision structure.
SOI PIX sensor is already a 3D integrated pixel sensor.

## Slide 21: SOFIST development
 | Ver. 1 | Ver. 2 | Ver. 3 | Ver. 4
Produced /Tested | 2016/2017 | 2017/2018 | 2018/2019 | 2018/2020
Wafer | SOI | DSOI | DSOI | DSOI
Pixel size (mm x mm) | 20x20 | 25x25 | 30x30 | 20x20
Charge memory | 2 | 0 | 3 | 3
Time stamp memory | 0 | 2 | 3 | 3
Chip size (mm x mm) | 3x3 | 4.5x4.5 | 6x6 | 4.5x4.5
Notes | Global shutter. Charge memories | Time memories | Time and charge | 3D integration
Performance of SOFIST Ver.1 was reported in HSTD10

## Slide 22: SOISFT Ver. 3 Beam test data @FNAL
Multiple hits in one sample can be separated with hit-time information in the time-stamp memory.

## Slide 23: SOFIST4: First SOIPIX sensor with 3D stacking
Lower chip Upper chip
Comp
Signal
AGnd
AVdd
AGnd
Comp
Signal
AVdd
20 mm
SOFIST Ver. 3
SOFIST Ver. 4

## Slide 24: Performance of SOFIST Ver. 4
Problem in the preamplifier
Bump bonding failure
Preliminary
Response to 90Sr b source
Analog output voltage versus bias voltage of the preamplifier. Extracted pixels whose gain is less than the design.
3 out of 102x102 pixels do not show response.
Connection yield = 99.97 %
(Preliminary)

## Slide 25: Radiation hardness of the 3D glue
70 MeV Proton irradiation to NIEL 5x1014 n-eq/cm2 and TID 0.4 MGy, similar to the environment of the LHC pixel detector.
Visual inspection was done (destructive tests are not allowed). No clacks, bubbles, color changes observed: The glue is enough rad-hard.
Before irradiation Two month after irradiation
3mm

## Slide 26: Advantages of the SOI micro-bump bonding:
Requirement to surface flatness is determined by the height of the cylinders: a few mm tolerance.
The soft cylindrical gold bumps results in high-connection yield.
TSV is not necessary: The through BOX via (TVB) for the back side are produced at the SOI CMOS circuit processes.
The circuit chip has SiO2 layer on both sides: The stacking process can be repeated.
Upper chip: Only CMOS circuit in SiO2 remains.
  The thickness is about 10 mm.
Remaining issues for the 3D stacking:
  Large area sensor
  Thinning of the wafer thickness

## Slide 27: Summary
The 3D stacking is a reasonable solution to improve the performance of pixel sensors.
The direct connection method and bump bonding method are briefly explained.
SOFIST Ver.4, the SOI PIX sensor with micro cylindrical bump showed a high bonding connection yield of 99.97 %.
The glue used for the stacking is radiation hard to NIEL 5x1014 n-eq/cm2 and TID 0.4 MGy.
We are preparing a beam test of the SOFIST Ver.4 chip in this winter.
Remaining issues for the micro bump bonding:
  Stacking of the large area sensors and thinned sensors

## Slide 28: Thank you for your attention.

## Slide 29
a