## Slide 2: Study of SC thin films on substrate
Dorothea Fonnesu TE/CRG-CI

## Slide 3: Contents
EASITrain
SRF cavities at CERN
Thin films for SRF
PhD goals
Tc test stand @Cryolab
Next steps
Conclusions

## Slide 4: EASITrain programme
Pushing the limits of particle colliders
International FCC collaboration
with CERN as host lab to study:
FCC-hh
FCC-ee
HE-LHC
FCC-he
Challenges:
Civil engineering
Stronger magnets
New detectors
Cryocooling power
Higher fields from SRF cavities
Work supported by the European Commission under the Horizon2020 projects EuroCirCol, grant agreement 654305

## Slide 5: EASITrain programme
2
3
4
5
15 ESRs
Materials
Manufacturing
Valorization
Cryogenics
Consortium:
13 beneficiaries
12 partners

## Slide 6: SRF cavities at CERN
M. Karppinen, CERN SRF Workshop 2016
C. Zanoni, Proceedings IPAC 2017
J. A. Rodriguez, CERN SRF Workshop 2016
LHC
4x RF cryomodules (4x elliptical cavities each)
Nb/Cu operated at 4.5 K
8-16 MV/beam
400 MHz
HiLumi
HIE-ISOLDE
Cryolab
M. Arzeo, FCC week 2018
16 crab cavities (2/beam/IP side)
bulk Nb operated at 2 K
3.4 MV/cavity
400 MHz
For R&D purposes (1.8 K):
QPR, bulk Nb, 400-800-1200 MHz
Elliptical, bulk Nb or Nb/Cu, 1.3 GHz
2x RF cryomodules (5x QWR each)
Nb/Cu
6 MV/m
100 MHz

## Slide 7: Thin films for SRF
From bulk Nb to Nb/Cu (since LEP):
Cu is cheaper
Cu has higher thermal conductivity
Q-slope not fully understood
Nb3Sn (A15 compound) on Cu:
Higher Tc
Lower surface resistance
Synthetize A15 crystalline phase
Achieve theoretical Tc on Cu substrate
Manage material stress and treatment
Investigate intermediate layer (Nb, Ta, Al2O3…)
Toward real cavity coatings for future leptonic machine compatible cavities

## Slide 8: Thin films for SRF
From bulk Nb to Nb/Cu (since LEP):
Cu is cheaper
Cu has higher thermal conductivity
Q-slope not fully understood
Nb3Sn (A15 compound) on Cu:
Higher Tc
Lower surface resistance
Synthetize A15 crystalline phase
Achieve theoretical Tc on Cu substrate
Manage material stress and treatment
Investigate intermediate layer (Nb, Ta, Al2O3…)
Toward real cavity coatings for future leptonic machine compatible cavities
G. Rosaz, FCC 2018

## Slide 9: Thin films for SRF
From bulk Nb to Nb/Cu (since LEP):
Cu is cheaper
Cu has higher thermal conductivity
Q-slope not fully understood
Nb3Sn (A15 compound) on Cu:
Higher Tc
Lower surface resistance
Synthetize A15 crystalline phase
Achieve theoretical Tc on Cu substrate
Manage material stress and treatment
Investigate intermediate layer (Nb, Ta, Al2O3…)
Toward real cavity coatings for future leptonic machine compatible cavities
A. M. Valente-Feliciano, FCC 2018
S. Aull

## Slide 10: Thin films for SRF
From bulk Nb to Nb/Cu (since LEP):
Cu is cheaper
Cu has higher thermal conductivity
Q-slope not fully understood
Nb3Sn (A15 compound) on Cu:
Higher Tc
Lower surface resistance
Synthetize A15 crystalline phase
Achieve theoretical Tc on Cu substrate
Manage material stress and treatment
Investigate intermediate layer (Nb, Ta, Al2O3…)
Toward real cavity coatings for future leptonic machine compatible cavities
K. Iliyna-Brunner, FCC 2018

## Slide 11: Thin films for SRF
From bulk Nb to Nb/Cu (since LEP):
Cu is cheaper
Cu has higher thermal conductivity
Q-slope not fully understood
Nb3Sn (A15 compound) on Cu:
Higher Tc
Lower surface resistance
Synthetize A15 crystalline phase
Achieve theoretical Tc on Cu substrate
Manage material stress and treatment
Investigate intermediate layer (Nb, Ta, Al2O3…)
Toward real cavity coatings for future leptonic machine compatible cavities
K. Iliyna-Brunner, FCC 2018

## Slide 12: Thin films for SRF
From bulk Nb to Nb/Cu (since LEP):
Cu is cheaper
Cu has higher thermal conductivity
Q-slope not fully understood
Nb3Sn (A15 compound) on Cu:
Higher Tc
Lower surface resistance
Synthetize A15 crystalline phase
Achieve theoretical Tc on Cu substrate
Manage material stress and treatment (microstructural features)
Investigate intermediate layer (Nb, Ta, Al2O3…)
Toward real cavity coatings for future leptonic machine compatible cavities
K. Iliyna-Brunner, FCC 2018

## Slide 13: Thin films for SRF
From bulk Nb to Nb/Cu (since LEP):
Cu is cheaper
Cu has higher thermal conductivity
Q-slope not fully understood
Nb3Sn (A15 compound) on Cu:
Higher Tc
Lower surface resistance
Synthetize A15 crystalline phase
Achieve theoretical Tc on Cu substrate
Manage material stress and treatment
Investigate intermediate layer (Nb, Ta, Al2O3…)
Toward real cavity coatings for future leptonic machine compatible cavities
K. Iliyna-Brunner, FCC 2018

## Slide 14: PhD goals
D. Fonnesu – CRG FPT Seminar – CERN 13.03.2019
Study of SC thin films on substrate
Investigate thermodynamic parameters of SC thin films on their substrate
  Measurement of critical temperature Tc on small samples
  Measurement of thermal diffusivity on medium size samples at QPR, i.e. in RF environment
  Test of coated real size 1.3 GHz cavity
Numerical simulation of thermal behaviour of SC film on substrate in RF environment, focus on:
  QPR
  film/substrate interface

## Slide 15: Tc test stand @Cryolab
Contactless, inductive measurement of the critical temperature of SC thin films on Cu

## Slide 16: Tc test stand @Cryolab

## Slide 17: Tc test stand @Cryolab
Sensors (re-) calibration
T-range of interest: 8 – 30 K

## Slide 18: Tc test stand @Cryolab
Sensors (re-) calibration
T-range of interest: 8 – 30 K

## Slide 19: Tc test stand @Cryolab
Observation of first transitions

## Slide 20: Tc test stand @Cryolab
Pickup coil response to temperature... ...for no/different samples and drive coil currents
Coils only

## Slide 21: Tc test stand @Cryolab
Pickup coil response to temperature... ...for no/different samples and drive coil currents
Cu substrate

## Slide 22: Tc test stand @Cryolab
Pickup coil response to temperature... ...for no/different samples and drive coil currents
Nb/Cu DCMS 1A
F. Avino TE/VSC-SCC

## Slide 23: Tc test stand @Cryolab
Pickup coil response to temperature... ...for no/different samples and drive coil currents: 3, 5 and 7 mA
D. Fonnesu – CRG FPT Seminar – CERN 13.03.2019
3 mA
5 mA
7 mA

## Slide 24: Tc test stand @Cryolab
Measurement of Tc - bulk Nb, EH 0.15 A, ID = 5 mA, fD = 7 Hz I – acquire signal amplitude transition and temperature
D. Fonnesu – CRG FPT Seminar – CERN 13.03.2019

## Slide 25: Tc test stand @Cryolab
Measurement of Tc - bulk Nb, EH 0.15 A, ID = 5 mA, fD = 7 Hz II.a – fit signal for regular intervals to get amplitude
D. Fonnesu – CRG FPT Seminar – CERN 13.03.2019

## Slide 26: Tc test stand @Cryolab
Measurement of Tc - bulk Nb, EH 0.15 A, ID = 5 mA, fD = 7 Hz II.b – get average temperature for same intervals
D. Fonnesu – CRG FPT Seminar – CERN 13.03.2019

## Slide 27: Tc test stand @Cryolab
Measurement of Tc - bulk Nb, EH 0.15 A, ID = 5 mA, fD = 7 Hz III – plot extracted A against <T> and fit
D. Fonnesu – CRG FPT Seminar – CERN 13.03.2019

## Slide 28: Tc test stand @Cryolab
Measurement of Tc - bulk Nb, EH 0.15 A, ID = 5 mA, fD = 7 Hz III – plot extracted A against <T> and fit
D. Fonnesu – CRG FPT Seminar – CERN 13.03.2019

## Slide 29: Tc test stand @Cryolab – next steps
Measurements:
HiPIMS Nb3Sn/Cu, DCMS Nb/Cu samples ready and available from TE/VSC-SCC (G. Rosaz, F. Avino)
Analysis:
Fit of temperature data
Evaluation of uncertainties
DAQ setup:
Noise reduction (cabling, filtering at amplifier, etc.)
Experimental setup:
Temperature stabilization (G10 chamber, mesh at vapour inlet, etc.)
Automatised system:
PID controller, DAQ GUI
D. Fonnesu – CRG FPT Seminar – CERN 13.03.2019

## Slide 30: PhD – next to next steps
D. Fonnesu – CRG FPT Seminar – CERN 13.03.2019
Study of SC thin films on substrate
Investigate thermodynamic parameters of SC thin films on their substrate
  Measurement of critical temperature Tc on small samples
  Measurement of thermal diffusivity on medium size samples at QPR, i.e. in RF environment
  Test of coated real size 1.3 GHz cavity
Numerical simulation of thermal behaviour of SC film on substrate in RF environment, focus on:
  QPR
  film/substrate interface

## Slide 31: PhD – next to next steps
D. Fonnesu – CRG FPT Seminar – CERN 13.03.2019
Study of SC thin films on substrate
Investigate thermodynamic parameters of SC thin films on their substrate
  Measurement of critical temperature Tc on small samples
  Measurement of thermal diffusivity on medium size samples at QPR, i.e. in RF environment
  Test of coated real size 1.3 GHz cavity
Numerical simulation of thermal behaviour of SC film on substrate in RF environment, focus on:
  QPR
  film/substrate interface

## Slide 32: PhD – next to next steps
D. Fonnesu – CRG FPT Seminar – CERN 13.03.2019
Study of SC thin films on substrate
Investigate thermodynamic parameters of SC thin films on their substrate
  Measurement of critical temperature Tc on small samples
  Measurement of thermal diffusivity on medium size samples at QPR, i.e. in RF environment
  Test of coated real size 1.3 GHz cavity
Numerical simulation of thermal behaviour of SC film on substrate in RF environment, focus on:
  QPR
  film/substrate interface

## Slide 33: Conclusions
EASITrain: familiarised myself with the EU standards and procedures
Requirements for measurement of Tc analysed
Measurement system established and commissioned
DAQ defined – to be now implemented
First diffusivity measurements done at QPR
Data analysis to be done
EASITrain – European Advanced Superconductivity Innovation and Training. This Marie Sklodowska-Curie Action (MSCA) Innovative Training Networks (ITN) has received funding from the European Union’s H2020 Framework Programme under Grant Agreement no. 764879

## Slide 35: Backup
O. Brunner, CERN SRF Workshop 2016

## Slide 36: SRF cavities at CERN - II
FCC study: two phases
High-gradient machine – FCC-ee
High-current machine – FCC-ee/hh
Acceleration efficiency
400-800 MHz
Bulk Nb? Nb/Cu? N cells?
Cavity shape optimization
400 MHz
Nb/Cu? A15/Cu?
Pictures from: O. Brunner, CERN SRF Workshop 2016
Long term R&D programs
EHF
Seamless fabrication
Nb3Sn and other A15 materials