## Slide 1: NEG studies update
Ruta Sirvinskaite

## Slide 2: Outline
Cryogenic test set up
NEG system upgrade
New samples
Experimental procedure
ESD at cryogenic temperatures
Alpha at cryogenic temperatures
Next steps

## Slide 3: Cooling efficiency test
Atmospheric pressure
Maximum power deposition during ESD measurements calculated
Reached 85.6 K without heating and 92.2 K with heater power of 78 W
Silicone heater mat
Thermocouples (K-type and PT100s
Copper chiller
Heat insulation

## Slide 4: NEG system upgrade for cryogenics
Installation of the new sample, bellows and filament on a vacuum system
Sample not activated after bake out
Conditioning of the filament (from 1e-6 mbar at 3 A and 2 V after bake out to 5.1e-10 mbar at 6 V and 7 A after activation at 180 °C and subsequent experiments)

## Slide 5: New samples
Two columnar TiZrV tubes deposited
One sample used for α measurements at RT
Another sample used for experiments at CT
  First test (after bake-out and activation to 180 °C)

## Slide 6: Experimental procedure
Bake out of non-coated parts
Cooling down with ESD
Cooling down with hot filament without ESD
NEG coating activation
ESD at RT for 1-2 hours
ESD as a function of temperature
Start ESD -> start cooling ->bombard as long as possible -> warm up -> turn off ESD
Short H2+CO injection to measure α at RT
Measurements of α at CT
Increase outgassing rate of the filament -> cool down while heating up the filament -> then warm up again (should be done with and without ion pump)

## Slide 7: ESD after bake out
ESD with cooling
Filament was off during bake out (degassing started at 150 °C) and still outgassing a lot after it

## Slide 8: Tests after bake out - ESD

## Slide 9: Sticking probability measurements with a hot filament - CT

## Slide 10: ESD after activation - RT
ESD at RT for 2 hours
Filament switched on during activation
The background was 2 times lower – slight pressure decrease after switching off the filament

## Slide 11: ESD after activation – CT
Bombardment at 89K for about 3 hours
The pressure started going up after and the became stable at 92 K

## Slide 12: ESD after activation

## Slide 13: Sticking probability measurements with hot filament -CT

## Slide 14: Cooling
SIP ON during the cooling

## Slide 15: Warming up
SIP OFF during warming up
Can see methane being released from the surface

## Slide 16: Calculating alpha at CT
If pump is closed,

## Slide 17: ESD results
Desorption yield as a function of electron dose decreased after activation and filament conditioning

## Slide 18: ESD results
Desorption yield as a function of desorbed gas reduced after sample activation and filament conditioning

## Slide 19: Next steps
Detailed data analysis of the results before and after activation to 180 °C
Cryogenics
Activation to 250 °C
Measurements of dense TiZrV sample possible
Zr coating
Completed surface characterisation (cross-section SEM and XPS)

## Slide 20: Thank you for your attention