## Slide 1
Test set-up at KARA:
Status report & next steps
Task4.6: Measurements on cryogenic
beam vacuum system prototype
1
2
3
4
5
L. A. Gonzalez,1
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps

## Slide 2
Irradiation Sawtooth
Irradiation LASE
3rd Prototype at KARA
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
1
PSD
Reflectivity
Heat loads
PSD
Reflectivity
Heat loads

## Slide 3
Re-Position of setup
3rd Prototype at KARA Irradiation of LASE - Reflectivity
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
2

## Slide 4
New irradiation conditions:
Reduction angle of incidence:
On sawtooth Θ = 18 mrad
On LASE Θ < 1 mrad
Reduction of the horizontal slits opening:
Slits aperture @ Sawtooth = 3.44 x Slits Apperture @Lase
Θ < 1 mrad
LASE
Irradiated
Region
3rd Prototype at KARA Irradiation of LASE
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
3

## Slide 5
α = -0.98
α = -0.34
α = -0.54
α = -0.16
3rd Prototype at KARA Irradiation of LASE - PSD
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
4

## Slide 6
PSD of LASE is considerably lower than for sawtooth, as expected due to the photoelectron yield of LASE being considerably lower than for sawtooth.
Plateau at very low doses indicates that LASE surface was not preconditioned during previous sawtooth irradiation. Such observation satisfactorily confirms the very low reflectivity of sawtooth profile.
PSD of Reflector is suspiciously low. Specially taking into account highly reflective rounded tip.
However, cleaning procedures of Proto#1 might have been more efficient than #3
α = -0.98
α = -0.34
α = -0.54
α = -0.16
3rd Prototype at KARA Irradiation of LASE - PSD
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
5

## Slide 7
3rd Prototype at KARA Irradiation of LASE - Reflectivity
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
6

## Slide 8
1
1
2
2
Base Line
First
Prototype
3rd Prototype at KARA Irradiation of LASE - Reflectivity
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
7

## Slide 9
Base Line
First
Prototype
3
3
Reflectivity of the laser ablated surface SEEMS to be higher than the rest.
A few considerations to be taken into account…
3rd Prototype at KARA Irradiation of LASE - Reflectivity
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
8
1
1
2
2

## Slide 10
Difference between experiments
Irradiation Sawtooth and Tip
Irradiation LASE
Angle of Incidence
Θ = 18 mrad
Angle of Incidence
Θ < 1 mrad
LID
NO LID
3rd Prototype at KARA Irradiation of LASE - Reflectivity
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
9

## Slide 11
Still need to explain the disagreement with the experiments carried out at BESSY
A few considerations to be taken into account…
3rd Prototype at KARA Irradiation of LASE - Reflectivity
Experiment at BESSY
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
10
3
1
2

## Slide 12
LASE Measured in BESSY
LASE Measured in BESTEX
Surface morphology of different samples
3rd Prototype at KARA Irradiation of LASE - Reflectivity
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
11

## Slide 13
3rd Prototype at KARA Irradiation of LASE - Reflectivity
The microstructure of LASE is extremely dependent on the laser parameters
The reflectivity is extremely dependent on the microstructure of the surface
LASE Measured in BESSY
LASE Measured in BESTEX
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
12

## Slide 14
Submission of PRAB
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
13

## Slide 15
Future Steps – R&D Proposals
8
Scientific
Continue acquiring dose in current sample at 77K OR Vent the system and repeat the experiment from low doses at 77K
Perform measurements on new samples
-SS with internal coating
Colaminated Cu
Sawtooth profile (Cu)
LASE structure (Cu) – Different LASE’s?
…
-RT and 77K
PSD – Unpublished for T=77K; Ec=4.5KeV
Reflectivity – Manufacturing new samples with a geometry favorable for reflectivity studies (Repeatibility).
Unpublished - Very small gracing angles available.
Photoelectron generation – New electrode design (not cold sprayed) –
Unpublished - Evolution with Dose
Heat loads
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
14

## Slide 16
Technological
Cryogenic Upgrade
-Construction of a LN2 line at KARA for permanent LN2 access at BESTEX. Currently finalizing details to start the purchasing and construction – Implies PLC software upgrade
-Perform measurements at 77 K using a Dewar
Cryogenic test of FCC-hh BS at CERN by using a Dewar
Construction of new samples for BESTEX (Two different options)
Calibration of RGA at CERN
Upgrade of the setup for irradiation without bake out of sample.
  Add Valves and pumps - Implies PLC software upgrade
  Shrink collimator-testbench connector
Documentation of BESTEX
8
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
15
Future Steps – R&D Proposals

## Slide 17
Technological
Cryogenic Upgrade
-Construction of a LN2 line at KARA for permanent LN2 access at BESTEX. Currently finalizing details to start the purchasing and construction – Implies PLC software upgrade
-Perform measurements at 77 K using a Dewar
Cryogenic test of FCC-hh BS at CERN by using a Dewar
Construction of new samples for BESTEX (Two different options)
Calibration of RGA at CERN
Upgrade of the setup for irradiation without bake out of sample.
  Add Valves and pumps - Implies PLC software upgrade
  Shrink collimator-testbench connector
Documentation of BESTEX
8
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
16
Future Steps – R&D Proposals

## Slide 18
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
Fututre steps BESTEX Cryogenic Upgrade
KARA’s LN2 line
17
The flux required for the experiment is
Calculated and KARA can provide it
The pressure of the LN2 is 400 mbar, we
must ensure that the pressure drop in our
system is lower than 400mbar
CryoLab and valve providers claim that
valve must be implemented (welded, same
insulation vacuum) in the line, not flanged.
The valve should be implemented as part of
the LN2 order. (CERN will give detailed
description)
To be discussed with technicians at KARA

## Slide 19
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
The flux required for the experiment is
Calculated and KARA can provide it
The pressure of the LN2 is 400 mbar, we
must ensure that the pressure drop in our
system is lower than 400mbar
CryoLab and valve providers claim that
valve must be implemented (welded, same
insulation vacuum) in the line, not flanged.
The valve should be implemented as part of
the LN2 order. (CERN will give detailed
description)
To be discussed with technicians at KARA
Fututre steps BESTEX Cryogenic Upgrade
KARA’s LN2 line
18

## Slide 20
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
Possibility of drilling holes at KARA’s wall to pass LN2 pipes from Dewar through
It is still to be reviewed how long a Dewar lasts
This option simplifies system and fastens up the cryogenic upgrade
Fututre steps BESTEX Cryogenic Upgrade
LN2 permanently from Dewar
19
KARA’s wall
LN2
Dewar
Holes drilled
at KARA’s wall

## Slide 21
Technological
Cryogenic Upgrade
-Construction of a LN2 line at KARA for permanent LN2 access at BESTEX. Currently finalizing details to start the purchasing and construction – Implies PLC software upgrade
-Perform measurements at 77 K using a Dewar
Cryogenic test of FCC-hh BS at CERN by using a Dewar
Construction of new samples for BESTEX (Two different options)
Calibration of RGA at CERN
Upgrade of the setup for irradiation without bake out of sample.
  Add Valves and pumps - Implies PLC software upgrade
  Shrink collimator-testbench connector
Documentation of BESTEX
Future Steps
8
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
20

## Slide 22
8
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
21
Future steps Construction of new samples
Three Samples:
Tubular SS with coating of inner wall
Sample#1 Co-laminated copper
Sample#2 Co-laminated copper ST
Sample#3 Co-laminated copper LASE
40-45mm
8 mm
LN2
LN2
In
Out
SR
Inner wall coating
Option 1

## Slide 23
8
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
22
Future steps Construction of new samples
Three Samples:
Tubular SS with coating of inner wall
Sample#1 Co-laminated copper
Sample#2 Co-laminated copper ST
Sample#3 Co-laminated copper LASE
2 m long
2 m
40-45mm
8 mm
LN2
LN2
In
Out
SR
Inner wall coating
Option 1

## Slide 24
8
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
23
Future steps Construction of new samples
40-45mm
8 mm
LN2
LN2
In
Out
SR
Inner wall coating
Three Samples:
Tubular SS with coating of inner wall
Sample#1 Co-laminated copper
Sample#2 Co-laminated copper ST
Sample#3 Co-laminated copper LASE
2 m long
Discontinuos welding
No pumping holes
2 m
Option 1

## Slide 25
8
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
24
Future steps Construction of new samples
Three Samples:
Tubular SS with coating of inner wall
Sample#1 Co-laminated copper
Sample#2 Co-laminated copper ST
Sample#3 Co-laminated copper LASE
2 m long
Discontinuos welding
No pumping holes
Chimney connection
-Fixed point
-We plan to modify the geometry to improve
leak tightness while keeping free of thermal
contact
2 m
Chimney
Option 1

## Slide 26
8
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
Future steps Construction of new samples
2 m
Chimney
Three Samples:
Tubular SS with coating of inner wall
Sample#1 Co-laminated copper
Sample#2 Co-laminated copper ST
Sample#3 Co-laminated copper LASE
2 m long
Discontinuos welding
No pumping holes
Chimney connection
-Fixed point
-We plan to modify the geometry to improve
leak tightness while keeping free of thermal
contact
Option 1
25

## Slide 27
8
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
26
Future steps Construction of new samples
Three Samples:
Tubular SS with coating of inner wall
Sample#1 Co-laminated copper
Sample#2 Co-laminated copper ST
Sample#3 Co-laminated copper LASE
2 m long
Discontinuos welding
No pumping holes
Chimney connection
-Fixed point
-We plan to modify the geometry to improve
leak tightness while keeping free of thermal
contact
Photoelectron electrode
+
-
~ 5 mm
~ 50 mm
UHV
Option 1

## Slide 28
8
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
27
Future steps Construction of new samples
Three Samples:
Tubular SS with coating of inner wall
Sample#1 Co-laminated copper
Sample#2 Co-laminated copper ST
Sample#3 Co-laminated copper LASE
2 m long
Discontinuos welding
No pumping holes
Chimney connection
-Fixed point
-We plan to modify the geometry to improve
leak tightness while keeping free of thermal
contact
Photoelectron electrode
+
-
~ 5 mm
~ 50 mm
UHV
Option 1

## Slide 29
8
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
28
Future steps Construction of new samples
Three Samples:
HALF PIPE SS with coating of inner wall
Sample#1 Co-laminated copper
Sample#2 Co-laminated copper ST
Sample#3 Co-laminated copper LASE
2 m long
Fix Sample mechanically (use of Ceramics)
Electrically isolate cooling pipes
Bias the sample and measure Photoelectron Yield
+
-
UHV
Option 2

## Slide 30
9
Future Steps
March | April | May | June | July | Aug | Sept | Oct | Nov | Dec
*Shut Down
Cryogenic Test
CERN-Check availability of cooling sample with Dewar.
1st Cool Down KARA
Installation LN2 line
RGA Calibration and Setup upgrades
Manufacturing 1st new sample, test and assembly
1 month
error
margin
Installation
and
Experiment
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
29

## Slide 31
9
Future Steps
March | April | May | June | July | Aug | Sept | Oct | Nov | Dec
*Shut Down
Cryogenic Test
CERN-Check availability of cooling sample with Dewar.
1st Cool Down KARA
Installation LN2 line
RGA Calibration and Setup upgrades
Manufacturing 1st new sample, test and assembly
1 month
error
margin
Installation
and
Experiment
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
30
If permanent cool down with Dewar is possible, from this moment we would be able to start the experiments as soon as samples are manufactured

## Slide 32
9
More R&D Follow Up Proposals
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
31
Valentin Nistor, et al Applied Surface Science, Volume 315, 2014, Pages 445-453, https://doi.org/10.1016/j.apsusc.2014.05.049.
LASE on Cu
Chemical etching on Ag

## Slide 33
9
More R&D Follow Up Proposals
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
32
Valentin Nistor, et al Applied Surface Science, Volume 315, 2014, Pages 445-453, https://doi.org/10.1016/j.apsusc.2014.05.049.
Chemical etching on Ag

## Slide 34
9
More R&D Follow Up Proposals
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
31
LASE on Cu
Magnetron sputteting on Ag
Magnetron sputteting on Ag - Luis Gonzalez PhD Thesis

## Slide 35
9
More R&D Follow Up Proposals
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
31
LASE on Cu
Magnetron sputteting on Ag
Filter #4
Magnetron sputteting on Ag - Luis Gonzalez PhD Thesis

## Slide 36
Conclusions
BESTEX was reoriented to irradiate the LASE surface.
PSD was found to be lower than for Sawtooth, I agreement with a lower photoelectron yield
Reflectivity measurements in LASE can not be compared with Sawtooth or Reflector
However it was confirmed that in terms of reflectivity, each LASE can behave differently depending on the manufacturing
parameters
PRAB is ready for submission
Two options for the new samples have been presented
Necessary Setup upgrades to be carried out have been presented
  Permanent LN2 line at KARA
  Cool down with Dewar
New scientific plan has been presented
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
33
Pros, contras and availabilities must still be reviewed to decide the most convenient strategy

## Slide 37: Acknowledgments
Thank You
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps
34

## Slide 38
Luis Gonzalez
CERN TE-VSC
ALBA. March 19th 2018
Test set-up at KARA: Status report & next steps