## Slide 1
Modelling of Electrodynamics in HTS Tapes and Coils
Workshop 13-14 June 2019
Lorenzo Bortot(1,2) on behalf of the STEAM team
Acknowledgements: J. Van Nugteren, C. Petrone
cern.ch/STEAM

## Slide 2: …Why HTS?
Circular accelerators for particle physics:
circular orbit
Just for fun
LHC tunnel + HTS dipoles @ 4.2 K, 30 T:
Collision energy of the Future Circular Collider (FCC): ]
… not so far away after all!

## Slide 3: High-Temperature Superconductors
Cuprate compounds (CuO2) doped with rare earth elements (La, Bi-Sr-Ca, Y-Ga-Ba …)
Higher Tc and Bc0 respect to the traditional LTS competitors
Higher performance comes with higher prices!
.. But in the early 2000s it was
Chart: J_eng(T) @ 5T
Chart: J_eng(B) @ 1.9K
ReBCO | 5.7212 | 5.6242 | 5.5183 | 5.4139 | 5.3111 | 5.2099 | 5.1102 | 5.0121 | 4.9154 | 4.8203 | 4.7266 | 4.6344 | 4.5437 | 4.4544 | 4.3665 | 4.2799 | 4.1948 | 4.111 | 4.0286 | 3.9475 | 3.8677 | 3.7892 | 3.712 | 3.636 | 3.5613 | 3.4878 | 3.4156 | 3.3445 | 3.2746 | 3.2059 | 3.1384 | 3.072 | 3.0067 | 2.9426 | 2.8795 | 2.8176 | 2.7567 | 2.6968 | 2.638 | 2.5803 | 2.5235 | 2.4678 | 2.413 | 2.3593 | 2.3064 | 2.2546 | 2.2036 | 2.1536 | 2.1045 | 2.0564

## Slide 4: Main Differences
Cable architecture:
LTS – filamentary compound
HTS – multi-layer tape
Resistivity : power law
anisotropic
CERNcourier.com
www.fujikura.co.uk
Tape cross section

## Slide 5: Outline
Introduction
Motivation
Formulation
Verification Theoretical references
Validation Measurements from Feather2
Summary and Outlook
Feather2 magnet: net magnetic flux density contribution due to screening currents (first quadrant)
B(T)
Notes: From Oberkampf book: […].veriﬁcation can simply be described as “solving the equations right” and validation as “solving the right equations.”

## Slide 6: Introduction: Screening (Eddy) Currents
ReBCO tape in an external magnetic density :
External magnetic field change :
 Persistent screening currents , due to  Persistent magnetization
Large filament size (~5 mm), significant persistent magnetization:
 Relevant for field quality, especially at low field
 Relevant for tape thermal behavior, dominant AC loss contribution
■ Copper ■ ReBCO ■ Substrate
Notes: Brief description of tape and superconducting layer in external field.
Introduction of eddy currents as persisting screening phenomenon. Large filament size  impact on field quality and AC loss

## Slide 7: Motivation
The analysis of future HTS magnets for accelerators needs to take into account the screening currents dynamics
At CERN, there is a need for a code:
Fast and numerically stable
Scalable to accelerator magnets
Capable of accounting for iron
Capable of field-circuit coupling
Validated, reliable (maintainable)
Our contributions
Investigation and extension of a suitable field formulation
Implementation in a proprietary software (*), using the Finite Element Method
Scaling of the implementation to an HTS magnet (Feather2)
(*) COMSOL Multiphysics® v. 5.3. www.comsol.com. Last access: 10/04/2018

## Slide 8: Formulation: Overview
Mixed potentials (*), starting from [1]
solved in (air, iron), where
solved in (conductors), where :
  Finite condition number  Stability
Model order reduction (e.g., [2, 3])
  High aspect ratio
  Tapes as surfaces in (lines in )  Speed-up
[1] Bíró, O. "Edge element formulations of eddy current problems." CMAM 169.3-4 (1999): 391-405.
[2] Carpenter, C. J. "Comparison of alternative formulations of 3-dimensional magnetic-field and eddy-current problems at power frequencies." Proceedings of the Institution of Electrical Engineers. Vol. 124. No. 11. IET Digital Library, 1977.
[3] Zhang, H., et al. "An efficient 3D finite element method model based on the T–A formulation for superconducting coated conductors.“ SuST, 30.2 (2016): 024005.
Domain decomposition
Model order reduction
(*) Paper accepted to COMPUMAG 2019
Notes: Math analysis not yet over
Analysis of stability criteria is ongoing We are aware about previous work in this direction: We do not like it too much since is not clearly described (e.g., gauge, interface) We like to do it more rigorously (with emphasis on field circuit coupling)
Before this work, there was no tools to carry out the field quality analysis

## Slide 9: Formulation: 2D Implementation
solved in
solved in
- link via electric field
Electric field balance in the superconductor
Externally applied
Resistive
Inductive
with
as winding density function [4]
external voltage supply
  Input, if voltage driven model
  Lagrange multiplier, if current driven model
: air
: coil
[4] Schöps, S., et al. "Winding functions in transient magnetoquasistatic field-circuit coupled simulations." COMPEL: The International Journal for Computation and Mathematics in Electrical and Electronic Engineering 32.6 (2013): 2063-2083.
Notes: Practical implementation in a 2D configuration. Electric field balance. Importance of the voltage supply in the power balance

## Slide 10: Outline
Introduction
Motivation
Formulation
Verification Theoretical references
    Critical State (Bean) Model
    Skin Effect
    Field Dependency
Validation
Summary and Outlook
Notes: Some of the verifications. Mention Current dependency, PEC behavior, comparison with other formulations..

## Slide 11: Verification – 1. Critical State (Bean) Model
Scenario: magnetic field diffusion
  ,
Geometry: slab of infinite height, modelled as stack of tapes
Source: boundary field
Reference: Analytical solution, e.g., [5]:
Chart: 
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
 | 0 | 1 | 1 | 0 | 0 | -1 | -1 | 0 | 0
: air
: conductor
Computational domain
Chart: 
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
 | 0 | 1 | 1 | 0 | 0 | -1 | -1 | 0 | 0
Chart: 
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8
 | 0 | 1 | 1 | 0 | 0 | -1 | -1 | 0 | 0
Source term
[5] Russenschuck, S. Field computation for accelerator magnets: analytical and numerical methods for electromagnetic design and optimization. John Wiley & Sons, 2011.

## Slide 12: Verification – 1. Critical State (Bean) Model
Numerical Solution: magnetic field diffusion
Magnetic flux density and normalized current density distribution
Chart: 
Chart: 
Chart: 
Chart: 
Chart: 
Chart: 
Chart: 
Chart: 
B (T)
J/Jc (-)
x (mm)
x (mm)
x (mm)
x (mm)
 Profiles consistent with theory [5]
[5] Russenschuck, S. Field computation for accelerator magnets: analytical and numerical methods for electromagnetic design and optimization. John Wiley & Sons, 2011.

## Slide 13: Verification – 2. Skin Effect
Scenario: magnetic field diffusion
  ,
Geometry: bulk material, modelled as stack of tapes
Source: boundary field
Reference: Analytical solution, e.g., [6]:
  Gaussian error function
  Similarity variable
  Magnetic diffusivity
Chart: 
| 0 | 0.999 | 1 | 2 | 3
 | 0 | 0 | 1 | 1 | 1
: air
: conductor
Computational domain
Chart: 
| 0 | 0.999 | 1 | 2 | 3
 | 0 | 0 | 1 | 1 | 1
Source term
[6] Knoepfel, H. E., Magnetic fields: a comprehensive theoretical treatise for practical use. John Wiley & Sons, 2008.

## Slide 14: Verification – 2. Skin Effect
Numerical Solution: magnetic field diffusion
Magnetic flux density distribution in the conductive slab
Magnetic flux density distribution at x=1 mm, as function of time: numerical solution (sol) and analytical solution (ref)
Chart: Field at x = 1 mm
| 0 | 2.6315789473684199 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35 | 36 | 37 | 38 | 39 | 40 | 41 | 42 | 43 | 44 | 45 | 46 | 47 | 48 | 49 | 50
sol | 0 | 0.48451 | 0.5175 | 0.57514 | 0.61614 | 0.64721 | 0.67179 | 0.69186 | 0.70865 | 0.72297 | 0.73537 | 0.74624 | 0.75587 | 0.76448 | 0.77224 | 0.77929 | 0.78571 | 0.79161 | 0.79704 | 0.80208 | 0.80675 | 0.81111 | 0.81519 | 0.81902 | 0.82262 | 0.82602 | 0.82923 | 0.83227 | 0.83516 | 0.83792 | 0.84054 | 0.84305 | 0.84545 | 0.84775 | 0.84996 | 0.85209 | 0.85414 | 0.85612 | 0.85803 | 0.85988 | 0.86167 | 0.86341 | 0.86509 | 0.86674 | 0.86833 | 0.86989 | 0.87141 | 0.87289 | 0.87434 | 0.87534
ref | 0 | 0.48451 | 0.62432 | 0.68975 | 0.7295 | 0.75723 | 0.7778 | 0.7939 | 0.80698 | 0.8178 | 0.827 | 0.83495 | 0.84187 | 0.848 | 0.85347 | 0.85838 | 0.86284 | 0.86689 | 0.87061 | 0.87534
 Consistent with theory [6]
Chart: Field diffusion
| -2 | -1.5 | -1 | -0.5 | -0.01 | 0 | 1E-4 | 2.0000000000000001E-4 | 5.0000000000000001E-4 | 0.81632653061224503 | 1.0204081632653099 | 1.22448979591837 | 1.4285714285714302 | 1.6326530612244901 | 1.83673469387755 | 2.0408163265306096 | 2.2448979591836702 | 2.4489795918367299 | 2.6530612244898002 | 2.8571428571428603 | 3.06122448979592 | 3.2653061224489801 | 3.4693877551020398 | 3.6734693877550999 | 3.87755102040816 | 4.0816326530612299 | 4.28571428571429 | 4.4897959183673493 | 4.6938775510204094 | 4.8979591836734704 | 5.1020408163265305 | 5.3061224489795906 | 5.5102040816326499 | 5.7142857142857206 | 5.9183673469387799 | 6.12244897959184 | 6.3265306122449001 | 6.5306122448979602 | 6.7346938775510194 | 6.9387755102040796 | 7.1428571428571397 | 7.3469387755101998 | 7.5510204081632697 | 7.7551020408163298 | 7.9591836734693899 | 8.1632653061224492 | 8.3673469387755102 | 8.5714285714285694 | 8.7755102040816304 | 8.9795918367346914 | 9.1836734693877595 | 9.3877551020408188 | 9.5918367346938798 | 9.7959183673469408 | 10
t=0 | 1 | 1 | 1 | 1 | 1 | 1 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
t=1 | 1 | 1 | 1 | 1 | 1 | 1 | 0.81914 | 0.64751 | 0.49284 | 0.3605 | 0.25308 | 0.17015 | 0.10944 | 0.067257 | 0.039447 | 0.022057 | 0.011746 | 0.0059514 | 0.0028662 | 0.0013108 | 0.00056855 | 0.00023351 | 9.1027e-05 | 3.3455e-05 | 1.1649e-05 | 3.8174e-06 | 1.18e-06 | 3.4225e-07 | 9.3286e-08 | 2.3853e-08 | 5.7594e-09 | 1.3159e-09 | 2.8347e-10 | 5.7014e-11 | 1.0749e-11 | 1.8971e-12 | 3.141e-13 | 4.8688e-14 | 7.0741e-15 | 9.6624e-16 | 1.2451e-16 | 1.5182e-17 | 1.7522e-18 | 1.9259e-19 | 2.0284e-20 | 2.0427e-21 | 1.9829e-22 | 1.86e-23 | 1.6925e-24 | 1.4976e-25 | 1.2847e-26 | 1.0775e-27 | 8.8053e-29 | 7.0718e-30 | 1.09e-30
t=5 | 1 | 1 | 1 | 1 | 1 | 1 | 0.90893 | 0.81905 | 0.7315 | 0.64732 | 0.5675 | 0.49266 | 0.42347 | 0.36031 | 0.30342 | 0.25284 | 0.20844 | 0.16998 | 0.1371 | 0.10935 | 0.086234 | 0.067234 | 0.051818 | 0.039474 | 0.029719 | 0.02211 | 0.016254 | 0.011805 | 0.0084706 | 0.0060039 | 0.0042058 | 0.0029119 | 0.0019914 | 0.0013452 | 0.00089759 | 0.00059141 | 0.00038431 | 0.00024739 | 0.00015655 | 9.8192e-05 | 6.0729e-05 | 3.7076e-05 | 2.2345e-05 | 1.3282e-05 | 7.7971e-06 | 4.5229e-06 | 2.5849e-06 | 1.4586e-06 | 8.1271e-07 | 4.4739e-07 | 2.4322e-07 | 1.3151e-07 | 7.3086e-08 | 4.4929e-08 | 3.66e-08
t=10 | 1 | 1 | 1 | 1 | 1 | 1 | 0.93921 | 0.87877 | 0.81903 | 0.76033 | 0.70303 | 0.64733 | 0.59354 | 0.54189 | 0.49259 | 0.4458 | 0.40165 | 0.36023 | 0.32159 | 0.28577 | 0.25275 | 0.22247 | 0.19489 | 0.1699 | 0.14739 | 0.12723 | 0.10928 | 0.093395 | 0.079416 | 0.067186 | 0.056556 | 0.04737 | 0.039472 | 0.032721 | 0.026983 | 0.022135 | 0.018063 | 0.014663 | 0.01184 | 0.0095092 | 0.0075971 | 0.0060373 | 0.0047726 | 0.0037534 | 0.0029372 | 0.002288 | 0.0017753 | 0.001374 | 0.001063 | 0.00082543 | 0.00064873 | 0.00052061 | 0.00043494 | 0.00038486 | 0.000369
t=50 | 1 | 1 | 1 | 1 | 1 | 1 | 0.97423 | 0.9485 | 0.92282 | 0.89724 | 0.87181 | 0.84651 | 0.82139 | 0.79648 | 0.77182 | 0.74742 | 0.72332 | 0.69955 | 0.67613 | 0.65308 | 0.63043 | 0.60821 | 0.58644 | 0.56514 | 0.54433 | 0.52403 | 0.50427 | 0.48505 | 0.4664 | 0.44834 | 0.43088 | 0.41404 | 0.39783 | 0.38226 | 0.36734 | 0.35309 | 0.33952 | 0.32663 | 0.31444 | 0.30295 | 0.29217 | 0.28211 | 0.27277 | 0.26416 | 0.25628 | 0.24914 | 0.24274 | 0.23708 | 0.23218 | 0.22802 | 0.22462 | 0.22197 | 0.22007 | 0.21893 | 0.21855
[6] Knoepfel, H. E., Magnetic fields: a comprehensive theoretical treatise for practical use. John Wiley & Sons, 2008.

## Slide 15: Verification – 3. Field Dependency
Scenario: AC loss due to screening currents
  ,
  as power law
Geometry: single tape, orthogonal to the field
Source: boundary field
Reference: Analytical solution, e.g., [7]: AC loss (J/cycle), penetration field
  if ,
  if
: air
: conductor
Chart: 
| 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9 | 0.95 | 1
 | 0 | 0.30902 | 0.58779 | 0.80902 | 0.95106 | 1 | 0.95106 | 0.80902 | 0.58779 | 0.30902 | 1.2251e-16 | -0.30902 | -0.58779 | -0.80902 | -0.95106 | -1 | -0.95106 | -0.80902 | -0.58779 | -0.30902 | -2.4503e-16
Source term
Chart: 
| 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9 | 0.95 | 1
 | 0 | 0.30902 | 0.58779 | 0.80902 | 0.95106 | 1 | 0.95106 | 0.80902 | 0.58779 | 0.30902 | 1.2251e-16 | -0.30902 | -0.58779 | -0.80902 | -0.95106 | -1 | -0.95106 | -0.80902 | -0.58779 | -0.30902 | -2.4503e-16
[7] Brandt, E.H., "Superconductors of finite thickness in a perpendicular magnetic field: Strips and slabs." Physical review B 54.6 (1996): 4246.
Computational domain

## Slide 16: Verification – 3. Field Dependency
Numerical Solution: AC loss due to screening currents
Ac loss per cycle, as function of the applied field
Ac loss per cycle, as function of frequency, for
Chart: AC loss / Cycle
| 5.0000000000000001E-4 | 1E-3 | 2E-3 | 5.0000000000000001E-3 | 0.01 | 0.02 | 0.05 | 0.1 | 0.2 | 0.5 | 1 | 2
n = 5 | 8.4185e-08 | 7.7364e-07 | 7.6021e-06 | 0.00015513 | 0.0014552 | 0.012318 | 0.14834 | 0.63661 | 1.945 | 6.7766 | 16.3147 | 38.338
n = 20 | 1.4463e-08 | 1.5982e-07 | 1.2841e-06 | 3.477e-05 | 0.00046778 | 0.0057847 | 0.10672 | 0.52501 | 1.5837 | 4.9632 | 10.8423 | 23.0321
n = 50 | 1.4463e-08 | 1.4384e-07 | 1.1724e-06 | 2.8572e-05 | 0.00034185 | 0.0046122 | 0.095894 | 0.49295 | 1.5053 | 4.6531 | 9.9837 | 20.8184
Chart: AC loss / Cycle
| 1E-3 | 0.01 | 0.1 | 1 | 10 | 100 | 0 | 0 | 0 | 0 | 0 | 0
n = 5 | 0.0045649 | 0.0027402 | 0.0014519 | 0.00071958 | 0.00034493 | 0.00016302 | 0 | 0 | 0 | 0 | 0 | 0
n = 20 | 0.00070325 | 0.00057325 | 0.000466 | 0.00039121 | 0.00030674 | 0.00024807 | 0 | 0 | 0 | 0 | 0 | 0
n = 50 | 0.0004085 | 0.0004092 | 0.00034013 | 0.00032062 | 0.00029195 | 0.00027318 | 0 | 0 | 0 | 0 | 0 | 0
n = 100 | 0.00032443 | 0.00031125 | 0.00029951 | 0.00029178 | 0.00029228 | 0.00026142 | 0 | 0 | 0 | 0 | 0 | 0
 Consistent with theory [7]
[7] Brandt, E H., "Superconductors of finite thickness in a perpendicular magnetic field: Strips and slabs." Physical review B 54.6 (1996): 4246.
Notes: Meissner is reversible. Losses per cycle are always zero

## Slide 17: Outline
Introduction
Motivation
Formulation
Verification
Validation Measurements on Feather2: Field quality assessment
    Magnetic Field Quality
    Screening Current Effects
Summary and Outlook

## Slide 18: Measurements on Feather2
: air
: coil
: iron
Scenario: magnetic field quality in the Feather M2 insert dipole magnet [8]
  ,
  as anisotropic power law, derived from data @ 77 K
  Resulting uncertainty in material properties (annex slide 28)
Geometry: tapes modelled as lines
Source: measured current
Reference: measurements done by C. Petrone (CERN)
[8] Van Nugteren, J., et al. "Powering of an HTS dipole insert-magnet operated standalone in helium gas between 5 and 85 K." SuST 31.6 (2018): 065002.
Feather2 magnet. Courtesy of J. Van Nugteren
Source term
Chart: 
| 0 | 30 | 150 | 200 | 320 | 370 | 490 | 540 | 660 | 710 | 830 | 880 | 1000 | 1050 | 1170 | 1220 | 1340 | 1390 | 1510 | 1560 | 1680 | 1730 | 1850 | 1900 | 2020 | 2070 | 2190 | 2220 | 2340
 | 0.1 | 0.25 | 0.25 | 0.5 | 0.5 | 0.75 | 0.75 | 1 | 1 | 1.25 | 1.25 | 1.5 | 1.5 | 1.75 | 1.75 | 1.5 | 1.5 | 1.25 | 1.25 | 1 | 1 | 0.75 | 0.75 | 0.5 | 0.5 | 0.25 | 0.25 | 0.1 | 0.1
Computational domain

## Slide 19: Field Quality Assessment
Pre-cycle first magnetization
Steps of 250 A, plateaus of 120 s: decay of inductive effects
Evaluation points ,
FEM simulation
Magnetic field quality calculation
Persistent screening currents contribution: Calculation of change in magnetic field quality (assuming screening currents as dominant mechanism)
Chart: t (s)
| 0 | 30 | 150 | 200 | 320 | 370 | 490 | 540 | 660 | 710 | 830 | 880 | 1000 | 1050 | 1170 | 1220 | 1340 | 1390 | 1510 | 1560 | 1680 | 1730 | 1850 | 1900 | 2020 | 2070 | 2190 | 2220 | 2340
 | 0.1 | 0.25 | 0.25 | 0.5 | 0.5 | 0.75 | 0.75 | 1 | 1 | 1.25 | 1.25 | 1.5 | 1.5 | 1.75 | 1.75 | 1.5 | 1.5 | 1.25 | 1.25 | 1 | 1 | 0.75 | 0.75 | 0.5 | 0.5 | 0.25 | 0.25 | 0.1 | 0.1
 | 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75 | 1.5 | 1.25 | 1 | 0.75 | 0.5 | 0.25
 | 0 | 1 | 1.75 | 1.75 | 1 | 0.1 | 0.1
Total magnetic flux density (T), 1 quadrant
B(T)
Notes: No iron hysteresis in the model
Uncertainties in Jc(T,B,theta)
Uncertainties of scaling from 3D to 2D (e.g. layer jump)

## Slide 20: Results – FEM Simulation
Normalized current density in the coil, shown for the first quadrant
a)
b)
c)
Current density distribution (*) in the coil:
same external current
different time steps
a)
b)
c)
(*) Current sharing resolved using a binary search algorithm (bisection method). Internal call for each time step
J/Jc (-)
J/Jc (-)
J/Jc (-)
Notes: Influence of screening currents

## Slide 21: Validation – 4. Magnetic Field Quality
field multipoles, as function of the normalized staircase time
Chart: 
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 0.16682 | 0.33069 | 0.6035 | 0.87668 | 1.15 | 1.422 | 1.6339 | 1.7861 | 1.9218 | 2.0439 | 2.1607 | 2.2749 | 2.3876 | 2.4621 | 2.389 | 2.2779 | 2.1649 | 2.0486 | 1.9265 | 1.7905 | 1.6379 | 1.4253 | 1.1523 | 0.87777 | 0.60397 | 0.33096 | 0.16715
sim | 0.14074 | 0.27788 | 0.41502 | 0.55203 | 0.68894 | 0.8258 | 0.96264 | 1.0994 | 1.236 | 1.3717 | 1.5052 | 1.6361 | 1.7626 | 1.8788 | 1.9823 | 2.0803 | 2.1757 | 2.2698 | 2.3636 | 2.4568 | 2.3661 | 2.2744 | 2.1814 | 2.0866 | 1.9886 | 1.8845 | 1.767 | 1.6396 | 1.5079 | 1.3737 | 1.2376 | 1.1006 | 0.96351 | 0.82637 | 0.68925 | 0.55214 | 0.41503 | 0.27791 | 0.14078
Chart: 
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 396.176 | 287.8211 | 239.1869 | 222.0029 | 214.3159 | 212.4014 | 214.2419 | 219.2723 | 220.9041 | 215.385 | 205.7201 | 194.2002 | 182.0771 | 174 | 174.1 | 192.395 | 202.9659 | 211.8436 | 217.1225 | 215.7858 | 211.6595 | 211.3379 | 215.8072 | 227.1275 | 246.8658 | 296.6789 | 403.7129
sim | 320.0853 | 248.7077 | 225.5965 | 215.1322 | 209.3754 | 205.5531 | 202.8011 | 200.8588 | 199.8246 | 199.8985 | 200.577 | 202.7649 | 207.1983 | 210.8754 | 208.7164 | 202.927 | 195.1216 | 186.3934 | 177.2141 | 167.9082 | 176.2786 | 184.6441 | 192.7971 | 200.4033 | 206.4032 | 209.0362 | 206.2008 | 203.3 | 202.8044 | 203.7059 | 205.0536 | 207.405 | 210.6531 | 214.8353 | 220.2992 | 228.2263 | 241.2036 | 267.2084 | 345.3282
Chart: 
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 68.7505 | 45.678 | 35.0365 | 30.9446 | 28.6503 | 26.5144 | 24.1974 | 21.2663 | 17.5851 | 14.6967 | 12.8643 | 11.7389 | 11.0782 | 10.84 | 11.088 | 11.6944 | 12.6825 | 14.4331 | 17.2236 | 20.9468 | 23.9186 | 26.3363 | 28.7482 | 31.4138 | 35.6783 | 46.2221 | 69.108
sim | 61.4558 | 41.2189 | 35.0234 | 31.9337 | 29.967 | 28.6082 | 27.5781 | 26.7855 | 26.1205 | 25.3861 | 24.5498 | 23.3887 | 21.4993 | 18.8405 | 16.6943 | 15.3611 | 14.6057 | 14.1898 | 14.041 | 14.0722 | 14.3001 | 14.6165 | 15.1238 | 15.9591 | 17.3832 | 19.61 | 22.2689 | 24.1055 | 25.2416 | 26.1382 | 26.9814 | 27.7605 | 28.653 | 29.7705 | 31.2311 | 33.374 | 36.9909 | 44.4431 | 67.2964
Chart: 
| 8.3270002777777768E-2 | 0.15268336111111108 | 0.22217659722222222 | 0.29185969444444448 | 0.36127797222222219 | 0.41690402777777774 | 0.45855190277777774 | 0.5 | 0.54188712500000003 | 0.58359297222222217 | 0.63875945833333336 | 0.70818063888888894 | 0.77788315277777775 | 0.84714761111111114 | 0.91661162361111104
meas | 0.32836 | 0.60123 | 0.87414 | 1.1473 | 1.4189 | 1.6303 | 1.782 | 1.9169 | 1.7827 | 1.6312 | 1.4197 | 1.1477 | 0.87399 | 0.60078 | 0.32807
0 deg | 0.054389 | 0.13668 | 0.27384 | 0.41089 | 0.54782 | 0.68474 | 0.82163 | 0.95847 | 1.0952 | 1.2318 | 1.3674 | 1.5007 | 1.6315 | 1.7575 | 1.8728 | 1.9762 | 1.8736 | 1.7584 | 1.6321 | 1.5012 | 1.3676 | 1.2318 | 1.095 | 0.95808 | 0.82116 | 0.68425 | 0.54733 | 0.41038 | 0.27343 | 0.13647 | 0.054264
Chart: 
| 8.3270002777777768E-2 | 0.15268336111111108 | 0.22217659722222222 | 0.29185969444444448 | 0.36127797222222219 | 0.41690402777777774 | 0.45855190277777774 | 0.5 | 0.54188712500000003 | 0.58359297222222217 | 0.63875945833333336 | 0.70818063888888894 | 0.77788315277777775 | 0.84714761111111114 | 0.91661162361111104
meas | 268.5344 | 228.6497 | 215.4613 | 210.3915 | 210.5213 | 213.9242 | 220.2013 | 222.3 | 221.1285 | 216.4372 | 215.5462 | 218.3265 | 226.817 | 243.7866 | 287.6951
0 deg | 386.2262 | 280.5091 | 247.3264 | 231.9384 | 222.7761 | 216.7518 | 212.7355 | 210.0629 | 208.7265 | 208.406 | 208.8699 | 211.2385 | 216.039 | 219.4111 | 216.8338 | 219.6605 | 217.011 | 213.6754 | 212.8643 | 214.047 | 216.126 | 219.3914 | 223.7655 | 229.1627 | 236.4414 | 247.3545 | 265.7473 | 302.9339 | 415.5836
Chart: 
| 8.3270002777777768E-2 | 0.15268336111111108 | 0.22217659722222222 | 0.29185969444444448 | 0.36127797222222219 | 0.41690402777777774 | 0.45855190277777774 | 0.5 | 0.54188712500000003 | 0.58359297222222217 | 0.63875945833333336 | 0.70818063888888894 | 0.77788315277777775 | 0.84714761111111114 | 0.91661162361111104
meas | 39.8036 | 31.8946 | 28.8959 | 27.1225 | 25.358 | 23.2981 | 20.4954 | 16.98 | 20.6136 | 23.5531 | 25.9182 | 27.8832 | 29.7798 | 33.0702 | 41.2508
0 deg | 64.5533 | 42.6031 | 35.7611 | 32.2885 | 30.1699 | 28.7176 | 27.7233 | 26.9918 | 26.3705 | 25.6468 | 24.8465 | 23.7173 | 21.8142 | 19.1782 | 17.1092 | 19.3649 | 22.1104 | 24.1216 | 25.4375 | 26.4591 | 27.3749 | 28.2139 | 29.1309 | 30.2364 | 31.6956 | 33.9056 | 37.6863 | 45.5399 | 69.8648
Chart: 
| 9.0992116434202561E-2 | 0.18195318981200725 | 0.27291271376591875 | 0.36391773802304422 | 0.45482680412371135 | 0.5 | 0.54535864160097025 | 0.63601561552456043 | 0.72710236810188 | 0.81809164038811399 | 0.90898068526379627
meas | 0.16017 | 0.3238 | 0.48709 | 0.65054 | 0.81375 | 0.89515 | 0.81365 | 0.65027 | 0.48676 | 0.32339 | 0.16009
0 deg | 0.052761 | 0.13504 | 0.27197 | 0.40878 | 0.54547 | 0.68197 | 0.81828 | 0.95466 | 0.81864 | 0.68209 | 0.54534 | 0.40857 | 0.27176 | 0.1349 | 0.052784
Chart: 
| 9.0992116434202561E-2 | 0.18195318981200725 | 0.27291271376591875 | 0.36391773802304422 | 0.45482680412371135 | 0.5 | 0.54535864160097025 | 0.63601561552456043 | 0.72710236810188 | 0.81809164038811399 | 0.90898068526379627
meas | 408.6229 | 295.2836 | 260.6113 | 245.7667 | 238.9375 | 238.3 | 243.5962 | 255.1541 | 274.1876 | 312.4602 | 429.2418
0 deg | 413.4029 | 298.6497 | 263.4089 | 248.3578 | 241.7463 | 239.392 | 238.8263 | 240.5296 | 247.3744 | 259.5205 | 278.954 | 317.7925 | 434.7402
Chart: 
| 9.0992116434202561E-2 | 0.18195318981200725 | 0.27291271376591875 | 0.36391773802304422 | 0.45482680412371135 | 0.5 | 0.54535864160097025 | 0.63601561552456043 | 0.72710236810188 | 0.81809164038811399 | 0.90898068526379627
meas | 64.8761 | 43.6858 | 36.7633 | 33.551 | 31.7576 | 31.42 | 32.5056 | 34.7951 | 38.5903 | 45.7734 | 67.6648
0 deg | 72.6661 | 47.0821 | 38.8651 | 35.1972 | 33.183 | 32.1981 | 32.0163 | 32.6592 | 34.3344 | 37.0526 | 41.2849 | 49.747 | 75.0961
B1 (T)
b3 (units)
b5 (units)
4.5 K
25.0 K
68.0 K
t (s)
t (s)
t (s)
 Very good agreement with measurements
Measurement
Simulation
Notes: Multipoles dominated by geometry and iron contributions: Screening currents only small contribution

## Slide 22: Validation – 5. Screening Currents
field multipole variations, as function of current (in kA)
Chart: 
| 0.29957012 | 0.60028197999999999 | 1.1006214999999999 | 1.6008191000000003 | 2.0986528 | 2.5993179 | 3.0016338 | 3.2984656999999999 | 3.5995850000000003 | 3.8981686999999998 | 4.2014339999999999 | 4.5019495000000003 | 4.8017586999999997
meas | 1.3544 | 1.1051 | 1.9063 | 4.4086 | 9.3474 | 13.6006 | 16.153 | 17.6595 | 19.2431 | 19.3901 | 16.8988 | 12.3109 | 5.8023
sim | 0.17712 | 0.18129 | 0.10459 | 0.034776 | 0.42488 | 1.2704 | 2.3111 | 3.5322 | 4.9068 | 6.4841 | 8.4736 | 10.9665 | 14.0313 | 17.6576 | 23.1819 | 25.9661 | 25.8476 | 23.3996 | 18.458 | 10.4672
Chart: 
| 0.29957012 | 0.60028197999999999 | 1.1006214999999999 | 1.6008191000000003 | 2.0986528 | 2.5993179 | 3.0016338 | 3.2984656999999999 | 3.5995850000000003 | 3.8981686999999998 | 4.2014339999999999 | 4.5019495000000003 | 4.8017586999999997
meas | 7.5369 | 8.8578 | 7.6789 | 5.1246 | 1.4913 | -1.0635 | -2.5824 | -3.4865 | -3.7816 | -3.5413 | -2.7543 | -1.8051 | -0.7092
sim | 48.5617 | 25.2429 | 18.5007 | 15.6071 | 13.0941 | 10.9238 | 9.2822 | 7.852 | 6.5462 | 5.229 | 3.8073 | 2.2275 | 0.53505 | -0.99758 | -1.8393 | -2.3132 | -2.5237 | -2.3245 | -1.7493 | -0.93546
Chart: 
| 0.29957012 | 0.60028197999999999 | 1.1006214999999999 | 1.6008191000000003 | 2.0986528 | 2.5993179 | 3.0016338 | 3.2984656999999999 | 3.5995850000000003 | 3.8981686999999998 | 4.2014339999999999 | 4.5019495000000003 | 4.8017586999999997
meas | 0.3575 | 0.54406 | 0.64176 | 0.46927 | 0.09792 | -0.17809 | -0.27878 | -0.31948 | -0.36157 | -0.26363 | -0.18183 | -0.044517 | 0.009789
sim | 12.1545 | 5.8405 | 3.2242 | 1.9675 | 1.4403 | 1.2642 | 1.1623 | 1.0749 | 0.975 | 0.86092 | 0.75204 | 0.69185 | 0.71681 | 0.76964 | 0.76958 | 0.68882 | 0.59794 | 0.51814 | 0.4267 | 0.2591
Chart: 
| 0.59954401999999996 | 1.0993202 | 1.5996714999999999 | 2.1013898000000002 | 2.6012013999999999 | 3.001709 | 3.3015737000000001
meas | -1.5373 | -2.3197 | -0.77252 | 1.9049 | 4.1991 | 4.694 | 3.9606
0 deg | -0.63013 | -1.0677 | -2.0652 | -2.5651 | -2.4856 | -2.4744 | -2.3833 | -1.9795 | -1.1557 | 0.062771 | 1.2897 | 2.4462 | 3.484 | 4.3087 | 3.9264
Chart: 
| 0.59954401999999996 | 1.0993202 | 1.5996714999999999 | 2.1013898000000002 | 2.6012013999999999 | 3.001709 | 3.3015737000000001
meas | 19.1607 | 15.1369 | 11.3557 | 7.935 | 5.025 | 2.5131 | 0.92724
0 deg | 55.7143 | 29.3574 | 22.4248 | 18.4209 | 15.4161 | 13.6654 | 12.411 | 11.03 | 9.3284 | 7.3994 | 5.641 | 3.9944 | 2.4369 | 0.97204 | 0.24939
Chart: 
| 0.59954401999999996 | 1.0993202 | 1.5996714999999999 | 2.1013898000000002 | 2.6012013999999999 | 3.001709 | 3.3015737000000001
meas | 1.4472 | 1.1755 | 0.88389 | 0.76068 | 0.56016 | 0.25494 | 0.1182
0 deg | 11.3078 | 5.3115 | 2.9367 | 1.9252 | 1.6171 | 1.5257 | 1.5188 | 1.4076 | 1.2221 | 1.0044 | 0.81233 | 0.59096 | 0.40433 | 0.29617 | 0.1867
Chart: 
| 0.30009200000000003 | 0.60008161999999998 | 0.90006613000000002 | 1.2002006999999999 | 1.5000188000000001
meas | -0.9215 | -4.5647 | -3.6451 | -3.0726 | -1.1658
0 deg | 0.2425 | -1.4646 | -2.2609 | -2.1564 | -1.3568 | 1.2655 | 3.8036
Chart: 
| 0.30009200000000003 | 0.60008161999999998 | 0.90006613000000002 | 1.2002006999999999 | 1.5000188000000001
meas | 20.6189 | 17.1766 | 13.5763 | 9.3873 | 4.6586
0 deg | 20.1855 | 21.3373 | 19.1428 | 15.5451 | 11.1627 | 5.6281 | 1.1376
Chart: 
| 0.30009200000000003 | 0.60008161999999998 | 0.90006613000000002 | 1.2002006999999999 | 1.5000188000000001
meas | 2.7887 | 2.0876 | 1.8269 | 1.2441 | 0.74801
0 deg | 3.8008 | 2.43 | 2.665 | 2.4198 | 1.8554 | 1.1515 | 0.46114
kA
kA
kA
 Good agreement with measurements, considering uncertainty in
B1 (T)
b3 (units)
b5 (units)
4.5 K
25.0 K
68.0 K
Measurement
Simulation

## Slide 23: Summary and Outlook
Summary
- weak formulation for FEM:
Excellent agreement with theory
Consistency with Feather2 measurements
Scalable and fast (few hours for ~ tapes in 2D models)
Thank you for your attention!
Outlook
Include heat balance equation
Develop field-circuit coupling interface
Include the models in the STEAM framework
Run field quality analysis and optimization
Run quench protection studies (e.g., Feather2 in FRESCA2)

## Slide 25
Annex

## Slide 26: Validation – D. Current dependency
Scenario: AC loss due to screening currents
  ,
  as power law
Geometry: single tape
Source: External current
Reference: previous work, e.g. [ref1]:
  if
  if field fully penetrated, const
Chart: 
| 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9 | 0.95 | 1
 | 0 | 0.30902 | 0.58779 | 0.80902 | 0.95106 | 1 | 0.95106 | 0.80902 | 0.58779 | 0.30902 | 1.2251e-16 | -0.30902 | -0.58779 | -0.80902 | -0.95106 | -1 | -0.95106 | -0.80902 | -0.58779 | -0.30902 | -2.4503e-16
: air
: conductor
Chart: 
| 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9 | 0.95 | 1
 | 0 | 0.30902 | 0.58779 | 0.80902 | 0.95106 | 1 | 0.95106 | 0.80902 | 0.58779 | 0.30902 | 1.2251e-16 | -0.30902 | -0.58779 | -0.80902 | -0.95106 | -1 | -0.95106 | -0.80902 | -0.58779 | -0.30902 | -2.4503e-16
Source term
[ref1] Grilli, F, et al. "Computation of Losses in HTS Under the Action of Varying Magnetic Fields and Currents." IEEE Transactions on Applied Superconductivity 24.1 (2014): 78-110.
Computational domain

## Slide 27: Validation – D. Current dependency
Solution of the transport + screening currents problem
Ac loss per cycle, as function of frequency, for . Trends are highlighted with dashed lines
Chart: AC loss / Cycle
| 1 | 10 | 50 | 100 | 250 | 500 | 750 | 1000 | 1250 | 1500 | 2000
n = 5 | 7.3834e-11 | 4.2243e-08 | 7.6652e-06 | 7.8292e-05 | 0.0017731 | 0.021031 | 0.10252 | 0.37937 | 1.2711 | 3.6481 | 20.1038
n = 20 | 1.1431e-11 | 8.0604e-09 | 1.1447e-06 | 1.4877e-05 | 0.00049992 | 0.0078275 | 0.045615 | 0.28617 | 18.7752 | 858.3055
n = 50 | 5.5355e-09 | 7.8244e-07 | 9.7064e-06 | 0.00035447 | 0.0059341 | 0.035477 | 0.24419 | 9737.4123
Ac loss per cycle, as function of the applied current. Trends are highlighted with dashed lines
Chart: AC loss / Cycle
| 1E-3 | 0.01 | 0.1 | 1 | 10 | 100
I/Ic=10% | 2.3048e-05 | 1.8532e-05 | 1.4914e-05 | 1.2047e-05 | 9.669e-06 | 7.8387e-06
I/Ic=50% | 0.013402 | 0.010154 | 0.0078172 | 0.0060806 | 0.0047594 | 0.0037509 | 0 | 0 | 0 | 0
I/Ic=75% | 0.10953 | 0.065904 | 0.045621 | 0.033349 | 0.025099 | 0.019222 | 0 | 0 | 0
 Consistent with previous research

## Slide 28: Project Overview
Protection of HTS-based high-field accelerator magnets
CERN
Technische Universität Darmstadt
Graduate School of Excellence Computational Engineering (GCE)
Dr. Matthias Mentink (TE-MPE-PE)
Prof. Dr. Sebastian Schöps (TU Darmstadt)
05.2018 – 05.2021
Gentner Programme at CERN (grant no. 05E12CHA)
‘Excellence Initiative’ of the German Government
GCE at TU Darmstadt

## Slide 29: Magnetic field dynamics in superconductors
Type I: Meißner Effect
Thermodynamical state, reversible
London equation
  , if
Type II: Abrikosov fluxons
Flux pinning and motion, irreversible
Power-law (phenomenological)
Faraday Law (eddy currents)
Bc1
Bc2
Tc
B
T
Type I
Type II
B-T Diagram

## Slide 30: Formulations
Conductivity based:
: magnetic vector potential
  ill-conditioned mass-conductivity matrix ( condition number)
Resistivity based:
: magnetic field strength
  everywhere, unphysical eddy currents , computationally inefficient
-: current vector potential-scalar magnetic potential
  cohomology basis functions for net currents in multiply connected domains
Mixed fields (from literature)
-: magnetic vector potential + magnetic field strength
Developed for 2D rotating machinery. Current driven, no external coupling
-: current vector potential + magnetic vector potential Current driven, no external coupling, gauge and interface conditions not given, Potentially inconsistent voltage balance

## Slide 31: Modelling of Jc (T, B, )
Jc data from Fujikura [9]
Fit from [10]
available only for Lift factor, calibrated with the measured
Lift factor assumed consistent with
[9] Fujikura, Y-based high temperature superconductor. Company leaﬂet at ICEC (2014).
[10] Fleiter, J., and A. Ballarino. "Parameterization of the critical surface of REBCO conductors from Fujikura." CERN internal note, EDMS 1426239 (2014).`
Measured
fit in the model
Pic. From [6]
 Anisotropy included in the model, but uncertainty on material properties

## Slide 32: Formulation - Mixed potentials
formulation, weak form:
Ampere-Maxwell Law
Faraday Law
Constraint on transport current
reluctance
current
resistance
flux
voltage
Advantages
finite conditon number
magnetostatic problem
Drawback
Weak form to be implemented

## Slide 33: High-Temperature Superconductors
Cuprate compounds (CuO2) doped with rare earth elements (La, Bi-Sr-Ca, Y-Ga-Ba …)
Higher Tc and Bc0 respect to the traditional LTS competitors
Higher performance comes with higher prices!
.. But in the early 2000s it was
Chart: J_eng(T) @ 5T
Chart: J_eng(B) @ 1.9K
ReBCO | 5.7212 | 5.6242 | 5.5183 | 5.4139 | 5.3111 | 5.2099 | 5.1102 | 5.0121 | 4.9154 | 4.8203 | 4.7266 | 4.6344 | 4.5437 | 4.4544 | 4.3665 | 4.2799 | 4.1948 | 4.111 | 4.0286 | 3.9475 | 3.8677 | 3.7892 | 3.712 | 3.636 | 3.5613 | 3.4878 | 3.4156 | 3.3445 | 3.2746 | 3.2059 | 3.1384 | 3.072 | 3.0067 | 2.9426 | 2.8795 | 2.8176 | 2.7567 | 2.6968 | 2.638 | 2.5803 | 2.5235 | 2.4678 | 2.413 | 2.3593 | 2.3064 | 2.2546 | 2.2036 | 2.1536 | 2.1045 | 2.0564

## Slide 34: Tapes and Cables
Tapes
ReBCO - Rare Earth Barium Copper Oxide tape
Batches of and beyond
Cost driven by production process
Features
Multi-layer, multi material
Aspect ratio ~ (tape), ~ (HTS layer)
HTS as anisotropic, nonlinear mono-filament
AC losses: eddy currents
Cables
Roebel geometry (1912)
“Coil-able”, bended on the long edge
Fully transposed: even current distribution
Aligned-coil concept against AC losses
■ Copper ■ ReBCO ■Substrate
Source: CDS. Coiled Roebel cable (Henry Barnard, CERN).

## Slide 35: Formulation - Crosscheck
Reference model [*] based on the formulation,
provided by http://www.htsmodelling.com
2D model of a Single HTS tape in self-field
Source: ,
Chart: Ohmic loss per cycle
| 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75 | 2
Ref. - 1Hz | 1.3507e-05 | 0.00022572 | 0.0012866 | 0.0069381 | 0.22171 | 1.5876 | 4.4346 | 8.6839
Ref. - 10Hz | 1.1861e-05 | 0.00017642 | 0.00095176 | 0.0037462 | 0.026446 | 0.16322 | 0.44802 | 0.87306
Ref. - 100Hz | 1.0655e-05 | 0.00014301 | 0.00072965 | 0.0025082 | 0.0073745 | 0.021555 | 0.050323 | 0.09312
Ref. - 1000Hz | 1.8165e-05 | 0.00015917 | 0.00062696 | 0.0016612 | 0.0034905 | 0.0063376 | 0.010404 | 0.015849
A-H - 1Hz | 1.4392e-05 | 0.00022396 | 0.0012754 | 0.006917 | 0.22164 | 1.5872 | 4.4345 | 8.6839
A-H - 10Hz | 1.1751e-05 | 0.00017469 | 0.00094137 | 0.0037227 | 0.026403 | 0.16307 | 0.4478 | 0.87295
A-H - 100Hz | 7.6794e-06 | 0.00013445 | 0.0007044 | 0.0024372 | 0.0072274 | 0.021355 | 0.050083 | 0.092956
A-H - 1000Hz | 2.5608e-06 | 0.000101 | 0.00046883 | 0.0013431 | 0.0029579 | 0.0055583 | 0.0094031 | 0.014658
Chart: Ohmic loss per cycle
| 0.25 | 0.5 | 0.75 | 1 | 1.25 | 1.5 | 1.75 | 2
Ref. - 1Hz | 1.3507e-05 | 0.00022572 | 0.0012866 | 0.0069381 | 0.22171 | 1.5876 | 4.4346 | 8.6839
Ref. - 10Hz | 1.1861e-05 | 0.00017642 | 0.00095176 | 0.0037462 | 0.026446 | 0.16322 | 0.44802 | 0.87306
Ref. - 100Hz | 1.0655e-05 | 0.00014301 | 0.00072965 | 0.0025082 | 0.0073745 | 0.021555 | 0.050323 | 0.09312
Ref. - 1000Hz | 1.8165e-05 | 0.00015917 | 0.00062696 | 0.0016612 | 0.0034905 | 0.0063376 | 0.010404 | 0.015849
A-H - 1Hz | 1.4392e-05 | 0.00022396 | 0.0012754 | 0.006917 | 0.22164 | 1.5872 | 4.4345 | 8.6839
A-H - 10Hz | 1.1751e-05 | 0.00017469 | 0.00094137 | 0.0037227 | 0.026403 | 0.16307 | 0.4478 | 0.87295
A-H - 100Hz | 7.6794e-06 | 0.00013445 | 0.0007044 | 0.0024372 | 0.0072274 | 0.021355 | 0.050083 | 0.092956
A-H - 1000Hz | 2.5608e-06 | 0.000101 | 0.00046883 | 0.0013431 | 0.0029579 | 0.0055583 | 0.0094031 | 0.014658
1 Hz
10 Hz
100 Hz
1000 Hz
Markers: (ref)
Lines:
[*] V. M. Rodriguez-Zermeno et al., "Towards Faster FEM Simulation of Thin Film Superconductors: A Multiscale Approach," in IEEE Transactions on Applied Superconductivity, vol. 21, no. 3, pp. 3273-3276, June 2011.

## Slide 36: Formulation - Benchmark
Forecasts on expected computational time:
1 tape
5 tapes
10 tapes
Same physics…
Increased computational cost
Chart: Computational time
| 1 | 5 | 10
H | 0.048611 | 0.20833 | 0.5
A-H | 0.020278 | 0.089722 | 0.12778 | 0.49833 | 0.96153
A-H opti | 0.0027778 | 0.0041667 | 0.005 | 0.026111 | 0.052778
Optimization of:
Mesh, solver, numerical implementation
8 h

## Slide 37: Formulation - PEC Limit Behavior
[1] Knoepfel, Heinz E. Magnetic fields: a comprehensive theoretical treatise for practical use. John Wiley & Sons, 2008.
Chart: AC loss / Cycle
| 1E-3 | 0.01 | 0.1 | 1 | 10 | 100
1.E-5 | 1.6483e-14 | 1.6483e-13 | 1.6501e-12 | 1.6487e-11 | 1.6483e-10 | 1.6499e-09
1.E-10 | 1.6456e-09 | 1.6456e-08 | 1.646e-07 | 1.6465e-06 | 1.6465e-05 | 0.00016502
1.E-15 | 0.00016447 | 0.0016301 | 0.008795 | 0.0028338 | 0.00042808 | 6.245e-05
1.E-20 | 6.2522e-05 | 1.0852e-05 | 2.493e-06 | 5.1255e-07 | 5.8408e-08 | 5.8664e-09
1.E-25 | 5.8666e-09 | 5.8669e-10 | 5.8669e-11 | 5.8669e-12 | 5.867e-13 | 5.867e-14
Chart: m(B) - normalized

## Slide 38: Field multipoles without eddy currents
Staircase Scenario at 4.5 K
“Eddy” considers the HTS tape dynamics
“No Eddy” assumes a homogeneous current density in the tapes
Chart: B1
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 0.16682 | 0.33069 | 0.6035 | 0.87668 | 1.15 | 1.422 | 1.6339 | 1.7861 | 1.9218 | 2.0439 | 2.1607 | 2.2749 | 2.3876 | 2.4621 | 2.389 | 2.2779 | 2.1649 | 2.0486 | 1.9265 | 1.7905 | 1.6379 | 1.4253 | 1.1523 | 0.87777 | 0.60397 | 0.33096 | 0.16715
eddy | 0.14269 | 0.27979 | 0.41689 | 0.55398 | 0.69107 | 0.82813 | 0.96518 | 1.1022 | 1.239 | 1.3749 | 1.5087 | 1.64 | 1.7668 | 1.8835 | 1.9875 | 2.0861 | 2.1821 | 2.2769 | 2.3713 | 2.4653 | 2.3743 | 2.2821 | 2.1887 | 2.0933 | 1.9948 | 1.89 | 1.772 | 1.6444 | 1.5126 | 1.3783 | 1.2419 | 1.1047 | 0.96738 | 0.83003 | 0.69266 | 0.55528 | 0.41791 | 0.28051 | 0.1431
no eddy | 0.054817 | 0.13704 | 0.27407 | 0.41109 | 0.5481 | 0.68511 | 0.82211 | 0.9591 | 1.096 | 1.2328 | 1.3687 | 1.5025 | 1.634 | 1.7613 | 1.8792 | 1.9862 | 2.0883 | 2.1878 | 2.2858 | 2.3828 | 2.4789 | 2.3828 | 2.2858 | 2.1878 | 2.0883 | 1.9862 | 1.8792 | 1.7613 | 1.634 | 1.5025 | 1.3687 | 1.2328 | 1.096 | 0.9591 | 0.82211 | 0.68511 | 0.5481 | 0.41109 | 0.27407 | 0.13704 | 0.054817
Chart: b3
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 396.176 | 287.8211 | 239.1869 | 222.0029 | 214.3159 | 212.4014 | 214.2419 | 219.2723 | 220.9041 | 215.385 | 205.7201 | 194.2002 | 182.0771 | 174 | 174.1 | 192.395 | 202.9659 | 211.8436 | 217.1225 | 215.7858 | 211.6595 | 211.3379 | 215.8072 | 227.1275 | 246.8658 | 296.6789 | 403.7129
eddy | 208.7441 | 182.8188 | 173.9306 | 169.432 | 166.7044 | 164.7608 | 163.2491 | 162.2379 | 161.8604 | 162.2516 | 163.1606 | 165.6545 | 170.4561 | 174.2853 | 172.0882 | 166.1619 | 158.1509 | 149.1862 | 139.7017 | 130.0044 | 138.278 | 146.6228 | 154.7428 | 162.3052 | 168.1661 | 170.5539 | 167.1716 | 163.4738 | 161.949 | 161.8093 | 162.0165 | 162.8702 | 164.1695 | 165.9088 | 168.3242 | 171.873 | 177.3644 | 188.0321 | 218.8501
no eddy | 193.3873 | 193.3767 | 193.3664 | 193.3567 | 193.3477 | 193.3465 | 193.3603 | 193.4304 | 193.8276 | 194.5772 | 195.2913 | 197.1637 | 200.3971 | 200.8202 | 194.2371 | 183.9559 | 171.9312 | 159.3324 | 146.6693 | 134.1758 | 146.6693 | 159.3324 | 171.9312 | 183.9559 | 194.2371 | 200.8203 | 200.3971 | 197.1637 | 195.2913 | 194.5772 | 193.8276 | 193.4304 | 193.3603 | 193.3465 | 193.3477 | 193.3567 | 193.3664 | 193.3767 | 193.3873
Chart: b5
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 68.7505 | 45.678 | 35.0365 | 30.9446 | 28.6503 | 26.5144 | 24.1974 | 21.2663 | 17.5851 | 14.6967 | 12.8643 | 11.7389 | 11.0782 | 10.84 | 11.088 | 11.6944 | 12.6825 | 14.4331 | 17.2236 | 20.9468 | 23.9186 | 26.3363 | 28.7482 | 31.4138 | 35.6783 | 46.2221 | 69.108
eddy | 50.0348 | 31.0474 | 24.5565 | 21.2737 | 19.2818 | 17.9156 | 16.899 | 16.131 | 15.4606 | 14.7093 | 13.8704 | 12.7436 | 10.9246 | 8.3058 | 6.1501 | 4.791 | 4.0286 | 3.6225 | 3.4948 | 3.5618 | 3.7663 | 4.0605 | 4.5547 | 5.3929 | 6.8418 | 9.1112 | 11.8371 | 13.7811 | 15.0529 | 16.0453 | 16.9144 | 17.6775 | 18.5107 | 19.5974 | 21.118 | 23.3724 | 27.0275 | 34.2361 | 55.1732
no eddy | 22.7371 | 22.734 | 22.7314 | 22.7294 | 22.7278 | 22.7245 | 22.7157 | 22.688 | 22.5636 | 22.1793 | 21.517 | 20.3725 | 18.3529 | 15.5322 | 13.1939 | 11.6699 | 10.7556 | 10.1882 | 9.8361 | 9.6363 | 9.8361 | 10.1882 | 10.7556 | 11.6699 | 13.1939 | 15.5322 | 18.3529 | 20.3725 | 21.517 | 22.1793 | 22.5636 | 22.688 | 22.7157 | 22.7245 | 22.7278 | 22.7294 | 22.7314 | 22.734 | 22.7371
Chart: b7
| 2.9957011999999998E-2 | 6.0028197999999998E-2 | 0.11006215 | 0.16008191000000002 | 0.20986527999999999 | 0.25993179 | 0.30016337999999998 | 0.32984656999999995 | 0.35995850000000001 | 0.38981686999999998 | 0.4201434 | 0.45019495000000004 | 0.48017586999999995 | 0.5 | 0.51971491999999997 | 0.54998099 | 0.57978400000000008 | 0.61006959999999999 | 0.63983082999999996 | 0.67005879000000002 | 0.69996807999999999 | 0.74017818000000002 | 0.78991632000000001 | 0.83997847999999997 | 0.88995036999999999 | 0.94000625000000004 | 0.96999857199999995
meas | 3.7792 | 2.3458 | 1.6227 | 1.2263 | 0.86529 | 0.56157 | 0.37796 | 0.35561 | 0.70747 | 1.1489 | 1.4986 | 1.7397 | 1.9484 | 2.074 | 1.9658 | 1.7814 | 1.514 | 1.1556 | 0.69635 | 0.34529 | 0.34038 | 0.45991 | 0.69695 | 1.0219 | 1.3776 | 2.0558 | 3.502
eddy | 10.2157 | 4.0881 | 1.9953 | 0.93811 | 0.29826 | 0.13139 | 0.43937 | 0.66833 | 0.85194 | 0.98077 | 1.0502 | 1.1015 | 1.0824 | 0.82466 | 0.41796 | 0.066984 | 0.19912 | 0.42263 | 0.62965 | 0.83389 | 0.71831 | 0.57067 | 0.39804 | 0.18083 | 0.12179 | 0.48111 | 0.67519 | 0.63637 | 0.54604 | 0.441 | 0.28172 | 0.076793 | 0.16688 | 0.49128 | 0.95067 | 1.6374 | 2.782 | 5.0634 | 11.7085
no eddy | 0.04484 | 0.044284 | 0.043799 | 0.043385 | 0.043048 | 0.04272 | 0.042082 | 0.041727 | 0.043914 | 0.022804 | 0.025391 | 0.067504 | 0.17534 | 0.53307 | 1.0218 | 1.4387 | 1.76 | 2.0288 | 2.2657 | 2.4781 | 2.2657 | 2.0288 | 1.76 | 1.4387 | 1.0218 | 0.53306 | 0.17534 | 0.067504 | 0.025391 | 0.022804 | 0.043914 | 0.041727 | 0.042082 | 0.04272 | 0.043048 | 0.043385 | 0.043799 | 0.044284 | 0.04484