## Slide 1: Temperature Stabilized Measurements of Laser Spectra
T. Flick, Wuppertal University
Mini Opto Workshop
4.-5. March 2010
CERN

## Slide 2: Overview
Introduction
  Measurement purpose
  Measurement principle
Setup
Performed measurements
  Temperature behavior
  Spectra
Status and future plans

## Slide 3: Introduction
In the innermost of the existing HEP detectors VCSEL need to stand severe radiation environments
This will get worse with future experiments
Main damaging effects for lasers:
  Radiation Damages
  Temperature effects inside the semiconductor material (at the junction)
Mostly both effects come along together, but heat can be cooled away.
This study is investigating the possibility to quantify a measure and prepare an improvement possibility for the cooling.
Similar work has been investigated by Markus Axer (Jan, Francois) for the CMS experiment and we inherit a lot from this work.
  I will use several slides from him to explain the principle

## Slide 4: Wavelength Spectrum
The wavelength spectrum emitted by a laser diode is a perfect indicator of the device’s internal temperature – the junction temperature Tj
The wavelength spectrum is red-shifted when the device is heated by increasing the ambient temperature or the input power
If a given cavity mode remains at the same wavelength, the junction temperature Tj must be constant
The change in junction temperature due to varying the input power Pin to the laser can be cancelled by a change in the heat sink temperature, so as to keep the selected mode fixed in wavelength (nulling method  Paoli method)
The thermal resistance is found from the ratio of the change in heat sink temperature to the change in input power.
Typical wavelength spectrum of a Fabry-Perot type laser measured with an Optical Spectrum Analyzer

## Slide 5: L-I Characteristic
Light-Current (L-I) characteristic of a non-irradiated laser at Tamb=20°C
Ith
DL
DI
Eff=DL/DI
Thermal rollover
  Threshold current Ith laser starts to emit coherent light
  Efficiency Eff slope of L-I curve in linear part
  Thermal rollover non-linear part of L-I curve where non-radiative recombination mechanisms (Auger) become dominant due to internal temperature

## Slide 6: Spectral Behavior during Irradiation
The behavior of certain mode peaks is unique for all LDs:
  “Slight” l red-shift with increasing fluence at the same input current level
  “Large” l red-shift when increasing the input current
10mA
25mA
45mA
55mA
Rs is constant during irradiation
 term is mainly affected by I
Ith increases during irradiation
 term is mainly affected by irradiation
 Popt is affected by I and by irradiation

## Slide 7: Paoli Method

## Slide 8: The Paoli Method

## Slide 9: The Paoli Method Step by Step
Extraction of spectrum properties
Cavity Mode
Gain

## Slide 10: Thermal Effects during Irradiation
A parameter that describes the device’s efficiency to release heat generated inside the laser is called Thermal Resistance Rth
Dl/DPin monitored during irradiation:
Dl/DTamb measured in an oven:

## Slide 11: Measurement Setup
In Wuppertal a similar setup as used by Markus has been realized:
  DUT is kept in a thermally isolated box
  Cooling and heating capabilities are realized using a Peltier element and a temperature control / regulation circuit
  Optical fibres connected to an OSA (Yokogawa A6319)
  Laser driving using external pulser / waveform generator and current source.

## Slide 12: Setup Schematic
Current Source
Waveform Generator
Temperature Regulation
PC
LabView Control Program
OSA
Thermal Enclosure
Peltier
DUT
Data Stream
Cooling
Spectra Mesaurement

## Slide 13: Setup Pictures
Thermal
Enclosure
Waveform Generator
Spectrum Analyser
Current Source for Laser

## Slide 14: Temperature Studies
Different regulation algorithms have been studied
PID algorithm has been chosen to control the Peltier element
Temperature regulation is very fast
  O(few mins)
Temperature remains very stable
  < ±0.05 °C
22 min

## Slide 15: Optical Measurements
OSA measurement time is depending on the resulotion and span:
  1.5 - 25 s per measurement (10 pm resolution)
Different analysis possible, directly in the OSA or offline on the raw data
Scan of temperature dependent spectra shows the wished behavior
Red shift of the spectrum while warming the laser

## Slide 16: Red Shift vs Temperature
Monitoring 3 peaks from the spectrum under temperature change
Temperature range 10-30°C in 1°C steps
Spectrum peaks change by
  0.0780 nm/K
  0.0779 nm/K
  0.0786 nm/K
Zooming into the range of 16-18°C measured in 0.1°C steps shows a jump
It is not yet fully understood and needs further investigation
Temperature [°C]
Temperature [°C]
Wavelength [nm]
Wavelength [nm]

## Slide 17: Interesting Topic to Look at
Peak does not shift, but more transforms into another
Polarization effect?
Wavelength [nm]
Intensity [dBm]

## Slide 18: Duty Cycle Dependency
First DC measurements performed
Increase of wavelength with introduced power
Error is RMS of the peak
Careful handling of the peak error needed
Inclusion of this measurement into the Paoli Method to be done
This measurement shows the working principle only

## Slide 19: Status of the Setup and Further Plans
The measurement itself (Paoli Method) is automized
Temperature depending spectra and duty cycle (power) depending spectra are taken automatically
Analysis tools are under investigation:
  Evaluate peaks
  Fit the Gaussian
  Extract the l shift and the gain curve
  Conclude for thermal resistance
  …
Different types of optical components (simple diode, transmitter board, …) need to be implemented, but this is prepared already.
Planned:
  Laser package optimization studies
  Test several different laser diodes (different materials, speed, wavelength … compare properties)
  Package optimization studies (heat coupling)
  Irradiation

## Slide 20: Summary and Outlook
The setup used at CERN for CMS studies has been reproduced in Wuppertal
First measurements have been taken
Spectra measured in dependence on temperature and power have been performed
Measurement can be run automatically
Analysis software is under way
More devices will be tested and the setup will be qualified further
Will be used to qualify lasers afterwards