## Slide 1: Sebastian Keckert
Overview Multilayers – RF Results
TTC Meeting
5 Feb 2020, CERN

## Slide 2: Motivation
On the way towards high gradient
S-I-S’ structure shields bulk superconductor (Nb)
  can be increased
  reduces surface resistance
[T. Kubo, Sc. Sci. Technol. 30, 023001, 2017]
[A. Gurevich, Appl. Phys. Lett. 88, 012511, 2006]

## Slide 3: Motivation
On the way towards high gradient
S-I-S’ structure promises high Bmax
More stable w.r.t. early vortex penetration?
Moderate decrease of RS
  Thick films needed for higher operating temperature !
Nb: Bsh=240 mT
NbTiN: Bsh=200 mT
S-I-S´: Bmax=273 mT
1.8 K
[T. Kubo, Sc. Sci. Technol. 30, 023001, 2017]
[A. Gurevich, Appl. Phys. Lett. 88, 012511, 2006]
Notes: Right: Assuming the same residual resistance for Nb and NbTiN

## Slide 4: Overview: Multilayer at SRF conferences
Nb3Sn / Al2O3 / Nb @ 7.5 GHz
TE011 sapphire loaded cavity 50mm disk sample
50nm Nb3Sn / Al2O3 / Nb
100nm Nb3Sn / Al2O3 / Nb
bulk Nb
[S. Sosa-Guitron, SRF’15]

## Slide 5: Overview: Multilayer at SRF conferences
100nm NbN @ 3.88 GHz, 1 mT
TE011 cavity
130mm disk sample
4x 25nm NbN / 14nm MgO
+ 5nm MgO top layer
Substrate: rough PC Nb
2x 50nm NbN / 14nm MgO
+ 5nm MgO top layer
Substrate: smooth LG Nb
[C. Baumier, SRF’13]

## Slide 6: Overview: Multilayer at SRF conferences
NbTiN / AlN / Nb @ 7.5 GHz
TE011 sapphire loaded cavity
50mm disk sample
[A.-M. Valente-Feliciano, SRF’13]
[A.-M. Valente-Feliciano, SRF’15]

## Slide 7: Overview: Multilayer at SRF conferences
75nm NbTiN / 15nm AlN / Nb @ 10 mT
[S. Keckert, SRF’19]
1286 MHz
414 MHz
845 MHz
HZB QPR, 75mm disk sample

## Slide 8: Overview: Multilayer at SRF conferences
75nm NbTiN / 15nm AlN / Nb @ 10 mT
[S. Keckert, SRF’19]
1286 MHz
414 MHz
845 MHz
HZB QPR, 75mm disk sample

## Slide 9: Overview: Multilayer at SRF conferences
S-I-S´ : 75nm NbTiN / 15nm AlN / Nb
S-S´ : 70nm NbTiN / Nb
[S. Keckert, SRF’19]
1286 MHz
414 MHz
845 MHz
[D. Tikhonov, SRF19]
HZB QPR, 75mm disk sample

## Slide 10: S-I-S´ penetration depth
9.25 K
14.3 K
Dashed lines:
Fits using S-I-S´
multilayer theory
75nm NbTiN / 15nm AlN / Nb
HZB QPR, 75mm disk sample
414 MHz, 845 MHz, 1286 MHz

## Slide 11: S-I-S´ penetration depth
14.3 K
Dashed lines: Fits using S-I-S´ multilayer theory
9.25 K
 | Nb | NbTiN
 | 9.25 | 14.3 (Lit: 17.3)
 | 44 … 46 | 240 … 250
RRR (sc) | 15 … 25 | 
RRR (nc) | 320 … 350 | 
 | 39 | (5)
 | 32 | (150 … 200)
 | Nb | NbTiN
 | 9.25 | 14.3 (Lit: 17.3)
 | 44 … 46 | 240 … 250
RRR (sc) | 15 … 25 | 
RRR (nc) | 320 … 350 | 
 | 39 | (5)
 | 32 | (150 … 200)
75nm NbTiN / 15nm AlN / Nb
HZB QPR, 75mm disk sample
414 MHz, 845 MHz, 1286 MHz

## Slide 12: S-S´ RF quench field
70nm NbTiN / Nb
No insulator
HZB QPR, 75mm disk sample
[D. Tikhonov, SRF19]

## Slide 13: S-I-S´ RF Quench field
Hard magnetic quench limit at 20-25 mT
Fit according to S-I-S´ multilayer theory
S-I-S´ allows increase of bulk limit
 | Nb | NbTiN
 | 9.3 | 14.3 (Lit: 17.3)
 | 220 … 250 | 17
 | Nb | NbTiN
 | 9.3 | 14.3 (Lit: 17.3)
 | 220 … 250 | 17
Solid lines: S-I-S´ Fit
Dashed: Extrapolation

## Slide 14: S-I-S´ RF Quench field
Hard magnetic quench limit at 20-25 mT
Fit according to S-I-S´ multilayer theory
S-I-S´ allows increase of bulk limit
 | Nb | NbTiN
 | 9.3 | 14.3 (Lit: 17.3)
 | 220 … 250 | 17
 | Nb | NbTiN
 | 9.3 | 14.3 (Lit: 17.3)
 | 220 … 250 | 17
Nb: 240 mT
NbTiN: 17 mT

## Slide 15: Conclusion
SRF characterization of multilayer structures with sample test cavities
So far: Mostly surface resistance data at high frequency and low field
Consistently: Lower RS than for Nb at higher temperature So far: Severe limitations by residual resistance
Penetration depth measurement agrees with S-I-S´ multilayer theory
First RF critical field measurements of S-I-S´ and S-S´ structures show low-field quenches
We need more data on the RF quench field !
Thank you for your attention!

## Slide 17: S-I-S´ Sample
75 nm NbTiN – 15 nm AlN – bulk Nb
[Courtesy of Anne-Marie Valente-Feliciano]

## Slide 18: S-I-S´ – R(T,B) – 845 MHz