## Slide 1
Thomas Proslier
TTC – CERN - 05/02/220
Correlations between Tunneling
Spectroscopy and SRF cavity perfomances
Notes: Saisir les champs « Titre », « P. Nom » et « Date.
Laisser ou retirer le bandeau.

## Slide 2
Collaborations:
KEK: T. Saeki, T. kubo, Marui. (thin films, theory, electropolishing)
IPNO: D. Longuevergne, M. Fouaidy, T. Pépin-donat
HZB: O. Kugeler (characterization, thin films)
DESY: M. Wenskat (characterization, thin films)
CERN: G. Rosaz, S. Calatroni (thin films)
STFC: R. Valizadeh (thin films, Nb3Sn)
INFN: C. Pira (thin films)
JLAB: A-M. Valente, G. Ciovati, D. Patshupati (Bulk Nb, thin films)
FNAL: S. Posen, A. Romanenko, A. Grassellino, M. Chechin (Bulk Nb, Nb3Sn)
ANL: A. Glatz – Theory (theory simulations)
IIT: J. Zasadzinski
TRIUMPH: T. Junginger (characterization)
Cornell: D. Hall, M. Liepe (Nb3Sn)
Team:
Technician: A. Four, E. Fayet, G. Jullien, C. Servouin
Scientist: S. Berry, C. Antoine, E. Cenni, G. Devanz, F. Eozenou, T. Proslier
Ph.D.: Sarra Bira (IPNO/CEA), Y. Kalboussi (CEA)
Internship: R. Dubroeucq, S. Habhab

## Slide 3
Point Contact Tunneling spectroscopy
Bulk Nb treatments
Nb3Sn/Nb
  Summary and future
Correlations between Tunneling
Spectroscopy and SRF cavity perfomances

## Slide 4
Point Contact Tunneling spectroscopy
Bulk Nb treatments
Nb3Sn/Nb
  Summary and future
Correlations between Tunneling
Spectroscopy and SRF cavity perfomances

## Slide 5
Tunneling spectroscopy: what do we measure and why?
Measure the fundamental superconducting parameters:
Δ, TC, HC2
Measure non-ideal signature: Γ.
Shape of the DOS give clues to microscopic origins:
Proximity effect, magnetic impurties, deleterious phases.
Direct correlation to SRF cavity performances.
Cartography.
Tc
principle
measure
Notes: Cliquez sur Insertion puis En-tête/Pied pour saisir les champs « Evènement – Date » et « Service » ; puis cliquer sur Appliquer partout.

## Slide 6
The Point Contact system at CEA
Electronics
Cryostat
Pneumatic foot
Gaz and Vacuum
Lines
Temp: 1,4 K
Magnetic field: 6 T
Cartography: 10 µm – 1 mm
Sample size: 10x10 mm
Fast measurements: 100-300 jonctions/5hrs
Transport (RRR, Tc vs H applied...)
Hall Effect
Used for Nb/Cu, bulk Nb doping, Nb3Sn, mutlilayers etc…

## Slide 7
Point Contact Tunneling spectroscopy
Bulk Nb treatments
Nb3Sn/Nb
  Summary and future
Correlations between Tunneling
Spectroscopy and SRF cavity perfomances

## Slide 8
Tunneling spectroscopy: Bulk Nb HFQS
BCP Nb – small grain Nb
Hot Spots:
spread of gap values as low as 1 meV
Inelastic scattering parameters Γ
Zero Bias Peaks
Cold Spots:
Narrow gap distibution 1.6 meV
Lower Inelastic scattering parameters Γ
No zero bias peaks

## Slide 9
Tunneling spectroscopy: bulk Nb - Why small gaps?
Presence of normal metal regions: 10 nm < dN < 15 nm -> reduce the quench field of SRF cavities: HB ~ Φ0 / (6 λN dN) Onset at 100 mT -> dN ≤ 20 nm consistent with PTC.
Transparent at low fields (Q0) but revealed at « higher » accelerating gradients.
Candidates: Nb Hydride phases at the surface (XRD at 90 K no sign of NbHX phases)
Proximity effects: MacMillan Model
Any Temperature.
Diffusive scattering
Low transparency interface (σ=0.1).
No spatial dependence
ΓS, ΓN, ΔSph , ΔNph
ΓN/S =ħ.VFN/S.σ/(2.B.dN/S)
Distinguish btw buried and surface normal metal phases

## Slide 10
Tunneling spectroscopy: Nb Doping: N and Ti
N / Ti Doping:
Narrow gap distribution
Very low Inelastic scattering Γ values
Near ideal DOS
No Zero Bias Peaks
But:
Gap values a bit lower (1.48 meV) than bulk Nb (1.6 meV)
Tc (8.7 K) < Bulk Nb Tc (9.2)
Ratio 2Δ/kTc = 4 (similar to this cavity)

## Slide 11
Tunneling spectroscopy: Nb
High Bias region
Undoped: reduced barrier height and thickness
Doped (Ti or N): higher barrier height and thickness
Points towards defects in the oxide mitigated by addition of dopants:
TLS – Hydrogen relationship and ZBP as signature
Qbits : magnetic impurities, H + O(?) as a source of it
Low fields measurements
d, thickness of the oxide
Φ, work function of the oxide
ΦTIP, work function of the tip

## Slide 12
Point Contact Tunneling spectroscopy
Bulk Nb treatments
Nb3Sn/Nb
  Summary and future
Correlations between Tunneling
Spectroscopy and SRF cavity perfomances

## Slide 13
Wupperthal method: diffusion of Sn in a Nb cavity
Nb3Sn Q0 at 4,2K ~ Nb Q0 at 2K
Moderate increase of Q0 between 4K to 2K -> Non-BCS
Q0 decrease at ~ 6K
Have we reached the limits of Nb3Sn ?
Sample position
Nb3Sn/Nb (Cornell)

## Slide 14
Nb3Sn/Nb (Cornell) - PCT
Δ > Nb and Γ/ Δ is small
-> Quality factor @ 4K is ~ Nb @ 2K
But pockets of Nb rich phases:
- Lower Tc and Δ
- Carbon contamination
ERL1-4 jan
CERES
TE1-7
Nb3Sn cavity RF tests
PCTS measurements

## Slide 15
Nb3Sn/Nb (Cornell) – TEM
phase riche Nb ~ 17.5 - 23%
Interface Nb-Nb3Sn , grain boundaries
Pockets near the surface
Crystallites ~ 100 - 200 nm (XRD)
TE1-7
CERES
ERL1-4 Jan

## Slide 16
Nb3Sn/Nb (Cornell - FNAL) – PCT
Quench field vs Average Gap
For large κ (λ/ξ = 24)
Linear dependence of Emax on the average surface gap (~300x300 µm)
HSH~3.5 times the HC1 but why this gap dependence? Roughness, effective penetration depth?
A15 compounds (V3Si, Nb3Sn, Nb3Al…) are good for Q0 and higher operation temp. (4,2 K)
But what about EMAX ? How to increase EMAX ?
Bulk Δ for Nb3Sn is 3.4 to 3.5 meV
Max expected Quench field is ~ 91 ± 2 mT = 22 MV/m

## Slide 17
Point Contact Tunneling spectroscopy
Bulk Nb treatments
Nb3Sn/Nb
  Summary and future
Correlations between Tunneling
Spectroscopy and SRF cavity perfomances

## Slide 18
Summary:
Enable testing surface treatments/heterostructures on coupons prior to cavity tests
Faster turner over and phase space exploration of growth parameters etc…
Measurement of Nb3Sn sample from FNAL
Nb3Sn : linear dependence of Emax and the superconducting gap.
Nb: à déterminer.
Future:
Faraday Cage to improve noise (ordered) ~ 3 months.
Measure of infusion in bulk Nb and Nb3Sn thin films from DESY, Jlab, STFC.
Bulk Nb: Correlation between inhomogeneous properties and samples measurements
Smaller scan areas < 1 μm.

## Slide 19
Thanks you
The END

## Slide 20
Summary
Funding Sources

## Slide 21
Tunneling spectroscopy: Nb
Hot Spot Nb
N Doped Nb
Cartography
N doping: Homogeneous bulk Nb gap values on the surface
Hot spot: Regions with low superconducting gap values that can be fitted with normal metal regions
on the surface (presumably hydrides)

## Slide 22
Rs depends on DOS(EF). DOS(EF) (B, T, Δ, r)
DOS (EF) ≠ 0 -> dissipation @ T=0 K
DOS(EF) (B, T, Δ, r), RS = <DOS(EF) (B, T, Δ)>r
Saturation mechanisms of the DOS? -> Inelastic scattering (Γ)
Higher Gap (Δ) -> Higher Q
Density of states
Tunneling spectroscopy: what do we measure and why?

## Slide 23
Cartography: calibration
Standard:
Lignes de Al(6 nm)/Nb (80 nm) sur Au (200 nm)
Calibration: X = 4,1 nm/V
Y = 4,9 nm/V
Détails la DOS

## Slide 24
Nb3Sn/Nb (Cornell) - Magnetometry
Measure critical penetration field In Bulk and thin films samples
Sample size: > 1 inch
4.2 K and 120 mT
The critical field measured by Magnetometry correlates with RF tests Quench fields
RF tests

## Slide 25
Comparaison Theory - experiments
Nb3Sn/Nb
Qualitative agreement between GL simul and PCT data
To be continued

## Slide 26
Case of surface layer Low Tc 6K + lower bulk Tc 14K
Nb3Sn/Nb - simulation
Lower bulk Tc also lead to lower penetration field.
14 K
18 K
6 K
W