## Slide 1: HEPDipo 15 T block type magnet for EPFL-SPC test facility Status of the design
06/06/19 - D. Martins Araujo
D. Martins Araujo, P. Ferracin, G. De Rijk, L. Bottura, E. Ravaioli (CERN)
P. Testoni, L. Reccia, F. Cau, A. Portone (F4E)
X. Sarasola, P. Bruzzone (EPFL-SPC)
I. Pong, G. Sabbi (LBL)

## Slide 2: Agenda
Goals and constraints
Baseline design and comparaison
3D models and results
06/06/19 - D. Martins Araujo

## Slide 3: Goals and constraints
06/06/19 - D. Martins Araujo
15 T in a rectangular aperture
Homogenous field length of 1000 mm
Rectangular aperture
Operation at 4.5 K
85% of SS

## Slide 4: Structures studied
06/06/19 - D. Martins Araujo
« Window frame »
Fresca2-like
Symmetric 3
double layered
2 double layered
Racetracks
Multiple
racetracks

## Slide 5: Window frame vs 3 double layered structure
Peak stress on the high field area
9% more superconductor
06/06/19 - D. Martins Araujo

## Slide 6: Agenda
Goals and constraints
Baseline design and comparaison
3D models and results
06/06/19 - D. Martins Araujo

## Slide 7: Baseline: 3 double layered structure
Baseline
06/06/19 - D. Martins Araujo
Cable data | 
d_strand | 1.1 mm
number of strands | 44
thickness | 2.25 mm
width | 26.5 mm
SC:Cu | 1:1
Following the FCC proposal

## Slide 8: A few block-type magnets
FRESCA2
HEPdipo
06/06/19 - D. Martins Araujo
HD2
Aperture: 100 x 150 mm
External dia: 1260 mm
100 mm
1030 mm
36 mm
704 mm

## Slide 9: A few block-type magnets (4.5 K)
FRESCA2
HEPdipo
06/06/19 - D. Martins Araujo
HD2
15 T (85%) ? | 
d_strand | 1.1 mm
n of strands | 44
thickness | 2.25 mm
width | 26.5 mm
Cu/SC | 1
13.9 T (83%) | 
d_strand | 1.0 mm
n of strands | 40
thickness | 1.89
width | 21.32 mm
Cu/SC | 1.3
13.8 T (87%) | 
d_strand | 0.8 mm
n of strands | 51
thickness | 1.4 mm
width | 22 mm
Non Cu % | 51, 54%

## Slide 10: Agenda
Goals and constraints
Baseline design and comparaison
3D models and results
06/06/19 - D. Martins Araujo

## Slide 11: Models
2D Mechanical: Ansys
2D Magnetic: Ansys, Opera and Roxie
3D Mechanical: Ansys
3D Magnetic: Ansys, Opera
06/06/19 - D. Martins Araujo

## Slide 12: Homogeneity - 2D vs 3D magnetic models Ansys and Opera - I = 14.157 kA
1% of homogeneity in 75 mm
B(0,0) = 15.2 T (3D result)
~1 % of homogeneity in 500 mm
06/06/19 - D. Martins Araujo

## Slide 13: 3D Mechanical Ansys
Pre-load
At cold
Nominal Field
Peak stress of
-43.4 MPa
Peak stress of
-119 MPa
Peak stress of
-124 MPa
06/06/19 - D. Martins Araujo