## Slide 1: Monte Carlo Model of High-Gradient Conditioning and Operation
Lee Millar1,2
1Lancaster University Engineering Department: Graeme Burt
2CERN, BE-RF Section: Walter Wuensch
RF Development Meeting
13/05/2020

## Slide 2: Backstory
Notes: Talks started a year ago.

## Slide 3: Disclaimer: Types of Conditioning
Intrinsic (BDR Conditioning):
Modification of the cavity material properties through repeated exposure to high fields.
Breakdowns nucleated by mobile dislocations in metal, largely stochastic behaviour.
Results in a sustained increase in propensity for establishing high fields.
I’ll be referring to this one today.
Extrinsic (Vacuum Conditioning):
Limited by vacuum activity.
Related to the removal of contamination on the surface. Breakdown may also be nucleated by such residual particulates.
Prevalent at low power in the early stages of conditioning, “cleans” component.
Notes: Tensile stress induces plastic behaviour, i.e. creates dislocations.
Dislocations move to surface to reduce energy.
Projection of dislocation on surface in nucleation point for continuation of breakdown process

## Slide 4: Contents
Overview of High Gradient Conditioning.
Motivation for Modelling.
Simulation Setup.
Results of the Model.
Conclusion and Future Work.

## Slide 5: High Power Conditioning
To date the Xbox test stands have successfully conditioned many structures (and high power RF components).
Generally follows three phases:
Increasing gradient/power while keeping constant BDR.
Drop the power, increase the pulse length (50, 100, 150, 200ns) and ramp back up.
Finally, the BDR drops.
Work hardened copper
Figure: A typical conditioning curve.

## Slide 6: High Power Conditioning
Conditioning is now automated and accomplished algorithmically [1,2].
Occasionally we must deviate from the “ideal” case, but the behaviour is typically comparable.
A key point is that conditioning takes many (≈hundreds of millions) pulses and is reproducible, implying a well defined underlying physical mechanism.
Figure: Initial conditioning of many structures conditioned to date normalised to BDR and Pulse length. Note the asymptotic behaviour.

## Slide 7: High Power Conditioning
Conditioning is now automated and accomplished algorithmically [1,2].
Occasionally we must deviate from the “ideal” case, but the behaviour is typically comparable.
A key point is that conditioning takes many (≈hundreds of millions) pulses and is reproducible, implying a well defined underlying physical mechanism.
Several other observations have emerged too…
Work hardened copper
Figure: Typical behaviour overlaid on existing structure test data.
“Typical” Behaviour
Notes: Dynamic, changes with time I.e long time and history, and short timescale (plasmons, pulse shape), single pulse i.e. bd

## Slide 8: High Power Conditioning Limit
However we cannot condition indefinitely, there is an intrinsic limit which cannot be exceeded (the asymptotic behaviour shown below).
Figure: Full conditioning history of a TD26CC [3].
Quasi-limit
Notes: 220MV/m, beta of 30 or at least 10s range means we have GV fields which rip deformations/emission sites apart.

## Slide 9: The Conditioning Process
Initially suspected that BDs were the quantity on which we condition.
Later proposed that structures condition on the number of pulses not the number of breakdowns [3].
Cleanliness of preparation was however shown to affect number of breakdowns during conditioning, not ultimate performance [4].
Figure: Scaled gradient vs. cumulative no. pulses (top) and scaled gradient vs. cumulative no. breakdowns (bottom) for four different structures[3].
Notes: Mevex still condition on BDs.
In 2010 SLAC conditioned two identical structures, one of which was built processed and hermetically sealed at KEK then assembled at SLAC under the best available conditions similar to those of superconducting cavities while the other was subject to conventional methods (18). nt: ≤ 3x10-7 bpp/m.

## Slide 10: Recent Evidence for Conditioning on Pulses
Figure: Superstructure test results showing structure A (top) and structure B (bottom).
The ongoing superstructure test shows one structure to have a BDR orders of magnitude lower than the other.
Structure A ≈ 11,000 BDs
Structure B ≈ 400 BDs (some of which were provoked)
Reasonable evidence for this hypothesis.
Notes: Provoked by reflected power in 2nd structure. Also we had software issues where it send a long flat pulse with same peak power, provoked BDs in both.

## Slide 11: Interpretation of Conditioning
If held sufficiently close to inducing breakdown, the surface’s propensity to establish high field/endure power flow increases (what we call conditioning).
Unconditioned = high BD probability at low power/field.
Conditioned = low BD probability below the level to which it has been conditioned.
However we can’t condition indefinitely, each material has an intrinsic ultimate limit above which we cannot condition/operate.
Electrical Quantity e.g. Input Power
Breakdown Probability
Characteristic of a poorly conditioned structure
Conditioning shifts this line.
Maximum Permissible BDR
Ultimate Field Limit
Characteristic of a well conditioned structure

## Slide 12: Interpretation of SuperStructure Results
Notes: With the BDR as our process variable our conditioning algorithm then acts as a PID loop which tracks this BD threshold.
It appears that the second structure has consistently been held sufficiently close to breakdown to condition, but not to induce the breakdown itself.
If this interpretation is correct, it has some interesting implications

## Slide 13: Low BDR Conditioning Regime
Suggests increasing the input power while remaining below the point of breakdown induction should allow conditioning to high power without inducing breakdown.
Currently impracticable, breakdowns are the mechanism on which we feed back (unless we use a sacrificial cavity).
But is it worthwhile to do so?
This is a talk for another occasion….
Cumulative RF Pulses (Log Scale)
-- Power required for __ __ __significant BD probability.
-- Conditioning Threshold
—Ultimate Limit
— Low BDR conditioning __Regime.
Input Power
Notes: In other words the breakdowns may be mostly inessential.
We accumulate thousands of BDs and still operate at HG.

## Slide 14: Contents
Overview of High Gradient Conditioning.
Motivation for Modelling.
Simulation Setup.
Preliminary Results of the Model.
Conclusion and Future Work.

## Slide 15: Automation of Conditioning
Several years ago a conditioning algorithm was developed on XB1 to automate conditioning using a two level hierarchy (respond to short and long term behavior).
Short-term behaviour (seconds to minutes):
Steps up in power regularly, BDs can cause a drop in power.
Long term behaviour:
BDR is measured in a user defined window.
If above the user defined threshold the power level can no longer be increased.
Subsequent breakdowns will still reduce the power as described previously.
A BD here would cause a drop in power by 2.5kW
Note: There are of course other interlocks which are not mentioned on this slide.

## Slide 16: Automation of Conditioning
Was implemented pragmatically, similar empirically derived procedures also in place at KEK, Daresbury, SLAC.
Has since conditioned many structures however to my knowledge was never the subjected to thorough modelling and optimisation.
Any features added/tuned were done so as a consequence of operational observations i.e. responsive implementation.
Figure: Conditioning curves for various X-band structures.
Notes: It worked and so parameters were carried forward, other facilities have their own algorithms in place

## Slide 17: Why Model Conditioning?
In recent years several suggestions have emerged:
Cluster management (implemented).
Recovery mode following large power drops.
Gaussian BDR measurement window to improve dynamic behaviour.
Of course tests require a long timeframe and significant expense…
Would be nice to examine the macroscopic consequences of such features without the risk (and monetary/temporal expense) of sacrificing a structure.
Figure: Comparison of BDRs calculated with different windowing presented by Jan Paszkiewicz in 2018 [5].

## Slide 18: Contents
Overview of High Gradient Conditioning.
Motivation for Modelling.
Simulation Setup.
Preliminary Results of the Model.
Conclusion and Future Work.

## Slide 19: Another disclaimer…..
As Sergio kindly pointed out a very nice study on the LES was also previously carried out however with some different objectives.
Today I’ll be focusing on macroscopic consequences of algorithmic changes in our conditioning procedure in the test stands.

## Slide 20: Conditioning Process
Evidence suggests we condition on pulses, the present model is then fundamentally built around the idea of progressive modification of the surface on a pulse to pulse basis.
Of course we’ll need some behavioural characteristics on which to base any assumptions we make.
Notes: Does exclude some features, pulse length, time of bd in pulse etc.

## Slide 21: Conditioning Simulation: Broad overview
Input Values
Pulse RF
Modify Surface
Software PID Loop
(Determines characteristics of next pulse)
Calculate BDR
Check for BD
Run
Exit simulation and plot
Pulse goal not met
Pulse goal met
Notes: Looks at probabilistic behaviour of test stand as a whole.
The present model is built around an idea of progressive
surface modification

## Slide 22: Conditioning Simulation: Broad overview
Input Values
Pulse RF
Modify Surface
Software PID Loop
(Determines characteristics of next pulse)
Calculate BDR
Check for BD
Run
Exit simulation and plot
Pulse goal not met
Pulse goal met
?
All but two of these functions are already well defined.
Notes: Looks at probabilistic behaviour of test stand as a whole.
The present model is built around an idea of progressive
surface modification

## Slide 23: Conditioning Simulator: BD Probability
We then need several functions which encapsulate our previously observed behaviour… let’s first define a few useful terms.
EOperate= The accelerating gradient at which we operate.
EState = Represents the conditioned state of the surface, modified on a pulse to pulse basis.
ESat = The maximum achievable gradient, i.e. saturation point (typically ≈ 110-120MV/m).
Notes: OR BDR=10^-5(Eoperate/Estate)^(15x(1+Eoperate/Estate))

## Slide 24: Conditioning Simulation: Surface Modification
Based on our previous interpretation let us assume the structure exists in a certain conditioning state, Estate and we pulse at a given field level Eoperate.
We need a term to modify the surface every pulse i.e. describe conditioning.
It must increases with Eoperate but approach zero in the later stages of conditioning as we reach the limit, Esat.
Gradient (MV/m)
Cumulative RF Pulses
Eoperate
ESat
EState
24
Figure: Visualisation of proposed quantities during conditioning.

## Slide 25: Conditioning Simulator: BD Probability
It has been proposed empirically that surface electric field and BDR have a strong relation [6,7].
There is generally a low probability of breakdown when operating close to the level at which it is conditioned (one in tens of thousands).
The probability of BD decreases as we condition i.e. as Estate increases while a high gradient, Eoperate increases the probability of breakdown.
The probability of a BD on a given pulse might then be defined:
x

## Slide 26: Conditioning Simulator: BD Probability
Data also shows breakdowns are statistically more likely to occur in groups (tend to occur spatially close together, presumably due to formation of new emission sites/sputtering)[8].
We can then simply add a probability density function based on existing data:
Thus the BDR curve progresses as we condition and the 1E-5 base value allows tuning.
Figure: Probability distribution of test stand data[4].

## Slide 27: Contents
Overview of High Gradient Conditioning.
Motivation for Modelling.
Simulation Setup.
Preliminary Results of the Model.
Conclusion and Future Work.

## Slide 28: Conditioning Simulation: Benchmarking
The model will obviously require some iterative tuning and adjustment.
For this purpose it is useful to define some sort of typical behaviour.
We don’t yet have a pulse length dependence, so we are limited to the preliminary behaviour.

## Slide 29: Typical Conditioning of Structures
“Typical” curve
(variance between structures, software settings, operational deviations etc.)
Figure: Proposed typical conditioning curve overlaid on test stand data.

## Slide 30: Typical Conditioning of Structures
“Typical” BD accumulation ends up in the thousands range.
Figure: Proposed typical BD accumulation overlaid on test stand data.

## Slide 31: Typical Conditioning of Structures
Gives us some approximate goal for tuning our parameters.
Figure: Benchmark used for tuning model.

## Slide 32: Preliminary Simulation Result
Figure: Results of preliminary simulation.

## Slide 33: Preliminary Simulation Result
BDR setpoint tracked.
Asymptotic conditioning.
Reasonably
Linear BD accumulation, could be improved.

## Slide 34: Result 1: Comparison with Real Data
Simulated conditioning in red

## Slide 35: Result 2: Running Longer Term

## Slide 36: Result 2: Running Longer Term
BDR begins to drop during flat run in at rate comparable to test stands.

## Slide 37: Result 3: Effect of Changing Setpoint.
Algorithm controls power to track the BDR Setpoint shown here.
Historically we have used 5E-5 (one breakdown in 20k pulses) but what happens when varied?

## Slide 38: Result 3: Effect of Setpoint on Conditioning.
Some experimental data:
PolariX Setpoint: 3E-5
Crab Setpoint: 5E-5
Result:
PolariX accumulated fewer BDs.

## Slide 39: Result 3: Effect of Changing BDR Setpoint.
Simulation run three times with a different BDR setpoint each time.
Still requires checking and more investigation but seems to indicate a similar result.

## Slide 40: Result 4: Dual Structure Simulation.
What about the case of two structures?
We set one to have a slightly higher limit, Esat or an initially higher Estate.
Does the idea of progressive modification or surface while being held at low BD probability agree?
In this example, the limit for the second structure was increased by 5MV/m.

## Slide 41: Result 4: Dual Structure Simulation.
Structure A
Structure B
Notes: Shows even a small difference in the limit (or the start point) yields the same conditioning curve but changes the number of accumulated BDs.

## Slide 42: Contents
Overview of High Gradient Conditioning.
Motivation for Modelling.
Simulation Setup.
Preliminary Results of the Model.
Conclusion and Future Work.

## Slide 43: Conditioning Simulator: Conclusion
Although in the early stages a very simple lumped model based on a pulse to pulse modification of the surface has been created and tuned to give reasonable agreement with test stand data.
Altering the PID loop settings yields results which align with those observed in the test stands.
May eventually be used to investigate the implications of algorithmic values/methods and provide a suggestion of “optimal” settings.

## Slide 44: Conditioning Simulator: Future Work
Validate and Correct Model:
Additional tuning.
Review past data control settings and implement in code to check for agreement.
Comparison with DC Test data.
Investigations:
Explore alternative algorithmic features (gaussian BDR window, alternative ramping, varying setpoints etc.).
Addition of pulse length dependence.
Vacuum conditioning model.
Power/ E-field BDR dependencies.

## Slide 45: Thank you. Questions/Discussion?

## Slide 46: References
[1] –B. Woolley, “High Power X-band RF Test Stand Development and High Power Testing of the CLIC Crab Cavity,” Lancaster University, United Kingdom, 2015.
[2] – L.Millar, “Conditioning and Operational Algorithms”, Presentation, Available online: https://indico.cern.ch/event/719535/
[3] – J. Giner Navarro, Breakdown Studies for High Gradient Rf Warm Technology in: CLIC and Hadron Therapy Linacs, University of Valencia, 2016.
[4] – Study of Basic Breakdown Phenomena in. Dolgashev, V.A. Tsukuba, Japan : s.n., 2010. XXV International Linear Accelerator Conference (Presentation).
[5] – J.Paszkiewicz, “X-Band RF Test Stands at CERN” Presentation at SINAP, Shanghai, 4-8 June 2018, Available online: https://indico.cern.ch/event/675785/contributions/3022037/attachments/1661499/2662246/CERN_Xboxes_Jan_Paszkiewicz_HG18.pdf
[6] –New local field quantity describing the high gradient limit of accelerating structure. Wuensch, W. et al. 10, s.l. : American Physical Society, 2009, Phys. Rev. ST Accel. Beams, Vol. 12.
[7] - https://indico.cern.ch/event/449801/contributions/1945266/attachments/1212465/1770218/korsback_clicworkshop16_v3.pdf
[8] – Statistics of vacuum breakdown in the high-gradient and low-rate regime. Wuensch, W. et al. 10, s.l. : American Physical Society, 2009, Phys. Rev. Accel. Beams 20, 011007 – Published 25 January 2017, Available online: https://journals.aps.org/prab/pdf/10.1103/PhysRevAccelBeams.20.011007
Notes: [9] –Defect model for the dependence of breakdown rate on external electric fields, Nordlund and F. Djurabekova, Phys. Rev. ST Accel. Beams 15, 071002 (2012).
[10] - Stochastic Model of Breakdown Nucleation under Intense Electric Fields, Zvi Engelberg et al. (2018). Physical Review Letters. 120. 10.1103/PhysRevLett.120.124801
[11] -- J.Paszkiewicz, “Breakdown-Loaded Electric Fieldas a High Gradient Limit” Presentation at MeVArc 2019, Padovaat, Available online:https://indico.cern.ch/event/774138/contributions/3507942/attachments/1908081/3151939/Breakdown_Limit_MeVArc_2019_Jan_Paszkiewicz.pdf

## Slide 47: Automation of the Conditioning Process
Several years ago a conditioning algorithm was developed on the XB1 software to automate this process using a two level hierarchy (respond to short and long term behavior).
Short-term behavior(seconds to minutes):
  A graphical representation pictured right. The vertical red bar scrolls to the right as time increases. If the red bar gets to the step-up in the blue curve, the power level is increased by the size of the step (in this case 10 kW). The timer is then reset and the red bar starts again from 0 seconds.
  If the structure is operating near its conditioned limit, the increase in power may trigger a breakdown shortly after. The slope in the blue line is designed to lower the power level if a breakdown occurs shortly after the previous “event”.
Long term behaviour:
  BDR is measured in a user defined window.
  If the measured BDR increases above a user defined threshold the power level can no longer be increased by the software.
  Subsequent breakdowns will however reduce the power as described previously.
A BD here would cause a drop in power by 2.5kW
Note: There are of course other interlocks which are not mentioned on this slide.

## Slide 48: Current Algorithm
I have attempted to condense the existing algorithm into a (greatly simplified) block diagram. (Pictured right)
Does not show PID loop gains and several other fine details for the sake of simplicity.
Power Step
Ramp Time
Step Time

## Slide 49: Ramp Settings in the Test Stands
Chart: Power Ramp in Operation
| 0 | 10000 | 15000 | 15000 | 16000
Line1 | -10 | 0 | 0 | 10 | 10
Line 2 | -10 | 0 | 0 | 10 | 10
Line 3 | -10 | 0 | 0 | 10
Line 4 | -10 | 0 | 0 | 10 | 10
XBOX2 | -10 | 0 | 0 | 10 | 10

## Slide 50: Initial Conditioning of Structures
Initial conditioning at 50ns Pulse length

## Slide 51: Superstructure BDR Distinction
The structures show an large discrepancy in the accumulated breakdowns to date.
Structure A: ≈ 12000
Structure B: ≈ 300
However they have been subjected to the same ramp in input power. Lets examine the conditioning in terms of their cumulative BDs instead…
Figure: Cumulative breakdowns vs pulse number for the CLIC superstructure constituents.

## Slide 52: Initial Conditioning of Structures
Initial conditioning at 50ns Pulse length