## Slide 1: HEL collector
Giorgia Gobbi, Antti Kolehmainen, Diego Perini
01/07/2019

## Slide 2: Specifications
Collector: used to collect electron cloud and dissipate its energy
Material: CuCr1Zr
Dimensions: 340xØ350 mm
Active cooling via circulating water
Power to absorb: 75 kW maximum value
Magnetic shield
  Electrical insulation
Restrictions:
  Cu max temperature < 90°C for UHV compatibility
  Initial flow speed max 1.0 m/s
  Size limitations
Cooling circuits - Lapland Design
electrical insulation
magnetic shield
cooling circuit
33 channels in parallel Ø = 10 mm

## Slide 3: CuCr1Zr - Results
Load: 50 kW
Vin water = 1.0 m/s
Material: CuCr1Zr  Tsoftening = 450 - 500 ºC
Tmax Cu = 63 ºC
ΔT water = 16 ºC
vmax water = 2.7 m/s

## Slide 4: CuCr1Zr - Results (1.5*Load)
Tmax Cu = 83 ºC
ΔT water = 24 ºC
vmax water = 2.7 m/s
Load: 75 kW
Vin water = 1.0 m/s
Material: CuCr1Zr  Tsoftening = 450 - 500 ºC

## Slide 5: Manufacturing and plan
electrical insulation
magnetic shield
cooling circuit
To be defined based on BINP beam dynamics simulations. It should include:
Electrodes
Resistive coil / permanent magnet
Flange SS brazed on CuCr1Zr
Drawings  2 months
Pieces manufactured  5 months
Inputs from BINP and BE/BI needed as soon as possible
Drill channels
Drill channels
Close with mechanical joint

## Slide 6: Conclusions
Collector simulations performed starting from previous outcome of particle trajectory
Recommend to use CuCr1Zr for higher softening temperature
With 50 kW and an initial water velocity of 1 m/s collector presents no issues
Tested also at 75 kW and no issues from a structural point of view were detected T to be checked with vacuum colleagues
Manufacturing feasibility checked with the EN-MME workshop
Waiting from inputs to start with the manufacturing

## Slide 7
Thanks for your attention

## Slide 8: Copper – Results
COMSOL: Coupling heat transfer – turbulent flow analysis
Load: 50 kW
Material: Copper
Vin water = 1.5 m/s
Tmax Cu = 52 ºC
ΔT water = 12 ºC
vmax water = 4 m/s

## Slide 9: Copper - Results (1.5*Load)
Tmax Cu = 75 ºC
ΔT water = 23 ºC
vmax water = 2.7 m/s
COMSOL: Coupling heat transfer – turbulent flow analysis
Load: 75 kW
Material: Copper
Vin water = 1.0 m/s