## Slide 1: The monolithic ASIC for the high precision preshower detector of the FASER experiment at the LHC
L. Paolozzi
on behalf of the FASER collaboration

## Slide 2: The FASER experiment at LHC
ForwArd Search ExpeRiment
Designed to search for light and weakly-interacting particles + study the interactions of high-energy neutrinos (FaserNu)
Fluxes of high-energy SM particles are supressed
Muons and neutrinos only exception
FASER can probe Axion-Like-Particles (ALPs) model
Zero degrees angle  huge LLPs flux
Picture taken from symmetry magazine. Artwork by Sandbox Studio, Chicago with Ana Kova.

## Slide 3: The upgrade of the FASER preshower detector
Current pre-shower:
2 layers of tungsten (1X0) + scintillating detectors No XY granularity.
The upgrade:
A high-granularity/high dynamic range pre-shower based on monolithic silicon pixel sensors.
Discriminate TeV scale electromagnetic showers.
Targeting data taking during last year of LHC run 3 and during HL-LHC.

## Slide 4: The upgrade of the FASER preshower detector
VETO
Decay Volume
Tracker
Current
pre-shower
Calorimeter
Two Fermion signal
VETO
Decay Volume
Tracker
Current
pre-shower
Calorimeter
Two Photon signal

## Slide 5: The upgrade of the FASER preshower detector
VETO
Decay Volume
Tracker
High-granularity
pre-shower
Calorimeter
Two Fermion signal
VETO
Decay Volume
Tracker
Calorimeter
Two Photon signal
High-granularity
pre-shower

## Slide 6: Motivations for a new pre-shower detector
Enables measurement:
  Axion-Like Particles (ALP) produced via aWW coupling.
  LLP with neutral pions in the final state.
  Neutrino background suppression.
Reinforces measurement:
  Dark photon and other LLPs decaying into charged fermions.
  LLP with charged and neutral pions in the final state.
Detector requirement:
  Discriminate photons with 200 µm separation to exploit the full potential of the experiment.
Discovery potential for ALP

## Slide 7
= 1 TeV
= 1 TeV
d(
PLANE 3
x [μm ]
y [μm ]
Events simulated
using Allpix squared
100 µm pixel pitch
Why 6 planes?
Why pixelated sensors?

## Slide 8
Events simulated
using Allpix squared
100 µm pixel pitch
Why 6 planes?
Why pixelated sensors?
PLANE 4
x [μm ]
y [μm ]
= 1 TeV
= 1 TeV
d(
High dynamic range for charge measurement

## Slide 9
Events simulated
using Allpix squared
100 µm pixel pitch
Why 6 planes?
Why pixelated sensors?
PLANE 5
x [μm ]
y [μm ]
= 1 TeV
= 1 TeV
d(

## Slide 10
Events simulated
using Allpix squared
100 µm pixel pitch
Why 6 planes?
Why pixelated sensors?
PLANE 6
x [μm ]
y [μm ]
= 1 TeV
= 1 TeV
d(

## Slide 11
Events simulated
using Allpix squared
100 µm pixel pitch
Why 6 planes?
Why pixelated sensors?
PLANE 6
x [μm ]
y [μm ]
= 1 TeV
= 1 TeV
d(
Fake cores from low energy electrons
Very large occupancy

## Slide 12: Monolithic ASIC architecture
65 μm
Chip size of 2.2 x 1.5 cm2, with matrix of 208 x 128 pixels (26’624 total pixels)
13 super-columns (SC) which consist of:
  An active region
  A digital column in the middle (40 µm width), which is inactive
  A SC is composed of 8 super-pixels (SP) of 16x16 pixels.
The dead area in the periphery consists of:
  720 µm on the readout side for the digital processing and I/Os
  270 µm on the guard ring sides
First large-area monolithic detector in SiGe BiCMOS

## Slide 13: Monolithic ASIC architecture: Super-pixel
Flash-ADC
The charge needs to be measured for each pixel: acts as an imaging device.
Data is stored on the capacitor in each pixel and converted on the fly with a flash ADC. 256-to-1 MUX.
The capacitor is charged with a constant current during the TOT.
The same ADC will poll all the pixels in a superpixel and convert them as needed.

## Slide 14: Monolithic ASIC architecture: Super-columns
Super-column logic: it masks the pixels, generates the test-pulses, drives the analog MUX, handles readout and communication with periphery.
Unusual aspect ratio: 1.4 cm by 40 µm.
Super-column level frame-based solution for readout logic in the periphery.
Two clock domains: 50 MHz (programming phase) and 200 MHz (readout phase).

## Slide 15: Monolithic ASIC architecture: Periphery and I/O
All the logic is in the super-column.
The periphery interrogates the super-columns from left to right, and handles the chip I/O.
Data are not stored in the chip, but they are sent out on the fly at 200 Mbit/s.
A second output line can be activated, that reads the columns from right to left.

## Slide 16: Monolithic ASIC layout
220 Ωcm resistivity substrate
Limitations on active area thickness

## Slide 17: Monolithic ASIC layout
220 Ωcm resistivity substrate
Limitations on active area thickness
Triple–well design
Isolation of pmos in pixel is not possible
HBT requires AC coupling to pixel
Limited integration of digital electronics in pixel

## Slide 18: Monolithic ASIC layout
220 Ωcm resistivity substrate
Limitations on active area thickness
Triple–well design
Isolation of pmos in pixel is not possible
HBT requires AC coupling to pixel
Limited integration of digital electronics in pixel
Signal routing after discrimination stage
Line shielding to avoid cross talk
Take advantage of HBT robustness to parasitics

## Slide 19: Front-end electronics
BJT-based preamp with MOS feedback inside pixel area.
Analog memory in pixel.
Low-power discriminator (inside the pixel area)
Memory control circuit outside pixel.
Discriminator output activates the charging of the capacitor Cmem.
FRONT-END
ANALOG MEMORY
MEMORY CTRL, MASK AND FAST-OR

## Slide 20: Front-end + Memory control

## Slide 21: Pre-production prototype
Large area, fully functional prototype.
Three alternative test layouts submitted:
  V1: 4-supercolumn reference design with MOS based discriminator (outside pixel).
  V2: 3-supercolumn variant with BJT-based discriminators featuring lower pixel-to-pixel mismatch (inside pixel).
  V3: 3-supercolumn variant with simplified readout architecture (no analog memory, counters for TOT measurement).
Tests start in June 2022.
7.5 mm
15 mm

## Slide 22: Test of pre-production prototypes
Pre-production wafers have arrived
3 standard wafers
3 special epi wafers
53 chips / layout / wafer

## Slide 23: HV test on probe station
Standard wafer
Scratch with needle
Internal guard ring not referred to ground
Epi wafer

## Slide 24: Test on board
First prototypes were bonded and are currently under test.

## Slide 25: Test with FAST-OR circuits: TOT mismatch
Analog: 0.7 µA / pixel
Analog: 2.3 µA / pixel
Some mismatch observed from amplifier response: need to increase the size of load transistors
Preliminary
Preliminary

## Slide 26: Test with FAST-OR circuits: TOT mismatch
Lesson learned:
Improvement of front-end response uniformity in production ASIC.
Front-end mismatch in pre-production prototype
(Cadence Spectre simulation)
Front-end mismatch in production ASIC
(Cadence Spectre simulation)

## Slide 27: Test with FAST-OR circuits: time resolution
Analog: 0.7 µA / pixel
Analog: 2.3 µA / pixel
Excellent timing performance for the entire range under test
Preliminary
Preliminary

## Slide 28: Test with Readout
The readout of V2 is identical to the one envisaged for the final chip.
Corresponding pixels from different super-pixels are read in parallel.
Results will be shown for a conservative readout speed of 20 MHz.
Tests at 50 MHz and 100 MHz were also successful, but they require to adapt the delays to match the cable length.
NOTE: drift of analog memory observed, will require action for final chip. Preproduction prototype can be tested only at high rate.

## Slide 29: Front-end + Memory control

## Slide 30: Test with Readout: memory drift
Memory drift, load 5
Memory drift, load 10
__ -40 C
__ 0 C
__ 20 C
__ 40 C
__ -40 C
__ 0 C
__ 20 C
__ 40 C
At room temperature the minimum hit rate is 700 Hz: leakage ~ 85 pA
At -40 C the minimum hit rate is 1 Hz: leakage ~ 60 fA
The pedestal is time dependent and it disappears at low temperature, suggesting the presence of a current leakage.
Moreover, the independence from the memory load current allowed to identify the issue as due to the leakage through the gates of the analog MUX.
A solution to this issue has been already implemented in the final chip.

## Slide 31: Test with Readout – testpulse calibration
Before calibration
After calibration
Injected charge

## Slide 32: Test with Readout – Calibrated laser response
The pixels below have names: they were selected due to their large mismatch

## Slide 33: Conclusions
FASER pre-shower upgrade will be instrumented with the SiGe MAPS designed and developed at UniGe. The chip will be a fast-imaging pixel detector for ultra-high-energy electromagnetic showers.
The pre-production chips delivered in June are working fine with the lab characterization.
Minor bugs have been identified and they will be corrected. Further studies are planned to consolidate the final chip design.
In the last year of Run-3 data taking FASER should have capability needed for two closely spaced photons detection and extend the sensitivity reach in the ALP phase-space.

## Slide 34: Backup

## Slide 36: Cross talk shielding from previous prototype

## Slide 37: TDC test (preliminary)
Independent from charge readout.
The ring oscillator can be operated at digital power supply or at dedicated voltage.
Operation at digital power supply: binning estimated at 160 ps.
0 0 1 0 1 0 1
0 1 1 0 1 0 1
0 1 0 0 1 0 1
0 1 0 1 1 0 1
0 1 0 1 0 0 1
0 1 0 1 0 1 1
0 1 0 1 0 1 0
1 1 0 1 0 1 0
1 0 0 1 0 1 0
1 0 1 1 0 1 0
1 0 1 0 0 1 0
1 0 1 0 1 1 0
1 0 1 0 1 0 0
1 0 1 0 1 0 1
7 bits, 14 states allowed, 114 states forbidden
Allowed states appear, showing that the TDC is operating as expected.

## Slide 38: TDC test (preliminary)
Very few forbidden states, mapped to -1.
Possibly bubble errors that can be corrected.
Poor DNL (one bit is essentially lost).
Increase size of Ring Oscillator.
Adjust voltage.
Don’t care

## Slide 39: 256:1 analog MUX
Proposed design: multi-stage approach.
8 stage of 2-to-1 MUXs in series.
Lower capacitance seen at each node than token ring solution.
A0
A1
A2
To
Flash-ADC
23=8 pixels example

## Slide 40: 256:1 analog MUX
Problem of the proposed design: the polling leads to the sharing of the charges of the pixels with ‘higher’ addresses.
This is due to the switching of the LSB of the address (A0 in the example).
Solution: additional switches connected to the MUX inputs.
A2A1A0=000
A2A1A0=001
A2A1A0=010

## Slide 41: 256:1 analog MUX
Solution: additional switches connected to the MUX inputs.
For this example:
  Pixel2-3: S2-3 AND with A1
  Pixel4-5: S4-5 AND with A2
  Pixel6-7: S6-7 AND with A1,A2
Pixel0
Pixel1
Pixel2
Pixel3
Pixel4
Pixel5
Pixel6
Pixel7
A1
A2
S0
S1
S2
S3
S4
S5
S6
S7

## Slide 42: 256:1 analog MUX
In a N-bit case, there will be 2N-1 couples of pixels.
The couples can be coded in binary words C of N-1 bit.
It is possible to demonstrate that the i-th couple needs a number of AND inputs equal to the number of 1s in the corresponding word C.
In the N=8 case the number of additional AND inputs needed will be:
In the token ring solution, 256 D-flip-flops are required.
Pixel0
Pixel1
Pixel2
Pixel3
Pixel4
Pixel5
Pixel6
Pixel7
A1
A2
S0
S1
S2
S3
S4
S5
S6
S7