## Slide 1: WP6a: HL-LHC Cold Powering
Amalia Ballarino
International Review of HL-LHC Magnet Circuits, 9th - 10th September 2019

## Slide 2: The HL-LHC Cold Powering System
MgB2 to HTS
-Plate
1
DF
T117 K
T250 K
MgB2
HTS
MgB2 to Nb-Ti
Nb-Ti to Nb-Ti
Nb-Ti – 1.9 K
2
SC Link (DSL)
3
DFH
4
Current Leads (DFLH)
Interface to WP3
Nb-Ti to Nb-Ti
WP3 - Magnets (-plate with Nb-Ti)
WP9 - Cryo
WP17 – WP6b
WP15 - Integration
WP16 - String
WP7 - Protection
WP12 - Vacuum
LHe
4.2 K
Tdesign MgB2  25 K
Tdesign HTS  60 K

## Slide 3: Cold Powering System in LHC underground
A. Ballarino
3
A. Ballarino
3
Q1 to Q3
CP
D1
D2
Q5
Q4
Atlas
Q6
Triplets
Matching Section
UL Gallery
LHC Tunnel
DFHX
DFHM
DFX
DFM

## Slide 4: Cold Powering System in LHC underground
D2 and DFM
DFHM
DFHX
DFX
VALVES BOX
SC Link for Triplets
≈ 100 m
D1
SC Link for
Matching Sections
≈ 130 m
Power converters
Power converters
Cryostat and leads
Cryostat and leads
 8 m
Shaft  = 1m

## Slide 5: Electrical components and design parameters
Number and type of components
Design currents
HV Withstand levels
Protection strategy

## Slide 6: Electrical circuits
One main 18 kA circuit
Two Trims: 22 kA (Q1 and Q3)
k-modulation: 10.035 kA (Q1a)
In addition: D1, Orbit Correctors and Higher Order Correctors individually powered:
Triplets
Matching Sections
D2 and its Correctors
individually powered

## Slide 7: Design Currents: Baseline for Triplets
Local Powering
(also k-mod
within WP3)
SC Link
SC Link
Itot (SC Link)  120 kA

## Slide 8: Design Currents: Baseline for Matching Sections
 | Iult (kA) | Ileads/cables (kA) | Nleads | Ncables
D2 | 13367 | 18 | 2 | 2
MCBRD | 0.422 | 0.6 | 8 | 8
D2 and its correctors
Itot(SC Link)  31 kA
Ratings for series units (ITs and MSs): 18 kA, 2 kA, 7 kA and 0.6 kA

## Slide 9: Number of components
Ten SC Links of two different types (4 for ITs plus 4 for MSs plus one spare per type) for powering the HL-LHC Triplets region and the HL-LHC Matching Sections
Ten DFH cryostats (4 for ITs plus 4 for MSs plus one spare per type)
Ten DF cryostats (4 for ITs plus 4 for MSs plus one spare per type)
176 HTS Current leads (148 for series plus few spares per lead type) for powering the HL-LHC ITs + 50 HTS Current leads (40 plus few spares per lead type) for powering the MSs (226 units in total)
Two Cold Powering System topologies (One for ITs and one for MSs)
Four Cold Powering Systems per topology

## Slide 10: HV Levels - Triplets
RT = Room Temperature (20 ± 5 °C)
NOC = Nominal Operating Conditions. For all WP6s components, it corresponds to
GHe at RT and 1.30 ± 0.05 bar

## Slide 11: HV Levels – Matching Sections
D2: treated as for a 18 kA circuit – conservative
18 kA
D2
D2 correctors: 0.6 kA rating, Worst case to ground = 590 V, Components test: 5.7 kV (RT) -
Components test 2.860 kV (NOC)

## Slide 12: Protection Strategy
System designed when cold diodes not in the baseline

## Slide 13: System design – Electrical components

## Slide 14: System design – Electrical components
MgB2 cables

## Slide 15: SC MgB2 Cable Design - Triplets
Baseline
ext  90 mm
7.5 mm
1
2
3
1,2,3  Instrumentation wires
Cu core
Cu braid

## Slide 16: MgB2 cable design – Triplets
- 18 kA
Protective insulation (outer layer)
 90 mm
+ 18 kA
3  2  2 kA
3 2  2 kA
3 7 kA
+ 13 kA
- 13 kA
MgB2 wire
Copper stabilizer
Filler
Insulation
3  7 kA
4  18 kA
6  2  3 kA
A. Ballarino

## Slide 17: MgB2 cable - Triplets
Bmax=0.76 T
+ 13kA
- 13kA
+ 18kA
- 18kA
A. Ballarino

## Slide 18: SC MgB2 Cable Design – Matching Sections
1
1  Instrumentation wires
ext  60 mm

## Slide 19: Status of cabling activity
Each cable type assembled and electro-mechanically characterized at CERN
Cables (18-strand sub-cable, 18 kA cable, 2 kA coaxial-cable) produced in industry (ICAS, cabling at Tratos cavi) via R&D contracts and electro-mechanically characterized at CERN (including HV testing in Ghe)
Contracts for full scale prototypes (80 m long, one copper and one MgB2, - for ITs and MSs) and for series production placed in industry – price enquiry in 2018 followed by adjudication (ICAS) at FC Dec 2018. Completed first 80 m long copper prototype cable for IT. Assembly of 80 m long MgB2 cable for Its is on-going in industry (delivery to CERN planned by end of October 2019)
Validation of cabling parameters and materials completed for ITs

## Slide 20: Example of qualification at CERN
cable = 6.5 mm
*
* Extracted from 18 kA cable
Measurement of cables (2 m long)

## Slide 21
TRATOS installations
used for MgB2 cables
1+30+36 planetary machine
(well suitable for the 2 kA and 7 kA cables)
1+12 planetary machine
(for the higher (and final!) stage cable assembly)
All equipped with tension (and many others parameters) fine control systems; wrapping machines; ….
Notes: Planetarymachine for torsion free strand

## Slide 22: Production of dummy cable – Triplets
 90 mm
Materials: Kapton tape for electrical insulation, NOMEX (tape and braid)
Kevlar wire cabled for fillers (the cable is braided)

## Slide 23: Insulation tests at the manufacturing place (in air)
Instrumentation:
  Zumbach DST 28A, chain electrodes, installed on-line immediately after application of polyimide insulation
Procedure: Fault  automatic machine stop  NCR
Applied successfully during first dummy (copper) cable - for Triplets - production (80 m). No faults detected
- On-line HV tests: DC spark testing at 12 kV
Off-line HV tests: 10 kV (50 V/s, 120 s). Ileakage  10 µA
On final assembly. Each cable to ground and between cables.
Temperature and relative humidity recorded. Applied successfully
during production of first dummy cable for Triplets. Ileakage to be implemented
Minimum tacking distance specified : 25 mm

## Slide 24: System design – Electrical components
SC Link cryostat

## Slide 25: SC Link cryostats
4-walls
2-walls
290 mm
176 mm
3.5 tons
2.3 tons
Baseline: passive cryostat

## Slide 26: System design – Electrical components
HTS Current Leads

## Slide 27: HTS Current leads: 18 kA prototype
Ltot =1 m
LHex =0.5 m
Hex=40 mm
z=15 mm
=160 mm
=100 mm
18 kA Prototype
Same technologies as for LHC HTS leads
REBCO HTS Superconductor (instead of
BSCCO Ag/Au 2223)
Design currents and HV tests as in slides 7 and 8
Prototype 18 kA built and qualified

## Slide 28: Protection

## Slide 29: Protection of Cold Powering System: interlocks
Room Temperature
MgB2
HTS
LHe
Joints MgB2/Nb-Ti
Joints MgB2/HTS
Connection RT Cables/Lead
As in LHC
Warmer end of HTS in each Lead
As in LHC (cryo-interlock)
Warmer end of MgB2 cable (cryo-interlock)
Temperature interlocks trigger a slow power abort
Nb3Sn wire integrated in the SC Link (Tc  18 K)

## Slide 30: Protection strategy: active protection
MgB2
Nb-Ti
Joint
HTS
Joint
Protection (MgB2 cable)
Monitoring
(splice)
Monitoring
(splice)
Nb-Ti
Monitoring
(splice)
Protection (Nb-Ti)
Protection of SC circuits
  MgB2 - Vthr = 50 mV (integration time up to 100 ms)
  Nb-Ti - Vth = 1mV to 5 mV (integration time up to 100 ms)
  REBCO - Vthr = 1 mV - 5 mV, as in LHC (integration time up to 100 ms)
  Resistive part of current leads – Vthr = 100 mV (integration time up to few seconds)
Monitoring of splices
Each signal is doubled for redundancy
Splices in DFX and DFH are accessible
in the tunnel
In DFX – In LHe
In DFH – In GHe

## Slide 31: Protection strategy and hot spot analysis – MgB2
Quench of 18 kA or 7 kA cables/leads  firing QPS of MQXF magnets
Quench of 13 kA cables/leads of D1  firing QPS of D1
Quench of 2 kA cables/leads Quench heaters or energy extraction
Quench of a SC link is a very rare event
Rating (kA) | ACu (mm2) | Total MIITs | Tmax
18* | 210 | 15+32 | 26
2** | 34 | 15+8 | 40
7*** | 60 | 15+5 | 30
T0=25 K
System designed when cold diodes not in the baseline
Cu in the MgB2 cables (core and braids): Cu ETP, Sn coated (5 µm) – RRR1,2  60
1 R273 K/R10 K after processing to final form/diameter
2 RRR measured on pre-production tests  80

## Slide 32: Nb-Ti in DFX
Each MgB2 cable includes and extension of Nb-Ti cables – to be routed in the tunnel inside the DFX
Two trial geometries of SC Link bus bar:
  35 LHC type 01 strands (Ø 1.07 mm) around a 11 mm diameter multi-filamentary copper core for:
    MQXF main (18 kA, 2 units), MQXF trims (7 kA during transients, 3 units), D1 (13 kA, 2 units)
  21 LHC type 02 strands (Ø 0.825 mm) around a 5 mm diameter multi-filamentary copper core for:
    MCBXF magnets
Electrical insulation:
  Multi-layer Kapton wrapping (50% overlap)
  Final layout under definition

## Slide 33: Nb-Ti in DFX: hot spot analysis
R = 125 mm
J. Fleiter, DFX Review, July 2019

## Slide 34: System Demonstration

## Slide 35: Demo 1
Constructed by WP6a and tested in the SM-18 at different stages.
Last measurement – March 2019 – validation of:
DDFX Demo, DDFH Demo, SC Link with 2×60 m MgB2 cables made in
industry, 2×18 kA HTS Prototype Current Leads

## Slide 36: Demo 1

## Slide 37: Demo 1
18.8 kA, 1 hour, Tmax MgB2 =26 K
Tc = 31.3 K at 18 kA
Few n resistances
Several
provoked quenches
Use of QPS as for
LHC

## Slide 38: Cold Powering the String
A full size Cold Powering System for the Triplets will be tested in the SM-18 in the first trimester 2021 – “Prototype System Test”
The Prototype System will incorporate pre-series components (DFX, DFH, current leads, SC Link with full length, instrumentation)
After full qualification, the Prototype System will be dismounted and integrated in the String. Integration in the String is requested not before mid-2021
Integration studies have started

## Slide 39: DFX
Detailed Design Review in June 2019

## Slide 40: DFH Space Reservation
Reservation of space in the tunnel : 10 m length and 1.75 m width

## Slide 41: DFH Working Reference
Two modules each 4 m long ø 1,2 m (length without current leads)
Total length with current leads  15 m (plus SC Link in between)
14.7 m between the modules

## Slide 42: DFH Design under study
One single 4 m long (length without current leads)
Total length – with current leads – 5.8 m (to be compared with 15 m + 14.7 m)
Location of 7 kA and 13 kA basically unchanged
Free space – because of removal of second module – to reduce length of 2 kA RT cables

## Slide 43: DFH Design under study
Conceptual Design Review by end of October 2019

## Slide 44: Baseline strategy for testing
Each SC Link is cold tested in nominal operating conditions before being lowered in the tunnel. This includes the test of the MgB2 to Nb-Ti splices
Each current lead is cold tested in nominal operating conditions before being lowered in the tunnel
DF and DFH are not cold tested
MgB2 to HTS and Nb-Ti to Nb-Ti splices are done in the tunnel

## Slide 45: DFH Design under study

## Slide 46: Conclusions
Several intermediate components and system tests performed.
Major recent efforts: optimization of cable assemblies during production in
industry and test of Demo 1
From the electrical point of view, the cold powering systems are designed to meet the circuits' requirements
Next validation test: Demo 2. Electrical qualification of full-scale MgB2 cable for
Triplets, with simultaneous powering of more than one circuit. The cable is being
assembled in industry, Demo 1 is being upgraded for tests in November 2019

## Slide 47: Thank you for your attention !

## Slide 48: MgB2 wire - Specification
Wire diameter | mm | 1 |  0.2
Wire ovality | mm |  0.015 | 
Cu fraction | % |  12 | 
Cu coating | m |  30 | 
Filaments eq. diameter | m |  60 | 
Filaments Twist Pitch | mm |  100 |  5
Tensile strain at RT * | % |  0.26 | 
Bending radius after HT* | mm |  100 | 
Unit Length | m |  500 | 
RRR (Cu) | - | > 100 | 
Ic(25 K, 0.9 T) | A |  186 | 
Ic(25 K, 0.5 T) | A |  320 | 
Ic(20 K, 0.5 T) | A |  480 | 
n-value@ 25 K and 0.9 T | - | > 20 | 
Cabling of wire
after reaction
* Zero Ic degradation