## Slide 1: Quench protection strategies of the magnet circuits
Arjan Verweij, TE-MPE-PE
With input from many, see slides
HL-LHC Circuit Review, 9-10 Sept 2019

## Slide 2: Contents
General strategy for quench protection & detection
MgB2 link and leads
Triplet
  Triplet: mains
  Triplet: RCBXFA/B correctors
  Triplet: High-order superferric correctors
RBXF (D1)
RBRD (D2)
RCBRD (D2 orbit correctors)
RB.A67 and RB.A78 including the MBH (11 T dipole)
Hollow e-lens
Conclusions on simulation results are shown in yellow throughout the slides.
VWL=Voltage Withstand Level
WRFS=Worst Realistic Failure Scenario

## Slide 3: General strategy
General strategy for circuit protection:
Study different protection methods and schemes, aiming a good balance between maximum voltage to ground (Ucoil-gnd) and maximum hot-spot temperature (Thot-spot); typically we like to keep Thot-spot <150 K (busbars), <200 K (Nb-Ti correctors), <300 K (Nb-Ti dipoles) and <350 K (Nb3Sn coils).
Perform simulations in a realistic but conservative way, considering:
  different quench origins (bus, coil-low-field, coil-high-field).
  realistic quench propagation, hence detection time (tdet).
  realistic detection threshold (Uthres) and evaluation time (teval).
  realistic delay in switches of protection equipment.
  realistic failure scenario’s.
  realistic variation in material properties (RRR, Cu/SC ratio).
Build in sufficient redundancy, in order to ‘optimise’ reliability vs availability.
See talk E. Todesco

## Slide 4
Protection methods:
Cryostability / cold-end recovery / dynamic stability
Self-protection: discharge governed by circuit inductance and coil resistance (due to fast quench propagation) and warm leads
Active protection:
  Energy extraction (EE): switch+dump or eventually warm-leads/crowbar
  Quench heaters (QH’s)
  Coupling Loss Induced Quench system (CLIQ)
General strategy
Who does what?
Protection studies on magnets made by CERN are done by MSC and cross-checked by MPE.
Protection studies on magnets made by collaborations are done by the collaborations and cross-checked by MSC.
Protection studies on busbars, circuits, CCT magnets, and magnets with CLIQ are done by MPE.

## Slide 5
General strategy
Experimental data
Once model/prototype/series magnets are made and tested, the simulations should be compared to the experimental data, see also talk A. Foussat.
Experimental protection studies should be performed at different quench levels (including training quenches), enabling to:
  Measure the voltage build-up from 0 to Uthres, and hence verify proper functioning of the QD and firing of QH (and CLIQ),
  Verify the current decay and MIITs,
  Calculate a conservative value of the hot-spot assuming that the quench originates in the peak field area of the coil, and assuming conservative local RRR and Cu/SC.
However:
  Conditions during individual magnet tests will be different from those in the tunnel; simulations are important to correlate both.
  The internal voltage distribution (hence Ucoil-gnd, Ucoil-QH) cannot be reliably deduced from the discharge curve, and (updated) simulations remain the baseline for these voltages.

## Slide 6
General strategy on Quench Detection:
Use a midpoint for quench detection, especially for inductive components (coils).
Decouple busbars and SC leads from the coils, each with their own quench detection threshold and evaluation time. For busbars and leads we usually favour low Uthres and long teval, whereas for coils we usually have high Uthres and small teval.
If needed, consider a current-dependent Uthres , especially to overcome the effect of flux jumps and possible converter-induced noise (0-V crossing).
Use 2 channels with independent voltage taps, and use 1oo2 voting.
Make sure that symmetric quenches will also be detected (e.g. use UP1-UP2, UP3-UP4 and also UP1+P2-UP4+P4)
See talk from R. Denz
General strategy

## Slide 7
General strategy
Busbar protection:
In circuits with active protection, protection of the busbar is usually straightforward.
In circuits without active protection the preferred solution is cryostable busbars. If not possible, sufficient copper stabiliser should be added to handle a slow decay, governed by the inductance of the circuit and the resistance of the warm leads and crowbar.
The effect of irregularities in the busbar, such as resistive joints, quench stoppers, plugs, expansion loops (lyra’s), areas with reduced stabiliser, etc., should be studied in detail.
Take a very conservative approach, also because more stabiliser is good for mechanical stabilisation.
For busbar layout see talk E. Todesco

## Slide 8: General strategy
Quench origin | Fast Power Abort
One of the 6 MQXFA/B magnets, 18 kA triplet lead, 7 kA trim lead, main triplet busbars | RQX, RTQX1, RTQX3, RTQXA1
MCBXFA-Hor/Vert, 2 kA corrector lead and busbar | Concerned circuit and the nested one
High-order corrector magnets | Concerned circuit
MBXF (D1), 18 kA D1 lead and busbar | RBXF
MBRD (D2), lead and busbar | RBRD
MCBRD, lead and busbar | RCBRD (both apertures)
MBH magnet or busbar, RTBH busbar | RB

## Slide 9: Contents
General strategy for quench protection & detection
MgB2 link and leads
Triplet
  Triplet: mains
  Triplet: RCBXFA/B correctors
  Triplet: High-order superferric correctors
RBXF (D1)
RBRD (D2)
RCBRD (D2 orbit correctors)
RB.A67 and RB.A78 including the MBH (11 T dipole)
Hollow e-lens

## Slide 10: MgB2 link
The main triplet, its trims, the D1, and the orbit correctors are powered through the same MgB2 link.
In principle, the QP will be designed in such a way that a quench in a given circuit will cause a FPA in that circuit, and a ramp down in all the other circuits.
18 kA
Triplet mains
3x7 kA
Triplet trims
12x2 kA (co-axial)
RCBXFA/B (hor/vert
orbit correctors)
18 kA
RBXF (D1)
A. Ballarino, https://indico.cern.ch/event/643197/contributions/2624569/

## Slide 11: MgB2 link
warm Cu bus
Uthres
teval
HTS part
of the lead
1-5 mV
O(100 ms)
MgB2 link
50-100 mV
O(100 ms)
Res. part
of the lead
10-100 mV
O(sec)
LTS bus
1-10 mV
O(100 ms)
Independent active protection of each part with customized detection voltage threshold and evaluation time. (see also presentation R. Denz)
Monitoring of the individual joints (HTS-MgB2, MgB2 to LTS) is possible if needed.
Temp. sensors at the warm ends of ‘Res part lead’, ‘HTS part lead’, and ‘MgB2 link’ will be used for interlocking (excursion will trigger slow power abort).
Longer LTS bus segments have individual quench detection.
T
T
T
A. Ballarino, https://indico.cern.ch/event/643197/contributions/2624569/

## Slide 12: MgB2 link
None of the MgB2 leads is expected to quench in case of a FPA of any of the circuits.
Each of the MgB2 leads has sufficient copper to handle the current discharge in case of a quench.
The 18 kA triplet leads will see a fast decaying current (a few 100 ms) but should not quench.
The 3 trim leads (7 kA) might see a transient up to 6.8 kA but should not quench.
During the SM18 string test and/or HWC after LS3 we will study the mutual coupling between the main triplet circuit, the trims, the D1, and the correctors.
Tripping the main triplet or D1 in case of a quench in one of the other circuits should be avoided.

## Slide 13: MgB2 link
Hot-spot, assuming 15 MA2s for detection (ref. A. Ballarino) and Tinit=25 K
Lead rating | Cu cross- section [mm2] | Detection MITTs [MA2s] | Detection tdet+teval [s] | Discharge MIITs [MA2s] | Discharge T [s] | Total MIITs [MA2s] | Thot-spot [K]
18 kA | 200 | 15 | 0.05 | 32 | 0.2 | 47 | 27
7 kA | 36 | 15 | 0.3 | 5 | 0.2 | 20 | 40
2 kA | 34 | 15 | 3.7 | 8 | 4 | 23 | 43
Lead rating | Cu cross- section [mm2] | Detection MITTs [MA2s] | Detection tdet+teval [s] | Discharge MIITs [MA2s] | Discharge T [s] | Total MIITs [MA2s] | Thot-spot [K]
18 kA | 200 | 64 | 0.2 | 2800 | 17 | 2860 | 100
7 kA | 36 | 10 | 0.2 | 83 | 3.4 | 93 | 100
2 kA | 34 | 1 | 0.2 | 83 | 42 | 84 | 100
Allowed MIITs for 100 K hot-spot, assuming 0.2 s for detection and Tinit=25 K
Conclusion: Protection-wise, the MgB2 leads are very safe

## Slide 14: Contents
General strategy for quench protection & detection
MgB2 link and leads
Triplet
  Triplet: mains
  Triplet: RCBXFA/B correctors
  Triplet: High-order superferric correctors
RBXF (D1)
RBRD (D2)
RCBRD (D2 orbit correctors)
RB.A67 and RB.A78 including the MBH (11 T dipole)
Hollow e-lens

## Slide 15: RQX+RTQX1/3+RTQXA1 (Triplet – main quads)
The circuit went through several iteration steps in the last years.
Protection studies have been performed by M. Mentink and E. Ravaioli, and lately also by V. Marinozzi (FNAL). Latest simulation results were presented by E. Ravaioli at the ‘Intl review on the IT Quadrupoles for HL-LHC’ (July 2019), see: https://indico.cern.ch/event/828604/contributions/3471709/

## Slide 16: RQX+RTQX1/3+RTQXA1
Nr of circuits | 4 (L1, R1, L5, R5)
Magnets per circuit | 4x MQXFA (US Acc Upgrade Project), 2x MQXFB (CERN)
Inom | 16470 A
L at Inom | 0.255 H
Estored at Inom | 34.5 MJ
Protection | 8 QH’s and 1 CLIQ per magnet (so 48 QH’s and 6 CLIQ’s in total)
WRFS | Failure of 2 QH circuits Failure of 1 QH circuits and 1 CLIQ
MQXF cross-section
(P. Ferracin, G. Ambrosio et al.)

## Slide 17
Main remarks:
No inner layer QH’s due to observed delamination, see S. Izquierdo Bermudez https://edms.cern.ch/document/1972818
Coils self protected <2 kA, OL-QH’s effective >1.5 kA, CLIQ effective >3 kA
Cold diodes only carry current for a short time (t≈0.17 s) in case of a FPA when there is a quench imbalance between magnets.
The combined protection of QH’s and CLIQ offers a lower hot-spot and increased redundancy, especially important at high currents.
QH characteristics and CLIQ configuration and parameters are optimized to have a fast transition of a large volume of the coil in case of activation.
Diodes, and the connection order and polarities of QH’s, CLIQ and poles are optimized to:
  Reduce the voltage to ground
  Reduce the hot-spot and voltage distribution in case of failures
  Reduce the dipole kick on the beam in case of a spurious triggering of the QH power supply (see also presentation D. Wollmann)
RQX+RTQX1/3+RTQXA1

## Slide 18
* Realistic conductor parameters provided by B. Bordini, indico.cern.ch/event/828604/contributions/3471761/
Temperatures at ultimate are about 20 K higher
Scenario | Reference parameters | Realistic* parameters randomly distributed | Realistic* parameters with optimised coil order within a magnet
No failures | 231 K | ≤254 K | ≤254 K
2 QH failures | ≤235 K | ≤259 K | ≤259 K
1 CLIQ and 1 QH failure | ≤357 K | ≤403 K | ≤403 K
Hot spot temperatures for MQXFB at Inom=16.5 kA, see https://indico.cern.ch/event/828604/contributions/3471709 (partially cross-checked by V. Marinozzi)
Hot-spot temperatures are well below 350 K. A hot-spot of about 400 K, in case of the unlikely event of a quench with combined failure of CLIQ and one QH, was deemed acceptable during the triplet review of 15-17 July 2019 (https://indico.cern.ch/event/828604)
RQX+RTQX1/3+RTQXA1

## Slide 19
Realistic conductor parameters provided by B. Bordini, indico.cern.ch/event/828604/contributions/3471761/
Max Ucoil-gnd at ultimate are about 160-200 V higher.
Scenario | Reference parameters | Realistic* parameters randomly distributed | Realistic* parameters with optimised coil order within a magnet
No failures | 594 V | ≤927 V | ≤636 V
2 QH failures | ≤641 V | ≤920 V | ≤657 V
1 CLIQ and 1 QH failure | ≤578 V | ≤820 V | ≤604 V
Optimising the order of the coils is important to reduce the maximum voltages. 660 V should be taken as the reference.
Peak voltages are reached when Tcoil=80-120 K and when the QH power supplies are almost fully discharged, so Ucoil-gnd=Ucoil-QH. It is important that Voltage Withstand Levels are also tested at these temperatures, see talk F. Rodriguez-Mateos.
RQX+RTQX1/3+RTQXA1
Maximum Ucoil-gnd for MQXFB at Inom=16.5 kA, see https://indico.cern.ch/event/828604/contributions/3471709 (partially cross-checked by V. Marinozzi)

## Slide 20: Triplet: 18 kA busbars
tdet+teval [s] | t [s] | MIITs [MA2s] | ACu for 100 K [mm2] | ACu for 150 K [mm2] | ACu for 200 K [mm2]
400 | 0.17 | 157 | 33 | 30 | 28
500 | 0.17 | 190 | 37 | 33 | 31
600 | 0.17 | 222 | 40 | 35.5 | 33
Estimate of required Cu cross-section, assuming Cu/SC=1.7, RRR=100
H. Prin and D. Duarte Ramos

## Slide 21: Triplet: 18 kA flat busbar
The flat busbar is an insulated pair of Rutherford-type cables:
34 strands, dstr=1.065 mm, Cu/SC=1.65, ACu=38 mm2, ASC= 23 mm2.
The hot-spot in this busbar is calculated by M. Mentink, see https://edms.cern.ch/document/2052319 , assuming Uthr=10 mV and teval=500 ms, varying RRR, self-field, cooling conditions, and quench current.
18 kA internal busbar (M. Baldini et al.)
A highest hot-spot of 110 K is obtained, in the case of a current of 18 kA and a RRR of 80.

## Slide 22: Triplet: 18 kA round busbar
Two round busbars have been considered in recent years, having Cu cross-sections of 84 and 102 mm2, so more than double the amount of the flat busbar.
V. Vitaly et al.
L. Bottura
Assuming a RRR>80, all 3 options would give hot-spot temperatures <100 K, as well as any other busbar with a Cu cross-section >50 mm2.
The preferred option is now a round busbar which is also used by WP6, with a cross-section of 78 mm2 Cu and 19 mm2 SC.

## Slide 23: Contents
General strategy for quench protection & detection
MgB2 link and leads
Triplet
  Triplet: mains
  Triplet: RCBXFA/B correctors
  Triplet: High-order superferric correctors
RBXF (D1)
RBRD (D2)
RCBRD (D2 orbit correctors)
RB.A67 and RB.A78 including the MBH (11 T dipole)
Hollow e-lens
MCBXF cross-section
(F. Toral, J. C. Perez et al.)

## Slide 24: Triplet corrector: RCBXFA/B
 | Vertical orbit corr., inner | Horizontal orbit corr., outer | Vertical orbit corr., inner | Horizontal orbit corr., outer
Nr of circuits | 4 | 4 | 8 | 8
Magnets per circuit | 1x MCBXFA | 1x MCBXFA | 1x MCBXFB | 1x MCBXFB
Magn. length [m] | 2.2 | 2.2 | 1.2 | 1.2
Conductor | 18 strand Rutherford cable, dstr=0.48 mm, Cu/SC=1.75, RRRmeas=140 |  |  | 
Inom [A] | 1584 | 1402 | 1625 | 1474
L at Inom [mH] | 107 | 232 | 58.4 | 125
Estored at Inom [kJ] | 134 | 239 | 77 | 143
Protection baseline | EE | EE | Self protected / crowbar | Self protected / crowbar
WRFS | none |  |  | 
Latest magnet simulation results were presented at the WP3 meeting on 13/2/2019 by A. Fernandez Navarro and F. Toral (CIEMAT), see https://indico.cern.ch/event/785928/
For the protection studies the nested inner and outer dipole coils are simulated independently. Possible quench back is not taken into account.

## Slide 25: Triplet corrector: MCBXFA (2.2 m)
No cooling to helium, Uthres=100 mV, tdet=20 ms, teval=10 ms. Quench at peak field.
A. Fernandez Navarro and F. Toral, https://indico.cern.ch/event/785928/
Current baseline: EE for both inner and outer dipole with REE=0.3 W.
Maximum voltage to be considered for HiPotting should be I*REE which is about 490 V at Inom and LHe temperature.

## Slide 26: Triplet corrector: MCBXFB (1.2 m)
*SQUID: resistive voltage. ROXIE: voltage to ground.
Quench origin in peak field.
Roxie is a 2D code and the added long. quench propagation is too slow, resulting in lower R, hence slower decay and higher hot spot.
Note that Ucoil-gnd (SQUID) is of course smaller than Ures,tot (ROXIE).
A. Fernandez Navarro and F. Toral, https://indico.cern.ch/event/785928/
Baseline is ‘self-protection’ but the coils will be equipped with taps for QD. Simulations using a third model should be done. Possibly the Outer needs EE.

## Slide 27: Triplet corrector: 2 kA RCBXFB busbar
tdet+teval [s] | t [s] | MIITs [MA2s] | ACu for 100 K [mm2] | ACu for 150 K [mm2] | ACu for 200 K [mm2]
500 | 4 | 10 | 8.5 | 7.6 | 7.1
Estimate of required Cu cross-section, assuming Cu/SC=1.7, RRR=100
H. Prin and D. Duarte Ramos

## Slide 28: Triplet corrector: RCBXFB busbars
The RCBXFA/B flat busbar comprises 18 Nb-Ti strands (d=0.48 mm, Cu/SC=1.75) shunted with a copper stabiliser (4.35 x 1.5 mm2). So: ACu=8.6 mm2, ASC=1.2 mm2.
Uthres | 10 mV
teval | 0.5 s
I | 1730 A
RRR | 80
Ba | 0.5 T
Rcrowbar | 30 mW
Rwarm leads | 1.6 mW
tcircuit | 4 s
Cooling to He | No
MIITs | 7.6 MA2s
Hot-spot temp. | 119 K
Various scenario’s have been simulated, such as:
Additional joint resistance,
Local areas without cooling,
Electrical separation between Ruth cable and the Cu stabiliser.
The round busbar will probably be the same as the LHC 6 kA bus (ACu=8 mm2, ASC=0.5 mm2), which would lead to hot-spots of about 175 K.
Simulations by M. Mentink, see https://edms.cern.ch/document/2222740 (Aug 2019).
For all cases the hot-spot remained below 120 K.

## Slide 29: Triplet corrector: 2 kA RCBXFA busbar
tdet+teval [s] | Current [A] | t [s] | MIITs [MA2s] | Thot-spot for flat busbar [K] | Thot-spot for round busbar [K]
500 | 1700 | 0.8 | 3.6 | 51 | 56
The flat and round busbars of the RCBXFA will be the same as for the RCBXFB.
Upon quench detection, the EE will be switched in, resulting in fast current decay, much lower MIITs (than RCBXFB), and hence lower hot-spot, <60 K.
H. Prin and D. Duarte Ramos

## Slide 30: Contents
General strategy for quench protection & detection
MgB2 link and leads
Triplet
  Triplet: mains
  Triplet: RCBXFA/B correctors
  Triplet: High-order superferric correctors
RBXF (D1)
RBRD (D2)
RCBRD (D2 orbit correctors)
RB.A67 and RB.A78 including the MBH (11 T dipole)
Hollow e-lens

## Slide 31: Triplet corrector: RQSXF
Nr of circuits | 4
Magnets per circuit | 1x MQSXF (skew quadrupole)
Magn. length | 0.41 m
Inom | 174 A
Ldiff at Inom | 1.53 H
Estored at Inom | 31 kJ
Conductor | 0.7 mm Nb-Ti strand, Cu/SC=2.3
Protection | EE
WRFS | none
Skew quadrupole cross-section
(M. Sorbi, M. Statera et al.)

## Slide 32: Triplet corrector: RQSXF
REE | 1.5 W
Thot-spot | <145 K
Total resistive voltage over the coil | 235 V
Without EE, the hot-spot in MQSXF magnet would go up to 132 K, but the peak Ucoil-to-gnd would go to 633 V.
The baseline is therefore to include EE with grounding in the centre, resulting in a total resistive voltage of 287 V. Simulations should be done to obtain a realistic value for the maximum Ucoil-gnd.
Initial magnet simulation results at Iult were presented at the WP3 meeting on 28/6/2017 by V. Marinozzi (INFN) using QLASA software, see https://indico.cern.ch/event/647416/
The table below shows recently updated numbers, presented on 19/6/2019 by M. Statera, for Inom and realistic RRR, see https://indico.cern.ch/event/813962/ .

## Slide 33: Triplet HO correctors: sext, oct, deca, dodeca
 | RCS(S)XF | RCO(S)XF | RCD(S)XF | RCT(S)XF
Nr of circuits | 8 | 8 | 8 | 8
Magnets per circuit | 1x MCS(S)XF (skew) sextupole | 1x MCO(S)XF (skew) octupole | 1x MCD(S)XF (skew) decapole | 1x MCT(S)XF (skew) dodecapole
Magn. length | 0.168 m | 0.145 m | 0.145 m | 0.469 / 0.099 m
Inom | 99 A | 102 A | 92 A | 85 A
L at Inom | 350 mH | 300 mH | 160 mH | 1000 / 210 mH
Estored at Inom | 1.7 kJ | 1.6 kJ | 0.68 kJ | 3.6 / 0.74 kJ
Conductor | 0.5 mm Nb-Ti strand, Cu/SC=2.3 |  |  | 
Protection | Self protection |  |  | 
WRFS | none |  |  | 
M. Sorbi, M. Statera et al.

## Slide 34
 | RCS(S)XF | RCO(S)XF | RCD(S)XF | RCTSXF | RCTXF
Thot-spot | 141 K | 164 K | 149 K | 150 K | 175 K
Ucoil-to-gnd | 39 K | 46 V | 18 V | 19 V | 90 V
Triplet HO correctors: sext, oct, deca, dodeca
Initial magnet simulation results at Iult were presented at the WP3 meeting on 28/6/2017 by V. Marinozzi (INFN) using QLASA software, see https://indico.cern.ch/event/647416/
Considering the MIITs calculated by INFN, M. Mentink cross-checked some of the simulation results, see https://edms.cern.ch/document/2222621 .
The table below shows recently updated numbers, presented on 19/6/2019 by M. Statera, for Inom and realistic RRR, see https://indico.cern.ch/event/813962/ .
Independent MIITs simulations are foreseen by M. Wilczek.
Conclusion: hot-spots remain <170 K, provided that the length of the bare conductor in the connection box is less than 16 mm.
Voltages to be used for the definition of the VWL are between 18 and 90 V.

## Slide 35: Triplet HO correctors: busbar
The baseline for the busbar is the LHC auxiliary N-line busbar with:
ACu=1.8 mm2
ASC=0.2 mm2.
Simulations done by M. Mentink, see https://edms.cern.ch/document/1897052
The N-line busbar is cryostable for currents below 200 A.

## Slide 36: Contents
General strategy for quench protection & detection
MgB2 link and leads
Triplet
  Triplet: mains
  Triplet: RCBXFA/B correctors
  Triplet: High-order superferric correctors
RBXF (D1)
RBRD (D2)
RCBRD (D2 orbit correctors)
RB.A67 and RB.A78 including the MBH (11 T dipole)
Hollow e-lens

## Slide 37: RBXF (D1)
Nr of circuits | 4
Magnets per circuit | 1x MBXF (KEK)
Inom | 12047 A
L at Inom | 27 mH
Estored at Inom | 1.9 MJ
Conductor | LHC dipole outer cable (36 strands, 0.825 mm, Cu/SC=1.95)
Protection | 8 QH’s in 4 circuits
WRFS | Failure of 2 QH circuits
D1 cross-section
(T. Nakamoto, M. Sugano et al.)

## Slide 38: RBXF (D1)
 | Default case | 1 QH circuit failing (2 QH strips) | 2 QH circuits failing (4 QH strips)
Iult | 13000 A |  | 
MIITs at 13 kA | 23.9 MA2s | 25 MA2s | 27.8 MA2s
Thot-spot | 180 K | 195 K | 240 K
 | Default case | 1 QH circuit failing (2 QH strips) | 2 QH circuits failing (4 QH strips)
Inom | 12047 A |  | 
Max Ucoil-gnd | 200 V | 250 V | 400 V
Most recent reference for the D1 magnet protection given by KEK (Sept 2018), see https://indico.cern.ch/event/759386/
Review 11-13 Mar 2019: https://indico.cern.ch/event/790845/contributions/3287033/
Uthres=100 mV, teval=10 ms. Quench at peak field.
Maximum voltage to be used to define the VWL is 400 V.

## Slide 39: RBXF: 13 kA busbars
tdet+teval [s] | t [s] | MIITs [MA2s] | ACu for 100 K [mm2] | ACu for 150 K [mm2] | ACu for 200 K [mm2]
400 | 0.35 | 97 | 27.5 | 24.4 | 22.7
500 | 0.35 | 114 | 29.8 | 26.4 | 24.6
600 | 0.35 | 131 | 32 | 28.3 | 26.4
Estimate of required Cu cross-section, assuming Cu/SC=1.95, RRR=100
H. Prin and D. Duarte Ramos

## Slide 40: 13 kA D1 and D2 busbars
The flat busbar is the Rutherford LHC dipole outer-layer cable (36 strands, dstr=0.825 mm, Cu/SC=1.95) stabilised with a 1.5x15.1 mm2 Cu strip.
So : ACu=35 mm2 and ASC=6.5 mm2.
The hot-spot in this busbar is calculated by M. Mentink, see https://edms.cern.ch/document/2110653 , assuming Uthr=10 mV and teval=500 ms, varying:
RRR,
self-field,
cooling conditions,
joint resistance,
expansion loop (1 m long without bonding between cable and strip)
quench current.
A highest hot-spot of 104 K is obtained in both the D1 and D2 busbar
The D2 circuit will use the same busbar as the D1, and will have similar MIITs of about 28 MA2s at ultimate current.

## Slide 41: Contents
General strategy for quench protection & detection
MgB2 link and leads
Triplet
  Triplet: mains
  Triplet: RCBXFA/B correctors
  Triplet: High-order superferric correctors
RBXF (D1)
RBRD (D2)
RCBRD (D2 orbit correctors)
RB.A67 and RB.A78 including the MBH (11 T dipole)
Hollow e-lens
D2 cross-section
(P. Fabbricatore, S. Farinon et al.)

## Slide 42: RBRD (D2)
Nr of circuits | 4
Magnets per circuit | 1x MBRD (INFN)
Inom | 12328 A
L at Inom | 30 mH
Estored at Inom | 2.26 MJ
Conductor | LHC dipole outer cable (36 strands, 0.825 mm, Cu/SC=1.95)
Protection | 16 QH’s in 8 circuits. 4 circuits used (1, 3, 6, 8)
WRFS | Failure of 1 QH circuit

## Slide 43: RBRD (D2)
 | Default case | 1 QH circuit failing (2 QH strips) | 2 QH circuits failing (4 QH strips)
Uthres | (100 mV) |  | 
teval | (10 ms) |  | 
I | 12 kA |  | 
Quench origin | (High field) |  | 
Thot-spot | 218 K | 250 K | 302 K
Max Ucoil-gnd | 130 V | 525 V | 483-779 V *
P. Fabbricatore Aug 2019, see: https://edms.cern.ch/ui/file/2222536
Thot-spot | 205 K | 230 K | -
Max Ucoil-gnd | 120 V | 490 V | -
Cross-check by S. Izquierdo Bermudez in May 2018 (non-published)
525 V is the reference voltage to be taken into account for the definition of the VWL.
*: 483 V if 2 QH’s fail in different apertures, 779 V if they fail in the same aperture

## Slide 44: Contents
General strategy for quench protection & detection
MgB2 link and leads
Triplet
  Triplet: mains
  Triplet: RCBXFA/B correctors
  Triplet: High-order superferric correctors
RBXF (D1)
RBRD (D2)
RCBRD (D2 orbit correctors)
RB.A67 and RB.A78 including the MBH (11 T dipole)
Hollow e-lens

## Slide 45: RCBRD (D2 orbit corr)
Nr of circuits | 16
Magnets per circuit | 1x MCBRD (CERN or IHEP)
Inom | 394 A / 425 A
Iult | 435 A / 470 A
L at Inom | 0.97 H per aperture
Estored at Inom | 75 kJ per aperture
Conductor | CERN: 0.825 mm, Cu/SC=1.95 IHEP: 0.825 mm, Cu/SC=1.3
Protection | EE + quenchback
WRFS | none
D2 corrector cross-section
(G. Kirby et al.)

## Slide 46: RCBRD (D2 orbit corr)
Variant | CERN | IHEP | IHEP
Reference | 1) | 1) | 2)
Uthres | 100 mV | 100 mV | 100 mV
teval + tswitch | 10 + 10 ms | 10 + 2 ms | 10 + 2 ms
Iult | 435 A | 435 A | 470
Strand RRR | 230 | 230 | 100
Former RRR | 8 | 8 | 
REE | 1.5 W / 1.29 W / var | 1.5 W / 1.29 W / var | 1.4 W / var
Thot-spot | 143 / 160 / 167 K | 156 / 177 / 192 K | 249 K / 252 K
Ucoil-gnd | 651 / 562 / 439 V | 651 / 562 / 439 V | 658 V / 496 V
Most recent reference for the MCBRD CCT magnet protection:
1) M. Mentink using STEAM-BBQ and ProteCCT, see https://edms.cern.ch/document/2222746/
2) Qingjin XU (IHEP) at WP3 meeting on 6/3/2019, see https://indico.cern.ch/event/801069/
With the actual baseline of 1.5 W, the maximum hot-spot and voltage will be about 150 K and 650 V (590 V at Inom). Reduction of the EE resistance or the use of a varistor could give a significant reduction of the voltage while still keeping the hot-spot <200 K.

## Slide 47: RCBRD busbar
The baseline for the RCBRD busbar is the LHC auxiliary N-line busbar with:
ACu=1.8 mm2
ASC=0.2 mm2
Simulations have been performed by M. Mentink, see: https://edms.cern.ch/document/2222746/
The total MIITs, including detection, validation, and current discharge remain in all cases (varying current and RRR) below 174 kA2s, corresponding to a hot-spot well below 100 K.

## Slide 48: Contents
General strategy for quench protection & detection
MgB2 link and leads
Triplet
  Triplet: mains
  Triplet: RCBXFA/B correctors
  Triplet: High-order superferric correctors
RBXF (D1)
RBRD (D2)
RCBRD (D2 orbit correctors)
RB.A67 and RB.A78 including the 11-T MBH (aka modified RB)
Hollow e-lens

## Slide 49: RB with MBH
Nr of circuits | 2 (L/R Pt 7)
Magnets per circuit | 2 x MBH (CERN)
Inom | 11850 A
L at Inom | 130 mH (per assembly)
Stored energy at Inom | 9.1 MJ
Conductor | Nb3Sn Rutherford
Protection | 32 QH’s per assembly in 16 circuits
WRFS | Failure of 2 QH circuits
The magnet and circuit have seen several modifications over the last years that have an impact on the protection. Since Thot-spot and Vcoil-gnd are relatively high, even small variations in the design or in some parameters can have an important impact.
Simulations are really numerous due to large number of combinations between quench current, quench location, protection settings, RRR and Cu/Sc distributions, failure scenario’s, etc.
Simulations are still ongoing for the most updated set of parameters.

## Slide 50: RB with MBH
Simulation code | Roxie | TALES |  | 
 | No QH failing | No QH failing | 1 QH circuit failing | 2 QH circuits failing
Thot-spot [K] | 310 | 320 | 327 | 333
Ucoil-gnd [V] | 350 | 245 | 570 | 950
Nominal current of 11850 A, impregnated QH’s
Cu/SC=1.15, strand RRR=100, Uthres=100 mV, tdet=5 ms*, teval=10 ms
MBH magnet studies WITHOUT EE, tQH=5 ms: carried out by S. Izquierdo Bermudez and A. Fernandez Navarro, see https://indico.cern.ch/event/778100 (11 T review, 11 Jan 2019)
Simulation code |  | STEAM: LEDET+PSPICE |  | 
 |  | No QH failing | 1 QH circuit failing | 2 QH circuits failing
Thot-spot [K] |  | 293 | 299 | 305
Ucoil-gnd [V] |  | 783 | 1038 | 1457
Thot-spot at max Ucoil-gnd [K] |  | 166 | 150 | 210
CIRCUIT studies WITH EE, tQH=2 ms: carried out by M. Maciejewski, see: https://edms.cern.ch/document/2157321
* See: S. Izquierdo Bermudez, https://ieeexplore.ieee.org/stamp/stamp.jsp?arnumber=8272459

## Slide 51: RB with MBH
Ultimate current of 12850 A, impregnated QH’s
Cu/SC=1.15, strand RRR=100, Uthres=100 mV, tdet=5 ms, teval=10 ms
MBH magnet studies WITHOUT EE, tQH=5 ms: carried out by S. Izquierdo Bermudez and A. Fernandez Navarro, see https://indico.cern.ch/event/778100 (11 T review, 11 Jan 2019)
Simulation code |  | STEAM: LEDET+PSPICE |  | 
 |  | No QH failing | 1 QH circuit failing | 2 QH circuits failing
Thot-spot [K] |  | 322 | 327 | 332
Ucoil-gnd [V] |  | 974 | 1217 | 1600
Thot-spot at max Ucoil-gnd [K] |  | 180 | 170 | 176
CIRCUIT studies WITH EE, tQH=2 ms: carried out by M. Maciejewski, see: https://edms.cern.ch/document/2157321
Simulation code | Roxie | TALES |  | 
 | No QH failing | No QH failing | 1 QH circuit failing | 2 QH circuits failing
Thot-spot [K] | 350 | 340 | 349 | 356
Ucoil-gnd [V] | 450 | 340 | 680 | 1070

## Slide 52: RB with MBH
Cu/SC ratio and RRR have an important impact on the quench behaviour, especially on the voltage distribution.
We have recently received the info that realistic variations for the production are Cu/SC=1.17-1.21 and RRR=150-200.
Simulations have been redone with STEAM using these new average values, see next slide.
Similar to the triplet circuit, also the variation in Cu/SC and RRR among the coils in the 11 T assemblies will have a significant impact on the voltage distribution. Simulations are ongoing.
Similar to the triplet circuit, it will be important to optimise the coil order in the MBH assembly to reduce the voltages as much as possible.

## Slide 53: Modified RB
Uthres=100 mV, tdet=5 ms, teval=10 ms, tQH=2 ms, impregnated QH’s
 | Cu/SC=1.19, strand RRR=175 |  | 
 | No QH failing | 1 QH circuit failing | 2 QH circuits failing
Thot-spot [K] | 287 | 294 | 307
Ucoil-gnd [V] | 660 | 1005 | 1469
Thot-spot at max Ucoil-gnd [K] | 150 | 174 | 148
 | Cu/SC=1.15, strand RRR=100 |  | 
 | No QH failing | 1 QH circuit failing | 2 QH circuits failing
Thot-spot [K] | 293 | 299 | 305
Ucoil-gnd [V] | 783 | 1038 | 1457
Thot-spot at max Ucoil-gnd [K] | 166 | 150 | 210
CIRCUIT studies at 11850 A, WITH EE
Simulations by M. Maciejewski, see: https://edms.cern.ch/document/2157321 using STEAM: LEDET + PSPICE

## Slide 54: Modified RB
Simulations before consider impregnated heaters. Using external heaters (with 60 um fiberglass wrap) will increase the hot-spot by about 30 K, see F. Savary https://indico.cern.ch/event/778100/contributions/3270000
The maximum Ucoil-gnd occurs when the local coil temperature is 150-200 K. It is therefor important that the VWL is also tested in this temperature range, see talk F. Rodriguez-Mateos.

## Slide 55: Contents
General strategy for quench protection & detection
MgB2 link and leads
Triplet
  Triplet: mains
  Triplet: RCBXFA/B correctors
  Triplet: High-order superferric correctors
RBXF (D1)
RBRD (D2)
RCBRD (D2 orbit correctors)
RB.A67 and RB.A78 including the MBH (11 T dipole)
Hollow e-lens

## Slide 56: Hollow e-lens
MainSol-2
MainSol-1
GunSol-2
GunSol-1
BendSol
Quench strategy:
Targets: Thot-spot < 200 K and Vgnd < 500 V
EE for each circuit
Assume Uthr=100 mV, teval=10 ms
D. Perini and M. Maciejewski at the HL-LHC TCC on 18/4/2019, see https://indico.cern.ch/event/814368/

## Slide 57: Hollow e-lens
Variant | GunSol-1 | GunSol-2 | BendSol | MainSol-1 & 2
Inom [A] | 320 | 257 | 335 | 330
L [H] | 0.81 / 0.92 | 0.83 / 0.97 | 2.1 / 2.4 | 8.9 / 9.1
Estored [kJ] | 47 | 32 | 135 | 494
Bnom [T] | 3.1 | 3.7 | 3.5 | 5
REE [W] | 0.6 (0.2-1.5) | 0.6 (0.12-1.9) | 0.9 (0.65-1.5) | 2.6 (2.5-3.0)
Thot-spot | 70 (200-45) | 55 (200-40) | 130 (200-70) | 175 (200-140)
Vcoil-gnd | 190 (60-500) | 150 (40-500) | 300 (220-500) | 430 (410-500)
Hot-spots <200 K and maximum Ucoil-gnd <500 V.
Grounding at the neg. terminal of the converter, except in the MainSol circuits, which should have the grounding in the middle of the EE resistor, to be confirmed with EPC.
Busbar protection should not be an issue since all circuits have EE.
Possibly the two circuits with lower Estored could be self-protected.
Further optimisation might be possible (e.g. adding parallel resistors).
D. Perini and M. Maciejewski, https://indico.cern.ch/event/814368/

## Slide 58: Overview, for I=Inom
 | Thot-spot [K] |  | Vcoil-gnd at Inom [V] |  | Remarks
 | Nominal | WRFS | Nominal | WRFS | 
RQX | 231 | 372 | 600 | 660 | 
RCBXFA | 147 | - | 490 | - | 
RCBXFB | 212 | - | 375 | - | Possibly outer with EE
RQSXF | 145 | - | 235 | - | Cross-check not yet made by CERN
HO triplet correctors | 141-175 | - | 18-90 | - | 
RBXF (D1) | 180 | 240 | 200 | 400 | 
RBRD (D2) | 200-250 | 302 | 120-150 | 525 | 
RCBRD (orbit corrector D2) | <140 | - | 590 | - | Reduction of the EE resistor value or use of varistor could be considered as long as quench back is guaranteed
RB with MBH | 287 | (307) | 660 | (1470) | Non-uniform distribution of Cu/SC and RRR not yet taken into account
Hollow e-lens | 55-175 | - | 150-430 | - | Preliminary results

## Slide 59: Overview MgB2 link and busbars
 | Thot-spot [K] | Remarks
MgB2 leads | <45 | 
RQX - flat busbar | <110 | 
RQX - round busbar | <100 | 
RCBXFA orbit corrector | <60 | 
RCBXFB orbit corrector – flat busbar | <120 | 
RCBXFB orbit corrector – round busbar | <175 | Possibly add 20% Cu
RQSXF | cryostable | 
HO triplet correctors | cryostable | 
RBXF (D1) | <105 | 
RBRD (D2) | <105 | 
RCBRD (orbit corrector D2) | <100 | 
BTW: 10 years of LHC have shown that most short-to-grounds occur in the busbar system. Add sufficient insulation and stay away from (sharp) metallic objects.

## Slide 60: Conclusion
During the design phase of the HL-LHC magnets and circuits, the protection behaviour is simulated by CERN and by external institutes. For the more critical circuits also Worst Realistic Failure Scenario’s have been considered.
As soon as model magnets are produced, comparison with experimental data is necessary, keeping however in mind that the measurements usually give average values, such as I(T), MIITs, Vcoil, whereas the local Ucoil-gnd, Ucoil-QH, and Thot-spot are key for protection.
It is important to keep the conductor parameters, especially Cu/SC and RRR, as uniform as possible during the production of the Nb3Sn conductors for the triplet and MBH, in order to reduce voltage imbalance and hence Ucoil-gnd.
In case of variations in Cu/SC and RRR, optimising the positioning of the coils in the Nb3Sn magnets is beneficial to lower the Ucoil-gnd.
Reliability of CLIQ is very important since it reduces the hot-spot considerably.
The Nb3Sn magnets see the maximum Ucoil-gnd at rather elevated temperatures of 80-200 K. It is important that this is reflected in the definition of the VWL’s.
PS: It would be useful to design the protection of Nb3Sn magnets based on a ‘maximum thermal-strain’ criterion (besides a ‘maximum hot-spot’ criterion).

## Slide 61: Annex slides

## Slide 63: Annex

## Slide 64: Overview circuits
Conceptual design review of the magnet circuits for the HL-LHC, 21-23 March 2016, https://indico.cern.ch/event/477759/
Circuit review 2017: 17 Mar 2017, https://indico.cern.ch/event/611018/timetable/
International Review of the Conceptual Design of the Cold Powering System for the HL-LHC Superconducting Magnets, 3-4 July 2017, https://indico.cern.ch/event/643197/
International review on the Inner Triplet Quadrupoles fo HL-LHC, 15-17 July 2019,
https://indico.cern.ch/event/828604/