## Slide 1: Impact of 440GeV Protons on Superconducting Wires and Tapes in a Cryogenic Environment
A. Will et al.
Karlsruhe Institute of Technology (KIT) / CERN (TE-MPE-PE)
Gentner Day 30.10.2019

## Slide 2: Beam impact on s.c. magnets - Example
Injection kicker magnets
Injection absorber
Superconducting magnet
particle shower
Quench ! Damage ?
One such event per year in today’s LHC possible. No damage observed so far.
in HL-LHC:
    increase of beam intensity
    new inner triplet magnets using Nb3Sn
  investigate the damage limits of superconducting magnets !
LHC BEAM
Injection Failure LHC
Slide Courtesy V. Raginel, EUCAS 2017, “First Experimental Results on Damage Limits of Superconducting Accelerator Magnet Components due to Instantaneous Beam Impact”

## Slide 3: Superconducting wires/ tapes
Nb-Ti strand (LHC)
Nb3Sn strand (HL-LHC)
HTS tapes
(future acc. magnets..?)
Image from C. Senatore, Lecture on Superconductivity, 2018
Image courtesy M. Meyer, CERN

## Slide 4: Beam impact experiment at cryogenic temperatures
First cryogenic beam impact experiment was performed in August 2018
Irradiation facility HiRadMat provides 440 GeV proton beams towards fixed targets
  1.2 x1011 ppb
  25 ns bunch spacing
  3.4 MJ max. per pulse
  beam size ~1mm
p+
horizontal stage
vertical stage
Notes: Maximum pulse parameters
  7.2 μs pulse length
  3.4 MJ stored beam energy

## Slide 5: Experimental set-up
Cryocooler based cryostat to cool samples to ~4K
s.c. strands placed within stacked copper holders
2 x 10 samples Nb-Ti
3 x 10 samples Nb3Sn
6 x 7 YBCO tapes
11 shots of 3e12 p @ 440 GeV
5

## Slide 6: Sample Holder
Energy deposition
  Temperature reached along a block of copper for 440 GeV proton beam, simulated with FLUKA
  Embedded samples along beam axis reach various hot spot temperatures
As in real failure case
  proton beam interacts with matter before impacting superconductors

## Slide 7: Visual inspection after beam impact
Nb3Sn, hot spot ~ 800 K
B1
B3
hot spot ~1200 K
Nb3Sn, hot spot ~ 1150 K
YBCO tape

## Slide 8: Ic in Nb-Ti strands after beam impact
No degradation of Ic observed
Ic measurements increasingly difficult at lower fields/higher currents, with increasing hot spot temperature
  Indicating issues with thermal stability of strands
Measurements indicate significant reduction of RRR at beam impact position  reduced minimum quench energy (MQE)
  MQE significantly reduced for samples with hot spots > 800 K
8

## Slide 9: Ic in Nb3Sn strands after beam impact
Significant Ic degradation for hot spots > 460 K
No measurable transport current for hot spots > 890K  samples destroyed
9

## Slide 10: Nb3Sn Strain dependence
Scaling law for Nb3Sn from literature
normalized strain dependent function s()
  s(=0) = 1
  monotonic decreasing towards zero for higher strains
Kramer form linearizes the Ic curve
Mentink, Goedeke et al.

## Slide 11: Bc2 of Nb3Sn strands after beam impact
Kramer fit:
Bc2 degrades with increasing hotspot temperatures due to plastic deformation of copper matrix
  Bc2 remains > 22 T for samples S1-S8
Ic degradation dominated by reduction of effective cross section due to filament breakage
11

## Slide 12: Results of thermo-mechanical simulations
Bc2 distribution from microscopic theory
Local lattice strain
Jc distribution from microscopic theory + cracked filaments
Axial strain
Thermo mechanical simulations performed* with ANSYS
  study the stresses within the strand cross-section due to thermal gradients and expansion
  study the interaction of the strands with the sample holder
  Use scaling laws from literature to predict Ic degradation of full strand
  Filament cracking via “strain irreversibility cliff” model (Cheggour et al.)
12
*Bachelor Thesis J. Schubert, to be submitted soon
Scaling laws

## Slide 13: Ic simulations for Nb3Sn
Measured Ic and Bc2 degradations well reproduced in the simulations
Absolute Ic degradation due to filament breaking hard to predict, but easy to fit, if Ic is measured.
  Results
  Bc2 degradation dominated by lattice strain
  Jc degradation combination of lattice & axial strain, major part due to filament cracking
13

## Slide 14: Conclusions & Outlook
Beam induced damage experiment performed with Nb-Ti, Nb3Sn strands and YBCO tapes @ 4.2 K reaching hot spot temperatures of up to 1200 K
Nb-Ti
  no Ic degradation observed
  Reduced thermal stability of strands (MQE)
Nb3Sn
  Significant Ic degradation for hot spots > 460 K
  Bc2 degradation observed in all samples
  Sources identified with the help of thermo-mechanical simulations
    Filament breaking due to too high axial strain  dominating factor for Ic degradation
    Residual strain from copper matrix and other copper/ bronze phases  Bc2 degradation & small Ic degradation
Microscopic analysis and tomography for most damaged Nb3Sn strands planned to verify model of filament breakage
YBCO tapes to be measured and compared to simulations
14

## Slide 15: A. Will, D. Wollmann, J. Schubert, A. Oslandsbotn, A. Monteuuis, K. Stachon, A.S. Mueller, A. Bernhard, M. Bonura, C. Senatore, M. Mentink, A. Verweij, B. Bordini Thanks to all Collaborators HiRadMat Team (F. Harden, A. Bouvard, V. Clerc, C. Saury, Y. Kadi, M. Butcher, J. Lendaro, J. Merino, L. Grec, ...), SPS OP shift crew, TE-MPE (F. Rodriguez Mateos, M. Bednarek, G. D'Angelo, M. Favre, B. Lindstrom, M. Vaananen, A. Liakopoulou, A. Siemko, R. Schmidt, R. Berberat, S. Kaufmann), TE-MSC (G. Kirby, A. Ballarino, B. Bordini, L. Bottura), TE-CRG (T. Koettig, ...), EN-STI-TCD (D. Grenier, ...), BE-BI (E. Effinger, C. Zamantos) University of Geneva (C. Senatore, M. Bonura, C. Barth, D. Zurmuehle) BRUKER (A. Usoskin) Scientific Magnetics (P. Penfold, B. Retz-Jones)
Work supported by the Wolfgang-Gentner-Program of the
German federal ministry of education and research