## Slide 1: Test results MCBXFBP1d HCMCBXFB001-E9000014
G. Willering, F. Toral, J.C. Perez, M. Bajko, J. Feuvrier, R. Bouvier, J.L. Guyon and with support from many others.
TE-MSC-TF SM18 magnet test facility
04-09-2019

## Slide 2: Test program and parameters
Test program outlined in EDMS 2166022

## Slide 3: Electrical Layout
Two independently powered nested dipoles.

## Slide 4: Individual powering

## Slide 5
Individual training Inner and outer Dipole
The inner dipole never quenched during individual powering.
Ramp rates:
At 1.9 K to 1755 A no quench at 2 A/s
11 Quenches in first cool down during initial training in assembly b
3 Quenches in first cool down of assembly c
0 quenches in assembly d
No detraining quenches following combined powering tests.
Coil memory very good.

## Slide 6: Quench locations Individually powered outer dipole
Outer layer
Inner layer
V3
V7
V4-V6
V10
V8
V9
V1
V1
Dipole | Coil | Segment | # quenches
Outer | 1 | Inner layer (V1-V3) | 2
Outer | 2 | Inner layer (V1-V3) | 3
Outer | 1 | Outer pole turn head (V6-V7) | 3
Outer | 2 | Outer pole turn head (V6-V7) | 1
Outer | 1 | Outer multiturn (V8-V9) | 1
Outer | 2 | Outer multiturn (V7-V8) | 1
 |  | Total | 11
Dipole | Coil | Segment | # quenches
Outer | 1 | Inner layer (V7-V8) | 3
 |  | Total | 3
Assembly b – CD 1
Assembly c – CD 1

## Slide 7: Combined powering

## Slide 8: Overview all powering
For completeness.

## Slide 9: Combined powering. Assembly b, c and d compared
Assembly b and c had limited performance. Highest percentage of about 50 % of the nominal torque reached.
Assembly d trained to nominal current in both dipoles. Later a maximum of 104 % of nominal torque was reached (102 % Inom)
Main conclusion
First assembly reaching nominal!

## Slide 10: Combined powering – changing torque direction
Training 1 was rather fast
Training 2 in the other quadrant (different torque direction) started at a lower current, but still reached nominal current.
Retraining in the first quadrant, started at a lower current than training 1, but was increasing faster.
Training 1
Training 2
Inversed
Retraining
Special training, switching torque direction each powering cycle, see next slide

## Slide 11: Changing torque direction from test to tests
With various directions of current
(IID = 0.5 IOD , IID = IOD and IID = 2 IOD)
In Quadrant 1 and 3 the quenches occur at a torque of 40 to 73 % and in quadrant 2 and 4 between 36 and 50 % of the torque.
Possibly some training effect seen.
Very laborious work, since we do not have bi-polar power converters yet. Manual invertion of the powering cables needed.

## Slide 12: No quench cycle
A cycle was made to shown a non-quench surface.
It follows the 40 % torque line in quadrant 1 and 3 and 30 % torque line in quadrant 2 and 4.
No quench was recorded, so this is a stable zone.

## Slide 13: No quench cycle
A second cycle is defined following input from our beams colleagues.
The cycle in orange is foreseen to be done today.

## Slide 14: Termal cycle

## Slide 15: Retraining after thermal cycle
CD 1 training: ramp inner, then outer dipole
CD 2 training: simultaneous ramp
(with quenches mainly in the inner coil, the diagonal may give a slight advantage in quench margin).
Note: Cool down 1 ended with a fully trained magnet in Quadrant 1.
Fraction of torque for easier characterization:
Virgin training in quadrant 1 started at rather high torque for first quench.
Cool down 2 retraining is in about the same rate as virgin training: loss of memory.
Training in quadrant 1 after having a fully trained magnet in quadrant 2 leads to longer retraining than thermal cycle.

## Slide 16: Conclusion
Individual powering: Great performance. No quenches in assembly d.
Combined powering: First magnet trained to 102 % of nominal current and 104 % of nominal torque!! Good performance.
Swapping torque directions creates significant detraining. This is is a main remaining challenge for this magnet.
Thermal cycle shows loss of memory, but reached again nominal current in combined powering.