## Slide 1
  Roberto Cardella
  ESR 9
  Sv. Petra Riedler (CERN)
  Sv. Heidi Sandaker (UiO)
  CERN EP-DT-DD
Advances on Integration of Monolithic Silicon Sensors in Pixel Trackers

## Slide 2: Outline
MALTA and MiniMALTA sensors
  From Assembly to Efficiency
  Rad Hardness studies
  Improvements and MiniMalta
A large area CMOS module
Chip To Chip Communication
Buried Microchannel in CMOS Devices
High Speed Data Transmission in Trackers
  LAPA testchip Results
Conclusions

## Slide 3: MALTA: Monolithic pixel detector from ALICE to ATLAS
3
DACs for analogue biases
LVDS driver
18.6 mm
The 512x512 pixel - 8 sectors
Small collection electrode sensor (shared with MONOPIX)
Low-power front-end (shared with MONOPIX)
Novel Asynchronous Readout architecture
For more details see presentation of I.Berdalovic and F.Piro

## Slide 4: Collection Efficiency Characterization - MALTA
ELSA-BONN Exposed MALTA to a 2.5 GeV electron beam during 3 days
SPS- CERN Down to in-pixel efficiency
Target Efficiency
>97% after

## Slide 5: Collection Efficiency Characterization - MALTA
Decreasing threshold from ~600 e- to ~250 e- (unirrad.)
Unirradiated: lowering the threshold gives full efficiency
3
3
3
3
3
3
Cannot go lower with threshold because of RTS noise and masking issue
See I.Berdalovic presentation
Notes: 60Mhit/s badwidth

## Slide 6: Collection Efficiency Characterization - MALTA
Could not reach lower threshold
(RTS + MASKING ISSUE)
Decreasing threshold from ~600 e- to ~250 e- (unirrad.)/350 e- (irrad.)
Unirradiated: lowering the threshold gives full efficiency
Neutron irradiated
inefficiency in pixel corners due to low lateral electric field
3
3
3
3
3
3
Notes: 60Mhit/s badwidth

## Slide 7: Efficiency vs. deep p-well coverage

## Slide 8: Efficiency vs. deep p-well coverage
Deep p-well only needed under n-wells of PMOS transistors
In-pixel efficiency can be correlated to deep p-well coverage around the collection electrode
Removed deep p-well results in higher overall efficiency due to higher lateral electric field

## Slide 9: Pixel design improvements
Additional “extra-deep p-well” layer
Already known by TowerJazz: no process R&D needed
Gap in the n- layer
requires only a change of the existing mask for the n-layer
Magdalena Munker
After irradiation simulated current pulse

## Slide 10: Mini MALTA pixel matrix
Pixel size: 36.4 μm x 36.4 μm
64x16 pixel matrix includes 8 sectors with splits on analogue front-end design, reset mechanism and process
MiniMALTA with synchronization and fixes for improved charge collection

## Slide 11: Testbeam campaigns
EUDAQ DURANTA telescope in DESY MALTA telescope in ELSA

## Slide 12: Mini MALTA Collection Efficiency
Before Irradiation

## Slide 13: Mini MALTA Collection Efficiency
Neutron Irradiated

## Slide 14: Mini MALTA Collection Efficiency
Neutron Irradiated
Matching ATLAS ITk requirements!

## Slide 15: CMOS development for the ATLAS ITk
Outermost layer of ITk Pixel Barrel
    2016 quad modules
    3m2 (~45% of outer barrel layers)
Monolithic CMOS sensors were considered as option for the outermost layer
    Saves bump bonding for ~45% of outer barrel system
    Substantial cost reduction and reduced module assembly time
    Requires “Drop-In” module compatibility to hybrid module
Hybrid Module
Monolithic Module
Notes: The outermost layer of he Itk pixel barrel covers an area of 3 square meters, around 45 % of the all barrel. The cost of assembly of the sensor modules is quite relevant in the case of Hbrid pixels. For this reason some R&D are on going to study the possibility of using Monolitics pixels, with a compatible drop in solution for the outermost layer, reducing cost and assembly time.

## Slide 16: Integrating a CMOS Module in a Tracker
Module Design
Sensor cooling
Dead Area Minimization
Data Transmission
Notes: The outermost layer of he Itk pixel barrel covers an area of 3 square meters, around 45 % of the all barrel. The cost of assembly of the sensor modules is quite relevant in the case of Hbrid pixels. For this reason some R&D are on going to study the possibility of using Monolitics pixels, with a compatible drop in solution for the outermost layer, reducing cost and assembly time.

## Slide 17: Sensor Cooling in HEP
NA62 Hybrid with Silicon Cooling Plate
Pixels operated at -30 ˚C to avoid thermal runaway
Critical Parameters
Good thermal conductivity
Low thermal expansion mismatch between parts
Integration with mechanics
Embedding the channels in the sensor!
Could improve all the three parameters
Buried Channels Technology (BCT)
  J. Bronuzzi, R. Callegari, R. Cardella, C. Lipp, A. Mapelli, P. Riedler
Notes: The outermost layer of he Itk pixel barrel covers an area of 3 square meters, around 45 % of the all barrel. The cost of assembly of the sensor modules is quite relevant in the case of Hbrid pixels. For this reason some R&D are on going to study the possibility of using Monolitics pixels, with a compatible drop in solution for the outermost layer, reducing cost and assembly time.

## Slide 18: BCT Process
DRIE of 30 µm deep trenches (3 x 10 µm)
XeF2 etching of microchannels (diam. 40 µm)
Trenches filled with Parylene (5 µm)
25 µm
50 µm
100 µm
Processed at the CMI – EPFL, Lausanne

## Slide 19: MALTA with BCT

## Slide 20: MALTA with BCT

## Slide 21: MALTA with BCT

## Slide 22: MALTA with BCT – Functional Test
55Fe source scan
  Peaks fit comparable
  Distance of the peaks within the gain dispersion of MALTA

## Slide 23: MALTA with BCT – Functional Test
55Fe source scan
  Peaks fit comparable
  Distance of the peaks within the gain dispersion of MALTA
Collection Efficiency
  Readout issue reduced the efficiency of ALL detectors to ~70%
  Comparable efficiency for the different ROIs

## Slide 24: MALTA with BCT – Functional Test
55Fe source scan
  Peaks fit comparable
  Distance of the peaks within the gain dispersion of MALTA
Collection Efficiency
  Readout issue reduced the efficiency of ALL detectors to ~70%
  Comparable efficiency for the different ROIs
BCT process does not change the device performance!

## Slide 25: BCT Thermal Test - No Cooling
Hot area about 29˚C

## Slide 26: 5ml/min -> 10 ml/min
Hot area from 29˚C to 24˚C, using “fresh” water

## Slide 27: Data Transmission from Module
Merged Output
Data
Several solutions to transmit data from a module to the readout
Master/Slaves configuration:
Avoid large number of output connections
Could simplify flex design
Only one sensor transmits data over a long distance
DATA

## Slide 28: Chip 2 Chip Communication
Wirebond connection
Flip chip connection
MALTA can transmit power and data asynchronously to a neighboring chip (via CMOS pad), merging the data of multiple pixel matrix in just one parallel output
Connection between neighboring chips using flip chip
Better for assembling
Allow additional electronics in the flipchip

## Slide 29: MALTA Chip to Chip Data Transmission
Wirebond connection
Flip chip connection
MALTA can transmit power and data asynchronously to a neighboring chip (via CMOS pad), merging the data of multiple pixel matrix in just one parallel output
Connection between neighboring chips using flip chip
Better for assembling
Allow additional electronics in the flipchip
Can save Power and Reduce the Material Budget!

## Slide 30: MALTA Chip2Chip data transmission
MALTA_C W7R22
MALTA_C W7R23

## Slide 31: MALTA Chip to Chip Data Transmission
90Sr source
MALTA_C W7R22
MALTA_C W7R23
Compatible results in both directions

## Slide 32: LAPA: pseudo-LVDS for the ATLAS Pixel Apparatus
280 X 240µm2 (2 pad pixel pitch)
Tunable DC current (7x 0.8mA )
Modular capacitive coupled pre-emphasis: 16 blocks driving 25fF each.
Vcm feedback control at 0.8V.
External 100 Ω differential termination
40 drivers integrated in MALTA (up to 2Gb/s)
Dedicated testchip
5Gb/s
280 µm
240 µm

## Slide 33: LAPA Receiver
320 X 240 {2 pad pixel pitch) µm2
Internal selectable 100 Ω termination resistor
5Gb/s

## Slide 34: LAPA eye diagram measurement
5Gb/s
1.28Gb/s (ITk specification)
Jitterp-p= 71ps
Jitterp-p= 38ps

## Slide 35: LAPA @1.28 Gbit/s on FLEX ITk prototype
Flex for data transmission out of the ITk system (length~5m)

## Slide 36: Conclusions
Several R&D towards the integration of CMOS pixel sensors have been carried on.
A CMOS compatible microchannel fabrication process, has been successfully performed with the MALTA sensor. The sensor test demonstrate that the chip performance are not degraded after processing. The preliminary cooling tests demonstrate that this approach could be use in future applications.
The data transmission in the tracker has been addressed with the development of a chip to chip communication schema and the design of a 5Gb\s low-power LVDS driver and receiver (LAPA). Both are promising to reduce power consumption, hence the overall material budget.
Studies on a CMOS module have been performed, aiming to define the constrains for the future CMOS sensor design, and minimize the dead area.
The small collection electrode shows a collection efficiency >97% after neutron irradiation to.
The first version of the sensor (MALTA), suffers from degraded efficiency in the pixel corners after irradiation.
Two process modifications have been developed using technology simulations, promising to improve the sensor radiation-hardness.
The two new versions of the pixel have been implemented in the MiniMALTA sensor, which confirmed the results of the simulations, achieving the target radiation hardness, matching the ATLAS ITk outermost layer requirements. However, the collaboration has chosen to use Hybrid Pixel as baseline solution for the detector upgrade.

## Slide 37: My Year
Exam @ UiO
IMEC - COURSE
ELSA- TESTBEAM
University of Glasgow
PIXEL2019 Taipei
Guiding in ATLAS cavern

## Slide 38: My Year
Exam @ UiO
IMEC - COURSE
ELSA- TESTBEAM
University of Glasgow
PIXEL2019 Taipei
Guiding in ATLAS cavern
Thank you for the attention

## Slide 39: LAPA H-BRIDGE
7 HBRIDGE blocks of 0.8mA - max: total 6mA

## Slide 40: LAPA-PRE-EMPHASIS
16 BLOCKS driving 25fF coupled with the output pad

## Slide 41: Pre Emphasis Simulations
Simulations of the LVDS OUTPUT

## Slide 42: LAPA Single Channel Schema
LVDS_IN_P<X>
LVDS_IN_N<X>
TR_EN
CMOS_IN<X>
LVDS_RX_EN
LVDS_RX_EN
LAPA_CMOS_DRIVER_SEL<X>
LAPA_CMOS_DRIVER_SEL<X>
CMOS_OUT<X>
LVDS_OUT_P<X>
LVDS_OUT_N<X>

## Slide 43: LAPA TESTCHIP SIMULATION
2.5GHz LVDS IN – LVDS OUT. 100Ω termination. 1pF load. Simulated jitter=45ps

## Slide 44: LAPA
Preliminary power consumption
Expected static power consumption
Measurements on test chip
Static+Dynamic 1.28Gb/s | Current [mA] | Power [mW]
5 Hbridge | 6 | 10.8
7 Hbridge | 8 | 14.4
Static | Current [mA] | Power [mW]
5 Hbridge | 4 | 7.2
7 Hbridge | 5.2 | 10

## Slide 45: First signs of life from MALTA
ANALOG pixel output
Digital signal from read-out
MALTA (not the one under test)

## Slide 46: First signs of life from MALTA
Happy Designers
ANALOG pixel output
Digital signal from read-out
MALTA (not the one under test)