## Slide 1: Project Plan Resume
WPO: Annealing of cooper sheets
WP1: 1,3GHz copper cavities spinning
WP2a: simulacra test on variable annealing temperatures
WP2b: simulacra test on intermediate dies

## Slide 2: 1,3 GHz Spinning and Spinnability Test
1,3 GHz Spinning:
  The old operator is retired, we are looking for the possibility to contract him for these treatments (next week we will have the final meeting)
Spinnability Test:
  Copper Sheet annealed with the standard treatment at 500°C for 2h
  We had a little delay for the contract with Padua University
  We established the hardness test and finalizing the test definition for the spinnability
1 Month delay from the original schedule

## Slide 3: Spinnability Test
First Half Cell:
Test Spinning with fixed Angle (copying the shape of the cavity) First
Tensile Test at the status of the material before the spinning

## Slide 4: Spinnability Test
First Half Cell:
Test Spinning with fixed Angle (copying the shape of the cavity) First
Tensile Test at the status of the material before the spinning

## Slide 5: Spinnability Test
Second Half Cell for 3 different Annealing Temperatures:
Test Spinning with fixed Angle (copying the shape of the cavity) Starting from the simulacrum obtained from the first half cell spinning
Tensile Test at the status of the material before the spinning of the second half cell at three different Annealing temperatures
Diameter of the base of the cone in the range 150-200 mm

## Slide 6: Spinnability Test
Second Half Cell for 3 different Annealing Temperatures:
Test Spinning with fixed Angle (copying the shape of the cavity) Starting from the simulacrum obtained from the first half cell spinning
Tensile Test at the status of the material before the spinning of the second half cell at three different Annealing temperatures
Diameter of the base of the cone in the range 150-200 mm
T1
T2
T3