## Slide 1: Electron transport via defect network
Ieva Guigaitė
Juozas Vaitkus
Darius Abramavičius

## Slide 2: Motivation
24th RD50 workshop, Bucharest
Irradiation by high energy particles induced defect network
Electron lifetimes are sensitive to geometry
Defects form nano-size clusters
Bulk theory is not sufficient

## Slide 3
High Energy Particle (HEP) destroys the lattice:
HEP
Vacancy-rich
region
Interstitial-
rich region
Disordered
region
TRIM and TCAS simulation results, presented by G. Lindstroem, 24th RD50 workshop, Bucharest, 2014.
After relaxation of cascade deffect and recombination of I-V pairs the rest of the vacancies and interstitials remain separated in space.

## Slide 4: Percolation network
Classical site percolation problem
p=0.25
p=0.35
p=0.65

## Slide 5: Quantum percolation network
Very sensitive to electron delocalization pattern

## Slide 6: Percolation network
Percolation behavior of electrical conduction has been well demonstrated in conductive polymer composites (CPC), carbon nanotubes.
Composites Science and Technology, v 170, 20 January 2019, Pages 70-76

## Slide 7: vacancy
interstitial
Electron density

## Slide 8
Vacancy and Interstitial defect
Vacancy defect, Td symmetry.
Wave function of a localized electron
in the acceptor site.
Neutral vacancy defect is known to be of
the acceptor type.
Interstitial defect, Td symmetry.
Wave function of a localized hole
in the donor site.
Interstitial defect in Td symmetry state is known
to be of the donor type (Ec – 0.39 eV)
Mukashev et al, Jpn. J. Appl. Phys. 21, 399 (1982).
simulations were performed by Ernestas Žąsinas (Vilnius University)

## Slide 9: Quantum percolation network
Very sensitive to electron delocalization pattern

## Slide 10: Electron transport network

## Slide 11: Electron transport theory
Tight binding Hamiltonian
(only defect sites)
Electron creation/annihilation operators
Phonon normal modes

## Slide 12: Coherent processes
Zero-order terms
Stationary eigenstates
Electron Green’s function
Transfer amplitude

## Slide 13: Incoherent processes
Electron scattering by phonons
Quantum master equation
Thermal equilibrium of phonons
Markovian Redfield equation
The “observed” kinetics

## Slide 14: Acoustic phonons
Hopping amplitude depends on distance
For acoustic phonons dispersion relation is simple, wavevectors
Finally the electron transfer rate

## Slide 15: Relaxation pathways (energy representation)
Chart: 
 | -1.9727e-05 | 1.332e-10 | 1.7231e-12 | 8.4496e-12 | 3.9177e-07 | 2.6861e-06 | 1.2654e-06 | 1.9835e-11 | 3.4826e-08 | 3.1098e-07 | 5.0634e-07 | 2.8625e-05 | 1.4457e-06 | 0.00077149 | 2.1873e-05 | 0.00038293 | 8.1639e-05 | 5.8905e-08 | 6.4783e-06 | 2.0381e-07 | 3.6531e-08 | 1.2271e-05 | 2.1129e-07 | 4.3766e-05 | 0.00011855 | 3.5031e-05 | 1.8884e-06 | 7.3691e-08 | 1.3951e-07 | 8.474e-07 | 4.7809e-08 | 3.6773e-06 | 5.5964e-06 | 7.0868e-08 | 2.6215e-05 | 2.4205e-05 | 0.0029642 | 5.1677e-06 | 3.4946e-05 | 3.1291e-06 | 1.7761e-05 | 5.7712e-07 | 3.9709e-06 | 2.6186e-05 | 1.7737e-09 | 9.7484e-06 | 8.9609e-06 | 7.288e-08 | 2.918e-06 | 2.8762e-07 | 0.00011348
 | 1.1985e-10 | -1.6996e-05 | 3.2211e-09 | 1.2075e-08 | 4.1219e-08 | 2.878e-07 | 1.36e-07 | 2.6525e-07 | 5.064e-06 | 6.1416e-06 | 8.4482e-07 | 2.3639e-05 | 5.7342e-06 | 9.2117e-05 | 1.42e-06 | 2.6477e-05 | 8.702e-05 | 7.9244e-06 | 8.6984e-05 | 4.2214e-06 | 1.2821e-06 | 0.00034011 | 3.1113e-05 | 0.0012863 | 0.00038738 | 0.00039759 | 5.609e-05 | 1.0941e-06 | 3.9723e-06 | 3.6027e-05 | 1.8925e-06 | 2.856e-05 | 8.8643e-05 | 6.402e-06 | 0.00019381 | 1.9026e-05 | 0.00023901 | 1.3459e-05 | 6.9798e-05 | 6.6663e-06 | 5.8903e-05 | 2.7803e-05 | 2.5296e-05 | 4.4303e-06 | 1.6173e-05 | 5.8616e-06 | 2.7995e-06 | 1.0784e-05 | 3.6681e-06 | 2.7362e-05 | 6.5133e-06
 | 1.5161e-12 | 3.1498e-09 | -3.2457e-06 | 2.1447e-09 | 7.9017e-10 | 5.5281e-09 | 2.3339e-09 | 3.2284e-05 | 2.417e-07 | 1.2619e-07 | 1.6737e-08 | 4.5579e-07 | 1.1077e-07 | 1.4785e-06 | 1.8542e-08 | 4.0973e-07 | 1.8653e-06 | 1.363e-07 | 1.5837e-06 | 9.6578e-08 | 7.7773e-08 | 5.0653e-06 | 0.00036932 | 2.4255e-05 | 4.6652e-06 | 2.3656e-05 | 1.4386e-06 | 2.4512e-08 | 8.3923e-08 | 7.5362e-07 | 3.5131e-08 | 6.1824e-07 | 1.9629e-06 | 1.0855e-07 | 3.9844e-06 | 4.3175e-07 | 2.6813e-06 | 2.6152e-07 | 1.117e-06 | 1.1504e-07 | 1.1139e-06 | 1.1805e-06 | 5.443e-07 | 7.2815e-08 | 0.00028465 | 1.0325e-07 | 4.899e-08 | 0.00010805 | 0.00011091 | 8.5678e-05 | 7.9596e-07
 | 7.2467e-12 | 1.1509e-08 | 2.0906e-09 | -7.5239e-06 | 4.4672e-10 | 3.155e-09 | 1.7865e-09 | 3.0972e-05 | 4.139e-07 | 6.3587e-08 | 8.1244e-09 | 2.61e-07 | 6.1387e-08 | 8.1537e-07 | 8.5604e-09 | 2.2401e-07 | 1.3706e-06 | 6.7899e-08 | 1.6376e-06 | 5.0334e-08 | 1.8087e-07 | 1.1096e-05 | 0.0011899 | 1.5795e-05 | 4.5586e-06 | 2.6931e-05 | 7.283e-07 | 1.3289e-08 | 5.7842e-08 | 4.9259e-07 | 1.8695e-08 | 2.5905e-07 | 1.1282e-06 | 6.0747e-08 | 3.3637e-06 | 5.0142e-07 | 1.5222e-06 | 1.5727e-07 | 4.8723e-07 | 7.4522e-08 | 6.3045e-07 | 1.7412e-06 | 4.0525e-07 | 4.1843e-08 | 0.00037117 | 5.4368e-08 | 3.6473e-08 | 1.1984e-05 | 0.00017151 | 0.00011373 | 7.0294e-07
 | 1.7006e-08 | 1.9886e-09 | 3.8983e-11 | 2.261e-11 | -0.00023832 | 6.9381e-06 | 2.9314e-05 | 2.7203e-13 | 3.5539e-11 | 5.6399e-05 | 8.016e-06 | 9.4412e-05 | 0.00035226 | 7.324e-06 | 5.7114e-08 | 1.4509e-07 | 2.4559e-05 | 2.4666e-09 | 0.00011102 | 3.2461e-05 | 7.9365e-05 | 3.5868e-05 | 1.4501e-07 | 2.0623e-05 | 1.5653e-05 | 6.5671e-06 | 3.0189e-08 | 2.8983e-07 | 2.0394e-07 | 2.7721e-08 | 5.3634e-07 | 2.8459e-08 | 0.00011639 | 5.0297e-09 | 2.6462e-05 | 0.0001837 | 9.6262e-06 | 3.5421e-05 | 7.1426e-05 | 1.0142e-05 | 0.00023591 | 5.7566e-06 | 3.6554e-05 | 0.00020776 | 5.1528e-10 | 0.00012307 | 0.0018914 | 2.2301e-08 | 1.6244e-07 | 1.1019e-08 | 1.368e-05
 | 1.0589e-07 | 1.2609e-08 | 2.4768e-10 | 1.4502e-10 | 6.3009e-06 | -0.00035948 | 1.2715e-05 | 4.6002e-13 | 1.5372e-10 | 0.00011053 | 1.4084e-05 | 0.00023692 | 9.2712e-05 | 1.223e-05 | 1.1609e-07 | 5.6098e-08 | 6.4255e-05 | 5.9424e-09 | 0.00025705 | 8.3715e-06 | 1.0513e-05 | 0.00025826 | 1.1436e-06 | 2.9976e-05 | 6.1303e-05 | 2.7451e-05 | 1.0705e-06 | 1.6513e-07 | 1.6228e-07 | 1.5431e-06 | 6.4798e-07 | 1.1315e-05 | 6.8399e-05 | 7.9569e-09 | 0.0002929 | 0.00027083 | 6.8565e-06 | 2.9479e-05 | 0.00011153 | 0.00030756 | 0.0011599 | 3.1028e-05 | 0.00018681 | 0.00016711 | 2.3036e-09 | 0.00036779 | 0.00049703 | 3.9166e-08 | 4.5458e-07 | 8.0858e-08 | 7.1781e-05
 | 3.2015e-08 | 3.8242e-09 | 6.7108e-11 | 5.27e-11 | 1.7085e-05 | 8.1601e-06 | -0.00024925 | 4.1322e-13 | 2.2444e-11 | 2.5883e-05 | 3.6445e-06 | 7.6983e-05 | 7.5966e-05 | 8.5363e-06 | 1.3271e-07 | 2.5301e-07 | 7.3991e-05 | 2.0527e-09 | 5.3832e-05 | 8.8083e-06 | 1.2034e-05 | 5.8904e-05 | 1.5494e-07 | 5.5135e-06 | 1.6586e-05 | 1.0789e-05 | 1.0067e-06 | 4.8487e-07 | 2.0747e-06 | 9.8505e-07 | 6.1754e-07 | 8.1737e-05 | 1.6685e-05 | 6.1368e-08 | 3.7462e-05 | 0.0001671 | 1.5531e-06 | 2.2525e-05 | 8.2837e-05 | 2.8967e-05 | 0.00015986 | 5.5272e-06 | 3.7688e-05 | 9.2968e-05 | 4.8255e-10 | 0.00056083 | 0.0003461 | 2.7321e-09 | 4.7286e-08 | 2.2748e-08 | 1.6423e-05
 | 4.3355e-13 | 6.4435e-09 | 8.0199e-07 | 7.8933e-07 | 1.3697e-13 | 2.5506e-13 | 3.57e-13 | -0.00013306 | 1.6089e-12 | 6.3826e-13 | 7.2025e-14 | 5.3553e-13 | 7.6653e-14 | 7.6072e-12 | 2.4081e-13 | 4.1653e-12 | 5.7219e-12 | 8.1724e-12 | 4.3649e-09 | 1.0109e-10 | 5.6678e-09 | 9.9467e-07 | 0.00033983 | 8.1454e-08 | 6.1169e-08 | 2.7784e-07 | 2.9072e-08 | 1.513e-10 | 6.8797e-11 | 1.1713e-10 | 5.7701e-11 | 3.5694e-09 | 4.5202e-10 | 7.5832e-12 | 3.1856e-09 | 8.6486e-11 | 2.6868e-09 | 2.6217e-11 | 5.3035e-12 | 2.2417e-12 | 1.8942e-10 | 8.1115e-10 | 2.2948e-11 | 1.3226e-11 | 4.8013e-07 | 4.3181e-11 | 2.7122e-10 | 0.00093394 | 0.00019736 | 0.00068296 | 1.1264e-07
 | 6.1131e-10 | 9.8792e-08 | 4.8218e-09 | 8.4711e-09 | 1.4371e-11 | 6.8446e-11 | 1.5572e-11 | 1.292e-12 | -2.1814e-05 | 1.4981e-11 | 1.4755e-10 | 3.3293e-10 | 5.1573e-11 | 1.0132e-08 | 4.0614e-10 | 3.3877e-08 | 2.6923e-09 | 2.2884e-05 | 2.587e-09 | 4.4327e-09 | 1.8761e-09 | 1.3771e-08 | 5.7634e-09 | 2.8362e-08 | 6.888e-07 | 1.704e-06 | 8.8316e-09 | 1.3581e-10 | 5.8694e-10 | 4.6425e-09 | 1.6746e-07 | 6.3025e-10 | 4.9875e-09 | 4.5259e-05 | 1.6255e-08 | 6.326e-09 | 3.4503e-07 | 1.1358e-07 | 2.7336e-08 | 1.9406e-09 | 1.6266e-08 | 1.2737e-05 | 2.2656e-06 | 5.3192e-08 | 2.0707e-08 | 3.5022e-09 | 7.1356e-09 | 6.7152e-06 | 3.3368e-05 | 5.602e-06 | 9.2584e-08
 | 5.0211e-09 | 1.1021e-07 | 2.3158e-09 | 1.1971e-09 | 2.0978e-05 | 4.5271e-05 | 1.6518e-05 | 4.7149e-13 | 1.3781e-11 | -0.00042515 | 2.6316e-07 | 3.7074e-05 | 2.3245e-06 | 9.023e-06 | 2.234e-07 | 5.1473e-06 | 5.8568e-05 | 3.4138e-08 | 7.6818e-05 | 2.3559e-07 | 5.9757e-05 | 2.1781e-05 | 1.0509e-07 | 3.0242e-05 | 7.1747e-06 | 2.3891e-06 | 7.3697e-06 | 3.8752e-07 | 1.4718e-06 | 3.1921e-06 | 3.2637e-06 | 1.2234e-05 | 1.7885e-05 | 3.7652e-07 | 9.2307e-05 | 0.00021251 | 2.1791e-07 | 0.00015048 | 1.6302e-05 | 4.5192e-05 | 1.3657e-05 | 2.9548e-06 | 3.4761e-05 | 0.00026181 | 2.209e-10 | 0.00036005 | 9.892e-06 | 1.1076e-06 | 1.603e-05 | 1.2275e-06 | 1.9449e-06
 | 7.9255e-09 | 1.4697e-08 | 2.9775e-10 | 1.4828e-10 | 2.8905e-06 | 5.5922e-06 | 2.2548e-06 | 5.1578e-14 | 1.3157e-10 | 2.5511e-07 | -0.00020068 | 4.1687e-06 | 5.2066e-07 | 1.5535e-05 | 1.9739e-07 | 3.9555e-05 | 9.2177e-06 | 2.4644e-07 | 1.5307e-05 | 0.00011946 | 1.2013e-05 | 1.6673e-06 | 1.2325e-08 | 3.2089e-06 | 9.8238e-07 | 4.1583e-07 | 6.5371e-07 | 4.4993e-08 | 1.0544e-07 | 6.1539e-07 | 1.9921e-05 | 1.6501e-06 | 1.2814e-06 | 4.1251e-06 | 1.0823e-05 | 1.1585e-05 | 7.6926e-06 | 0.00042715 | 0.0002479 | 1.0631e-05 | 1.7591e-06 | 3.5459e-06 | 3.9016e-05 | 2.916e-05 | 9.0773e-11 | 4.3567e-05 | 1.1225e-06 | 1.4451e-07 | 2.1432e-06 | 1.2119e-07 | 5.0455e-06
 | 3.5618e-07 | 3.2691e-07 | 6.4458e-09 | 3.7867e-09 | 2.7063e-05 | 7.4783e-05 | 3.7862e-05 | 3.0487e-13 | 2.3601e-10 | 2.857e-05 | 3.3139e-06 | -0.00067625 | 1.7781e-06 | 2.5756e-07 | 6.9664e-10 | 1.7609e-07 | 8.1281e-06 | 5.0705e-09 | 1.2191e-05 | 3.7011e-06 | 2.8141e-06 | 2.2704e-05 | 7.9535e-08 | 1.7609e-06 | 1.2567e-05 | 8.0304e-06 | 8.3479e-07 | 3.5246e-06 | 4.1854e-06 | 2.3752e-07 | 1.0776e-06 | 1.0495e-05 | 2.0342e-05 | 1.9418e-09 | 8.2465e-05 | 0.00012119 | 4.9801e-06 | 4.1201e-06 | 2.6e-05 | 0.00010055 | 0.00030818 | 7.8357e-06 | 6.0701e-05 | 0.00011962 | 1.0239e-09 | 0.0016054 | 0.001391 | 2.661e-06 | 3.686e-05 | 2.1008e-06 | 0.00021326

## Slide 16: Relaxation pathways (energy representation)
Chart: 
 | -1.9727e-05 | 1.332e-10 | 1.7231e-12 | 8.4496e-12 | 3.9177e-07 | 2.6861e-06 | 1.2654e-06 | 1.9835e-11 | 3.4826e-08 | 3.1098e-07 | 5.0634e-07 | 2.8625e-05 | 1.4457e-06 | 0.00077149 | 2.1873e-05 | 0.00038293 | 8.1639e-05 | 5.8905e-08 | 6.4783e-06 | 2.0381e-07 | 3.6531e-08 | 1.2271e-05 | 2.1129e-07 | 4.3766e-05 | 0.00011855 | 3.5031e-05 | 1.8884e-06 | 7.3691e-08 | 1.3951e-07 | 8.474e-07 | 4.7809e-08 | 3.6773e-06 | 5.5964e-06 | 7.0868e-08 | 2.6215e-05 | 2.4205e-05 | 0.0029642 | 5.1677e-06 | 3.4946e-05 | 3.1291e-06 | 1.7761e-05 | 5.7712e-07 | 3.9709e-06 | 2.6186e-05 | 1.7737e-09 | 9.7484e-06 | 8.9609e-06 | 7.288e-08 | 2.918e-06 | 2.8762e-07 | 0.00011348
 | 1.1985e-10 | -1.6996e-05 | 3.2211e-09 | 1.2075e-08 | 4.1219e-08 | 2.878e-07 | 1.36e-07 | 2.6525e-07 | 5.064e-06 | 6.1416e-06 | 8.4482e-07 | 2.3639e-05 | 5.7342e-06 | 9.2117e-05 | 1.42e-06 | 2.6477e-05 | 8.702e-05 | 7.9244e-06 | 8.6984e-05 | 4.2214e-06 | 1.2821e-06 | 0.00034011 | 3.1113e-05 | 0.0012863 | 0.00038738 | 0.00039759 | 5.609e-05 | 1.0941e-06 | 3.9723e-06 | 3.6027e-05 | 1.8925e-06 | 2.856e-05 | 8.8643e-05 | 6.402e-06 | 0.00019381 | 1.9026e-05 | 0.00023901 | 1.3459e-05 | 6.9798e-05 | 6.6663e-06 | 5.8903e-05 | 2.7803e-05 | 2.5296e-05 | 4.4303e-06 | 1.6173e-05 | 5.8616e-06 | 2.7995e-06 | 1.0784e-05 | 3.6681e-06 | 2.7362e-05 | 6.5133e-06
 | 1.5161e-12 | 3.1498e-09 | -3.2457e-06 | 2.1447e-09 | 7.9017e-10 | 5.5281e-09 | 2.3339e-09 | 3.2284e-05 | 2.417e-07 | 1.2619e-07 | 1.6737e-08 | 4.5579e-07 | 1.1077e-07 | 1.4785e-06 | 1.8542e-08 | 4.0973e-07 | 1.8653e-06 | 1.363e-07 | 1.5837e-06 | 9.6578e-08 | 7.7773e-08 | 5.0653e-06 | 0.00036932 | 2.4255e-05 | 4.6652e-06 | 2.3656e-05 | 1.4386e-06 | 2.4512e-08 | 8.3923e-08 | 7.5362e-07 | 3.5131e-08 | 6.1824e-07 | 1.9629e-06 | 1.0855e-07 | 3.9844e-06 | 4.3175e-07 | 2.6813e-06 | 2.6152e-07 | 1.117e-06 | 1.1504e-07 | 1.1139e-06 | 1.1805e-06 | 5.443e-07 | 7.2815e-08 | 0.00028465 | 1.0325e-07 | 4.899e-08 | 0.00010805 | 0.00011091 | 8.5678e-05 | 7.9596e-07
 | 7.2467e-12 | 1.1509e-08 | 2.0906e-09 | -7.5239e-06 | 4.4672e-10 | 3.155e-09 | 1.7865e-09 | 3.0972e-05 | 4.139e-07 | 6.3587e-08 | 8.1244e-09 | 2.61e-07 | 6.1387e-08 | 8.1537e-07 | 8.5604e-09 | 2.2401e-07 | 1.3706e-06 | 6.7899e-08 | 1.6376e-06 | 5.0334e-08 | 1.8087e-07 | 1.1096e-05 | 0.0011899 | 1.5795e-05 | 4.5586e-06 | 2.6931e-05 | 7.283e-07 | 1.3289e-08 | 5.7842e-08 | 4.9259e-07 | 1.8695e-08 | 2.5905e-07 | 1.1282e-06 | 6.0747e-08 | 3.3637e-06 | 5.0142e-07 | 1.5222e-06 | 1.5727e-07 | 4.8723e-07 | 7.4522e-08 | 6.3045e-07 | 1.7412e-06 | 4.0525e-07 | 4.1843e-08 | 0.00037117 | 5.4368e-08 | 3.6473e-08 | 1.1984e-05 | 0.00017151 | 0.00011373 | 7.0294e-07
 | 1.7006e-08 | 1.9886e-09 | 3.8983e-11 | 2.261e-11 | -0.00023832 | 6.9381e-06 | 2.9314e-05 | 2.7203e-13 | 3.5539e-11 | 5.6399e-05 | 8.016e-06 | 9.4412e-05 | 0.00035226 | 7.324e-06 | 5.7114e-08 | 1.4509e-07 | 2.4559e-05 | 2.4666e-09 | 0.00011102 | 3.2461e-05 | 7.9365e-05 | 3.5868e-05 | 1.4501e-07 | 2.0623e-05 | 1.5653e-05 | 6.5671e-06 | 3.0189e-08 | 2.8983e-07 | 2.0394e-07 | 2.7721e-08 | 5.3634e-07 | 2.8459e-08 | 0.00011639 | 5.0297e-09 | 2.6462e-05 | 0.0001837 | 9.6262e-06 | 3.5421e-05 | 7.1426e-05 | 1.0142e-05 | 0.00023591 | 5.7566e-06 | 3.6554e-05 | 0.00020776 | 5.1528e-10 | 0.00012307 | 0.0018914 | 2.2301e-08 | 1.6244e-07 | 1.1019e-08 | 1.368e-05
 | 1.0589e-07 | 1.2609e-08 | 2.4768e-10 | 1.4502e-10 | 6.3009e-06 | -0.00035948 | 1.2715e-05 | 4.6002e-13 | 1.5372e-10 | 0.00011053 | 1.4084e-05 | 0.00023692 | 9.2712e-05 | 1.223e-05 | 1.1609e-07 | 5.6098e-08 | 6.4255e-05 | 5.9424e-09 | 0.00025705 | 8.3715e-06 | 1.0513e-05 | 0.00025826 | 1.1436e-06 | 2.9976e-05 | 6.1303e-05 | 2.7451e-05 | 1.0705e-06 | 1.6513e-07 | 1.6228e-07 | 1.5431e-06 | 6.4798e-07 | 1.1315e-05 | 6.8399e-05 | 7.9569e-09 | 0.0002929 | 0.00027083 | 6.8565e-06 | 2.9479e-05 | 0.00011153 | 0.00030756 | 0.0011599 | 3.1028e-05 | 0.00018681 | 0.00016711 | 2.3036e-09 | 0.00036779 | 0.00049703 | 3.9166e-08 | 4.5458e-07 | 8.0858e-08 | 7.1781e-05
 | 3.2015e-08 | 3.8242e-09 | 6.7108e-11 | 5.27e-11 | 1.7085e-05 | 8.1601e-06 | -0.00024925 | 4.1322e-13 | 2.2444e-11 | 2.5883e-05 | 3.6445e-06 | 7.6983e-05 | 7.5966e-05 | 8.5363e-06 | 1.3271e-07 | 2.5301e-07 | 7.3991e-05 | 2.0527e-09 | 5.3832e-05 | 8.8083e-06 | 1.2034e-05 | 5.8904e-05 | 1.5494e-07 | 5.5135e-06 | 1.6586e-05 | 1.0789e-05 | 1.0067e-06 | 4.8487e-07 | 2.0747e-06 | 9.8505e-07 | 6.1754e-07 | 8.1737e-05 | 1.6685e-05 | 6.1368e-08 | 3.7462e-05 | 0.0001671 | 1.5531e-06 | 2.2525e-05 | 8.2837e-05 | 2.8967e-05 | 0.00015986 | 5.5272e-06 | 3.7688e-05 | 9.2968e-05 | 4.8255e-10 | 0.00056083 | 0.0003461 | 2.7321e-09 | 4.7286e-08 | 2.2748e-08 | 1.6423e-05
 | 4.3355e-13 | 6.4435e-09 | 8.0199e-07 | 7.8933e-07 | 1.3697e-13 | 2.5506e-13 | 3.57e-13 | -0.00013306 | 1.6089e-12 | 6.3826e-13 | 7.2025e-14 | 5.3553e-13 | 7.6653e-14 | 7.6072e-12 | 2.4081e-13 | 4.1653e-12 | 5.7219e-12 | 8.1724e-12 | 4.3649e-09 | 1.0109e-10 | 5.6678e-09 | 9.9467e-07 | 0.00033983 | 8.1454e-08 | 6.1169e-08 | 2.7784e-07 | 2.9072e-08 | 1.513e-10 | 6.8797e-11 | 1.1713e-10 | 5.7701e-11 | 3.5694e-09 | 4.5202e-10 | 7.5832e-12 | 3.1856e-09 | 8.6486e-11 | 2.6868e-09 | 2.6217e-11 | 5.3035e-12 | 2.2417e-12 | 1.8942e-10 | 8.1115e-10 | 2.2948e-11 | 1.3226e-11 | 4.8013e-07 | 4.3181e-11 | 2.7122e-10 | 0.00093394 | 0.00019736 | 0.00068296 | 1.1264e-07
 | 6.1131e-10 | 9.8792e-08 | 4.8218e-09 | 8.4711e-09 | 1.4371e-11 | 6.8446e-11 | 1.5572e-11 | 1.292e-12 | -2.1814e-05 | 1.4981e-11 | 1.4755e-10 | 3.3293e-10 | 5.1573e-11 | 1.0132e-08 | 4.0614e-10 | 3.3877e-08 | 2.6923e-09 | 2.2884e-05 | 2.587e-09 | 4.4327e-09 | 1.8761e-09 | 1.3771e-08 | 5.7634e-09 | 2.8362e-08 | 6.888e-07 | 1.704e-06 | 8.8316e-09 | 1.3581e-10 | 5.8694e-10 | 4.6425e-09 | 1.6746e-07 | 6.3025e-10 | 4.9875e-09 | 4.5259e-05 | 1.6255e-08 | 6.326e-09 | 3.4503e-07 | 1.1358e-07 | 2.7336e-08 | 1.9406e-09 | 1.6266e-08 | 1.2737e-05 | 2.2656e-06 | 5.3192e-08 | 2.0707e-08 | 3.5022e-09 | 7.1356e-09 | 6.7152e-06 | 3.3368e-05 | 5.602e-06 | 9.2584e-08
 | 5.0211e-09 | 1.1021e-07 | 2.3158e-09 | 1.1971e-09 | 2.0978e-05 | 4.5271e-05 | 1.6518e-05 | 4.7149e-13 | 1.3781e-11 | -0.00042515 | 2.6316e-07 | 3.7074e-05 | 2.3245e-06 | 9.023e-06 | 2.234e-07 | 5.1473e-06 | 5.8568e-05 | 3.4138e-08 | 7.6818e-05 | 2.3559e-07 | 5.9757e-05 | 2.1781e-05 | 1.0509e-07 | 3.0242e-05 | 7.1747e-06 | 2.3891e-06 | 7.3697e-06 | 3.8752e-07 | 1.4718e-06 | 3.1921e-06 | 3.2637e-06 | 1.2234e-05 | 1.7885e-05 | 3.7652e-07 | 9.2307e-05 | 0.00021251 | 2.1791e-07 | 0.00015048 | 1.6302e-05 | 4.5192e-05 | 1.3657e-05 | 2.9548e-06 | 3.4761e-05 | 0.00026181 | 2.209e-10 | 0.00036005 | 9.892e-06 | 1.1076e-06 | 1.603e-05 | 1.2275e-06 | 1.9449e-06
 | 7.9255e-09 | 1.4697e-08 | 2.9775e-10 | 1.4828e-10 | 2.8905e-06 | 5.5922e-06 | 2.2548e-06 | 5.1578e-14 | 1.3157e-10 | 2.5511e-07 | -0.00020068 | 4.1687e-06 | 5.2066e-07 | 1.5535e-05 | 1.9739e-07 | 3.9555e-05 | 9.2177e-06 | 2.4644e-07 | 1.5307e-05 | 0.00011946 | 1.2013e-05 | 1.6673e-06 | 1.2325e-08 | 3.2089e-06 | 9.8238e-07 | 4.1583e-07 | 6.5371e-07 | 4.4993e-08 | 1.0544e-07 | 6.1539e-07 | 1.9921e-05 | 1.6501e-06 | 1.2814e-06 | 4.1251e-06 | 1.0823e-05 | 1.1585e-05 | 7.6926e-06 | 0.00042715 | 0.0002479 | 1.0631e-05 | 1.7591e-06 | 3.5459e-06 | 3.9016e-05 | 2.916e-05 | 9.0773e-11 | 4.3567e-05 | 1.1225e-06 | 1.4451e-07 | 2.1432e-06 | 1.2119e-07 | 5.0455e-06
 | 3.5618e-07 | 3.2691e-07 | 6.4458e-09 | 3.7867e-09 | 2.7063e-05 | 7.4783e-05 | 3.7862e-05 | 3.0487e-13 | 2.3601e-10 | 2.857e-05 | 3.3139e-06 | -0.00067625 | 1.7781e-06 | 2.5756e-07 | 6.9664e-10 | 1.7609e-07 | 8.1281e-06 | 5.0705e-09 | 1.2191e-05 | 3.7011e-06 | 2.8141e-06 | 2.2704e-05 | 7.9535e-08 | 1.7609e-06 | 1.2567e-05 | 8.0304e-06 | 8.3479e-07 | 3.5246e-06 | 4.1854e-06 | 2.3752e-07 | 1.0776e-06 | 1.0495e-05 | 2.0342e-05 | 1.9418e-09 | 8.2465e-05 | 0.00012119 | 4.9801e-06 | 4.1201e-06 | 2.6e-05 | 0.00010055 | 0.00030818 | 7.8357e-06 | 6.0701e-05 | 0.00011962 | 1.0239e-09 | 0.0016054 | 0.001391 | 2.661e-06 | 3.686e-05 | 2.1008e-06 | 0.00021326

## Slide 17: Relaxation pathways (energy representation)
Electron delocalization extent
Poor correlation with electron energy

## Slide 18: Short range transfer (27-th)
27-th electron, delocalization = 2,72
Composition in site-basis
4->2 electron transfer

## Slide 19: Long range transfer (27-th)
Composition in site-basis
31->45 electron transfer
39-th electron, delocalization = 14,99

## Slide 20: Extensions
Lindblad equation approach
Non Markovian description
Time dependent variational approach
Time dependent delocalization

## Slide 21: Interstitials
Phys Rev Lett. 83, 2351, 1999
The split-110,
hexagonal,
(c) tetrahedral interstitial,
(d) the saddle point
Formation energies

## Slide 22
Vacancy – Interstitial pair (Frenkel pair ) defect
When vacancy and interstitial are approached to each other to form a pair
then the extra electrons given by interstitial are “pumped” away from the
interstitial site to the vacancy site. (Like in a ionic type molecule or crystal
electrons mainly are located nearby more electronegative ion.)
! Interstitial and vacancy exchange their roles:
Interstitial turns into acceptor and vacancy into donor:
Charged (+) system, one electron removed.
The hole wave function is located nearby
vacancy site (or the electron is donated away
by vacancy site).
Charged (-) system, one electron added.
The electron wave function (~80% of it) is
located nearby interstitial site (or the electron
is accepted by interstitial site).
simulations were performed by Ernestas Žąsinas (Vilnius University)

## Slide 23: Conclusions
Formation of clusters of the defect sites depends strongly on concentration of defects
Acoustic phonon description allows for simple model formulation for incoherent energy transport
Overlap of electron delocalized wavefunctions is necessary for electron transfer
Electron transport pathways can be visualized
Transition from coherent to diffusive transport may be important for various size clusters
Acknowledgement
Some simulations were performed by Ernestas Žąsinas
This work is coherent with CERN RD50 collaboration.
Thanks to Lithuanian Academy of Sciences for the grant LMA-CERN