## Slide 1
Istituto SPIN-CNR
Universita’ di Napoli Federico II
Dipartimento di Fisica “Ettore Pancini”
INFN Sezione di Napoli
Ruggero Vaglio
BASIC PRINCIPLES OF RF SUPERCONDUCTIVITY
EASISchool 3, Genova Sept. 28, 2020

## Slide 2
Two –fluid model
n
s
«local limit»

## Slide 3
(frequency independent)

## Slide 4
BCS (Matthis-Bardeen theory) :
1
1
0
Ns(E)/NN

## Slide 5
~
;
Surface impedance
d
d
S=d2

## Slide 6
Normal metals (Ohm law+Maxwell equations):
Superconductors (local limit):
Thin films :
d : film thikness

## Slide 7
Superconductors:

## Slide 8
Two fluid model:
HTS superconductors :

## Slide 9
BCS :
Low frequency limit :
Low temperature :

## Slide 10
Rs (a.u.)
BCS
Two-fluid
Chart: 
| 0 | 2.0000000000000052E-2 | 4.0000000000000112E-2 | 6.0000000000000338E-2 | 8.0000000000000224E-2 | 0.1 | 0.12000000000000002 | 0.14000000000000001 | 0.16000000000000075 | 0.18000000000000024 | 0.20000000000000004 | 0.22000000000000075 | 0.24000000000000021 | 0.26 | 0.28000000000000008 | 0.30000000000000032 | 0.32000000000000173 | 0.34000000000000186 | 0.36000000000000032 | 0.38000000000000184 | 0.40000000000000008 | 0.42000000000000032 | 0.4400000000000015 | 0.4600000000000003 | 0.48000000000000032 | 0.50000000000000011
 | 0 | 0.00040005 | 0.0016008 | 0.0036039 | 0.0064123 | 0.01003 | 0.014463 | 0.019717 | 0.0258 | 0.032722 | 0.040493 | 0.049126 | 0.058634 | 0.069034 | 0.080344 | 0.092583 | 0.10577 | 0.11994 | 0.13511 | 0.15132 | 0.16859 | 0.18698 | 0.20651 | 0.22724 | 0.24923 | 0.27253
HTS
BCS
HTS

## Slide 11
Non-local theory (Pippard 1950)

The local limit applies always well enough in superconducting compounds
and alloys (l small compared to λ , «local dirthy limit)) and HTS (ξo small
compared to λ, «local clean limit»), but not for high purity bulk Nb !
Nb, T=4.2K, f=1.5GHz
Benvenuti et al, Physica C
Physica C 316 ,153 (1999)
local limit validity zone
(l < ξo , RRR<20)
Full non-local theoretical calculation
(Halbritter code)
Setting :
with :
extends the validity of the BCS low
frequency, low temperature,dirthy
limit approximate formulas up to

## Slide 12
RsBCS for different superconducting materials in the local limit
Lines of equal RsBCS in the (n, TC) plane at T = 4.2 K and  = 0.5 GHz (V. Palmieri, Thesis , 1985)
128 n
64
32
16
8
4
2
1 n
0.5
0.25
8 10 12 14 16 18
100
10
1
Nb Thin film
MoRe
NbTiN
NbTiN (TS = 200 °C)
NbN
NbN (TS = 200 °C)
Nb3Sn
V3Si
MgB2

## Slide 13
Nb3Sn, T=4.2K
Rs BCS(Ω)
Nb, T=4.2K
Cu 77K
Superconductors :
Normal metals :
BCS
two fluid
RsBCS frequency dependence
10-3
10-1
10-2
10-6
10-5
10-4
0.1
10
1
100
YBCO measured values at 77K
YBCO polycrystalline, measured values at 77k
f (GHz)

## Slide 14
A.Andreone, A.Cassinese, A. DiChiara, M.Salluzzo , R. Vaglio, JAP 78,1862 (1995).
Ro
V3Si (BCS)
Measurements of the surface impedance temperture dependence :
Rs(μΩ)
T(K)
T(K)
Xs(T)/Xs(0)=λ(T)/ λ(0)
BCS theory, local limit
BCS theory, local limit

## Slide 15
Surface impedance measurements (Nb film)
Nb, 1.5GHz
Ro

## Slide 16
Honma et al, Physica C 484, 46 (2013)
Surface resistance measurements (YBCO film)
Ro

## Slide 17
BCS surface resistance dependence on the rf field amplitude
The following phenomenological expression appears to be approximately valid :
(up to intermediate rf fields)
There is no full consensus on the theoretical interpretation. One approach is to perform the
Matthis-Bardeen BCS calculations using the full DOS as modified in a current-carrying state :
Xiao et al, Physica C 490, 26 (2013)
Δ/Δo
For very pure samples negative α values have been
observed and can be justified within this model

## Slide 18
3) Defects due to localized «normal» or magnetic inclusions
4) ………………………………..
Residual resistivity possible origins :
2) Trapped magnetic flux
1) Grain boundaries (in policrystalline materials)

## Slide 19
Grain boundaries (polycrystalline materials)
S1, ψ1
S2,ψ2
Weak superconducting links : Josephson effect
Non-linear Josephson inductance
I
V
Ic
RJ

## Slide 20
Vaglio et al, Physical Review B 43, 6128 (1991)
S1, ψ1
S2,ψ2
Rogb
Brf/ BcJ
1
2

## Slide 21
Trapped magnetic flux
magnetic flux lines :
supercurrents
normal core
x
fluxon viscosity per unit lenght
m : fluxon mass per unit lenght 0
:
«depinning frequency»
̴
Gittleman and Rosenblum:
Phys Rev. Lett. 16, 734 (1966)

## Slide 22
+ Maxwell equations
General expression for the surface impedance of a superconductor in presence
of rigidly oscillating vortices , with the rf current perpendicular to the magnetic field
Surface reactance
Surface resistance
S. Calatroni, R.Vaglio : IEEE Trans. Superconductivity 2017

## Slide 23
For small fields, i.e. for a small number of trapped vortices :
with
The observed rf field dependence can be due to a nonlinear pinning force,
Calatroni, Vaglio, PRB Acc. & Beams 22, 022001 (2019)

## Slide 24
Istituto SPIN-CNR
Universita’ di Napoli Federico II
Dipartimento di Fisica “Ettore Pancini”
INFN Sezione di Napoli
Ruggero Vaglio
BASIC PRINCIPLES OF RF SUPERCONDUCTIVITY
Conclusions
Rf properties of materials are well characterized by their surface impedance. Superconductors present a non zero surface resistance but lower that any other material at low-intermediate frequencies
The rf properties of “conventional” superconductors are very well described by the BCS theory, but for the presence of a “residual” (temperature independent) term Ro. The rf field dependence is a still open theoretical issue
For most BCS superconductors of practical interest the local limit applies, where The BCS equations take a simple form at low frequency and T<Tc/2 (only for high purity, high RRR bulk Nb this is not true)
HTS are well described by a modified 2-fluid model. Also in this case a significant residual term is present a low temperatures.
The residual term Ro can have different origins and different frequency and rf field dependence. Some of the possible mechanisms (weak grain boundaries, trapped flux and others ) are well theoretically understood.
EASISchool 3, Genova Sept. 28, 2020