## Slide 1: SRF Cavity Fabrication
D. Sertore
Istituto Nazionale di Fisica Nucleare Laboratorio Acceleratori e Superconduttività Applicata Segrate - Italy

## Slide 2: Outline
SRF Cavity fabrication, a long chain …
From EM design to fabrication
A fabrication cycle
From raw Nb to sheets
From sheets to cavity
Cavity treatments

## Slide 3: Fabrication activities at LASA
INFN LASA has a long experience on cavity design and, in collaboration with industry, in fabrication of cavities
  We have significantly contributed to the design of the SNS cavities at 805 MHz
  TRASCO cavities were design at LASA and fabricated at 704.4 MHz
  LASA was deeply involved in the mass production of the 800 cavities for XFEL at 1.3 GHz
  20 3.9 GHz cavities for the third harmonic module of XFEL were designed at LASA and fabricated
  38 704.4 MHz cavities for the Medium Beta Section of the European Spallation Source
  2 650 MHz prototype cavities for the Low Beta Section of PIP-II in preparation for the 38 cavities in-kind contribution

## Slide 4: SC cavities production: a long chain, but…
    A chain is as strong as its weakest link !!!
Chain of - Material - Fabrication - Surface Preparation incl. cleanroom, media, procedures, human factor - Vacuum - Quality assurance
For high gradient / low loss SRF cavities all aspects have to be fulfilled

## Slide 5: SC cavities may have various “illness”

## Slide 6: Anomalous loss mechanism

## Slide 7: Some general statements
Anomalous loss mechanisms:
  Quench (local thermal instability) => material + fabrication (=> cleanliness)
  Field emission => Cleanliness of surface treatment, assembly, handling + vacuum
  Q-drop (without field emission) + Q-slope => ?
  Multipacting => Cavity shape + RF surface condition
  Hydrogen Q-disease => Chemical surface treatment
  Increased residual surface resistance => Cleanliness of surface treatment, assembly, handling + vacuum

## Slide 8: Present picture of field emission: observations
Metallic (conducting) particles or “scratches” of irregular shape; typical size: 0.5 - 20 µm
Only 5% - 10% of the particles emit
Hydrocarbon contamination of the vacuum system
Sulphur contamination after electropolishing process
Modified Fowler-Nordheim’s law :
typical -values between 50 and 500 for SRF cavities
AFN (FN emission area) not directly correlated to physical size of emitter
Notes: A short summary of field emission:
FE originates mainly from irregular shaped, electrical conducting particles. The typical size is in the order of µm. Regular shaped metallic particles show much less FE. Isolating particles show no or only weak FE. Typically only 5% - 10% of the particles emit.
Ebenfalls wichtig: hydrocarbon Verunreinigungen des Vakuumsystems
Both, dc and rf FE is well described by the modified FN-equation, which gives the exponential relation between current and local electrical surface field. Parameters are A and .  is the so-called field-enhancement factor. It varies between 50 and 500. A is the emission area, which is not identical with the physical emitter size.  is the Nb work function and C a constant.
For the major effects there is no substantial difference between rf and dc behaviour.

## Slide 9: FE onset field vs. defect size: correlations? YES
A. Dangwal, G. Müller Wuppertal University

## Slide 10: Some general statements: field emission
Field Emission is critical, more for multi-cell cavities for high RF accelerating fields
P. Kneisel + B. Lewis, SRF Workshop 1995: “Progress towards routinely achieving higher gradients for future applications of RF-superconductivity goes hand in hand with shifting the onset of field emission loading towards higher fields.”
“It is generally accepted that the field emission behavior of a niobium cavity reflects the level of cleanliness of the superconducting surfaces subject to the RF-fields.”
Improved clean preparation techniques allow an increased field emission onset
Notes: As you all know by your experience field emission is the major limitation of srf cavities of the last 5-10 years. It results in rapidly increasing losses limiting the operating gradient of the cavity and in accelaerator operation in dark currents limiting the machine performance.
The sentences of Peter given in his paper at the Saclay Workshop 10 years ago are absolutely valid:

## Slide 11: From EM design to fabrication

## Slide 12: Few considerations
From the EM point of view, the cavity is design at the operative conditions (usually 2 K, in vacuum, with tuner).
When you fabricate the cavity, you are at room temperature, in air and the cavity needs to be treated before being operational
You need then to consider
  Thermal shrinkage from 2 K to 300 K (geometry, frequency)
  Pressure effect (frequency)
  Dielectric constant effect (frequency)
  Over-metal for chemical treatment (geometry, frequency)
  Pre-tuning (frequency)
P.S. When you fabricate a cavity, be sure that the design couples with the feasibility of the processes you are going to apply

## Slide 13: The ESS example
Step | Df [MHz] | Cavity Frequency [MHz] | Comment
Goal Frequency |  | 704.420 MHz | 2 K in vacuum
Pre-load for tuner | -0.100 MHz | 704.320 MHz | Unloaded cavity at cold
Room Temperature | -1.028 MHz | 703.292 MHz | Shrinkage from 2 K to 300 K a
In Air | -0.234 MHz | 703.058 MHz | Dielectric constant b
Etching | +0.480 MHz | 703.538 MHz | Before Chemistry (150 mm) c
Weld Seam | +0.000 MHz | 703.538 MHz | Weld Seam perturbation d
a Integral shrinkage from 2 K to 300 K tabulated
b Inversely proportional to square root of dielectric constant
c Estimated from Slater’s perturbation on cavity inner surface
d Estimated from direct measurement. More significant for high frequency cavities

## Slide 14: A fabrication cycle

## Slide 15: The ESS fabrication cycle
Cavity EBW
Bulk BCP
180 mm
Annealing
De Hydrog.
Tuning
Final BCP: 20 mm + HPR
Accessories installation
Final Check and delivery
Subcomponents preparation
Cavity integration (He tank)
DESY
Nb sheets and raw materials
CEA
Al1
Al2
Al3
EC
EC
PC
PC
IC
ID
PD
CD
EGP
EGC
Al4
Al5

## Slide 16: From raw Nb to cavity

## Slide 17: Niobium
Niobium is THE material for fabrication of supercondiucting cavities
  Critical temperature Tc = 9.25 K
  High critical field (Hc(0 K)  240 mT)
  Chemically inert (surface covered by Niobium pentoxide Nb2O5)
  Easily machined and deep drawn
  Available as bulk and sheets of any size and different shapes
Highest between pure metals

## Slide 18: Niobium Production
CBMM, Arexà,Brazil
8 km

## Slide 19: Niobium Production
The leading use of niobium (about 75 %) is in the production of high strength steel alloys used in pipelines, transportation infrastructure, and structural applications.
Niobium is primarily derived from the complex oxide minerals of the pyrochlore group and carbonatites, usually together with Tantalum
The estimated global reserves appear more than sufficient to meet global demand for the foreseeable future, possibly the next 500 years

## Slide 20: Niobium Prodution Process
The ore (Pyroclore in this case) is treated and refined at different stages untill it reaches the purity necessary for the Electron Beam Refining.
The Electron Beam process reduces the impurites present in the incoming Niobium
EB Refining
2.75 m
35 cm

## Slide 21: Niobium sheets production

## Slide 22: Nb Technical Specifications (typical)

## Slide 23: Nb sheets QC at productor premises
Ingot
  RRR
  Mechanical Properties
  Gas analysis
  Crystallography
All sheets
  Visual Inspection
    Defects (i.e. scratches)
    Delamination
  “Rust” test
    Coarse check for Fe inclusions
Sample preparation for RRR measurement
Visual Inspections
Microstructure
Final Report

## Slide 24: Residual Resistance Ratio (RRR)
Electrical resistivity of metals at low temperatures is related to the impurity concentrations. The residual resistivity at T = 0 K is caused mainly by scattering of electrons by impurities.
Residual Resistivity Ratio
RRR depends on impurity content in the material (typical RRR for cavity is around 300)
RRR is linked to the Nb thermal conductivity by

## Slide 25: Nb Eddy Current Scanning
DESY Eddy Current principle
When an AC current flows in a coil in close proximity to a conducting surface the magnetic field of the coil will induce circulating (eddy) currents in that surface.
The magnitude and phase of the eddy currents will affect the loading on the coil and thus its impedance. If there is a deep crack in the surface immediately underneath the coil, it will interrupt or reduce the eddy current flow, thus decreasing the loading on the coil and increasing its effective impedance.
The operating frequency is between 100 kHz to few MHz and can span from the surface down into the materials for some hundreds of microns.
Iron Defect, probably included during rolling

## Slide 26: Eddy Current results
ESS Nb Sheets (456)
W. Singer et al., SUST 28 (2015) 085014
European XFEL
On the 15612 sheets
  26% scanned on both sides
  2% rejected (foreign material > 100 mm, delamination, etc.)
EXFEL Defects Analysis

## Slide 27: From sheets to cavity

## Slide 28: Cavity components

## Slide 29: Dumb-bell Fabrication (an example)
Nb sheets cutting
Deep drawing
Mechanical measurement
Cleaning (by ultrasonic cleaning +rinsing)
Trimming of iris region and reshaping of cups if needed
Cleaning
Rf measurement of cups
Buffered chemical polishing + rinsing (for welding of Iris)
Welding of Iris
Welding of stiffening rings
Mechanical measurement of dumb-bells
Reshaping of dumb bell if needed
Cleaning
Rf measurement of dumb-bell
Trimming of dumb-bells ( Equator regions )
Cleaning
Intermediate chemical etching ( BCP /20- 40 µm ) + rinsing
Visual Inspection of the inner surface of the dumb-bell
Local grinding if needed + (second chemical treatment + inspection )

## Slide 30: Mechanical QC
3D profile
Mechanical measurements
Half Cell dime control
Visual Inspection

## Slide 31: Frequency QC
Co.Co.De for HC and DB RF measurements
Measure frequency and length to determine how much to trim at the equator to obtain target frequency and length of the cavity fully welded
Pen Cells

## Slide 32: Mechanical Grinding
Mechanical grinding of visible local defects (deeper than 15 mm for EXFEL) with aluminum oxide grinding discs or rubberized abrasive (CRATEX®)
Rubberized abrasive

## Slide 33: Cavity parts EB welding
EC
EC
PC
PC
IC
Mxxx
ID
PD
CD
EGP
EGC
Degreasing and rinsing of parts
Drying under clean condition
Chemical etching at the welding area (equator)
Careful and intensive rinsing with Ultra Pure Water
Dry under clean conditions
Install parts to fixture under clean conditions
Install parts into Electron Beam (EB) welding chamber (no contamination on the weld area allowed)
Pump down to vacuum in the EBW chamber in the 10-5 mbar range
Welding and cool down of Nb to T < 150 °C, then venting with N2
Leak check of welds

## Slide 34: Electron Beam Welding
Welding under good vacuum, 10-5 mbar range
Broad welding seam
  Operate with defocussed beam
  Smooth underbead
Overlap at end of welding to avoid accumulation of impurities
Wait to cool down before opening chamber
Welding Scheme (circular raster)
Electron beam (Р0-power of the beam, r-spot radius on the surface, L-scanning amplitude, V- velocity of the beam movement)
Nb sheet
melting zone (z-depth of the melting zone)
JLAB EBW
ESS Weld Seam
4 mm

## Slide 35: Mechanical and frequency QC
After EBW, the cavity is mechanical measured, inner inspected and the frequency is controlled
Dimensional check

## Slide 36: Cavity treatment

## Slide 37: Overview
Claire Antoine CAS Erice

## Slide 38: A general consideration
Do not apply treatments that affect the Nb surface and could not be “accepted” by the next step
If a mistake is done, go back in the procedure until the step where contaminant can be removed without contaminating the system
Chemical reactions in many cases can not be stopped simply removing acid (residuals, no cooling, …). Rinsing is needed!
Do not contaminate US bathes with material that can not be diluted, as for silicone grease, oil, etc. Moreover take care of contaminants that can float over the liquid surface!
Wet components are more “sensitive” for collecting particles.
Duration limit for a final treated cavity is about 24 hours (XFEL) Do not leave open cavities for longer time
Do not make Nb surface worst than before with the next treatment!

## Slide 39: Cavity preparation for SRF qualification
Degreasing surfaces to remove contaminates
Chemical removal of exterior films incurred from welding
Removal of damage layer of niobium from fabrication ( 150÷200 mm)
Removal of hydrogen from bulk Nb
Mechanical tuning
Chemical removal of internal surface for clean assembly (10-20 mm)
– Additional “cleaning” steps if Electropolishing (EP) is used
High Pressure Rinsing (HPR) to remove particulates from interior surfaces (incurred during chemistry and handling)
Drying of cavity for assembly in cleanroom (reduce risk of particulate adhesion and reduce wear on vacuum systems)
Clean assembly
Clean evacuation
Low-temperature baking

## Slide 40: Cavity preparation for SRF qualification
Degreasing surfaces to remove contaminates
Chemical removal of exterior films incurred from welding
Removal of damage layer of niobium from fabrication ( 150÷200 mm)
Removal of hydrogen from bulk Nb
Mechanical tuning
Chemical removal of internal surface for clean assembly (10-20 mm)
– Additional “cleaning” steps if Electropolishing (EP) is used
High Pressure Rinsing (HPR) to remove particulates from interior surfaces (incurred during chemistry and handling)
Drying of cavity for assembly in cleanroom (reduce risk of particulate adhesion and reduce wear on vacuum systems)
Clean assembly
Clean evacuation
Low-temperature baking

## Slide 41: Degreasing and surface preparation
After mechanical fabrication, all contaminants (fingerprints, oil, residuals from machining and QC) must be removed, similar to preparation of Ultra High Vacuum components.
Typical process:
  Water rinsing with specific detergent (Tikopur TR33, Micro -90, Liqui-Nox) usually 1-3%
    For “dirty” component, alcohol and acetone could be used before
  Water is usually Ultra Pure Water with 18 M cm and filtered below 200 nm
  Often in HEPA filter environment
For entering ISO7 clean room, dishwashers are used for small components and car-wash for large components
For entering ISO4 clean room, UltraSound is mandatory

## Slide 42: Ultra Pure Water
UPW Specifications
  Resistivity: 18.2 M cm
  Total organic carbon (TOC): < 5 ppb
  Particulate counts (> 0.3 mm/l): < 10
  Bacteria counts: < 0.1 CFU/100 ml
The water quality is as for the semiconductor industry: ASTM- D 5127-07 E-1.2
Water softener
Filter
Tap water
RO - Revers osmosis
First stage
RO - Revers osmosis
Second stage
DRAIN
DRAIN
STORAGE TANK
N2
Hg UV
lamp
Circulation
pump
UPW loop (PVDF)
POU
with filter
Diaphragm
for trickle
flow
Filter
Ultra filtration +
resins
Hg UV lamp
E
D
I
Hg UV lamp
Typical UPW plant

## Slide 43: Ultra Pure Water QA
Conductivity: ion concentration, indicates water purity with respect to “salts”, ions, metals, anions, etc.
TOC: Total Organic (oxidizable) Carbon. Organic carbon, but for instance lubricant oils are hard to be oxidized and therefore are not easily measured with TOC monitor.
Particle count: number of particles suspended or in flow in the water. Counting is done using devices (laser counter) similar with the ones used for clean room particle monitoring (for the air).
Bacteria: colonies count. Usually sampling and incubation on Petri capsule.
Hydrocarbon (oils): they MUST NOT be present. OFFLINE extraction method (with hexane) and gas chromatographic analysis.

## Slide 44: Industrial and laboratory plant
Large system:
Production: 3000 l/h
Storage: 9000 l
Typ. TOC: 3 ppb
Small lab production plant:
Production: 170 l/h
Storage: 6000 l
Typ. TOC: 3 ppb
LASA

## Slide 45: Ultrasonic Cleaning
Immersion of components in DI water and detergent medium
Wave energy forms microscopic bubbles on component surfaces
Bubbles collapse (cavitation) on surface loosening particulate matter
Transducer provides high intensity ultrasonic fields that set up standing waves. Higher frequencies lowers the distance between nodes which produce less dead zones with no cavitation
Ultrasonic transducers are available in many different wave frequencies from 18 kHz to 120 kHz, the higher the frequency the lower the wave intensity
Cavities and all hardware components (Flanges, nuts & bolts…)
have to be degreased with ultrasonic cleaning

## Slide 46: US Cleaning efficiency
https://sonosys.de/en/ultrasonic-megasonic.html

## Slide 47: Water Break Test on Nb Sample
It’s a standard test for testing cleaning procedure with UPW and US
Not efficient cleaning
After good US cleaning procedure
ASTM F22 - 02(2007) Standard Test Method for Hydrophobic Surface Films by the Water-Break Test.

## Slide 48: Small parts cleaning
Water: UPW (r >10 MW×cm)
Inline particle filter
Standard dish washer machine are successfully used, with a few corrosion problem (lifetime)
Special stainless-steel dish washer for chemical and bio labs are available on the market (but expensive)
Detergent can be the same used in US bath (foam!) as Tickopur
No additives: salt or cleanser
Rapid cycling (5 min) dish washer available

## Slide 49: Large parts cleaning
UPW( r >10 MΩ×cm)
Pressure: 100 bar
Pump: car wash piston pump
Detergent as TICKOPUR R 33, but not used at companies for EXFEL
Automatic systems with rotating table supporting the cavity frame
5 min spray with detergent, if used
Water Rinse (5 – 10 min)
Widely used for cleaning before entering Clean Room

## Slide 50: Ultrasonic tanks for cavity cleaning
DESY Courtesy

## Slide 51: Cavity preparation for SRF qualification
Degreasing surfaces to remove contaminates
Chemical removal of exterior films incurred from welding
Removal of damage layer of niobium from fabrication ( 150÷200 mm)
Removal of hydrogen from bulk Nb
Mechanical tuning
Chemical removal of internal surface for clean assembly (10-20 mm)
– Additional “cleaning” steps if Electropolishing (EP) is used
High Pressure Rinsing (HPR) to remove particulates from interior surfaces (incurred during chemistry and handling)
Drying of cavity for assembly in cleanroom (reduce risk of particulate adhesion and reduce wear on vacuum systems)
Clean assembly
Clean evacuation
Low-temperature baking

## Slide 52: Removal of damage layer
After all the mechanical operations, a thin layer of about 200 mm must be removed
P. Kneisel

## Slide 53: Centrifugal Barrel Polishing (CBP)
Implementation:
Plastic stones and liquid abrasive added inside cavity and rotated
Stones rubbing on surface removes material thus smoothing the surfaces (including weld areas)
Benefit is less overall chemistry needed (80 mm) and smooth weld areas
Removal of material 2x on equators then irises. Average removal rate  5 mm/h
KEK 2001
Inside equator EBW
Before CBP
After CBP

## Slide 54: Barrel Polishing Machine @ JLAB
USED
Medium
Coarse
Coarse
Medium
Coarse
Coarse
NEW
Removal rate  3 – 4 mm/h

## Slide 55: (Electro-)Chemical Nb removal
Nb is resistant to chemical attack
  HNO3: oxidation of Nb surface and passivation, i.e. no more corrosion of the metal.
  HF: dissolve only Nb oxides, but doesn’t attack Nb itself
  HCl: no attack
  H2SO4: no attack
  Strong alkaline solution (NaOK, KOH, NH4OH): no attack
Two effects have to be coupled: Nb oxidation (e.g. HNO3) and Nb oxides dissolution (HF).

## Slide 56: Buffer Chemical Polishing and Electro Polishing
Buffer Chemical Polishing (BCP)
  A mixture of Hydrofluoric (HF), Nitric Acid (HNO3) and Phosphoric acid (H3PO4), usually in 1:1:1 or 1:1:2 ratio in volume
Electro Polishing (EP)
  A mixture of Hydrofluoric Acid (HF) and Sulfuric Acid (H2SO4) + electric current
Sometimes, the two processes are used together to achieve better surface polishing (see EXFEL final steps)
Final EP
BCP Flash
EXFEL Cavity preparation

## Slide 57: Buffered Chemical Process (BCP)
Mixture of concentrated Hydrofluoric Acid (HF, 40%), Nitric acid (HNO3, 70%) and Phosphoric Acid (H3PO4, 85%)
H3PO4 doesn’t participate the reaction: it act like a buffer slowing down the speed of the exothermic reaction (self exiting!).
1:1:2, generally used, 1 mm/min @ 20 °C
Oxidation
Brownish gas
Dissolve

## Slide 58: Use of BCP Process
1:1:1 still used for subcomponents due to high etching rate ( 8 mm/min)
1:1:2 used for cavity treatment ( 1 mm/min)
BCP must mixed before used because it stratifies
BCP is usually cool down before and during etching to mitigate temperature increase and hydrogen content (starts at 3-5 °C and ends around 20 °C)
(XFEL max Nb content
is 4 g/l) for flash BCP
Gas content of Nb at different etching temperatures (Schölz).
Etching time 20 min, BCP 1:1:4
Hydrogen content vs BCP Temperature
Etching rate versus dissolved Nb

## Slide 59: BCP smoothing
“Simple” process
Roughness of 2 -5 mm (100 x 100 mm2 scale) after 100 mm etching
High etching rate
Courtesy G. Ciovati

## Slide 60: BCP Plant Layout
All components in the acid mixture circuit MUST be resistant to acid attack
Operative temperature: below 20 °C, to reduce hydrogen diffusion in Nb. Usually treatment starts at about 5°C ÷ 6 °C
Exothermic reaction: heat exchanger or cooled barrel is needed
Cavity held in vertical position, acid flow from the bottom part
Temperature gradient causes increased etching from one end to the other
Usually etching rate on iris is 2 x the equator one
Used both for bulk removal and final etching: for EXFEL only for final etching of half of cavities
SCRUBBER
ACID
BARREL
Pump
UPW Plant
for rinsing
and leak test
Filter
Flow
meter
Fast dumping
basin
N2 for dumping
Bypass lines for “small” port etching
Filter
Chiller
Heat
exchanger

## Slide 61: BCP Plant in Operation in Labs
DESY BCP
BCP Cabinet JLAB

## Slide 62: BCP Plant in Operation at Qualified Vendors
Automatic BCP system for subcomponents @ Ettore Zanon for EXFEL (etching + rinsing)

## Slide 63: Electropolishing (EP)
A constant voltage is kept between an Aluminum electrodes and the cavity immerse in a mixture of Hydrofluoric Acid (HF, 49%) and Sulfuric Acid (H2SO4, 96%) in a ratio 1:9 (typical) in volume.
Reaction is not self sustained: no current - no reaction
Oxidation
Dissolve

## Slide 64: EP Mechanism
Anodization of Nb in H2SO4 forces growth of Nb2O5
F- dissolves Nb2O5
These competing processes result in current flow and material removal
Above a certain anodization potential, the reaction rate plateaus, limited by how fast fresh F- can arrive at the surface (diffusion-limited)
The diffusion coefficient sets a scale for optimum leveling effects
Compact Salt Film
( nm)

## Slide 65: EP V vs J
Kenji Saito, KEK, 1989
V1 V2
V3
Current Density
0-V2: Concentration Polarization occurs, active dilution of niobium
V2-V3: Limiting Current Density, viscous layer on niobium surface
>V3: Additional Cathodic Processes Occur, oxygen gas generated
Potential

## Slide 66: Surface Polishing BCP vs EP
The main difference between BCP and EP is smoothening of grain boundaries.
As received
After 120 mm BCP
After 120 mm EP

## Slide 67: Basic EP for SRF cavity
Cavity
Rotates
EP mixture
level
EP mixture
Overflow &
level control
Al 99%
Cathode
(not rotating)
EP mixture inlet
holes / nozzles
At each equator
Insulators to avoid excessive iris etching
Net for Hydrogen confinement
EP mixture
level
DC Power Supply
-
+
V
I
Acid flow direction

## Slide 68: Electropolishing of SRF cavities
Etching rate typical 0.3 ÷ 0.4 mm/min
Cavity (or electrode) is rotating
It requires ethanol rinsing to remove Sulphur
The current density (30-100 mA/cm2) in the plateau region:
  decreases linearly with lower HF/H2SO4 ratio
  increases with increasing temperature
Temperature during the process is maintained between 25 – 35 °C
Current oscillations often observed during polishing (dynamic balance between oxide formation and dissolution). It’s not a necessary condition for good surface finishing but indication of good processing parameters (temperature, voltage, agitation, HF concentration)
Finding the right balance among the processing parameters becomes complicated when polishing multi-cell cavities!

## Slide 69: EP Systems
DESY
CERN

## Slide 70: EP Ethanol Rinse
Motivation: during EP process sulfur is produced and can cause field emission
Sulfur segregates out of the acid as a reaction with the Al electrode, and is deposited all over the system, and also on the Nb surface
Risk of reaction with Nb during 800 °C heat treatment: S must be removed before this step
Sulfur is insoluble in water, but (slightly) soluble in ethanol
Either ethanol rinse or cleaning with detergent + US necessary
PVDF tube before and after ethanol cleaning
Sulfur removed from a PVDF tube

## Slide 71: BCP vs EP
BCP
  2 Volumes of H3PO4 (buffer, very viscous)
  1 Volume of HNO3 (oxidant, transforms Nb into Nb5+)
  1 Volume of HF (complexant of Nb5+, dissolves the oxide layer formed by HNO3 into NbF5)
  Pros
    Easy to handle, middle stirring necessary
    Fast etching rate
    Very reproducible
  Cons
    This is not “polishing” but “etching”: all crystalline defects are preferentially attacked (etching pits, etching figures)
    Grains with various orientations are not etched at the same rate, which induced roughness!
    Except for a few cases Eaccmax25-30 MV/
  Caution!
    Do not process at temperatures higher than 25 °C
    Risk of runaway

## Slide 72: BCP vs EP
EP
  9 Volumes of H2SO4 (buffer, very viscous)
  1 Volume of HF (complexant of Nb5+, dissolves the oxide layer formed due to the high potential applied to Nb)
  Pros (Ideal condition, i.e. viscous layer present)
    This is really “polishing”, not sensitive to crystallographic defects – it produces a smooth surface
    Should not be sensitive to the cathode-anode distance - the same etching rate everywhere
    It gives (but not always) the best ever Eaccmax  45 MV/m (TESLA shape -> 180 mT)
  Cons
    It is not possible to reach an ideal state in most of our processing conditions
    Very sensitive to stirring condition, temperature, and aging of the mixture
    Not very reproducible
    Safety issues (acid mixture sensitive to water, H2 evolution, etc.)
  Caution!
    If T increases: the etching rate increases but there is also a risk of pitting, H loading and HF evolution
    It V increases: the etching rate increases but there is also a risk of pitting, the generation of Sulphur particles and sensitivity to the cathode-anode distance
How to Achieve the Best SRF Performance: (Practical) Limitations and Possible Solutions1
C. Z. Antoine

## Slide 73: Cavity preparation for SRF qualification
Degreasing surfaces to remove contaminates
Chemical removal of exterior films incurred from welding
Removal of damage layer of niobium from fabrication ( 150÷200 mm)
Removal of hydrogen from bulk Nb
Mechanical tuning
Chemical removal of internal surface for clean assembly (10-20 mm)
– Additional “cleaning” steps if Electropolishing (EP) is used
High Pressure Rinsing (HPR) to remove particulates from interior surfaces (incurred during chemistry and handling)
Drying of cavity for assembly in cleanroom (reduce risk of particulate adhesion and reduce wear on vacuum systems)
Clean assembly
Clean evacuation
Low-temperature baking

## Slide 74: Annealing – Cavity firing at high temperature
H diffuses in the bulk during the various etching treatments. See R. E. Ricker and G. R. Myneni, J. Res. Natl. Inst. Stand. Technol. 115, 353-371 (2010), Evaluation of the Propensity of Niobium to Absorb Hydrogen During Fabrication of Superconducting Radio Frequency Cavities for Particle Accelerators.
Nb is an active metal with respect to various gases: it acts like a getter.
Hydrogen makes a solid solution in Nb, H2 equilibrium pressure is driven by Sievert Law
ln pH2 = 2lnQHbulk + B/T + A
where QHBulk is the concentration of H2 in the metal, B and A are constants.
Equilibrium pressure is temperature dependent and increasing the temperature, maintaining a low H2 partial pressure, H2 is desorbed from the bulk (Nb)

## Slide 75: Hydrogen in Niobium Q “disease”
Cavities that remain at 70-150 K for several hours (or slow cool-down, < 1 K/min) experience a sharp increase of residual resistance
More severe in cavities which have been heavily chemically etched
H is readily absorbed into Nb where the oxide layer is removed (during chemical etching or mechanical grinding)
H has high diffusion rate in Nb, even at low temperatures.
H precipitates to form a hydride phase with poor superconducting properties: Tc=2.8 K, Hc=60 G
At room temperature the required concentration to form a hydride is 103- 104 wppm
At 150 K it is < 10 wppm

## Slide 76: Annealining
Hydrogen outgassing => most efficient at 750°C – 800°C, 2h under good vacuum
Recrystallization (goal is close to 100% with highest RRR)
  Removing of defects and curing of dislocations
  Nucleation of new grains and growing of new crystals
  Grain growth (depending on temperature and purity)
Nb becomes softer and this facilitate the cavity tuning process
Different parameters at different labs:
  600 °C/10 h at Jlab
  800 °C/2 h at DESY
  750 °C/3 h at KEK
No completely recrystallized Nb
Completely recrystallized Nb

## Slide 77: EZ Furnace

## Slide 78: Cavity preparation for SRF qualification
Degreasing surfaces to remove contaminates
Chemical removal of exterior films incurred from welding
Removal of damage layer of niobium from fabrication ( 150÷200 mm)
Removal of hydrogen from bulk Nb
Mechanical tuning
Chemical removal of internal surface for clean assembly (10-20 mm)
– Additional “cleaning” steps if Electropolishing (EP) is used
High Pressure Rinsing (HPR) to remove particulates from interior surfaces (incurred during chemistry and handling)
Drying of cavity for assembly in cleanroom (reduce risk of particulate adhesion and reduce wear on vacuum systems)
Clean assembly
Clean evacuation
Low-temperature baking

## Slide 79: Frequency tuning
After the treatments, the cavity needs to be tuned to the right frequency and field flatness.
This operation is done by tuning each single cell to achieve proper field distribution
f
f
3.9 GHz EXFEL cavity

## Slide 80: Cavity preparation for SRF qualification
Degreasing surfaces to remove contaminates
Chemical removal of exterior films incurred from welding
Removal of damage layer of niobium from fabrication ( 150÷200 mm)
Removal of hydrogen from bulk Nb
Mechanical tuning
Chemical removal of internal surface for clean assembly (10-20 mm)
  Additional “cleaning” steps if Electropolishing (EP) is used
High Pressure Rinsing (HPR) to remove particulates from interior surfaces (incurred during chemistry and handling)
Drying of cavity for assembly in cleanroom (reduce risk of particulate adhesion and reduce wear on vacuum systems)
Clean assembly
Clean evacuation
Low-temperature baking

## Slide 81: Post EP treatment
The early EP treatment was quite unstable and with large scatter in the results
A proper post EP treatment was found ….
9-cell cavity data

## Slide 82: Post EP treatment
Ethanol Rinse (DESY)
“Flash” BCP (10 m) (DESY)
“Flash” EP (3 m, fresh acid, no re-circulation) (KEK)
Ultrasonic Degreasing with Micro-90 and hot water (JLab)
Courtesy G. Ciovati

## Slide 83: Cavity preparation for SRF qualification
Degreasing surfaces to remove contaminates
Chemical removal of exterior films incurred from welding
Removal of damage layer of niobium from fabrication ( 150÷200 mm)
Removal of hydrogen from bulk Nb
Mechanical tuning
Chemical removal of internal surface for clean assembly (10-20 mm)
  Additional “cleaning” steps if Electropolishing (EP) is used
High Pressure Rinsing (HPR) to remove particulates from interior surfaces (incurred during chemistry and handling)
Drying of cavity for assembly in cleanroom (reduce risk of particulate adhesion and reduce wear on vacuum systems)
Clean assembly
Clean evacuation
Low-temperature baking

## Slide 84: High Pressure Rinsing
The final step in cavity assembly is the Rinsing with a High Pressure UPW jet to remove particulate from the handling and residual from chemical treatments
Water jet must be moved continuously: if jet impacts stably in one-point Nb surface can be damaged
Continuous motion of the cavity respect jets (drawing a spiral behavior that cover completely the Nb surface)
Ultra pure (6.0) filtered (40 nm) nitrogen protection gas injection coaxial with water to reduce risk of particles entering
Cavity must be grounded otherwise it will be electrically charged
 100 bar
 0.02 mm
Oxidation induced by fixed HPR jets

## Slide 85: HPR Process
Hydrodynamic model allows estimating the shear stress  of the water jet, which depends on flow rate and pressure
Particle removal by rolling if the water shear stress is greater than a critical shear stress 0, related to the particle size, adhesion force and surface roughness
https://doi.org/10.1063/1.4949242

## Slide 86: HPR Effect
Cavity had a problem in the 120°C treatment (vacuum system power failure) that produced a rapid change of pressure (a bump) in the cavity during last pump-down, with particle movement in the system. Consequences are clearly visible (dark blue curve).
After HPR, with no further chemical etching, cavity performances are completely recovered.

## Slide 87: HPR Systems
Rinsing cabinet of “old“ DESY HPR system
Rinsing cabinet of “new“ DESY HPR system with “plastic” cavity
CEA HPR system

## Slide 88: HPR QA
Examples of QC at HPR systems (DESY, EXFEL cavities production@ companies)
Check of Point-of-use supply water quality:
  UPW conductivity
  Particles: online particle counter
  Particles: off-line sampling & identification (SEM optical microscope)
  TOC: online monitoring
  TOC drain line: sampling, after maintenance
  Bacteria (=> offline)
HPR Head QA
HPR Water Collector

## Slide 89: HPR Spray Head Optimization
For a given pump displacement the nozzle opening diameter and number of nozzles sets the system pressure and flow rate
The HPR spray head needs to be optimized for each cell geometry!
Very effective on irises
Equator fill with water too high flow rate

## Slide 90: HPR Water Jet Characterization (INFN-LASA)
Use a load-cell to measure the jet force
u = velocity Q = flow
p = pressure
r = density
Test at DESY
Jet Profile
Jet Evolution
Jet Force vs Pressure

## Slide 91: Cavity preparation for SRF qualification
Degreasing surfaces to remove contaminates
Chemical removal of exterior films incurred from welding
Removal of damage layer of niobium from fabrication ( 150÷200 mm)
Removal of hydrogen from bulk Nb
Mechanical tuning
Chemical removal of internal surface for clean assembly (10-20 mm)
  Additional “cleaning” steps if Electropolishing (EP) is used
High Pressure Rinsing (HPR) to remove particulates from interior surfaces (incurred during chemistry and handling)
Drying of cavity for assembly in cleanroom (reduce risk of particulate adhesion and reduce wear on vacuum systems)
Clean assembly
Clean evacuation
Low-temperature baking

## Slide 92: What is a cleanroom? The ISO 44644 definition
“A room in which the concentration of airborne particles is controlled, and which is constructed and used in a manner to minimize the introduction, generation and retention of particles inside the room and in which other relevant particles inside the room and in which other relevant parameters, e.g. temperature, humidity and pressure, are controlled as necessary.”
A cleanroom is likely to have between some tens of air changes per hour up to many hundreds of them.
A cleanroom uses filters that would normally be 99.97 % and more efficient in removing particles greater than 0.3 mm from the room air supply. These filters are known as High Efficiency Particle Air (HEPA) filters, although Ultra Low Particle Air (ULPA) filters, which have a higher efficiency, are used in microelectronic fabrication areas.

## Slide 93: Particulate in air
Cleanroom technology is required to prevent airborne particulates from settling on the surface of SRF cavities
Particle size (m)

## Slide 94: Type of cleanrooms
Unidirectional airflow type
Non-Unidirectional airflow type
Utility and equipment chase
Perforated floor
Return air
Supply fresh air from fans
Class 1/100
Return air
FAN
FAN
FAN
FAN
FAN
100 % HEPA ceiling with distributed fans with independent speed control
Unidirectional airflow type with recirculation

## Slide 95: Cleanroom classification
Cavity
assembly
Cleanroom for SRF

## Slide 96: Human generated particle

## Slide 97: Clean room «dress» code
People are a major source of particulate contamination inside a clean room through:
  Body Regenerative Processes - Skin flakes, oils, perspiration and hair.
  Behavior - Rate of movement, sneezing and coughing.
  Attitude - Work habits and communication between workers.

## Slide 98: Particle counters
To ensure the proper cleanness, all components before installation need to be washed, rinsed and particle counted

## Slide 99: Cavity Assembly
The cavity strings have to be vacuum tight to a leak rate of < 1 10-10 mbar l/sec
The sealing gaskets and hardware have to be reliable and particulate-free
The clamping hardware should minimize the space needed for connecting the beamlines
UHV Gasket
  Present choice for SRF cavities:
diamond-shaped AlMg3 –gaskets +
NbTi flanges + bolts
AlMg-Gasket

## Slide 100: Cavity preparation for SRF qualification
Degreasing surfaces to remove contaminates
Chemical removal of exterior films incurred from welding
Removal of damage layer of niobium from fabrication ( 150÷200 mm)
Removal of hydrogen from bulk Nb
Mechanical tuning
Chemical removal of internal surface for clean assembly (10-20 mm)
  Additional “cleaning” steps if Electropolishing (EP) is used
High Pressure Rinsing (HPR) to remove particulates from interior surfaces (incurred during chemistry and handling)
Drying of cavity for assembly in cleanroom (reduce risk of particulate adhesion and reduce wear on vacuum systems)
Clean assembly
Clean evacuation
Low-temperature baking

## Slide 101: Slow Pumping – Slow Venting
  Avoid particle transport from outside into the vacuum system and avoid movement of particles already in the vacuum system
  For abs. pressure p > 1 mbar and differential pressure Δp > 1 mbar (e.g. opening of valves, start pumping) => movement of particles observed
  For abs. pressure p < 1 mbar => no movement of particles observed
  Manual dosing valves cannot safely avoid particle transport

## Slide 102: SPSV motivation
Both rapid venting and rapid pumping introduce particle motion

## Slide 103: SPSV at INFN LASA
Dry pump 1: scroll pump, Triscroll 600
TMP1: Pfeiffer TMP
TMP2: TMP of the LDS1000 Oerlikon LD
LD1: LDS1000 Oerlikon Inficon sensing head
V6, V8, V9, V10, V3: Varian Viton seal on the bonnet, metal seal on the body
MFC1: MKS, 5 slm flow controller
MFC2: MKS, 100 slm flow controller
He
Pump down from atmospheric pressure
Pumpdown at p< 1 mbar
Leak check
Slow venting

## Slide 104: SPSV at LASA
Pumping line: controller and valves
Cal. leak
Venting line: controller and valves
Connection to the TMP

## Slide 105: Residual Gas Analysis (RGA)
UHV partial pressure measurement system used for:
  Partial pressure evaluation of various gases: e.g. for discriminate water desorption from leaks and outgas
  Vacuum quality check
    Leak check
    Impurities and contaminants evaluation: specific fingerprint are available for some components (for instance for isopropanol, acetone, ethanol, etc.)
Evaluation of Hydrocarbon content
Detector
Mass (m/e) filter
Ion source
(from NIST, http://webbook.nist.gov/chemistry/name-ser.html).

## Slide 106: Definition of hydrocarbon free parts for EXFEL
Appropriate proofs have to be performed using a sufficiently sensitive residual gas analyzer, usually equipped with a secondary electron multiplier (SEM).
Components are considered free of hydrocarbons if in a leak-free system with a total pressure below 10-7 mbar the sum of the partial pressures of masses above mass 45 is less than 10-3 of the total pressure (1 : 1000).
NOK Hydrocarbon contaminated
OK Hydrocarbon free

## Slide 107: Cavity preparation for SRF qualification
Degreasing surfaces to remove contaminates
Chemical removal of exterior films incurred from welding
Removal of damage layer of niobium from fabrication ( 150÷200 mm)
Removal of hydrogen from bulk Nb
Mechanical tuning
Chemical removal of internal surface for clean assembly (10-20 mm)
  Additional “cleaning” steps if Electropolishing (EP) is used
High Pressure Rinsing (HPR) to remove particulates from interior surfaces (incurred during chemistry and handling)
Drying of cavity for assembly in cleanroom (reduce risk of particulate adhesion and reduce wear on vacuum systems)
Clean assembly
Clean evacuation
Low-temperature baking

## Slide 108: Why low temperature baking (120 °C)?
EP
EP+ baking
  Baking: shifts high field dissipation to higher field
      Discovered at Saclay in 1998 (B. Visentin)
      Low temperature treatment : 110-120°C, 48 H : few changes expected
      Dramatic effect on performances
      Still resists full explanation

## Slide 109: 120 °C baking
  Cure of characteristic Q-drop
  Standard recipe:
    T = 110 - 125°C for 48h
    Active pumping (TMP)
    Oil free vacuum system, UHV-conditions
    Fully assembled cavity
    Nitrogen or argon external atmosphere to avoid oxidation
    External volume: purging with vacuum before inert gas (N2 or Ar) filling
UHV TMP system
Heaters
Cavity
N2
Rough pumping system
CEA Infrared Heater

## Slide 110: If everything went well you will get …
Ep  80 MV/m, Bp  170 mT can be achieved in the vertical test of 9-cell ILC cavities ( 1 m2 of Nb surface)
JLAB
DESY

## Slide 111: Thanks!!

## Slide 112: Reference
http://cas.web.cern.ch/CAS/Spain-2006/PDFs/Taborelli.pdf
NIST, http://webbook.nist.gov/chemistry/name-ser.html
Paolo Chiggiato, CAS school on vacuum
Ed by W. White, Cleanroom design
W. Kern ed., Handbook of Semiconductor Wafer Cleaning Technology
A User's Guide to Vacuum Technology , O. Hanlon
C. Antoine, Erice School
L.Gail, H.P.Hortig, Reinraumtechnik (in german), 2002
P. Kneisel,B. Lewis, SRF Workshop, 1995
P. Kneisel, Contamination Workshop Jlab, 1997
H.Padamsee, J.Knobloch, T.Hays, RF Superconductivity f. Accelerators, 1998
D.L. Tolliver, Handbook of Contamination Control in Microelectronics, 1988
G. Ciovati “Cavity fabrication” and “Surface Preparation”, USPAS 2015
P. Michelato “Cavity Processing: EP/BCP, heat treatments, baking and clean room techniques”, SRF2013 Tutorial
P. Kneisel, “Lecture 11”, 1st ILC School, 2005
W. Singer, “SRF Cavity Fabrication and Materials”
- In general all Proceedings of:
USPAS Schools
SRF Workshop Tutorials
ILC Schools
CAS School