## Slide 1
Large Detector Magnets
P.Fabbricatore INFN Genova
Photos taken during the construction of BEBC, CMS and ATLAS magnets

## Slide 2
The development of Detector Magnets has pushed forward the applications of the superconductivity, specially in the sixties and seventies.
For this reason this lecture is organised according an historical approach starting with the availability of the first superconducting wires (around 1960) and finishing with the very large sc magnet foreseen for future high energy colliders.
PROLOGUE

## Slide 3
Summary
  What we ask to a detector magnet
  The developments of sc wires and cables
  The story of detector magnets
  Design progresses
  Construction technologies
  Future
Some photos were provided by H.Desportes and F.Wittegenstein. I also use slides shown by E.Baynham at MT19 and by A.Yamamoto in presentations available on the web. Other photos from CERN site

## Slide 4
Summary
  What we ask to a detector magnet
  The developments of sc wires and cable
  The story of detector magnets
  Design progresses
  Construction technologies
  Future

## Slide 6
y
x
q
r
s
y1
y2
y3
L
Superconducting magnets with large dimensions

## Slide 7
A very remarkable requirement
for Detector Magnets
(further than high B field in a large volume)
It is strictly required that the magnet has a large safety margin when working at the normal operation. In fact a failure of a magnet component, such as a short to ground, a defective electrical slice or a leaking pipe for LHe circulation etc., can lead to dismount a big part of the detector !!

## Slide 8
Summary
  What we ask to a detector magnet
  The developments of sc wires and cables
  The story of detector magnets
  Design progresses
  Construction technologies
  Future

## Slide 11
As John Hulm recalled some years later :
“Those tiny, primitive magnets were, of course, terribly unstable and tended to damage themselves on normalization, for reasons that are now well understood. One had to have faith to believe that these erratic toys of the low temperature physicists would ever be of any consequence as large engineered devices”

## Slide 12
1- Development of practical material: II type with pinning centers
2- Flux jumps instabilities Fine filaments
3- Coupling currents  Twist pitch
Why 50 years before magnet applications: Steps towards the development of sc wires for application

## Slide 13
Critical magnetic field and temperature for the low_Tc superconductors
Among all these materials only NbTi and Nb3Sn have been massively involved in the applications

## Slide 14
The critical current density Jc vs the magnetic field
Electrical transport properties are determined by impurities or defects in the material, acting as pinning centers for fluxons

## Slide 15
Superconducting materials involved in conductors

## Slide 16
Magnetic instability in type-II superconductors with pinning centers
An heat input causes a temperature increases of ΔT. The critical current density decreases of -ΔJc . Due to the critical state model
Magnetic flux penetrates the sc material
This flux penetration causes a dissipation
The dissipation causes a furter temperature increase
B
B
DQ
DT
Df
-ΔJc
The process is potentially destructive for the superconductivity, but it could converge to T<Tc in case the conductor is enough thin, i.e. if the radius a is:

## Slide 18
Summary
  What we ask to a detector magnet
  The developments of sc wires and cables
  The story of detector magnets
  Design progresses
  Construction technologies
  Future

## Slide 19
One of the first very large magnets for Particle Physics was developed in the sixtes . At that time the development of first NbTi conductors employing a technology was still far to be mature
The split coil solenoid for the 12-ft bubble chamber built at Argonne (J.Purcell) in the ZGS accelerator (1968) followed by the 15-ft (Purcell -Desportes)
Magnetic field 1.8T in 4.5m diameter and 3m heigth.
Stored Energy 80MJ. Conductor in NbTi (40 km).

## Slide 20
12-ft and successors were pool boiling based on the Stability Stekly criterion (Zdenek J. J. Stekly)

## Slide 21
Thanks to
F. Wittgenstein
BEBC during the winding

## Slide 22
BEBC during the assembly

## Slide 23
Forced flow magnets : the LHe volume dramatically reduced
An idea of M.Morpurgo
(CERN)

## Slide 24
Winding technology in common with power applications

## Slide 25
The development of colliding beams demanded for solenoidal magnets (axi-symmetric field) transparent to radiation (calorimeters placed outside).
It was realized that a powerful cooling system was useless for dc magnets, provided that a good stability is guaranteed and the disturbances of mechanical nature limited.  The thin high field solenoids.
The first magnet of this class can be considered CELLO , built at Saclay for Petra Collider at DESY. CELLO was wound with an aluminium stabilized conductor. The cooling was indirect, in the sense that the cooling pipes were connected to the supporting structure, made by aluminium alloy.
THE ERA OF ALUMINIUM STABILISED MAGNETS

## Slide 26
Pure Al stabilised conductors
The idea of using of pure Al directly embedded in the conductors is supported by two main reason.
Good conductor with low mass density (a factor 3 wrt copper)
Higher Minimum Quench Energy wrt copper
Drawback: the pure Al is a very soft material σyield ~20 MPa.
We need additional mechanical supporting material

## Slide 27
CELLO (1978) – Indirect cooling – Pure Al-stabilised conductor
Indirect coooling
External support
Al-stabilised conductor
Mandrel
Monolithic wire soft soldered to Al-pure stabiliser
Basic ideas
Parameters |  | 
Field | 1.5 | T
Coil Radius | 0.85 | m
Length | 3.6 | m
Stored Energy | 5.1 | MJ
Cold mass | 1 | t

## Slide 28
CDF (1984)– First co-extrude conductor – Al-alloy support- Shrink-fit
Cooling pipes directly welded on Al5083 cylinder
After the winding the coil is shrink-fitted inside the outer cylindrical support
Parameters |  | 
Field | 1.5 | T
Coil Radius | 01.5 | m
Length | 4.8 | m
Sored Energy | 30 | MJ
Notes: Note
Shrink fitting high risk operation
Tight tolerances on coil and cylinder dimensions

## Slide 29
ALEPH (1987)– Rutherford cable- Resin VPI – Thermo-siphon
35mm
Parameters |  | 
Field | 1.5 | T
Coil Radius | 2.75 | m
Length | 6.4 | m
Sored Energy | 130 | MJ
Thermo-siphon
J C Lottin

## Slide 31
BESS Polar – The thinnest one . No support!!
Al-Ni alloy
NbTi/Cu SC
Diameter 900mm
Length 1000mm
Field 1T
Wall 1gm/cm^2 ~ 0.05Xo
3.4mm

## Slide 32
BESS Polar : As thin as a can!!
Coil thickness/diameter ~ 0.34%
thickness/diameter ~ 0.2%

## Slide 35
1994- TECHNICAL PROPOSAL of CMS at LHC : The magnets looks to be beyond the technological limits
Magnetic Field 4 T
Current 20000 A
Stored Energy 2520 MJ
Peak field 4.6T
LuMagnet length 12.5 m
Inner Diameter 6320 mm
External diameter 6950 mm
Four layers

## Slide 36
B
Fradial
Faxial
Magnetic forces on solenoids
The radial component of the B field causes an axial compressive force. The axial component a radially outward forces
A thi solenoid can be seen a vessel with an internal pressure (the magnetic presuure)

## Slide 37
A basic parameter for comparing different magnets
The ratio E/M Stored Energy [kJoule])/ Cold Mass [kg]
Where e is the strain , Y the elastic modulus, d the density,
a is the fraction of the mechanical resistent material
The ratio E/M gives a direct information of the mechanical deformation. For CMS e=0.15%
E/M gives also an information of the max temperature in the coil after a quench.

## Slide 38
E/M ratio vs E for several detector magnets

## Slide 39
The basic idea in CMS design was to include the mechanical reinforcement in the conductor. This choice allow to minimize the shear stresses in the winding
Reinforced Conductor
A (thin ) mandrel is still present for:
Homogenizing the temperature of the coil during cool-down
Protection- Quench back
Supporting the winding during construction
Anchoring the supporting system of the cold mass in the vacuum chamber
64.0 mm
21.6 mm
127 mm
186 mm

## Slide 40
A 5 module coil (250 t), requiring R&D developments at industrial level of conductor and winding technologies
CMS (2006) – The reinforced conductor
CERN CEA ETH-Z INFN
Parameters |  | 
Field | 4 | T
Coil Radius | 3.5 | m
Length | 12.5 | m
Stored Energy | 2600 | MJ

## Slide 41
Continuous EB-welding of each 2.5 km length (20 in total)

## Slide 42
1998-1999 Development in Ansaldo Magneti of an inner winding technology with INFN

## Slide 43
1999: Construction of a model  Input for designing a winding line

## Slide 44
Developments of the winding techniques for a reinforced conductor
Conductor Bending
Winding
Epoxy vacuum impregnation of 50 t modules

## Slide 45
Rollers A,A’ guide the conductor . Rollers B, C’ and D bend it a a radius R1 (B’ e C not active). Rollers E,F and G bend the conductopr at final radius e R2 <R1
Small variation in conductor width (0.1 mm off 64 mm) or 10% variation of mechanical properties are not affecting final radius.
Two step bending

## Slide 46
After impregnation le large coil could have excess of epoxy resin at the inner surface. An issue due to potential thermal disturbances causing premature quenching.

## Slide 47
Inner machining for removing excess of resin!

## Slide 48
Also transportation of these large coils is not trivial!!

## Slide 49
7400 mm

## Slide 54
ATLAS TOROIDS – largest field volume (7000 m3)

## Slide 55
Barrel Toroid: 8 coils in separate cryostats
  20 m diameter
  25 m length
  8200 m3 volume
  118 t superconductor
  370 t cold mass
  830 t total weight
  56 km conductor
  20.5 kA current
  3.85 T peak field
  1 GJ stored energy
  4.8 K indirectely cooled
  Force 1100 t/coil

## Slide 56
ATLAS Barrel Toroid
Challenge
Scale of components and integration accuracy
Tolerances << 1 mm in 26m

## Slide 58
A challenge for large sc magnets: assembly and handling
Lift down to the cavern of CMS coil with central yoke module (12000 t)
Lift down to the cavern of a ATLAS barrel coil

## Slide 59
Summary
  What we ask to a detector magnet
  The story of detector magnets
  Design progresses
  Construction technologies
  Future

## Slide 60
What about the future? (Linear Collider or FCC ?)

## Slide 61
The load lines in I-B graph and stability margin

## Slide 62
For NbTi Tc0 = 9.25 K Bc20 = 13.9 T.
At B = 4.6 T (Peak field in CMS) Tc = 7.35 K
The interesting parameter is the current sharing temperature
Iop =19140 A, Ic(T=4.5K ,B= 4.6 T) = 55600 A Tg = 6.35 K.
The temperature margin in CMS is consequently DT=6.35-4.5=1.85 K
At 5.2 T central field the margin is lower: 1.4 K (still acceptable considering that CMS worked up to a temperature of 5.4 K ). I personally believe that a margin of 1 K is enough. That means a central field of 6 T (at I/Ic=0.33)
Temperature Margin

## Slide 64
Presented by ten Kate at FCC meeting in Rome (April 2016)

## Slide 65
It seems that next large detector magnet will still based on NbTi tecnology. Any chances for different materials (HTcS)?

## Slide 66
CONCLUSIONS
The detector magnets are evolving since 50+ years, requiring any time developments at the edge of the up-to-date technology.
As the accelerated particle energy increased, the requirement in momentum resolution demanded for new technologies for superconducting cables.
In the sixties and seventies the detector magnet had an important role in pushing the superconducting technology
Next large detector magnet will presumibly still involve LTcS

## Slide 67
Additional slides

## Slide 68
Notes: Buttons. Click on any particle type to display the relevant slide with animations. Clicking again will return to this slide.
Recommend putting this slide in the middle of your presentation and putting the other 5 slides at the end.
If you have any difficulties, contact David.Barney@cern.ch

## Slide 69
Notes: Charged hadron: Bends in the magnetic field and leaves signals in the tracker layers; passes through the electromagnetic calorimeter leaving essentially no signal, and is “stopped” by the hadron calorimeter

## Slide 70
Notes: Neutral hadron: Does not bend in the magnetic field and does not leave any signal in the tracker layers; passes through the electromagnetic calorimeter leaving essentially no signal, and is “stopped” by the hadron calorimeter

## Slide 71
Notes: Electron: Bending in the magnetic field, leaving hits in the tracker layers and being “stopped” by the electromagnetic calorimeter

## Slide 72
Notes: Photon: passes through the tracker without bending in the magnetic field or leaving hits, is “stopped” by the electromagnetic calorimeter

## Slide 73
Notes: Muon: passing through CMS, bending in the field (both ways, depending on when it is inside or outside of the solenoid) leaving hits in the Tracker layers and the muon chambers before escaping completely

## Slide 75
y
x
p┴=qBr
( N > 10 )
Superconducting magnets with large dimensions
q
r
s
y1
y2
y3
L

## Slide 77
Maddock Criterion
Maddock demonstrated that a less restrictive criterion can be used. It is sufficient that the excess of dissipation is compensated by an excess of heat exchange. The theorem of equal are.