## Slide 1: Large magnets for fusion application
L. Muzzi / FSN – Superconductivity Division
EASI School 3 – Superconductivity and its applications
October 6th, 2020

## Slide 2: Outline
Magnetic confinement fusion: the tokamak concept
Magnet system of a tokamak reactor
Cable-in-Conduit conductors (CICCs)
ITER CICCs and optimization margins
Key components of fusion coils: the example of the Italian DTT Project.
Summary and concluding remarks

## Slide 3: Outline
Magnetic confinement fusion: the tokamak concept
Magnet system of a tokamak reactor
Cable-in-Conduit conductors (CICCs)
ITER CICCs and optimization margins
Key components of fusion coils: the example of the Italian DTT Project.
Summary and concluding remarks

## Slide 4: Nuclear fusion principles
Nuclear reaction, where light atoms (Hydrogen) fuse, and form one (Helium), with a net energy release (E=Dm c2)
n (14.1MeV)
He (3.5MeV)
D
T
Lawson’s criterium for D-T fusion:
n tE T ≥ 1.2 1021 m-3 keV s
  n: gas density (~ 1020 ions/m3)
  tE: confinement time (~1 s)
  T: Kinetic energy (T ~ 150・106 °C)

## Slide 5: Magnetic Confinement Fusion: the Tokamak
Torodial Field: for confinement of charged particles in plasma
Poloidal Field: for control of plasma radial position, shaping and vertical stability
Central Solenoid:
Plasma discharge initiation by transformer effect
TOKAMAK
toroidal'naya kamera s aksial'nym magnitnym polem (toroidal chamber with an axial magnetic field)
("тороидальная камера в магнитных катушках“)

## Slide 6: Magnetic Confinement Fusion: the Tokamak
Torodial Field: for confinement of charged particles in plasma
Poloidal Field: for control of plasma radial position, shaping and vertical stability
Central Solenoid:
Plasma discharge initiation by transformer effect
TOKAMAK
toroidal'naya kamera s aksial'nym magnitnym polem (toroidal chamber with an axial magnetic field)
("тороидальная камера в магнитных катушках“)

## Slide 7: Magnetic Confinement Fusion: the Tokamak
TOKAMAK
toroidal'naya kamera s aksial'nym magnitnym polem (toroidal chamber with an axial magnetic field)
("тороидальная камера в магнитных катушках“)
Stability quantified by the parameter:
Fusion Power:
Gas Pressure
Magnetic Field Pressure

## Slide 8: Fusion magnets: the ITER coils
Magnetic confinement fusion: the tokamak concept

## Slide 9: Fusion magnets: the ITER coils
Magnetic confinement fusion: the tokamak concept

## Slide 10: Fusion magnets: the ITER coils
Magnetic confinement fusion: the tokamak concept

## Slide 11: Fusion magnets: the ITER coils
Magnetic confinement fusion: the tokamak concept

## Slide 12: D-shaped superconducting tokamaks
6.2m
EAST
KSTAR
1.8m
1.1m
SST-1
JT-60SA
3.1m
1.7m
ITER
2.1m
DTT
9 m
DEMO
 | Btoroidal (T) | Iplasma (MA)
JT-60SA | 2.25 | 5.5
ITER | 5.3 | 15.0
DEMO | 5.2 | 17.9
SST-1 | 5.5 | 0.22
EAST | 3.5 | 1.0
KSTAR | 3.5 | 2.0
DTT | 6.0 | 5.5

## Slide 13: D-shaped superconducting tokamaks
6.2m
EAST
KSTAR
1.8m
1.1m
SST-1
JT-60SA
3.1m
1.7m
ITER
2.1m
DTT
9 m
DEMO
 | Btoroidal (T) | Iplasma (MA)
JT-60SA | 2.25 | 5.5
ITER | 5.3 | 15.0
DEMO | 5.2 | 17.9
SST-1 | 5.5 | 0.22
EAST | 3.5 | 1.0
KSTAR | 3.5 | 2.0
DTT | 6.0 | 5.5
Ampere’s law:

## Slide 14: D-shaped superconducting tokamaks
6.2m
EAST
KSTAR
1.8m
1.1m
SST-1
JT-60SA
3.1m
1.7m
ITER
2.1m
DTT
9 m
DEMO
 | Btoroidal (T) | Iplasma (MA)
JT-60SA | 2.25 | 5.5
ITER | 5.3 | 15.0
DEMO | 5.2 | 17.9
SST-1 | 5.5 | 0.22
EAST | 3.5 | 1.0
KSTAR | 3.5 | 2.0
DTT | 6.0 | 5.5
Ampere’s law:
Overall TF magnet system current

## Slide 15: D-shaped superconducting tokamaks
 | Btoroidal (T) | Iplasma (MA)
JT-60SA | 2.25 | 5.5
ITER | 5.3 | 15.0
DEMO | 5.2 | 17.9
SST-1 | 5.5 | 0.22
EAST | 3.5 | 1.0
KSTAR | 3.5 | 2.0
DTT | 6.0 | 5.5
Ampere’s law:
Overall TF magnet system current
JT-60SA TF Magnet system
Image courtesy of: A. Cucchiaro

## Slide 16: D-shaped superconducting tokamaks
 | Btoroidal (T) | Iplasma (MA)
JT-60SA | 2.25 | 5.5
ITER | 5.3 | 15.0
DEMO | 5.2 | 17.9
SST-1 | 5.5 | 0.22
EAST | 3.5 | 1.0
KSTAR | 3.5 | 2.0
DTT | 6.0 | 5.5
Ampere’s law:
1 TF coil current
JT-60SA TF coil
Image courtesy of: A. Cucchiaro

## Slide 17: D-shaped superconducting tokamaks
 | Btoroidal (T) | Iplasma (MA)
JT-60SA | 2.25 | 5.5
ITER | 5.3 | 15.0
DEMO | 5.2 | 17.9
SST-1 | 5.5 | 0.22
EAST | 3.5 | 1.0
KSTAR | 3.5 | 2.0
DTT | 6.0 | 5.5
Field on conductor:
In DTT, ITER, DEMO:
DEMO Magnetic Field Maps
Images courtesy of: S. Turtù
Ampere’s law:

## Slide 18: Superconductivity and fusion energy
Superconductivity as Enabling technology

## Slide 19: Superconductivity and fusion energy
Superconductivity as Enabling technology
In the latest generation of plasma devices, which are larger and have longer confinement times, the superconducting coils are a key enabling technology

## Slide 20: Superconductivity and fusion energy
Superconductivity as Enabling technology
Electrical cables at CERN – LEP vs. LHC (Photo by Cockcroft Institute)
For: - magnetic field levels (≈10 T)
- magnet size (≈10 m) and stored energy (≈10 GJ)
- pulse duration (≈100 ÷ 1000 sec)
the use of superconducting coils is inevitable

## Slide 21: Some nomenclature
  in other words …..
  what I would like to show you

## Slide 22: Some nomenclature
Wire (or strand)
  Cable
    Conductor
      Coil

## Slide 23: Some nomenclature
Wire (or strand)
  Cable
    Conductor
      Coil

## Slide 24: Some nomenclature
Wire (or strand)
  Cable
    Conductor
      Coil

## Slide 25: Some nomenclature
Wire (or strand)
  Cable
    Conductor
        Coil

## Slide 26: Superconducting wires (strands): stability
It’s thus necessary to couple (stabilize) the material for example with Copper or Aluminum
Superconductor
Cu
a = Cu/nonCu ratio
In the normal state the superconductor, has high electrical resistivity and low thermal conductivity
2kA(Tc-Top)/l = Jc2rAl

## Slide 27: Superconducting wires (strands): stability
AC hysteresis losses + Flux Jumping
AC coupling losses

## Slide 28: Multi-filamentary superconducting wires
Superconductor
Copper
The superconduct. wire is formed of many thin filaments of s.c. materials, twisted within a Cu stabilizing matrix
Wire diameter | 0.5÷1 mm
# supecond. filaments | 1000÷10000
Filament diameter | 5÷50 m
Cu/non Cu | 4/1 ÷ 1/1
Wire
Filament
Bundle
Photo courtesy of Peter Lee, FSU
Photo courtesy of J. Minervini MIT
Φ = 0.81 mm
Φ  50-100 µm
Φ  few µm

## Slide 29: Practical Materials

## Slide 30: Practical Materials
NbTi
Nb3Sn

## Slide 31: Practical Materials
NbTi
Nb3Sn
 | Tc(B=0) | Bc2(T=0) | 
NbTi (type II) | 9.2 K | 15 T | Ductile alloy – bcc structure - cheap
Nb3Sn (type II) | 18 K | 27 T | Intermetallic compound – brittle – A15 structure – expensive

## Slide 32: Practical Materials
NbTi
Nb3Sn
Bpeak determines the choice of the s.c. material to be used
ITER TF
ITER PF

## Slide 33: The ITER strands

## Slide 34: Fabrication of s.c. wires
NbTi

## Slide 35: Fabrication of s.c. wires
Nb3Sn
Courtesy of:
A. Godeke, Performance Boundaries in Nb3Sn Superconductors (2005)

## Slide 36: Fabrication of s.c. wires
Nb3Sn
Courtesy of:
A. Godeke, Performance Boundaries in Nb3Sn Superconductors (2005)
It requires a heat treament at 650 °C to form the s.c. phase.
Once formed, it is a brittle material!

## Slide 37: Outline
Magnetic confinement fusion: the tokamak concept
Magnet system of a tokamak reactor
Cable-in-Conduit conductors (CICCs)
ITER CICCs and optimization margins
Key components of fusion coils: the example of the Italian DTT Project.
Summary and concluding remarks

## Slide 38: Heat Loads in fusion coils
Source of losses:
Hysteresis
AC
Coupling
Eddy-
Neutrons
Thermal radiation & Conduction
  ITER design experience:
R. Vallcorba_MATEFU School 2009

## Slide 39: Heat Loads in fusion coils
Source of losses:
Hysteresis
AC
Coupling
Eddy-
Neutrons
Thermal radiation & Conduction
Due to varying field and currents
Specific of CS / PF conductors
R. Vallcorba_MATEFU School 2009
; Iplasma (MA)

## Slide 40: AC losses in DTT CS coil
L1 (HF)
CS currents
Computed AC losses
Temperature margin

## Slide 41: Heat Loads in fusion coils
Source of losses:
Hysteresis
AC
Coupling
Eddy-
Neutrons
Thermal radiation & Conduction
  ITER design experience:
Specific of TF conductors
R. Vallcorba_MATEFU School 2009

## Slide 42: Nuclear heat load (in JT-60SA)
Villari
Fus Eng Des 09

## Slide 43: Heat Loads in fusion coils
Source of losses:
Hysteresis
AC
Coupling
Eddy-
Neutrons
Thermal radiation & Conduction
  ITER design experience:
Due to varying field and currents
Specific of CS / PF conductors
Specific of TF conductors
R. Vallcorba_MATEFU School 2009

## Slide 44: Cable-in-Conduit Conductors (CICCs)
Typically: T ~ 4.5K, P ~ 6 10 bar
Steel
jacket
Empty fraction for forced He circulation
1000  5000
filaments
strand
Pressure relief channel
Strand bundle
Convective heat transfer:
BUT: Low JENG
Effective cooling
Mechanically strong
Flexible layout
Effective electrical insulation
Hoenig; Montgomery; Iwasa (1975):
high cooling efficiency of single phase (supercritical) He in turbulent flow and in direct contact with a large wetted surface

## Slide 45: D-shaped superconducting tokamaks
6.2m
EAST
KSTAR
1.8m
1.1m
SST-1
JT-60SA
3.1m
1.7m
ITER
2.1m
DTT
10.0 kA - 5.1 T NbTi
14.3 kA - 5.8 T NbTi
35.2 kA - 7.2 T Nb3Sn
68.0 kA - 12 T Nb3Sn
25.7 kA - 5.7 T NbTi
 42.5 kA – 11.9 T Nb3Sn
EAST
KSTAR
SST-1
ITER
DTT
JT-60SA

## Slide 46: Cable-in-Conduit Conductors

## Slide 47: Outline
Magnetic confinement fusion: the tokamak concept
Magnet system of a tokamak reactor
Cable-in-Conduit conductors (CICCs)
ITER CICCs and optimization margins
Key components of fusion coils: the example of the Italian DTT Project.
Summary and concluding remarks

## Slide 48: The ITER CICCs: the state-of-the-art
TF CICC: 68 kA @ 11.8 T
F = 43.7 mm
CS CICC: 46 kA @ 13 T; L = 49 mm
PF CICC:
52 kA @ 6.4 T
L = 53.8 mm

## Slide 49: CICC qualification tests: the SULTAN facility
SULTAN facility at the:

## Slide 50: CICC qualification tests: the SULTAN facility
Sample configuration: 2 “Legs”, connected by a bottom joint, and fed in series. Full set of instrumentation (Temperature, voltage, pressure sensors acquired)
B (up to 12T)
I (up to 100 kA)
I (up to 100 kA)
SULTAN facility at the:

## Slide 51: CICC qualification tests: Tcs
Typical Current Sharing Temperature (Tcs) test
SULTAN facility at the:
Repeated after e.m. loading cycles + Warm-up-Cooldown (WUCD) cycles
Breschi_SUST 2012

## Slide 52: Degradation issue in Nb3Sn CICC
ITER TF: Tcs measurements with cycles
SULTAN facility at the:
M. Breschi – A. Devred

## Slide 53: Strain effects in Nb3Sn CICCs
Nb3Sn inside CICC is subject to various strain components:
- mismatch of heat expansion coefficients of different materials, between 650 °C (reaction heat treatment) and 4.2K (operating Temp.):
eaxial  - 0.7% ÷ - 0.4%

## Slide 54: Strain effects in Nb3Sn CICCs
Nb3Sn inside CICC is subject to various strain components:
- mismatch of heat expansion coefficients of different materials, between 650 °C (reaction heat treatment) and 4.2K (operating Temp.):
eaxial  - 0.7% ÷ - 0.4%
 only about 50% ÷ 80% of the current carrying capability of the material is actually available
Cheggour_IEEE TAS 2012

## Slide 55: Strain effects in Nb3Sn CICCs
Nb3Sn inside CICC is subject to various strain components:
- mismatch of heat expansion coefficients of different materials, between 650 °C (reaction heat treatment) and 4.2K (operating Temp.):
eaxial  - 0.7% ÷ - 0.4%
- large e.m. loads together with cable structure and intrinsic presence of voids cause bending at the strand level (+ contact stress, etc.)
ebending  0.2% ÷ 0.3%
Nijhuis_SUST 2008

## Slide 56: Degradation issue in Nb3Sn CICC
Post-mortem metallographic studies of tested CICCs
C. Sanabria - NHMFL
Sanabria_SUST 2015

## Slide 57: Back to …. strain effects in Nb3Sn CICCs
Nb3Sn inside CICC is subject to various strain components:
- mismatch of heat expansion coefficients of different materials, between 650 °C (reaction heat treatment) and 4.2K (operating Temp.):
eaxial  - 0.7% ÷ - 0.4%
- large e.m. loads together with cable structure and intrinsic presence of voids cause bending at the strand level (+ contact stress, etc.)
ebending  0.2% ÷ 0.3%
(Reversible or irreversible) degradation is intrinsic in the nature of CICC

## Slide 58: Degradation issue in Nb3Sn CICC
 improve strand support, by:
- reducing the void fraction;
- optimizing cable twist pitches;
- changing conductor aspect ratio.
(BUT trade-off with AC losses and cooling requirements)
To mitigate the phenomenon down to acceptable levels
(i.e. maintaining sufficient DTmargin):
The ITER CS example:

## Slide 59: Degradation issue in Nb3Sn CICC
 improve strand support, by:
- reducing the void fraction;
- optimizing cable twist pitches;
- changing conductor aspect ratio.
(BUT trade-off with AC losses and cooling requirements)
To mitigate the phenomenon down to acceptable levels
(i.e. maintaining sufficient DTmargin):
The ITER CS example:

## Slide 60: The ITER CS development strategy
 | Sample 6 (STP design) | Samples 1, 2, 3 (REF. design) | Sample 4 (REF. design) | Sample 5 (LTP design)
Wire Cu:nonCu | 1 | 1.5 | 1 | 1
Cable layout | (2+1)x3x4x4x6 | 3x3x4x4x6 | (2+1)x3x4x4x6 | (2+1)x3x4x4x6
Twist Pitch sequence (mm) | 20/45/80/150/450 | 45/85/145/250/450 | 45/85/145/250/450 | 110/117/125/132/352
Proposal supported by e.m. and mechanical simulations by A. Nijhuis (Un. Twente)

## Slide 61: The ITER CS development strategy
short cable twist pitch cures Tcs degradation
Devred_SUST 2014

## Slide 62: From ITER to (EU)-DEMO
DEMO CAD model (30 April 2014)
www.euro-fusion.org/eurofusion/roadmap/
DEMOnstrate: 500 MW electric power

## Slide 63: From ITER to (EU)-DEMO
TF magnet | ITER | July 2013 | April 2015 | July 2018
Major radius (m) | 6.2 | 9 | 9.072 | 9.073
Toroidal field on axis (T) | 5.2 | 6.8 | 5.7 | 5.3
Plasma current (MA) | 9.1 | 14 | 19.6 | 17.9
Number of TF coils | 18 | 16 | 18 | 16
TF magnet ITOT (MA) | 164 | 305.8 | 257.1 | 238.7
Stored energy/TF coil (GJ) | 2.28 | 9.07 | 7.54 | 10.04
2014
2014
2018
16 TF coils
ITFcoil=14.9 MA
2015
2015
18 TF coils
ITFcoil=14.3 MA
Bpeak=12.2 T
2013
16 TF coils
ITFcoil=19.1 MA
Bpeak=13.3 T
since 2011 R&D activities in EU on the magnet system

## Slide 64: From ITER to (EU)-DEMO
TF magnet | ITER | July 2013 | April 2015 | July 2018
Major radius (m) | 6.2 | 9 | 9.072 | 9.073
Toroidal field on axis (T) | 5.2 | 6.8 | 5.7 | 5.3
Plasma current (MA) | 9.1 | 14 | 19.6 | 17.9
Number of TF coils | 18 | 16 | 18 | 16
TF magnet ITOT (MA) | 164 | 305.8 | 257.1 | 238.7
Stored energy/TF coil (GJ) | 2.28 | 9.07 | 7.54 | 10.04
CICC Operating Current | 68 kA | 70 – 95 kA |  | 
CICC Peak Magn. Field | 12 T | 11.5 – 13.5 T |  | 
E.m. Load (kN/m) | 816 | 800 – 1200 |  | 
DTmargin | 0.7 K | 1.5 – 2 K |  | 
since 2011 R&D activities in EU on the magnet system

## Slide 65: From ITER to (EU)-DEMO
TF magnet | ITER | July 2013 | April 2015 | July 2018
Major radius (m) | 6.2 | 9 | 9.072 | 9.073
Toroidal field on axis (T) | 5.2 | 6.8 | 5.7 | 5.3
Plasma current (MA) | 9.1 | 14 | 19.6 | 17.9
Number of TF coils | 18 | 16 | 18 | 16
TF magnet ITOT (MA) | 164 | 305.8 | 257.1 | 238.7
Stored energy/TF coil (GJ) | 2.28 | 9.07 | 7.54 | 10.04
CICC Operating Current | 68 kA | 70 – 95 kA |  | 
CICC Peak Magn. Field | 12 T | 11.5 – 13.5 T |  | 
E.m. Load (kN/m) | 816 | 800 – 1200 |  | 
DTmargin | 0.7 K | 1.5 – 2 K |  | 
From ITER to DEMO,
CICC design is required to be:
With optimized performance;
With stable behavior;
Cost-effective!
Quite some effort is being spent on technology development
since 2011 R&D activities in EU on the magnet system

## Slide 66: Optimization margins for Nb3Sn CICCs
Space for optimization of:
Materials: different type of strand, structural material, ….

## Slide 67: Optimization margins for Nb3Sn CICCs
Space for optimization of:
Materials: different type of strand, structural material, ….
CICC layout: cable twist pitches, conductor geometry, manufacturing approach.

## Slide 68: Optimization margins for Nb3Sn CICCs
Space for optimization of:
Materials: different type of strand, structural material, ….
CICC layout: cable twist pitches, conductor geometry, manufacturing approach.
MAIN AIM: improved strain management.

## Slide 69: The SPC R&W flat cable CICC

## Slide 70: The SPC R&W flat cable CICC
“Rutherford-like” cable
Steel jacket
Mixed matrix stabilizer
He channels
React & Wind (R&W) approach (reduced ethermal ; more effective use of Nb3Sn)
Reduced cable size to allow winding with reduced e bending;
Quasi-Monolithic cable (increased cable stiffness).

## Slide 71: The SPC R&W flat cable CICC
DC Test results
Nominal operating conditions:
12.2 T ; 63.3 kA
(load: 770 kN/m)
eeff = -0.27% ; no performance degrad. with cycling

## Slide 72: The W&R rectangular CICC

## Slide 73: The W&R rectangular CICC
outer dimensions | 38.8 mm x 80.6 mm
measured jacket thickness | 6.9 mm
local VF in cable bundle | 24.6%

## Slide 74: The W&R rectangular CICC: DC test results
  Tcs(@ 81.7kA and 13T)= 6.95 K ÷ 7.15 K
  with stable performance during cycling.
Muzzi_IEEE TAS 2017

## Slide 75: The W&R rectangular CICC: DC test results
Long Twist Pitch cable configuration … BUT
Rectangular geometry AND low void fraction
HERE:
ITER CS
Very Short Twist Pitch cable
WR1 DEMO TF
Devred_SUST 2014

## Slide 76: Outline
Magnetic confinement fusion: the tokamak concept
Magnet system of a tokamak reactor
Cable-in-Conduit conductors (CICCs)
ITER CICCs and optimization margins
Key components of fusion coils: the example of the Italian DTT Project.
Summary and concluding remarks

## Slide 77: Divertor Tokamak Test (DTT) facility
Divertor concept;
Magnetic configurations
Liquid metal plasma facing components
Construction starting in Frascati:
(strand contract already assigned)
General objective: create a research infrastructure addressed to the solution of the power exhaust issues in view of DEMO.
Test Divertor alternative solutions & improve experimental knowledge in the PEX scientific area
R Martone et al., eds. DTT Divertor Tokamak Test facility Interim Design Report
ENEA (ISBN 978-88-8286-378-4), April 2019

## Slide 78: DTT Magnet System
  18 TF coils:
  Nb3Sn CICC: 42.5 kA – 11.9 T
  providing 6.0 T over plasma major radius (2.19 m)
  6 CS modules (indipendently fed)
  Nb3Sn CICC: 31.3 kA – 13.6 T
  providing 16.6 Weber magnetic flux for plasma initiation at breakdown
  6 PF coils
  Nb3Sn (PF1 & PF6) CICC: 28.3 kA – 9.1 T
  NbTi (PF2 to PF5) CICC: 27.1 kA – 4.2 T
  NbTi (PF3 to PF4) CICC: 28.6 kA – 5.3 T
  + 6 in-vessel Cu axial-symmetric coils
  + 18 in-vessel Cu not-axial-symmetric coils
  Identical in pairs to guarantee full top/down symmetry

## Slide 79: Main components of fusion coils
TF coils are made of:
- Winding Pack (current carrying element)
- Steel casing
- Structures and supports
PF / CS coils are made of:
- Winding Pack (current carrying element)
- Pre-compression structure

## Slide 80: Main components of fusion coils
TF coils are made of:
- Winding Pack (current carrying element)
- Steel casing
- Structures and supports
PF / CS coils are made of:
- Winding Pack (current carrying element)
- Pre-compression structure

## Slide 81: The DTT TF Coils
- CICC operating current: 42.5 KA
- Bpeak: 11.9 T
- 3 rDP; 2 sDP; 84 turns
- Turn insulation: Fiber-glass + resin
WindReactInsulateImpregnate
Overall TF energy: 2 GJ; L (1 TF coil): 48 mH
Volt. at discharge < 1 kV (terminal to terminal)
TF coil height ≈ 6 m; TF coil width ≈ 3.2 m

## Slide 82: ITER TF Coil: completed, with casing and structures
337 Tons

## Slide 83: Toroidal Field Coils: forces
Slide courtesy of A. Portone
ITER
ITER

## Slide 84: Toroidal Field Coils: in-plane loads
Centering force (Fc) is reacted by wedging on the casing «nose»
Fc
Fc
(ITER)
(DTT)

## Slide 85: Toroidal Field Coils: in-plane loads
Centering force (Fc) is reacted by wedging on the casing «nose»
Bursting force (Fz) translates into a Tension along the winding pack
Fc
(ITER)
(DTT)
(ITER)
(DTT)
Fz
Fz

## Slide 86: Toroidal Field Coils: out-of-plane loads
Slide courtesy of A. Portone

## Slide 87: Toroidal Field Coils: out-of-plane loads

## Slide 88: DTT Toroidal Field Coils: out-of-plane loads
≤ 13.0 mm*
Stress intensity
Lateral displacement

## Slide 89: DTT Toroidal Field Coils: out-of-plane loads
Out-of-plane loads are sustained by inter-coil structures
Inner Inter-coil structures (IIS) - upper
Outer Inter-coil structures (OIS)
Inner Inter-coil structures (IIS) - lower

## Slide 90: Main components of fusion coils
TF coils are made of:
- Winding Pack (current carrying element)
- Steel casing
- Structures and supports
PF / CS coils are made of:
- Winding Pack (current carrying element)
- Pre-compression structure

## Slide 91: CS Coil – overview and winding
5.3 m
1,5 m
45 tons
The flux swing capability of the CS:
To drive the plasma to the desired flat-top value Ip:

## Slide 92: CS Coil – overview and winding
5.3 m
1,5 m
45 tons
Design choices:
6 identical but independent modules
Layer wound (optimized JE --> Flux > 16.6 Weber
Optimized concepts for inter-grade joints and terminations
High Field Section
810 s.c. wires
4.9 mm jacket
Low Field Section
180 s.c. wires
2.0 mm jacket
G-10 inter-module spacers
Medium Field Section
300 s.c. wires
3.9 mm jacket

## Slide 93: CS Coil currents and loads
CS currents-SN scenario
CS and PF turn on the plasma and keep it stable;

## Slide 94: CS Coil currents and loads
CS and PF turn on the plasma and keep it stable;
A plasma scenario has various stages: induction of plasma current (a)  ovalization (b)  shaping to triangular (c).
b)
c)
a)
b)
c)
CS - SN
PF - SN

## Slide 95: CS Coil electromagnetic loads
CS currents-SN scenario
L. Giannini_IEEE TAS 20
SN - IM
SN - EOF
DN – Flat-top
The hoop stress is maximum at the inner radius and it drops as the soleoid gets thicker

## Slide 96: CS Coil electromagnetic loads
15,29
-60,4
-19,2
10,2
57,16
18
Electro-magnetic loads
SN - IM
SN - EOF
DN – Flat-top
15.3 MN
- 60.4 MN
- 19.2 MN
10.2 MN
57.2 MN
18.0 MN
SN - IM
SN - EOF

## Slide 97: CS Coil electromagnetic loads
Electro-magnetic loads
Essentially reacted internally, through the steel jacket
Require external structures

## Slide 98: CS Coil – structures
CS Pre-compression structure

## Slide 99: CS Coil – structures
CS Pre-compression structure
Tie plates

## Slide 100: CS Coil – structures
Centering system
CS Pre-compression structure
Tie plates

## Slide 101: CS Coil – structures
Centering system
CS Pre-compression structure
Tie plates
CS gravity support

## Slide 102: PF coils: overview
COIL | PF1/6 | PF2/5 | PF3/4
Bmax (T) | 8.5 | 4.4 | 5.4
Iop max (kA) | 28.3 | 27.1 | 28.6
Hydraulic length (m) | 178 | 193 | 381
Vmax (V) | 2150 | 1350 | 3290
Weight (ton) | 15 | 16 | 28
Delay / discharge const. | 1.5 s / 6 s |  | 
CICC dimensions (mm) | 23.4 x 28.3 | 26.4 x 27.7 | 26.4 x 27.7
Jacket thickness (mm) | 3.0 | 3.0 | 3.0
# SC / Cu strands; 0.82 mm | 180 (Nb3Sn) / 216 | 162 (NbTi) / 324 | 324 (NbTi) / 162
PF Double or Quadri-pancake winding and joint (praying or shaking hands) boxes
DP winding for PF2 to 5

## Slide 103: Outline
Magnetic confinement fusion: the tokamak concept
Magnet system of a tokamak reactor
Cable-in-Conduit conductors (CICCs)
ITER CICCs and optimization margins
Key components of fusion coils: the example of the Italian DTT Project.
Mechanics of fusion magnets.
Summary and concluding remarks

## Slide 104: Summary
Steel
jacket
Empty fraction for forced He circulation
1000  5000
filaments
strand
Pressure relief channel
Strand bundle
Fusion magnets are wound by Cable-in-Conduit Conductors, i.e. multi-stage cables compacted inside steel jacket, and cooled by forced flow of supercritical Helium.

## Slide 105: Summary
Fusion magnets are wound by Cable-in-Conduit Conductors, i.e. multi-stage cables compacted inside steel jacket, and are cooled by forced flow of supercritical Helium.
large-size Nb3Sn CICCs subject to large e.m. loads may exhibit performance degradation with loading cycles.

## Slide 106: Summary
Fusion magnets are wound by Cable-in-Conduit Conductors, i.e. multi-stage cables compacted inside steel jacket, and are cooled by forced flow of supercritical Helium.
large-size Nb3Sn CICCs subject to large e.m. loads may exhibit performance degradation with loading cycles.
The phenomenon is intrinsic in the nature of CICC, but may be mitigated by proper design choices.
ITER CS

## Slide 107: Summary
Fusion magnets are wound by Cable-in-Conduit Conductors, i.e. multi-stage cables compacted inside steel jacket, and are cooled by forced flow of supercritical Helium.
large-size Nb3Sn CICCs subject to large e.m. loads may exhibit performance degradation with loading cycles.
The phenomenon is intrinsic in the nature of CICC, but may be mitigated by proper design choices.
ITER represents the state-of-the-art of CICC technology, but further developments and extension of performance range have been demonstrated e.g. within the DEMO conductor development program.

## Slide 108: Summary
Fusion magnets are made of a winding pack (current carrying element) and massive structures to sustain the very high mechanical loads.

## Slide 109: Summary
Fusion magnets are made of a winding pack (current carrying element) and massive structures to sustain the very high mechanical loads.
TF coil structures include: casing; inter-coil structures; gravity supports; PF and CS weight supports.

## Slide 110: Summary
Fusion magnets are made of a winding pack (current carrying element) and massive structures to sustain the very high mechanical loads.
TF coil structures include: casing; inter-coil structures; gravity supports; PF and CS weight supports.
PF and CS Hoop forces are reacted internally. But pre-compression structures are required, to sustain axial separating forces.

## Slide 111
Luigi Muzzi
luigi.muzzi@enea.it

## Slide 112: Back-up Slides

## Slide 113: ITER TF Coils: winding pack
Conductor is wound in Double-Pancakes
15 m
9 m

## Slide 114: ITER TF Coils: winding pack
Radial Plates

## Slide 115: ITER CS Coils

## Slide 116: DTT Toroidal Field Coils: 2D stress analysis
Stress intensity (MPa)

## Slide 117: DTT Toroidal Field Coils: 2D and 3D stress analysis
Stress intensity (MPa)

## Slide 118: CS Coil – mechanics: 2D static assessment
Stress Intensity equivalent stress
[Pa]
SINT
EOF @ SN scenario